Copyright 2021 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 032000 - CONCRETE REINFORCING

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

MasterSpec includes provisions for LEED 2009, LEED v4, IgCC, and Green Globes. Sustainable design requirements may be inserted in the Section Text using the hypertext links.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Steel reinforcement bars.

          - Welded-wire reinforcement.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 033816 "Unbonded Post-Tensioned Concrete" for reinforcing related to post-tensioned concrete.

          - Section 034100 "Precast Structural Concrete" for reinforcing used in precast structural concrete.

          - Section 034500 "Precast Architectural Concrete" for reinforcing used in precast architectural concrete.

          - Section 321313 "Concrete Paving" for reinforcing related to concrete pavement and walks.

          - Section 321316 "Decorative Concrete Paving" for reinforcing related to decorative concrete pavement and walks.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

          - Review the following:

            - Special inspection and testing and inspecting agency procedures for field quality control.

            - Construction contraction and isolation joints.

            - Steel-reinforcement installation.

      - ACTION SUBMITTALS

        - Product Data: For the following:

          - Each type of steel reinforcement.

          - Epoxy repair coating.

          - Zinc repair material.

          - Bar supports.

          - Mechanical splice couplers.

          - Structural thermal break insulated connection system.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for recycled content.>

          - <Double click to insert sustainable design text for regional materials.>

          - <Double click here to insert sustainable design text for Type III Environmental Product Declaration.>

          - <Double click here to insert sustainable design text for sourcing of raw materials.>

          - <Double click here to insert sustainable design text for manufacturer inventory.>

        - Shop Drawings: Comply with ACI SP-066:

          - Include placing drawings that detail fabrication, bending, and placement.

          - Include bar sizes, lengths, materials, grades, bar schedules, stirrup spacing, bent bar diagrams, bar arrangement, location of splices, lengths of lap splices, details of mechanical splice couplers, details of welding splices, tie spacing, hoop spacing, and supports for concrete reinforcement.

          - For structural thermal break insulated connection system, indicate general configuration, insulation dimensions, tension bars, compression pads, shear bars, and dimensions.

        - Construction Joint Layout: Indicate proposed construction joints required to build the structure.

          - Location of construction joints is subject to approval of Architect.

Retain "Delegated Design Submittal" Paragraph below if design services have been delegated to Contractor.

        - Delegated Design Submittal: For structural thermal break insulated connection system, including analysis data signed and sealed by the qualified professional engineer responsible for their preparation.

      - INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as supplemented in "Quality Assurance" Article. If inserting additional entities or specialists, add qualifications in "Quality Assurance" Article.

Retain first option in "Qualification Statements" Paragraph below if design services have been delegated to Contractor. Retain second option if Contractor is responsible for field quality-control testing and inspections.

        - Qualification Statements: For [delegated design engineer] [testing and inspection agency].

        - Delegated Design Engineer Qualifications: Include the following:

          - Experience providing delegated design engineering services of the type indicated.

          - Documentation that delegated design engineer is licensed in the [jurisdiction] [state] in which Project is located.

Retain "Welding certificates" Paragraph below if retaining "Welding Qualifications" Paragraph in "Quality Assurance" Article.

        - Welding certificates.

          - Reinforcement To Be Welded: Welding procedure specification in accordance with AWS D1.4/D1.4M.

        - Material Certificates: For each of the following, signed by manufacturers:

          - Epoxy-Coated Reinforcement: CRSI's "Epoxy Coating Plant Certification."

          - Dual-Coated Reinforcement: CRSI's "Epoxy Coating Plant Certification."

        - Material Test Reports: For the following, from a qualified testing agency:

          - Steel Reinforcement:

            - For reinforcement to be welded, mill test analysis for chemical composition and carbon equivalent of the steel in accordance with ASTM A706/A706M.

          - Mechanical splice couplers.

Retain "Field quality-control reports" Paragraph below if Contractor is responsible for field quality-control testing and inspecting.

        - Field quality-control reports.

Retain paragraph below if preinstallation conference is held.

        - Minutes of preinstallation conference.

      - QUALITY ASSURANCE

Retain "Testing Agency Qualifications" Paragraph below if Contractor retains testing and inspection agency for field quality control. Retain option if field quality-control testing and inspection agency employed by Contractor must be approved by authorities having jurisdiction.

        - Testing Agency Qualifications: An independent agency,[ acceptable to authorities having jurisdiction,] qualified in accordance with ASTM C1077 and ASTM E329 for testing indicated.

Retain "Welding Qualifications" Paragraph below if shop or field welding is required. If retaining, also retain "Welding certificates" Paragraph in "Informational Submittals" Article. AWS states that welding qualifications remain in effect indefinitely unless welding personnel have not welded for more than six months or there is a specific reason to question their ability.

        - Welding Qualifications: Qualify procedures and personnel in accordance with AWS D1.4/D 1.4M.

Retain "Mockups" Paragraph below if required. If retaining, indicate location and other details of mockups on Drawings or by inserts. Revise wording if only one mockup is required or if mockup in another location in a building is required.

        - Mockups: Reinforcing for cast-concrete formed surfaces, to demonstrate tolerances and standard of workmanship.

Revise size of panel in first subparagraph below if required. Panel for slab-on-grade may need to be enlarged if powered riding trowels are used and if it is a portion of the floor slab.

          - Build panel approximately [100 sq. ft. (9.3 sq. m) for formed surface] <Insert area> in the location indicated on Drawings or, if not indicated, as directed by Architect.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

Retain option in "Steel Reinforcement" Paragraph below if zinc-coated, epoxy-coated, or dual-coated steel reinforcement is required.

        - Steel Reinforcement: Deliver, store, and handle steel reinforcement to prevent bending and damage[ and to avoid damaging coatings on steel reinforcement].

          - Store reinforcement to avoid contact with earth.

          - Do not allow epoxy-coated reinforcement to be stored outdoors for more than 60 days without being stored under an opaque covering.

          - Do not allow dual-coated reinforcement to be stored outdoors for more than 60 days without being stored under an opaque covering.

          - Do not allow stainless steel reinforcement to come into contact with uncoated reinforcement.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - PERFORMANCE REQUIREMENTS

Retain "Delegated Design" Paragraph below if Contractor is required to assume responsibility for structural thermal break insulated connection system design.

        - Delegated Design: Engage a qualified professional engineer, as defined in Section 014000 "Quality Requirements," to design structural thermal break insulated connection system, including attachment to building construction.

        - Structural Performance of Structural Thermal Break Insulating Connection System: Structural thermal break insulated connection system to withstand the following loads and stresses:

          - Dead Loads: As indicated on Drawings.

            - Shear Load: As indicated on Drawings.

            - Bending Moment: As indicated on Drawings.

          - Live Loads: As indicated on Drawings.

            - Shear Load: As indicated on Drawings.

            - Bending Moment: As indicated on Drawings.

Retain "Seismic Performance of Structural Thermal Break Insulated Connection System" Paragraph below for projects requiring seismic design. Model building codes and ASCE/SEI 7 establish criteria for buildings subject to earthquake motions. Verify requirements of authorities having jurisdiction.

        - Seismic Performance of Structural Thermal Break Insulated Connection System: Structural thermal break Insulated connection system to withstand the effects of earthquake motions determined according to [ASCE/SEI 7] <Insert requirement>.

          - Component Importance Factor: <Insert requirement>.

      - STEEL REINFORCEMENT

Revise this article to suit steel-reinforcement requirements; delete if not required.

        - <Double click here to insert sustainable design text for recycled content.>

          - <Double click to insert sustainable design text for regional materials.>

        - Reinforcing Bars: ASTM A615/A615M, [Grade 60 (Grade 420)] [Grade 75 (Grade 520)] [Grade 80 (Grade 550)] [Grade 100 (Grade 690)], deformed.

Retain "Low-Alloy Steel Reinforcing Bars" Paragraph below for reinforcement that is welded or if added ductility is sought.

        - Low-Alloy Steel Reinforcing Bars: ASTM A706/A706M, deformed.

        - Headed-Steel Reinforcing Bars: ASTM A970/A970M.

        - Galvanized Reinforcing Bars:

          - Steel Bars: [ASTM A615/A615M, Grade 60 (Grade 420)] [ASTM A615/A615M, Grade 75 (Grade 520)] [ASTM A615/A615M, Grade 80 (Grade 550)] [ASTM A615/A615M, Grade 100 (Grade 690)] [ASTM A706/A706M], deformed bars.

Retain one zinc coating class "Zinc Coating" Subparagraph below. Class I has at least 50 percent more zinc weight than Class II. Class I is normally specified for general construction.

          - Zinc Coating: ASTM A767/A767M, [Class I] [Class II] zinc coated after fabrication and bending.

        - Epoxy-Coated Reinforcing Bars:

          - Steel Bars: [ASTM A615/A615M, Grade 60 (Grade 420)] [ASTM A615/A615M, Grade 75 (Grade 520)] [ASTM A615/A615M, Grade 80 (Grade 550)] [ASTM A615/A615M, Grade 100 (Grade 690)] [ASTM A706/A706M], deformed bars.

In "Epoxy Coating" Subparagraph below, ASTM A775/A775M bars are usually epoxy coated before fabrication; ASTM A934/A934M bars are epoxy coated after fabrication and should not be field bent or rebent.

          - Epoxy Coating: [ASTM A775/A775M] [or] [ASTM A934/A934M] with less than 2 percent damaged coating in each 12-inch (305-mm) bar length.

        - Dual-Coated Reinforcing Bars: ASTM A1055/A1055M.

          - Steel Bars: [ASTM A615/A615M, Grade 60 (Grade 420)] [ASTM A615/A615M, Grade 75 (Grade 520)] [ASTM A615/A615M, Grade 80 (Grade 550)] [ASTM A615/A615M, Grade 100 (Grade 690)] [ASTM A706/A706M], deformed bars.

In "Zinc Coating" Subparagraph below, Type I coating is applied by a thermal-spray method, and Type II is hot-dipped galvanized in accordance with ASTM A1094/A1094M.

          - Zinc Coating: ASTM A1055/A1055M [Type I] [Type II].

In "Epoxy Coating" Subparagraph below, ASTM A775/A775M bars are usually epoxy coated before fabrication; ASTM A934/A934M bars are epoxy coated after fabrication and should not be field bent or rebent.

          - Epoxy Coating: [ASTM A775/A775M] [or] [ASTM A934/A934M] with less than 2 percent damaged coating in each 12-inch (300-mm) bar length.

Retain "Stainless Steel Reinforcing Bars" Paragraph below for stainless steel reinforcement. Retain third or fourth option for reinforcement type.

        - Stainless Steel Reinforcing Bars: ASTM A955/A955M, [Grade 60 (Grade 420)] [Grade 75 (Grade 520)], [Type 304] [Type 316L], deformed.

        - Steel Bar Mats: ASTM A184/A184M, fabricated from [ASTM A615/A615M, Grade 60 (Grade 420)] [ASTM A615/A615M, Grade 40 (Grade 280)] [ASTM A706/A706M], deformed bars, assembled with clips.

        - Plain-Steel Welded-Wire Reinforcement: ASTM A1064/A1064M, plain, fabricated from as-drawn steel wire into flat sheets.

        - Deformed-Steel Welded-Wire Reinforcement: ASTM A1064/A1064M, flat sheet.

        - Galvanized-Steel Welded-Wire Reinforcement: ASTM A1064/A1064M, plain, fabricated from galvanized-steel wire into flat sheets.

        - Epoxy-Coated Welded-Wire Reinforcement: ASTM A884/A884M, Class A coated, Type 1, [plain] [deformed] steel.

      - REINFORCEMENT ACCESSORIES

Insert other products for dowels or dowel sleeves if required. These include circular and rectangular plastic dowel sleeves, square dowels, and plastic-surfaced or reinforced-paper-covered dowels.

        - Joint Dowel Bars: ASTM A615/A615M, Grade 60 (Grade 420), plain-steel bars, cut true to length with ends square and free of burrs.

        - Epoxy-Coated Joint Dowel Bars: ASTM A615/A615M, Grade 60 (Grade 420), plain-steel bars, ASTM A775/A775M epoxy coated.

        - Bar Supports: Bolsters, chairs, spacers, and other devices for spacing, supporting, and fastening reinforcing bars and welded-wire reinforcement in place.

          - Manufacture bar supports from steel wire, plastic, or precast concrete in accordance with CRSI's "Manual of Standard Practice," of greater compressive strength than concrete and as follows:

Retain one or more of first three subparagraphs below; revise to suit Project.

            - For concrete surfaces exposed to view, where legs of wire bar supports contact forms, use CRSI Class 1 plastic-protected steel wire, all-plastic bar supports, or CRSI Class 2 stainless steel bar supports.

            - For epoxy-coated reinforcement, use CRSI Class 1A epoxy-coated or other dielectric-polymer-coated wire bar supports.

            - For dual-coated reinforcement, use CRSI Class 1A epoxy-coated or other dielectric-polymer-coated wire bar supports.

            - For zinc-coated reinforcement, use galvanized wire or dielectric-polymer-coated wire bar supports.

            - For stainless steel reinforcement, use CRSI Class 1 plastic-protected steel wire, all-plastic bar supports, or CRSI Class 2 stainless steel bar supports.

        - Mechanical Splice Couplers: ACI 318 (ACI 318M) [Type 1] [Type 2], same material of reinforcing bar being spliced; [compression-only type] [tension-compression type] [dowel-bar type] [mechanical-lap type].

Retain "Structural Thermal Break Insulated Connection System" Paragraph below if required, typically at concrete balconies.

        - Structural Thermal Break Insulated Connection System:

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Tension Rods: [Carbon steel with crimped Type 316 stainless steel rods] [Carbon steel, welded with ASTM A276/A276M, Type 316 stainless steel].

          - Shear Reinforcement Rods: [ASTM A276/A276M, Type 316 stainless steel tube] [Carbon steel, welded with ASTM A276/A276M, Type 316 stainless steel bar].

          - Pressure pads: ASTM A276/A276M, Type 316 stainless steel.

          - Insulation body: Polystyrene.

        - Steel Tie Wire: ASTM A1064/A1064M, annealed steel, not less than 0.0508 inch (1.2908 mm) in diameter.

Retain third option in "Finish" Subparagraph below for use with epoxy-coated and dual-coated reinforcing bars.

          - Finish: [Plain] [Galvanized] [ASTM A884/A884M, Class A, Type 1, epoxy coated, with less than 2 percent damaged coating in each 12-inch (305-mm) wire length].

Retain "Stainless Steel Tie Wire" Paragraph below for architectural concrete.

        - Stainless Steel Tie Wire: ASTM A1022/A1022M, not less than 0.0508 inch (1.2908 mm) in diameter.

        - Epoxy Repair Coating: Liquid, two-part, epoxy repair coating; compatible with epoxy coating on reinforcement and complying with ASTM A775/A775M.

        - Zinc Repair Material: ASTM A780/A780M.

      - FABRICATING REINFORCEMENT

        - Fabricate steel reinforcement according to CRSI's "Manual of Standard Practice."

- EXECUTION

      - PREPARATION

        - Protection of In-Place Conditions:

          - Do not cut or puncture vapor retarder.

          - Repair damage and reseal vapor retarder before placing concrete.

        - Clean reinforcement of loose rust and mill scale, earth, ice, and other foreign materials that reduce bond to concrete.

      - INSTALLATION OF STEEL REINFORCEMENT

        - Comply with CRSI's "Manual of Standard Practice" for placing and supporting reinforcement.

        - Accurately position, support, and secure reinforcement against displacement.

          - Locate and support reinforcement with bar supports to maintain minimum concrete cover.

          - Do not tack weld crossing reinforcing bars.

        - Preserve clearance between bars of not less than 1 inch (25 mm), not less than one bar diameter, or not less than 1-1/3 times size of large aggregate, whichever is greater.

        - Provide concrete coverage in accordance with ACI 318 (ACI 318M).

        - Set wire ties with ends directed into concrete, not toward exposed concrete surfaces.

        - Splices: Lap splices as indicated on Drawings.

          - Bars indicated to be continuous, and all vertical bars to be lapped not less than 36 bar diameters at splices, or 24 inches (610 mm), whichever is greater.

          - Stagger splices in accordance with ACI 318 (ACI 318M).

Retain first subparagraph below if couplers are permitted or required.

          - Mechanical Splice Couplers: Install in accordance with manufacturer's instructions.

Retain subparagraph below if welding is permitted or required.

          - Weld reinforcing bars in accordance with AWS D1.4/D 1.4M, where indicated on Drawings.

Retain first paragraph below if structural thermal break insulated connection system is required.

        - Install structural thermal break insulated connection system in accordance with manufacturer's instructions.

        - Install welded-wire reinforcement in longest practicable lengths.

          - Support welded-wire reinforcement in accordance with CRSI "Manual of Standard Practice."

            - For reinforcement less than W4.0 or D4.0, continuous support spacing to not exceed 12 inches (305 mm).

          - Lap edges and ends of adjoining sheets at least one wire spacing plus 2 inches (50 mm) for plain wire and 8 inches (200 mm) for deformed wire.

          - Offset laps of adjoining sheet widths to prevent continuous laps in either direction.

          - Lace overlaps with wire.

Retain "Epoxy-Coated Reinforcement" Paragraph below if using epoxy-coated reinforcement.

        - Epoxy-Coated Reinforcement: Repair cut and damaged epoxy coatings with epoxy repair coating in accordance with ASTM D3963/D3963M.

Retain "Dual-Coated Reinforcement" Paragraph below if using dual-coated reinforcement.

        - Dual-Coated Reinforcement: Repair cut and damaged epoxy coatings with epoxy repair coating in accordance with ASTM D3963/D3963M.

Retain "Zinc-Coated Reinforcement" Paragraph below if using zinc-coated reinforcement.

        - Zinc-Coated Reinforcement: Repair cut and damaged zinc coatings with zinc repair material in accordance with ASTM A780/A780M.

      - JOINTS

Revise criteria for locating construction joints in "Construction Joints" Paragraph below to suit Project.

        - Construction Joints: Install so strength and appearance of concrete are not impaired, at locations indicated or as approved by Architect.

          - Place joints perpendicular to main reinforcement.

          - Continue reinforcement across construction joints unless otherwise indicated.

          - Do not continue reinforcement through sides of strip placements of floors and slabs.

        - Doweled Joints: Install dowel bars and support assemblies at joints where indicated. Lubricate or asphalt coat one-half of dowel length, to prevent concrete bonding to one side of joint.

      - INSTALLATION TOLERANCES

        - Comply with ACI 117 (ACI 117M).

      - FIELD QUALITY CONTROL

Retain "Special Inspections" or "Testing Agency" Paragraph below.

Retain first option in "Special Inspections" Paragraph below if authorities having jurisdiction require Owner to engage a special inspector. Retain last option if Owner engages testing agency, with or without a special inspector. See "Testing and Inspecting Considerations" Article in the Evaluations.

        - Special Inspections: Owner will engage a [special inspector] [and] [qualified testing and inspecting agency] to perform field tests and inspections and prepare test reports.

Retain "Testing Agency" Paragraph below if Contractor engages testing agency.

        - Testing Agency: Engage a qualified testing and inspecting agency to perform tests and inspections and to submit reports.

        - Inspections:

Retain three subparagraphs below if special inspections are required. Items below are examples of special inspections and are based on IBC requirements; revise to insert other inspections or to suit requirements of other building codes.

          - Steel-reinforcement placement.

          - Steel-reinforcement mechanical splice couplers.

          - Steel-reinforcement welding.

Retain "Manufacturer's Inspections" Paragraph below if structural thermal break insulated connection system is required.

        - Manufacturer's Inspections: Engage manufacturer of structural thermal break insulated connection system to inspect completed installations prior to placement of concrete, and to provide written report that installation complies with manufacturer's written instructions.

END OF SECTION 032000