Copyright 2021 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 033543 - POLISHED CONCRETE FINISHING

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Access Manufacturer-Provided, AIA MasterSpec-Based Sections:

<Double click here for this Section based on specific manufacturer’s products set as Basis-of-Design at ProductMasterSpec.com.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

MasterSpec includes provisions for LEED 2009, LEED v4, IgCC, and Green Globes. Sustainable design requirements may be inserted in the Section Text using the hypertext links.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Polished concrete finishing[, including staining] [and scoring].

          - Concrete for polished concrete, including concrete materials, mixture design, placement procedures, initial finishing, and curing is specified in Section 033000 "Cast-in-Place Concrete."

        - Related Requirements:

Retain subparagraph below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 033000 "Cast-in-Place Concrete" for concrete not designated as polished concrete.

      - DEFINITIONS

Retain terms that remain after this Section has been edited for a project.

Retain "Design Reference Sample" Paragraph below if design reference sample, chosen by Architect during Contract documentation, is proposed.

        - Design Reference Sample: Sample designated by Architect in the Contract Documents that reflects acceptable surface quality and appearance of polished concrete.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference. Preinstallation conference helps minimize misunderstandings and reviews Project conditions that might lead to significant problems.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

Retain first subparagraph below if warranted by complexity of design mixtures and quality control of concrete materials.

          - Before submitting design mixtures, review concrete design mixture and examine procedures for ensuring quality of concrete materials. Require representatives of each entity directly concerned with polished concrete to attend, including the following:

            - Contractor's superintendent.

            - Independent testing agency responsible for concrete design mixtures.

            - Ready-mix concrete manufacturer.

            - Cast-in-place concrete subcontractor.

            - Polished concrete finishing Subcontractor.

          - Review [cold- and hot-weather concreting procedures,] [curing procedures,] [construction joints,] [concrete repair procedures,] [concrete finishing,] and protection of polished concrete.

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for stains and liquid floor treatments.>

        - Polishing Schedule: Submit plan showing polished concrete surfaces and schedule of polishing operations for each area of polished concrete before start of polishing operations. Include locations of all joints, including construction joints.

Delete "Samples for Initial Selection" Paragraph below if colors and other characteristics are preselected and specified or scheduled.

        - Samples for Initial Selection: For each type of product requiring color selection.

Retain "Samples for Verification" Paragraph below with or without "Samples for Initial Selection" Paragraph above.

        - Samples for Verification: For each type of exposed color.

      - INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

        - Qualification Data: For Installer.

Retain "Material Certificates" Paragraph below to require submittal of material certificates from manufacturers.

        - Material Certificates: For each of the following, signed by manufacturers:

          - Repair materials.

          - Stain materials.

          - Liquid floor treatments.

      - QUALITY ASSURANCE

Field sample panels may be used to verify that Contractor can produce polished concrete of required finish, color, and consistency of appearance. On simple projects, field samples may suffice and make mockups unnecessary. For more complex projects, field samples may be needed before producing full-scale mockups.

        - Field Sample Panels: After approval of verification sample and before casting concrete, produce field sample panels to demonstrate the approved range of selections made under Sample submittals. Produce a minimum of three sets of full-scale panels, approximately 48 by 48 inches (1200 by 1200 mm) minimum, to demonstrate the expected range of finish, color, and appearance variations.

          - Locate panels as indicated or, if not indicated, as directed by Architect.

          - Maintain field sample panels during construction in an undisturbed condition as a standard for judging the completed Work.

          - Demolish and remove field sample panels when directed.

Retain "Mockups" Paragraph below unless field sample panels will suffice and added expense of mockups is not required. If retaining, indicate location, size, and other details of mockups on Drawings or by inserts. Revise wording if only one mockup is required.

        - Mockups: Before casting concrete, build mockups to verify selections made under Sample submittals and to demonstrate typical joints, surface finish, tolerances, and standard of workmanship. Build mockups to comply with the following requirements, using materials indicated for the completed Work:

          - Build mockups in the location and of the size indicated or, if not indicated, as directed by Architect.

          - Demonstrate curing, finishing, and protecting of polished concrete.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - FIELD CONDITIONS

        - Traffic Control: Maintain access for vehicular and pedestrian traffic as required for other construction activities.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - STAIN MATERIALS

        - Reactive Stain: Acidic-based stain with wetting agents and high-grade, UV-stable metallic salts that react with calcium hydroxide in cured concrete to produce permanent, variegated, or translucent color effects.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - <Double click to insert sustainable design text for floor treatment products.>

        - Penetrating Stain: Water-based, acrylic latex, penetrating stain with colorfast pigments.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - <Double click to insert sustainable design text for floor treatment products.>

      - LIQUID FLOOR TREATMENTS

        - Penetrating Liquid Floor Treatments for Polished Concrete Finish: Clear, waterborne solution of inorganic silicate or siliconate materials and proprietary components; odorless; that penetrates, hardens, and is suitable for polished concrete surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - <Double click to insert sustainable design text for floor treatment products.>

- EXECUTION

      - POLISHING

        - Polish: [Level 1: Matte finish, 100 grit] [Level 2: Low sheen, 400 grit] [Level 3: High sheen, 800 grit] [Level 4: Gloss shine, 3000 grit] [Match design reference sample].

        - Apply polished concrete finish system to cured and prepared slabs to match accepted mockup.

          - Machine grind floor surfaces to receive polished finishes level and smooth[ and to depth required to reveal aggregate to match approved mockup].

          - Apply reactive stain for polished concrete in polishing sequence and according to manufacturer's written instructions.

          - Apply penetrating liquid floor treatment for polished concrete in polishing sequence and according to manufacturer's written instructions, allowing recommended drying time between successive coats.

          - Apply penetrating stain for polished concrete in polishing sequence and according to manufacturer's written instructions.

          - Continue polishing with progressively finer-grit diamond polishing pads to gloss level, to match approved mockup.

          - Control and dispose of waste products produced by grinding and polishing operations.

          - Neutralize and clean polished floor surfaces.

      - STAINING

Retain this article if stained concrete is required.

Concrete must cure prior to application of stain. Some stain colors require longer concrete curing time to meet water-vapor transmission limitations; some colors should not be used for exterior applications. Verify, with stain manufacturer, the minimum age of concrete for colors required and insert in first paragraph below. See the Evaluations.

        - Newly placed concrete to be at least [14] [30] <Insert number> days old before staining.

        - Prepare surfaces according to manufacturer's written instructions and as follows:

First subparagraph below is generally applicable to new concrete with little surface contamination. More aggressive cleaning, consisting of grinding, sanding, or shot blasting, may be required for older concrete with dense, sealed, or highly contaminated surface.

          - Clean concrete thoroughly by scraping, applying solvents or stripping agents, sweeping and pressure washing, or scrubbing with a rotary floor machine and detergents recommended by stain manufacturer. Rinse until water is clear and allow surface to dry.

Retain first subparagraph below if reactive stains are required.

            - Do not use acidic solutions to clean surfaces.

Retain one of two options for surface-preparation method in first subparagraph below. Retain first option if penetrating stains are required and acid etching is stain manufacturer's preferred method of profiling concrete surfaces. Retain second option for either reactive or penetrating stain system.

          - Test surfaces with droplets of water. If water beads and does not penetrate surface, or penetrates only in some areas, profile surfaces by [acid etching] [grinding, sanding, or abrasive blasting]. Retest and continue profiling surface until water droplets immediately darken and uniformly penetrate concrete surfaces.

Retain both subparagraphs below if acid etching of concrete surfaces for penetrating stains is required.

          - Apply acidic solution to dampened concrete surfaces, scrubbing with uncolored, acid-resistant nylon-bristle brushes until bubbling stops and concrete surface has texture of 120-grit sandpaper. Do not allow solution to dry on concrete surfaces. Rinse until water is clear. Control, collect, and legally dispose of runoff.

Waterborne stains are pH sensitive. Revise pH value or test method in subparagraph below to suit Project.

          - Neutralize concrete surfaces and rinse until water is clear. Test surface for residue with clean white cloth. Test surface according to ASTM F710 to ensure pH is between [7 and 8] <Insert values>.

Retain "Scoring" Paragraph below if scoring patterns in concrete surfaces are required. If unstained joints are required or only one color is used, score joints after staining.

        - Scoring: Score decorative jointing in concrete surfaces 1/16 inch (1.6 mm) deep with diamond blades to match pattern indicated. Rinse until water is clear. Score [after] [before] staining.

          - Joint Width: [3/8 inch (10 mm)] <Insert dimension>.

Retain first paragraph below with either reactive or penetrating stain.

        - Allow concrete surface to dry before applying stain. Verify readiness of concrete to receive stain according to ASTM D4263 by tightly taping 18-by-18-inch (450-by-450-mm), 4-mil- (0.1-mm-) thick polyethylene sheet to a representative area of concrete surface. Apply stain only if no evidence of moisture has accumulated under sheet after 16 hours.

        - Reactive Stain: Apply reactive stain to concrete surfaces according to manufacturer's written instructions and as follows:

          - Apply stain by uncolored bristle brush, roller, or high-volume, low-pressure sprayer and immediately scrub into concrete surface with uncolored, acid-resistant nylon-bristle brushes in continuous, circular motion. Do not spread stain after fizzing stops. Allow to dry four hours and repeat application of stain in sufficient quantity to obtain color consistent with approved mockup.

          - Remove stain residue after four hours by wet scrubbing with commercial-grade detergent recommended by stain manufacturer. Rinse until water is clear. Control, collect, and legally dispose of runoff.

        - Penetrating Stain: Apply penetrating stain to concrete surfaces according to manufacturer's written instructions and as follows:

          - Apply first coat of stain to dry, clean surfaces by airless sprayer or by high-volume, low-pressure sprayer.

          - Allow to dry four hours and repeat application of stain in sufficient quantity to obtain color consistent with approved mockup.

          - Rinse until water is clear. Control, collect, and legally dispose of runoff.

END OF SECTION 033543