Copyright 2021 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 047200 - CAST STONE MASONRY

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Wall panels[ with engraved inscriptions].

          - Trim units.

          - Decorative elements.

          - Mortar materials.

          - Accessories.

        - Related Requirements:

Retain subparagraph below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 034500 "Precast Architectural Concrete."

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

Usually, retain subparagraph below for cast stone items that are manufacturer's stock units.

          - For cast stone units, include construction details, material descriptions, dimensions of individual components and profiles, and finishes.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for regional materials.>

Usually, retain "Shop Drawings" Paragraph below for custom-made units.

        - Shop Drawings: Show fabrication and installation details for cast stone units. Include dimensions, details of reinforcement and anchorages if any, and indication of finished faces.

          - Include building elevations showing layout of units and locations of joints and anchors.

Delete "Samples for Initial Selection" Paragraph below if mortar is specified in Section 042000 "Unit Masonry" or Section 042613 "Masonry Veneer."

Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples.

        - Samples for Initial Selection: For colored mortar.

        - Samples for Verification:

          - For each color and texture of cast stone required, [4 inches (100 mm) square] <Insert dimension> in size.

          - For each trim shape required, [4 inches (100 mm)] <Insert dimension> in length.

Delete subparagraph below if mortar is specified in Section 042000 "Unit Masonry" or Section 042613 "Masonry Veneer."

          - For colored mortar, make Samples using same sand and mortar ingredients to be used on Project.[ Label Samples to indicate types and amounts of pigments used.]

        - Full-Size Samples: For each [color] [texture] [engraving] [and] [shape] of cast stone unit required.

          - Make available for Architect's review at Project site[ or at manufacturing plant, if acceptable to Architect].

Option in first subparagraph below may present timing problems. If Samples are not made far enough in advance, changing materials may be impossible (although adjustment of mixes and finishing techniques may be possible). However, if Samples are made too far in advance, they may not be made from materials from same lot used for production of units for Project.

          - Make Samples from materials to be used for units used on Project[ immediately before beginning production of units for Project].

          - Approved Samples may be installed in the Work.

      - INFORMATIONAL SUBMITTALS

Usually, retain "Qualification Data" Paragraph below unless manufacturers are limited to those known to produce only acceptable products. Coordinate with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

        - Qualification Data: For [manufacturer] [and] [testing agency].

Consider deleting subparagraph below. Unless testing to verify compliance with ASTM C1364 was required for previous projects, manufacturers may not be able to supply test reports.

          - Include copies of material test reports, indicating compliance of cast stone with ASTM C1364.

Consider deleting "Material Test Reports" Paragraph below if only a few units are required or if tests are considered unnecessary.

        - Material Test Reports: For each mix required to produce cast stone, based on testing according to ASTM C1364.

          - Provide test reports based on testing within previous six months.

      - QUALITY ASSURANCE

The certification programs in "Manufacturer Qualifications" Paragraph below are not all the same. PCI certification is only applicable for unreinforced, specialty wet-cast stone products.

        - Manufacturer Qualifications: A qualified manufacturer of cast stone units similar to those indicated for this Project, that has sufficient production capacity to manufacture required units, and is a plant certified by [CSI] [or] [APA] [or] [PCI for Group A, Category AT].

Retain "Testing Agency Qualifications" Paragraph below if Contractor is required to retain an independent testing agency for testing required by ASTM C1364.

Testing Agency Qualifications: Qualified according to ASTM E329 for testing indicated. Retain one of two paragraphs below if mockups are required. First paragraph is for supplying trim units for installation within a masonry wall. Second is for larger or standalone installations.

        - Furnish cast stone for installation in mockups specified in [Section 042000 "Unit Masonry."] [Section 042613 "Masonry Veneer."]

        - Mockups: Build mockups to verify selections made under Sample submittals and to demonstrate aesthetic effects[ and to set quality standards for materials and execution].

          - Build mockup for <Insert description> installation[ including accessories].

            - Size: <Insert dimension> [As indicated on Drawings].

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Coordinate delivery of cast stone[ with unit masonry work] to avoid delaying the Work[ and to minimize the need for on-site storage].

        - Pack, handle, and ship cast stone units in suitable packs or pallets.

          - Lift with wide-belt slings; do not use wire rope or ropes that might cause staining. Move cast stone units if required, using dollies with wood supports.

          - Store cast stone units on wood skids or pallets with nonstaining, waterproof covers, securely tied. Arrange to distribute weight evenly and to prevent damage to units. Ventilate under covers to prevent condensation.

Delete both paragraphs below if installation of cast stone is specified in Section 042000 "Unit Masonry" or Section 042613 "Masonry Veneer."

        - Store cementitious materials on elevated platforms, under cover, and in a dry location. Do not use cementitious materials that have become damp.

        - Store mortar aggregates where grading and other required characteristics can be maintained and contamination can be avoided.

      - PROJECT CONDITIONS

Delete this article if installation of cast stone is specified in Section 042000 "Unit Masonry" or Section 042613 "Masonry Veneer."

        - Cold-Weather Requirements: Do not use frozen materials or materials mixed or coated with ice or frost. Do not build on frozen substrates. Comply with cold-weather construction requirements in TMS 602.

          - Cold-Weather Cleaning: Use liquid cleaning methods only when air temperature is 40 deg F (4 deg C) and above and will remain so until cast stone has dried, but no fewer than seven days after completing cleaning.

        - Hot-Weather Requirements: Comply with hot-weather construction requirements in TMS 602.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - MANUFACTURERS

        - Source Limitations for Cast Stone: Obtain cast stone units from single source from single manufacturer.

Delete "Source Limitations for Mortar Materials" Paragraph below if installation of cast stone is specified in Section 042000 "Unit Masonry" or Section 042613 " Masonry Veneer."

        - Source Limitations for Mortar Materials: Obtain mortar ingredients of a uniform quality, including color, from one manufacturer for each cementitious component and from one source or producer for each aggregate.

      - CAST STONE MATERIALS

Delete this article if material requirements in ASTM C1364 are sufficient or if only stock units are required.

        - General: Comply with ASTM C1364.

"Portland Cement" Paragraph below is more restrictive than requirements in ASTM C1364.

        - Portland Cement: ASTM C150/C150M, Type I or Type III, containing not more than 0.60 percent total alkali when tested according to ASTM C114. Provide natural color or white cement as required to produce cast stone color indicated.

Revise "Coarse Aggregates" and "Fine Aggregates" paragraphs below if specific aggregates and gradations are required. Coarse aggregates are optional for dry tamp method.

        - Coarse Aggregates: Granite, quartz, or limestone complying with ASTM C33/C33M; gradation and colors as needed to produce required cast stone textures and colors.

        - Fine Aggregates: Natural sand or crushed stone complying with ASTM C33/C33M, gradation and colors as needed to produce required cast stone textures and colors.

Retain option in "Color Pigment" Paragraph below typically. If using pigments containing carbon black, carbon black must be limited to 2 percent of portland cement by weight or 1 percent of masonry or mortar cement.

        - Color Pigment: ASTM C979/C979M, synthetic mineral-oxide pigments or colored water-reducing admixtures; color stable,[ free of carbon black,] nonfading, and resistant to lime and other alkalis.

        - Admixtures: Use only admixtures specified or approved in writing by Architect.

          - Do not use admixtures that contain more than 0.1 percent water-soluble chloride ions by mass of cementitious materials. Do not use admixtures containing calcium chloride.

          - Use only admixtures that are certified by manufacturer to be compatible with cement and other admixtures used.

Retain option in "Air-Entraining Admixture" Subparagraph below if air entrainment is required for exterior units (for freeze-thaw resistance in wet cast only).

          - Air-Entraining Admixture: ASTM C260/C260M.[ Add to mixes for units exposed to the exterior at manufacturer's prescribed rate to result in an air content of 4 to 6 percent, except do not add to zero-slump concrete mixes.]

          - Water-Reducing Admixture: ASTM C494/C494M, Type A.

          - Water-Reducing, Retarding Admixture: ASTM C494/C494M, Type D.

          - Water-Reducing, Accelerating Admixture: ASTM C494/C494M, Type E.

Retain "Reinforcement" Subparagraph below to suit Project.

        - Reinforcement:

Revise first subparagraph below if another grade of steel is required. ASTM C1364 states that reinforcement "shall be noncorrosive" where exposed faces have less than 1-1/2 inches (38 mm) of cover. Welded-wire reinforcement is only applicable to wet-cast units.

          - Deformed steel bars complying with ASTM A615/A615M, Grade 40 (Grade 280). Use galvanized or epoxy-coated reinforcement when covered with less than 1-1/2 inches (38 mm) of cast stone material.

            - Epoxy Coating: ASTM A775/A775M.

            - Galvanized Coating: ASTM A767/A767M.

          - Plain-Steel, Welded-Wire Reinforcement: ASTM A1064/A1064M, plain, fabricated from as-drawn steel wire into flat sheets.

          - Galvanized-Steel, Welded-Wire Reinforcement: ASTM A1064/A1064M, plain, fabricated from galvanized-steel wire into flat sheets.

          - Fiber Reinforcement: ASTM C1116/C1116M.

Retain one of three options in "Embedded Anchors and Other Inserts" Paragraph below if embedded items are required. Retain first option unless higher corrosion resistance of Type 316 in second option is required; third option for minimal corrosion resistance is the most economical.

        - Embedded Anchors and Other Inserts: Fabricated from [stainless steel complying with ASTM A240/A240M, ASTM A276/A276M, or ASTM A666, Type 304] [stainless steel complying with ASTM A240/A240M, ASTM A276/A276M, or ASTM A666, Type 316] [steel complying with ASTM A36/A36M and hot-dip galvanized to comply with ASTM A123/A123M].

      - CAST STONE UNITS

CSI and APA have lists of manufacturers on their websites. Not all APA manufacturers produce cast stone; its directory is searchable by product category.

        - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - <Double click to insert sustainable design text for cast stone.>

        - Cast Stone Units: Comply with ASTM C1364.

Retain one of last three options in subparagraph below to limit method of manufacture. First option complies with ASTM C1364 requirement that manufacturer should select the manufacturing method.

          - Units are manufactured using the [manufacturer's selected] [vibrant dry tamp] [wet-cast] [machine-made] method.

Retain remaining subparagraphs below to suit Project.

          - Wall Panels: [Sizes as indicated on Drawings] <Insert dimension(s)>.

Retain "Engravings" Subparagraph below if engraving is included. Add descriptive text or typeface and font selection to suit Project if not indicated on Drawings.

            - Engravings: As indicated on Drawings.

          - Trim units including [window sills] [lintels] [surrounds] [mullions] [copings] [cornices] [wall caps] [belt courses] [water tables] [quoins] [keystones] [items as indicated on Drawings].

          - Decorative elements including [pilasters] [column covers] [medallions] [balustrades] [steps] [steps and risers] [bollards] [benches] [curbing] [fountains] [items as indicated on Drawings].

        - Fabricate units with sharp arris and accurately reproduced details, with indicated texture on all exposed surfaces unless otherwise indicated.

          - Slope exposed horizontal surfaces 1:12 to drain unless otherwise indicated.

          - Provide raised fillets at backs of sills and at ends indicated to be built into jambs.

          - Provide drips on projecting elements unless otherwise indicated.

        - Fabrication Tolerances:

Tolerances in "Variation in Cross Section"; "Variation in Length"; "Warp, Bow, and Twist"; and "Location of Grooves, False Joints, Holes, Anchorages, and Similar Features" subparagraphs below are based on CSI's recommendations.

          - Variation in Cross Section: Do not vary from indicated dimensions by more than 1/8 inch (3 mm).

          - Variation in Length: Do not vary from indicated dimensions by more than 1/360 of the length of unit or 1/8 inch (3 mm), whichever is greater, but in no case by more than 1/4 inch (6 mm).

          - Warp, Bow, and Twist: Not to exceed 1/360 of the length of unit or 1/8 inch (3 mm), whichever is greater.

          - Location of Grooves, False Joints, Holes, Anchorages, and Similar Features: Do not vary from indicated position by more than 1/8 inch (3 mm) on formed surfaces of units and 3/8 inch (10 mm) on unformed surfaces.

        - Cure Units as Follows:

First two subparagraphs below are based on CSI's recommendations.

          - Cure units in enclosed, moist curing room at 95 percent relative humidity and temperature of 100 deg F (38 deg C) for 12 hours or 70 deg F (21 deg C) for 16 hours.

          - Keep units damp and continue curing to comply with one of the following:

            - No fewer than five days at mean daily temperature of 70 deg F (21 deg C) or above.

            - No fewer than seven days at mean daily temperature of 50 deg F (10 deg C) or above.

Method in first paragraph below is standard for finishing cast stone units; revise if another method is required.

        - Acid etch units after curing to remove cement film from surfaces to be exposed to view.

Retain one of three options in "Colors and Textures" Paragraph below, or provide descriptions of colors and textures required. Exact matches of existing units may be impossible. Creating Architect's sample with known ingredients that is an acceptable approximate match is more feasible for manufacturers than producing an exact match.

        - Colors and Textures: [Match Architect's samples] [Match existing units] [As selected by Architect from manufacturer's full range] <Insert description>.

      - MORTAR MATERIALS

Delete this article if installation is specified in Section 042000 "Unit Masonry" or Section 042613 "Masonry Veneer."

        - Provide mortar materials that comply with [Section 042000 "Unit Masonry."] [Section 042613 "Masonry Veneer."]

Retain paragraph above or select from remaining paragraphs below. Coordinate selection of paragraphs below with requirements in "Mortar Mixes" Article.

        - <Double click to insert sustainable design text for mortar and grout.>

Retain one or more of "Portland Cement," "Hydrated Lime," "Portland Cement-Lime Mix," "Masonry Cement," and "Mortar Pigments" paragraphs below. Delete masonry cement and mortar cement if not allowed by "Mortar Mixes" Article. See the Evaluations in Section 042000 "Unit Masonry" for discussion of masonry cement and mortar cement.

        - Portland Cement: ASTM C150/C150M, Type I or II, except Type III may be used for cold-weather construction. Provide natural color or white cement as required to produce mortar color indicated.

        - Hydrated Lime: ASTM C207, Type S.

Mix in "Portland Cement-Lime Mix" Paragraph below allows better control of proportions than job-mixed, portland cement-lime mortar. If retaining, also retain "Portland Cement" and "Hydrated Lime" paragraphs above.

        - Portland Cement-Lime Mix: Packaged blend of portland cement and hydrated lime containing no other ingredients.

        - Masonry Cement: ASTM C91/C91M.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Retain "Mortar Pigments" Paragraph below for colored cement or for pigments added at Project site.

        - Mortar Pigments: Natural and synthetic iron oxides and chromium oxides, compounded for use in mortar mixes and complying with ASTM C979/C979M. Use only pigments with a record of satisfactory performance in masonry mortar.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Mixes in "Colored Cement Products" Paragraph below allow better control of color than job-mixed colored mortar. If retaining, also retain paragraphs above that specify materials included in the mixes retained below.

        - Colored Cement Products: Packaged blend made from [portland cement and hydrated lime] [masonry cement] [or] [mortar cement] and mortar pigments, all complying with specified requirements, and containing no other ingredients.

          - Colored Portland Cement-Lime Mix:

            - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Colored Masonry Cement:

            - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Formulate blend as required to produce color indicated or, if not indicated, as selected from manufacturer's standard colors.

Retain one of two subparagraphs below, or both, to suit types of cement retained above. Percentages are for pigments containing only metallic oxides. If using pigments containing carbon black, carbon black must be limited to 2 percent of portland cement by weight or 1 percent of masonry or mortar cement.

          - Pigments do not exceed 10 percent of portland cement by weight.

          - Pigments do not exceed 5 percent of [masonry cement] [or] [mortar cement] by weight.

Mixes in "Preblended Dry Mortar Mix" Paragraph below allow better control over quality and less waste than job-mixed mortar. If retaining, also retain paragraphs above that specify materials included in the mixes retained below.

        - Preblended Dry Mortar Mix: Packaged blend made from [portland cement and hydrated lime] [masonry cement] [or] [mortar cement], sand, [mortar pigments,] [water repellents,] and admixtures and complying with ASTM C1714/C1714M.

          - Preblended Dry Portland Cement Mortar Mix:

            - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Preblended Dry Masonry Cement Mortar Mix:

            - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Aggregate for Mortar: ASTM C144.

          - For mortar that is exposed to view, use washed aggregate consisting of natural sand or crushed stone.

          - For joints less than 1/4 inch (6 mm) thick, use aggregate graded with 100 percent passing the No. 16 (1.18-mm) sieve.

          - White-Mortar Aggregates: Natural white sand or crushed white stone.

Retain "Colored Aggregates" Subparagraph below for colored-aggregate mortar.

          - Colored Aggregates: Natural sand or crushed stone of color necessary to produce required mortar color.

        - Water: Potable.

      - ACCESSORIES

Retain one of three options in "Anchors" and "Dowels" subparagraphs below. First option is typical, unless higher corrosion resistance of Type 316 in second option is required; third option for minimal corrosion resistance is the most economical.

        - Anchors: Type and size indicated, fabricated from [Type 304 stainless steel complying with ASTM A240/A240M, ASTM A276/A276M, or ASTM A666] [Type 316 stainless steel complying with ASTM A240/A240M, ASTM A276/A276M, or ASTM A666] [steel complying with ASTM A36/A36M and hot-dip galvanized to comply with ASTM A123/A123M].

        - Dowels: 1/2-inch- (12-mm-) diameter round bars, fabricated from [Type 304 stainless steel complying with ASTM A240/A240M, ASTM A276/A276M, or ASTM A666] [Type 316 stainless steel complying with ASTM A240/A240M, ASTM A276/A276M, or ASTM A666] [steel complying with ASTM A36/A36M and hot-dip galvanized to comply with ASTM A123/A123M].

Delete "Proprietary Acidic Cleaner" Paragraph below if cleaning is specified in Section 042000 "Unit Masonry" or Section 042613 "Masonry Veneer." Before retaining, verify compatibility with surrounding masonry.

        - Proprietary Acidic Cleaner: Manufacturer's standard-strength cleaner designed for removing mortar/grout stains, efflorescence, and other new construction stains from new masonry without discoloring or damaging masonry surfaces. Use product expressly approved for intended use by cast stone manufacturer and expressly approved by cleaner manufacturer for use on cast stone and adjacent masonry materials.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

      - MORTAR MIXES

Retain one of first two paragraphs below.

        - Comply with requirements in [Section 042000 "Unit Masonry"] [Section 042613 "Masonry Veneer"] for mortar mixes.

        - Do not use admixtures including pigments, air-entraining agents, accelerators, retarders, water-repellent agents, antifreeze compounds, or other admixtures unless otherwise indicated.

          - Do not use calcium chloride in mortar or grout.

Retain one or more options in subparagraph below to indicate acceptable mortar types.

          - Use [portland cement-lime] [masonry cement] [or] [mortar cement] mortar unless otherwise indicated.

Retain one of first two paragraphs below. Preblended mortar mix only requires the addition of water.

        - Comply with ASTM C270, Proportion Specification.

Retain one mortar type in each of two subparagraphs below. CSI recommends Type N; other types may be required by special circumstances.

          - For setting mortar, use [Type S] [Type N].

          - For pointing mortar, use [Type N] [Type O].

        - Preblended dry mortar mix complying with ASTM C1714/C1714M and capable of producing mortar strength as indicated in ASTM C270.

Retain one mortar type in each of two subparagraphs below. CSI recommends Type N; other types may be required by special circumstances.

          - For setting mortar, use [Type S] [Type N].

          - For pointing mortar, use [Type N] [Type O].

        - Pigmented Mortar: Use colored cement product[ or select and proportion pigments with other ingredients to produce color required. Do not add pigments to colored cement products].

Retain first three subparagraphs below if retaining option in "Pigmented Mortar" Paragraph above. Percentages in first two subparagraphs are for pigments containing only metallic oxides. If using pigments containing carbon black, carbon black must be limited to 2 percent of portland cement by weight or 1 percent of masonry cement or mortar cement.

          - Pigments do not exceed 10 percent of portland cement by weight.

          - Pigments do not exceed 5 percent of [masonry cement] [or] [mortar cement] by weight.

Insert materials and proportions used for sample in first subparagraph below if known.

          - Mix to match Architect's sample.

          - Application: Use pigmented mortar for exposed mortar joints.

        - Colored-Aggregate Mortar: Produce required mortar color by using colored aggregates and natural color or white cement as necessary to produce required mortar color.

Insert materials and proportions used for sample in first subparagraph below if known.

          - Mix to match Architect's sample.

          - Application: Use colored-aggregate mortar for exposed mortar joints.

      - SOURCE QUALITY CONTROL

Consider deleting this article if only a few units are required or if testing is considered unnecessary. Revise if Owner employs testing agency.

        - Engage a qualified independent testing agency to sample and test cast stone units according to ASTM C1364.

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of the Work.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - SETTING CAST STONE IN MORTAR

In this article, retain only first paragraph below to follow CSI's recommendation referring all installation procedures to TMS 604 in lieu of listing requirements in specifications.

        - Set cast stone as indicated in TMS 604.

Delete first paragraph below if considered unnecessary or if Section 042000 "Unit Masonry" or Section 042613 "Masonry Veneer" are not used.

        - Install cast stone units to comply with requirements in [Section 042000 "Unit Masonry."] [Section 042613 "Masonry Veneer."]

Retain applicable remaining paragraphs below, with or without paragraph above.

        - Set cast stone as indicated on Drawings. Set units accurately in locations indicated, with edges and faces aligned according to established relationships and indicated tolerances.

          - Install anchors, supports, fasteners, and other attachments indicated or necessary to secure units in place.

          - Coordinate installation of cast stone with installation of flashing specified in other Sections.

        - Wet joint surfaces thoroughly before applying mortar or setting in mortar.

        - Set units in full bed of mortar with full head joints unless otherwise indicated.

Retain applicable subparagraphs below; delete those not applicable.

          - Set units with joints [1/4 to 3/8 inch (6 to 10 mm)] [3/8 to 1/2 inch (10 to 13 mm)] <Insert dimension> wide unless otherwise indicated.

          - Build anchors and ties into mortar joints as units are set.

          - Fill dowel holes and anchor slots with mortar.

Retain first subparagraph below for composite masonry.

          - Fill collar joints solid as units are set.

          - Build concealed flashing into mortar joints as units are set.

          - Keep head joints in copings and between other units with exposed horizontal surfaces open to receive sealant.

          - Keep joints at shelf angles open to receive sealant.

Retain first two paragraphs below unless cast stone is set in mortar without pointing.

        - Rake out joints for pointing with mortar to depths of not less than 3/4 inch (19 mm). Rake joints to uniform depths with square bottoms and clean sides. Scrub faces of units to remove excess mortar as joints are raked.

        - Point mortar joints by placing and compacting mortar in layers not greater than 3/8 inch (10 mm). Compact each layer thoroughly and allow it to become thumbprint hard before applying next layer.

Revise first paragraph below if another joint profile is required.

        - Tool exposed joints slightly concave when thumbprint hard. Use a smooth plastic jointer larger than joint thickness.

Retain first two paragraphs below if joints are pointed with sealant.

        - Rake out joints for pointing with sealant to depths of not less than 3/4 inch (19 mm). Scrub faces of units to remove excess mortar as joints are raked.

        - Point joints with sealant to comply with applicable requirements in Section 079200 "Joint Sealants."

          - Prime cast stone surfaces to receive sealant and install compressible backer rod in joints before applying sealant unless otherwise indicated.

Retain paragraph below for movement joints whether cast stone is pointed with mortar or sealant.

        - Provide sealant joints at head joints of copings and other horizontal surfaces; at expansion, control, and pressure-relieving joints; and at locations indicated.

          - Keep joints free of mortar and other rigid materials.

          - Build in compressible foam-plastic joint fillers where indicated.

          - Form joint of width indicated, but not less than [3/8 inch (10 mm)] [1/2 inch (13 mm)] <Insert dimension>.

          - Prime cast stone surfaces to receive sealant and install compressible backer rod in joints before applying sealant unless otherwise indicated.

          - Prepare and apply sealant of type and at locations indicated to comply with applicable requirements in Section 079200 "Joint Sealants."

      - SETTING ANCHORED CAST STONE WITH SEALANT-FILLED JOINTS

In this article, retain only first paragraph below to follow CSI's recommendation referring all installation procedures to TMS 604 in lieu of listing requirements in specifications.

        - Set cast stone as indicated in TMS 604.

        - Set cast stone as indicated on Drawings. Set units accurately in locations indicated, with edges and faces aligned according to established relationships and indicated tolerances.

          - Install anchors, supports, fasteners, and other attachments indicated or necessary to secure units in place.

          - Shim and adjust anchors, supports, and accessories to set cast stone in locations indicated with uniform joints.

Cavities in first paragraph below are recommended; local codes may require space to be grouted solid.

        - Keep cavities open where unfilled space is indicated between back of cast stone units and backup wall; do not fill cavities with mortar or grout.

        - Fill anchor holes with sealant.

          - Where dowel holes occur at pressure-relieving joints, provide compressible material at ends of dowels.

        - Set cast stone supported on clip or continuous angles on resilient setting shims. Use material of thickness required to maintain uniform joint widths. Hold shims back from face of cast stone a distance at least equal to width of joint.

        - Keep joints free of mortar and other rigid materials. Remove temporary shims and spacers from joints after anchors and supports are secured in place and cast stone units are anchored. Do not begin sealant installation until temporary shims and spacers are removed.

          - Form open joint of width indicated, but not less than [3/8 inch (10 mm)] [1/2 inch (13 mm)] <Insert dimension>.

        - Prime cast stone surfaces to receive sealant and install compressible backer rod in joints before applying sealant unless otherwise indicated.

        - Prepare and apply sealant of type and at locations indicated to comply with applicable requirements in Section 079200 "Joint Sealants."

      - INSTALLATION TOLERANCES

Delete this article if tolerances in Section 042000 "Unit Masonry" or Section 042613 "Masonry Veneer" govern. Tolerances in paragraphs below are based on those included in Section 042000 "Unit Masonry." First options in "Variation from Plumb" and "Variation from Level" paragraphs are based on recommendations from CSI. If retaining, revise to suit Project.

        - Variation from Plumb: Do not exceed [1/4 inch in 10 ft. (6 mm in 3 m)] [1/8 inch in 10 ft. (3 mm in 3 m)], [3/8 inch in 20 ft. (10 mm in 6 m)] [1/4 inch in 20 ft. (6 mm in 6 m)], or 1/2 inch (12 mm) maximum.

        - Variation from Level: Do not exceed [1/4 inch in 10 ft. (6 mm in 3 m)] [1/8 inch in 10 ft. (3 mm in 3 m)], [3/8 inch in 20 ft. (10 mm in 6 m)] [1/4 inch in 20 ft. (6 mm in 6 m)], or 1/2 inch (12 mm) maximum.

        - Variation in Joint Width: Do not vary joint thickness more than 1/8 inch in 36 inches (3 mm in 900 mm) or one-fourth of nominal joint width, whichever is less.

        - Variation in Plane between Adjacent Surfaces (Lipping): Do not vary from flush alignment with adjacent units or adjacent surfaces indicated to be flush with units by more than 1/16 inch (1.5 mm), except where variation is due to warpage of units within tolerances specified.

      - ADJUSTING AND CLEANING

        - Remove and replace stained and otherwise damaged units and units not matching approved Samples. Cast stone may be repaired if methods and results are approved by Architect.

        - Replace units in a manner that results in cast stone matching approved Samples, complying with other requirements, and showing no evidence of replacement.

Delete "In-Progress Cleaning" and "Final Cleaning" paragraphs below if installation and cleaning are specified in Section 042000 "Unit Masonry" or Section 042613 "Masonry Veneer."

        - In-Progress Cleaning: Clean cast stone as work progresses.

          - Remove mortar fins and smears before tooling joints.

          - Remove excess sealant immediately, including spills, smears, and spatter.

        - Final Cleaning: After mortar is thoroughly set and cured, clean exposed cast stone as follows:

          - Remove large mortar particles by hand with wooden paddles and nonmetallic scrape hoes or chisels.

          - Test cleaning methods on sample; leave one sample uncleaned for comparison purposes. Obtain Architect's approval of sample cleaning before proceeding with cleaning of cast stone.

Delete first two subparagraphs below if no cleaners are allowed or specified in Part 2.

          - Protect adjacent surfaces from contact with cleaner by covering them with liquid strippable masking agent or polyethylene film and waterproof masking tape.

          - Wet surfaces with water before applying cleaners; remove cleaners promptly by rinsing thoroughly with clear water.

Retain one of two subparagraphs below.

          - Clean cast stone by methods described in Cast Stone Institute Technical Bulletin #39.

Coordinate subparagraph below with products retained in Part 2. If high-pressure water cleaning or other methods are acceptable, revise subparagraph and insert applicable requirements.

          - Clean cast stone with proprietary acidic cleaner applied according to manufacturer's written instructions.

END OF SECTION 047200