Copyright 2017 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 050170.63 - DECORATIVE METAL REFINISHING

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section includes refinishing bare decorative metal surfaces as follows:

          - Refinishing metal in place.

          - Removing metal for shop refinishing; reinstalling refinished metal.

          - Integral metal finishes.

          - Clear protective coatings.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 013516 "Alteration Project Procedures" for general remodeling, renovation, repair, and maintenance requirements.

          - Section 099423 "Gilding" for gilding on metalwork.

      - ALLOWANCES

Retain products and Work included in this Section that are covered by cash or quantity allowance. Do not include amounts. Insert descriptions of items in Part 2 or 3 to provide information affecting the cost of the Work that is not included under the allowance. Delete this article if all decorative metal refinishing is done by lump-sum price.

Quantity allowances require a Schedule of Quantity Allowances coordinated with a Unit-Price Schedule. See "Planning the Work" Article in the Evaluations for a discussion of the bidding method.

        - Allowances for decorative metal refinishing are specified in Section 012100 "Allowances."

If using quantity allowances, retain three subparagraphs below or include similar language in Section 012100 "Allowances" to clarify how work covered by quantity allowances is to be authorized.

          - Perform decorative metal refinishing under quantity allowances and only as authorized. Authorized work includes [work required by Drawings and Specifications and] [only] work as directed in writing by Architect.

Retain first subparagraph below to suit Project.

          - Notify Architect [weekly] <Insert time interval> of extent of work performed that is attributable to quantity allowances.

          - Perform work that exceeds quantity allowances only as authorized by Change Orders.

Paragraph below is an example only; revise to suit Project. Insert additional allowances according to retained types of work and allowances established. If there are multiple drawing designations for types of work, establish separate allowances for each drawing designation.

        - Refinishing <Insert item description> is part of <Insert name of allowance>.

      - UNIT PRICES

Retain this article if Work specified in this Section is measured and paid for under the provisions of unit prices. Do not include amounts. Insert descriptions of items in Part 2 or 3 to provide information affecting the cost of the Work that is not included under the unit price.

Retain this article with "Allowances" Article for unit-price adjustments to quantity allowances.

Retain this article without "Allowances" Article if using a single Unit-Price Schedule with a column of estimated quantities on which bids are priced and evaluated.

        - Work of this Section is affected by unit prices specified in Section 012200 "Unit Prices."

          - Unit prices apply to authorized work covered by [quantity allowances] [estimated quantities].

          - Unit prices apply to authorized additions to and deletions from the Work as authorized by Change Orders.

      - DEFINITIONS

Retain terms that remain after this Section has been edited for a project.

Pressure spray values are not standardized but are typical for preparatory cleaning without abrasives; revise to suit Project. If abrasives are used, consider revising values because these pressures may be too high.

        - Low-Pressure Spray: [100 to 400 psi (690 to 2750 kPa); 4 to 6 gpm (0.25 to 0.4 L/s)] <Insert range of values>.

        - Medium-Pressure Spray: [400 to 800 psi (2750 to 5510 kPa); 4 to 6 gpm (0.25 to 0.4 L/s)] <Insert range of values>.

        - High-Pressure Spray: [800 to 1200 psi (5510 to 8250 kPa); 4 to 6 gpm (0.25 to 0.4 L/s)] <Insert range of values>.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

          - Include recommendations for product application and use.

          - Include test data substantiating that products comply with requirements.

Retain "Shop Drawings" Paragraph below if this information is not indicated on Drawings.

        - Shop Drawings:

          - Include plans, elevations, and sections showing locations and extent of refinishing work.

          - Include field-verified dimensions.

Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs below for two-stage Samples.

        - Samples for Initial Selection: For the following:

          - A range of each type of exposed finish prepared on metal of the same alloy matching existing metal.

        - Samples for Verification: For the following products in manufacturer's standard sizes unless otherwise indicated, finished as required for use in the Work:

Retain and revise subparagraph below and insert others to suit Project.

          - Each type of exposed finish prepared on metal of the same alloy matching existing metal; 6 inches (150 mm) long in least dimension.

      - INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

        - Qualification Data: For decorative metal refinishing specialist.

      - QUALITY ASSURANCE

In "Decorative Metal Refinishing Specialist Qualifications" Paragraph below, insert additional, specific requirements for demonstrating unique skills of firm and personnel to suit Project. See Section 014000 "Quality Requirements" for general qualifications of entities engaged by the Contractor.

        - Decorative Metal Refinishing Specialist Qualifications: A qualified decorative metal refinishing specialist.

Retain "Single Specialist" Subparagraph below if required; revise to suit Project. If also retaining "Decorative Metal Refinishing Specialist Firms" Paragraph in "Decorative Metal Refinishing Specialist" Article below, coordinate the listed specialists in the cited Sections.

          - Single Specialist: Subject to compliance with requirements, engage the same specialist firm to perform the work of [Section 050170.51 "Decorative Metal Cleaning"] [Section 050170.61 "Decorative Metal Repair"] and the work of this Section.

Retain required mockups in "Mockups" Paragraph below; insert others to suit Project. Test areas that were prepared or are required as part of a separate contract to evaluate and establish decorative metal refinishing materials and processes are not mockups. Generally, retain option because separate mockups may not adequately show blending of new work with existing construction.

        - Mockups: Prepare mockups of decorative metal refinishing processes[ on existing surfaces] to demonstrate aesthetic effects and to set quality standards for materials and execution. Prepare mockups so they are inconspicuous.

Mockups in "Waxing Bronze," "Refinishing Decorative Metal," "and "Repairing Decorative Metal Finish" subparagraphs below are examples only.

          - Waxing Bronze: Wax a cleaned area [approximately 2 sq. ft. (0.2 sq. m)] [as indicated on Drawings] <Insert dimension> of [each type of] bronze [sculpture] [paneling] [and] [hardware] <Insert item description>.

          - Refinishing Decorative Metal: Refinish [one] <Insert number> decorative <Insert item description> for each type of metal indicated to be refinished.

          - Repairing Decorative Metal Finish: Repair finish of [one] <Insert number> decorative <Insert item description> for each type of metal finish indicated to be repaired.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups. These mockups are typically installed as part of the existing building rather than erected separately.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Pack, deliver, and store decorative metal items in suitable packs, heavy-duty cartons, or wooden crates; surround with sufficient packing material to ensure that products are not deformed, cracked, or otherwise damaged.

        - Store decorative metal inside a well-ventilated area, away from uncured concrete and masonry and protected from weather, moisture, soiling, abrasion, extreme temperatures, and humidity.

        - Protect strippable protective covering on decorative metal from exposure to sunlight and high humidity, except to the extent necessary for the period of decorative metal installation.

      - FIELD CONDITIONS

Usually retain this article; revise to suit Project.

        - Weather Limitations: Proceed with decorative metal refinishing only when existing and forecasted weather conditions are within the environmental limits set by each manufacturer's written instructions and specified requirements.

- PRODUCTS

Manufacturers and products listed in SpecAgent and MasterWorks Paragraph Builder are neither recommended nor endorsed by the AIA or Deltek. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - PREPARATORY CLEANING MATERIALS

For a decorative metal item having a mix of materials, such as painted and bare metals, consider using cleaning materials and a single cleaning method selected for gentleness to all the materials and finishes on the item. See Section 050170.51 "Decorative Metal Cleaning" for additional cleaning materials and methods.

Retain materials in this article to suit Project and required cleaning methods. Acidic cleaners are generally not used on exposed metals unless they will be painted.

If local water is known to be unsuitable, consider informing Contractor of this in "Water" Paragraph below. Hard or softened water may be unsuitable even though potable.

        - Water: Potable.

Retain "Hot Water" Paragraph below if heated water is required.

        - Hot Water: Water heated to a temperature of 140 to 160 deg F (60 to 71 deg C).

Retain remaining paragraphs below to suit Project.

Revise "Detergent Solution, Job Mixed" Paragraph below for specific laundry detergent requirements if known. Detergent products vary in composition.

        - Detergent Solution, Job Mixed: Solution prepared by mixing 2 cups (0.5 L) of tetrasodium pyrophosphate (TSPP), 1/2 cup (125 mL) of laundry detergent, and 20 quarts (20 L) of hot water for every 5 gal. (20 L) of solution required.

Revise "Nonacidic Liquid Chemical Cleaner" Paragraph below to suit Project. Always test cleaners on substrates to be cleaned; strongly alkaline solutions can damage bare aluminum.

        - Nonacidic Liquid Chemical Cleaner: Manufacturer's standard mildly alkaline liquid cleaner, formulated for removing organic soiling from ordinary building materials, including polished stone, brick, copper, brass, bronze, aluminum, stainless steel, plastics, wood, and glass.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Abrasives can be used for paint removal as well as for cleaning surfaces, depending on the abrasive type and how it is used.

        - Abrasive Materials:

          - Abrasive Pads for Copper-Alloy Cleaning: Extra-fine bronze wool or plastic abrasive pads.

          - Blasting Abrasive: [Pulverized walnut shells] [Powdered aluminum silicate] <Insert material>.

Revise "Abrasives for Ferrous Metal Cleaning" Subparagraph below if mechanically cleaning stainless-steel surfaces; allow only stainless-steel tools. Carbon-steel residues can rust and stain stainless-steel surfaces.

          - Abrasives for Ferrous Metal Cleaning: Aluminum oxide paper, emery paper, fine steel wool, steel scrapers, and steel-wire brushes of various sizes.

      - PROTECTIVE COATING MATERIALS

Retain "Wax Coating" or "Organic Coating" Paragraph below, or both, to suit Project; if retaining more than one coating, indicate location of each on Drawings or by inserts. First paragraph specifies a wax coating commonly used for application to exterior bronze statuary after cleaning and patinizing; it generally requires reapplying annually or biennially. Waxes can also be applied to other metals but are generally not applied over painted coatings. Generally, retain last option in first paragraph if using hot-wax method of application. Verify with Owner that wax coating is appropriate for Owner's continuing maintenance capability.

        - Wax Coating: Inert, high-melting-point wax or wax blend, consisting primarily of [carnauba] [or] [microcrystalline petroleum] wax[ and no solvents].

Products in "BWC Company, Inc. (The)" Subparagraph below are carnauba-based waxes with solvents. First option is amber, second option is clear, and third option is dark brown.

Products in "Real Milk Paint Co. (The)" Subparagraph below are pure carnauba wax flakes (yellow) without solvent (first option) and carnauba wax with solvent (second option).

Products in "Talas" Subparagraph below are waxes without solvents. First option is amber microcrystalline wax; second option is pure carnauba wax flakes (yellow); third and fourth options are clear microcrystalline waxes.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

"Organic Coating" Paragraph below specifies a resin coating commonly used for application to exterior bronze statuary after cleaning and patinizing; it generally requires removing and reapplying every five years or less. It can be applied to other metals but is generally not applied over painted coatings. Verify, with Owner, that this coating is appropriate for Owner's continuing maintenance capability.

        - Organic Coating: Clear, waterborne, air-drying, acrylic lacquer called "Incralac"; specially developed for coating copper-alloy products; consisting of a solution of methyl methacrylate copolymer with benzotriazole UV inhibitor.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Product in "Copper-Alloy Corrosion Inhibitor" Paragraph below is commonly used to stabilize residual cuprous chloride. Revise "water" to "ethanol" if required; ethanol penetrates cracks and crevices better than water.

        - Copper-Alloy Corrosion Inhibitor: Solution of [1] [to] [3] <Insert number> percent benzotriazole in water.

      - MISCELLANEOUS MATERIALS

Product in "Liquid Strippable Masking Agent" Paragraph below does not protect against strong chemicals, such as those used for removing paint.

        - Liquid Strippable Masking Agent: Manufacturer's standard liquid, film-forming, strippable masking material for protecting glass, metal, glazed masonry, and polished stone surfaces from damaging effects of acidic and alkaline cleaners.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Masking Tape: Nonstaining, nonabsorbent material; compatible with chemical solutions being used and substrate surfaces, and that will easily come off entirely, including adhesive.

        - Other Products: Select materials and methods of use based on the following, subject to approval of a mockup:

          - Previous effectiveness in performing the work involved.

          - Little possibility of damaging exposed surfaces.

          - Consistency of each application.

          - Uniformity of the resulting overall appearance.

          - Do not use products or tools that could do the following:

            - Remove, alter, or in any way harm the present or future condition of existing surfaces, including surrounding surfaces not in the Contract.

            - Leave an unintended residue on surfaces.

      - FINISHES, GENERAL

        - Protect mechanical finishes on exposed surfaces from damage by applying a strippable, temporary protective covering before shipping.

        - Appearance of Finished Work: Noticeable variations in same piece are not acceptable. Variations in appearance of adjoining components are acceptable if they are within the range of approved Samples and are assembled or installed to minimize contrast.

      - ALUMINUM FINISHES

Retain finishes for bare aluminum in this article to suit Project. If retaining more than one, indicate location of each on Drawings or by inserts. Primers and paint finishes for aluminum are specified in other Sections.

        - Unfinished: No applied finish; only preparatory cleaning.

Retain one of first two options in "Clear Anodic Finish" Paragraph below. This finish is shop applied. Class II finish is standard with many manufacturers; Class I finish is heavy anodized. Verify availability with manufacturers. Revise last three options if custom mechanical finish is required and availability is verified.

        - Clear Anodic Finish: AAMA 611, [Class I, 0.018 mm] [Class II, 0.010 mm] or thicker over a [satin (directionally textured)] [polished (buffed)] [nonspecular as fabricated] <Insert requirement> mechanical finish.

Retain one of first two options in "Color Anodic Finish" Paragraph below. This finish is shop applied. Class II finish is standard with many manufacturers; Class I finish is heavy anodized. Verify availability with manufacturers. Revise last three options if custom mechanical finish is required and availability is verified. Indicate color on Drawings or in the Decorative Metal Refinishing Schedule.

        - Color Anodic Finish: AAMA 611, [Class I, 0.018 mm] [Class II, 0.010 mm] or thicker over a [satin (directionally textured)] [polished (buffed)] [nonspecular as fabricated] <Insert requirement> mechanical finish.

      - COPPER-ALLOY FINISHES

Retain finishes for bare copper alloys in this article to suit Project. If retaining more than one, indicate location of each on Drawings or by inserts.

        - General: Finish designations for copper alloys comply with the system defined in NAAMM's "Metal Finishes Manual for Architectural and Metal Products (AMP 500-06)."

"Buffed Finish," "Buffed Finish, Lacquered," "Satin Hand-Rubbed Finish," and "Satin Hand-Rubbed Finish, Lacquered" paragraphs below specify natural-color finishes. Retain first paragraph for finish that weathers and changes color naturally over time unless clear coated with wax, oil, or organic coating. First option in first paragraph is mirrorlike; second option is less bright. Insert wax or oil coating if required. NAAMM's "Metal Finishes Manual for Architectural and Metal Products (AMP 500-06)" does not have a number for waxes and oils.

        - Buffed Finish: [M21 (Mechanical Finish: buffed, smooth specular)] [M22 (Mechanical Finish: buffed, specular)] <Insert description>.

        - Buffed Finish, Lacquered: [M22 (Mechanical Finish: buffed, specular; specified clear organic coating)] <Insert description>.

Retain "Satin Hand-Rubbed Finish" Paragraph below for finish that weathers and changes color naturally over time unless clear coated with wax, oil, or organic coating. Insert wax or oil coating if required. NAAMM's "Metal Finishes Manual for Architectural and Metal Products (AMP 500-06)" does not have a number for waxes and oils.

        - Satin Hand-Rubbed Finish: [M32-M34 (Mechanical Finish: directionally textured, medium satin and hand rubbed)] <Insert description>.

        - Satin Hand-Rubbed Finish, Lacquered: [M32-M34-06x (Mechanical Finish: directionally textured, medium satin and hand rubbed; specified clear organic coating)] <Insert description>.

Remaining four paragraphs below specify patinated finishes. Chemical patinization is difficult to control to achieve a precise color; the skill of the Applicator is important. Patinated finishes are generally used in nontraffic locations where there is little or no maintenance; clear organic coating, hot wax, or oil can be applied to improve wear resistance. Hot wax and oil tend to saturate and darken the surface more than an organic coating. Verify, with manufacturers, the suitability of patinas for exterior exposure, if required, and requirements for clear protective coatings.

        - Satin Finish with Statuary Conversion Coating: [M32-C55 (directionally textured, medium satin; sulfide conversion coating)] <Insert description>.

First and second options in "Color" Subparagraph below are preferred methods of specifying to accommodate variations in color.

          - Color: [Match design reference sample] [Match existing] [Match Architect's sample] <Insert color>.

Coarseness of finish in "Brushed Finish with Patina Conversion Coating" Paragraph below is controlled by diameter and speed of wheel and pressure exerted.

        - Brushed Finish with Patina Conversion Coating: M35-C12-C52 (directionally textured, rotary brushed and buff polished, nonetched cleaned; ammonium sulfate conversion coating).

First and second options in "Texture and Color" Subparagraph below are preferred methods of specifying to accommodate variations in texture and color.

          - Texture and Color: [Match design reference sample] [Match existing] [Match Architect's sample] <Insert description>.

"Bright-Relieved Statuary Conversion Coating, Lacquered" Paragraph below is an example of a more complex finish requiring the highest skill level. It specifies finish for castings; revise for other forms of metal or if deeper color, such as blackening, is required.

        - Bright-Relieved Statuary Conversion Coating, Lacquered: M12-C55-M2x-06x (matte finish as cast; sulfide conversion coating; buffed to brighten high spots; specified clear organic coating):

First and second options in "Color and Buffing" Subparagraph below are preferred methods of specifying to accommodate variations in color and extent of bright relief (buffing).

          - Color and Buffing: [Match design reference sample] [Match existing] [Match Architect's sample] <Insert description>.

Retain paragraph below for proprietary patina finish not listed above. Patina finishes are available from manufacturers listed in "Listed Manufacturers" Article in the Evaluations.

        - <Insert name> Patina Finish: <Insert description>.

      - FERROUS METAL FINISHES

Retain "Patina Finish" Paragraph below for patina finish on bare iron or steel. Insert other finishes to suit Project. Copy article and revise for different iron and steel finishes. Primers and paint finishes for iron are specified in other Sections. Patina finishes are available from manufacturers listed in "Listed Manufacturers" Article in the Evaluations. Verify, with manufacturers, the suitability of patinas for exterior exposure, if required, and requirements for clear protective coatings.

        - Patina Finish: <Insert description>.

For exact finish, insert names of finish manufacturers and products.

      - STAINLESS STEEL FINISHES

Retain finishes for bare stainless steel in this article to suit Project. These finishes can be shop or field applied. If retaining more than one, indicate location of each on Drawings or by inserts.

        - Surface Preparation: Remove tool and die marks and stretch lines from new replacement stainless steel, or blend into finish.

Retain "Restored Finish" Paragraph below for finish applied to match existing stainless steel or Architect's sample.

        - Restored Finish: Grind and polish surfaces to produce uniform, directionally textured, polished finish to match [existing finish] [Architect's sample], free of cross scratches.

          - Run grain to match existing metal.

          - When polishing is completed, passivate and rinse surfaces. Remove embedded foreign matter and leave surfaces chemically clean.

Generally, retain "Polished Finishes" Paragraph below for stainless steel not required to match existing stainless steel; revise to suit Project.

        - Polished Finishes: Grind and polish surfaces to produce uniform finish, free of cross scratches.

Retain first subparagraph below for directional finishes.

          - Run grain of directional finishes with long dimension of each piece.

          - When polishing is completed, passivate and rinse surfaces. Remove embedded foreign matter and leave surfaces chemically clean.

          - Directional Satin Finish: ASTM A480/A480M, No. 4.

          - Dull Satin Finish: ASTM A480/A480M, No. 6.

          - Reflective, Directional Polish: ASTM A480/A480M, No. 7.

          - Mirrorlike Reflective, Nondirectional Polish: ASTM A480/A480M, No. 8.

Insert other metals and finishes to suit Project.

- EXECUTION

      - DECORATIVE METAL REFINISHING SPECIALIST

Retain this article if list of preapproved firms is considered necessary as a quality-control procedure for the Project. Retaining this article will restrict Contractor and may increase cost.

If retaining second option in "Decorative Metal Refinishing Specialist Firms" Paragraph below, include procedure for approving other firms in Document 002213 "Supplementary Instructions to Bidders."

        - Decorative Metal Refinishing Specialist Firms: Subject to compliance with requirements, [provide decorative metal refinishing by one of the following] [firms that may provide decorative metal refinishing include, but are not limited to, the following]:

          - <Insert, in separate subparagraphs, names of decorative metal refinishing specialist firms>.

      - PROTECTION

        - Comply with each manufacturer's written instructions for protecting building and other surfaces against damage from exposure to its products. Prevent chemical solutions from coming into contact with people, motor vehicles, landscaping, buildings, and other surfaces that could be harmed by such contact.

          - Cover adjacent surfaces with materials that are proved to resist chemical solutions being used unless products being used will not damage adjacent surfaces. Use protective materials that are waterproof and UV resistant. Apply masking agents to comply with manufacturer's written instructions. Do not apply liquid masking agent to painted or porous surfaces. When no longer needed, promptly remove masking to prevent adhesive staining.

          - Do not apply chemical solutions during winds of enough force to spread them to unprotected surfaces.

          - Neutralize alkaline and acid wastes before disposal.

          - Dispose of runoff from operations by legal means and in a manner that prevents soil erosion, undermining of paving and foundations, damage to landscaping, and water penetration into building interiors.

      - DECORATIVE METAL REFINISHING, GENERAL

Retain "Refinishing Appearance Standard" Paragraph below to control overall appearance from a distance.

        - Refinishing Appearance Standard: Refinished surfaces are to have a uniform appearance as viewed from [20 feet (6 m)] [50 feet (15 m)] <Insert distance> away by Architect.

        - Execution of the Work: In refinishing items, disturb remaining existing work as minimally as possible and as follows:

          - Remove dirt and corrosion.

          - Sequence work to minimize time before protective coatings are reapplied.

          - Refinish items in place where possible and according to required appearance.

Retain option in "Refinish Decorative Metal Item" and "Repair Finish of Decorative Metal Item" paragraphs below if required; revise to suit Project.

        - Refinish Decorative Metal Item: Remove existing metal finishes on item unless otherwise indicated[, including integral polished and patinated finishes,] and reapply them.

        - Repair Finish of Decorative Metal Item: Restore areas of deteriorated or missing finish on item and blend restored finish with existing, adjacent finish[, including integral polished and patinated finishes].

      - PREPARATORY CLEANING

Retain cleaning methods in this article for cleaning metal before refinishing; insert other methods to suit Project.

        - General: Use those methods indicated for each type of decorative metal and its location.

          - Brushes: If using wire brushes, use brushes of same base metal composition as metal being treated. Use brushes that are resistant to chemicals being used.

          - Spray Equipment: Use spray equipment that provides controlled application at volume and pressure indicated, measured at nozzle. Adjust pressure and volume to ensure that spray methods do not damage surfaces.

            - Equip units with pressure gages.

Retain first subparagraph below unless spray application of chemical cleaners is unacceptable. Wind drift of chemical cleaners is often a problem with spray application.

            - For chemical-cleaner spray application, use low-pressure tank or chemical pump suitable for chemical cleaner indicated, equipped with nozzle having a cone-shaped spray.

Fan-spray angle in first subparagraph below is considered efficient for low and medium pressure and less harmful than sprays with narrower angles. Never use a fan spray with an angle of less than 15 degrees.

            - For water-spray application, use fan-shaped spray that disperses water at an angle of 25 to 50 degrees.

Retain first subparagraph below if high-pressure spray is permitted.

            - For high-pressure water-spray application, use fan-shaped spray that disperses water at an angle of at least 40 degrees.

Retain first subparagraph below if heated water is required. Revise temperature range to suit Project.

            - For heated water-spray application, use equipment capable of maintaining temperature between 140 and 160 deg F (60 and 71 deg C) at flow rates indicated.

          - Uniformity: Perform each cleaning method in a manner that results in uniform coverage of all surfaces, including corners, contours, and interstices, and that produces an even effect without streaks or damaging surfaces.

          - Protection: After cleaning is complete, remove protection no longer required. Remove tape and adhesive marks.

        - Water Cleaning: Clean with [cold] [hot] water applied by [low] [medium] [high]-pressure spray. Supplement with [natural-fiber] [or] [plastic]-bristle brush. Use small brushes to remove soil from joints and crevices.

        - Detergent Cleaning:

          - Wet surface with [cold] [hot] water applied by low-pressure spray.

          - Scrub surface with detergent solution and [natural-fiber] [or] [plastic]-bristle brush until soil is thoroughly dislodged and can be removed by rinsing. Use small brushes to remove soil from joints and crevices. Dip brush in solution often to ensure that adequate fresh detergent is used and that surface remains wet.

Retain one of first two options and one of last three options in subparagraph below.

          - Rinse with [cold] [hot] water applied by [low] [medium] [high]-pressure spray to remove detergent solution and soil.

        - Nonacidic Liquid Chemical Cleaning: Apply chemical cleaner to surfaces according to chemical-cleaner manufacturer's written instructions.

Alkaline cleaners work better with hot water.

          - Wet surface with [cold] [hot] water applied by low-pressure spray.

          - Apply cleaner to surface[ in two applications] by brush[ or low-pressure spray].

Retain one option in first subparagraph below; revise to suit Project. Third option is an example only.

          - Let cleaner remain on surface for period [recommended in writing by chemical-cleaner manufacturer] [established by mockup] [of two to three minutes] <Insert requirement>.

Retain one of first two options and one of last three options in "Nonferrous Metals" Subparagraph below.

          - Nonferrous Metals: Rinse with [cold] [hot] water applied by [low] [medium] [high]-pressure spray to remove chemicals and soil.

          - Ferrous Metals: Do not rinse ferrous metals with water; neutralize chemical cleaner on ferrous metals as recommended in writing by manufacturer. Dry immediately with clean soft cloths. Follow direction of grain in metal.

Generally, retain first option in "Cleaning with Abrasive Pads" Paragraph below for decorative metals with desirable patina. This method can remove patina if used aggressively.

        - Cleaning with Abrasive Pads: Clean surfaces to remove dirt[, leaving uniform patina intact,] by light rubbing with abrasive pads and water. [Rinse with cold water to remove residue. Apply rinse by low-pressure spray] [Do not rinse ferrous metals with water; wipe with damp cloths to remove residue] <Insert requirement>.

Generally, retain first option in "Cleaning by Abrasive Blasting" Paragraph below for decorative metals with desirable patina. Abrasive blasting can remove patina if used aggressively or with hard abrasives.

        - Cleaning by Abrasive Blasting: Clean surfaces to remove dirt[, leaving uniform patina intact,] by dry blasting with specified blasting abrasive at pressure and distance from surface indicated below. [Rinse with cold water, low-pressure spray to remove residue.] [Do not rinse ferrous metals with water; wipe with damp cloths to remove residue] <Insert requirement>.

Retain one of two "Pressure and Distance from Surface" subparagraphs below.

          - Pressure and Distance from Surface: Maximum pressure of [60 psi (415 kPa)] [100 psi (690 kPa)] [200 psi (1375 kPa)] <Insert value> with specified blasting abrasive propelled from a distance of [6 to 12 inches (152 to 305 mm)] [12 to 18 inches (305 to 457 mm)] <Insert dimension> from the surface.

          - Pressure and Distance from Surface: As established by mockup.

      - PROTECTIVE COATING

Retain "Protective Hot-Wax Coating" or "Protective Organic Coating" Paragraph below, or both, to suit Project; if retaining both, indicate location of each on Drawings or by inserts. Pretreatment option is commonly used to stabilize residual cuprous chloride.

        - Protective Hot-Wax Coating:[ Pretreat cleaned copper-alloy surfaces with copper-alloy corrosion inhibitor, wipe off excess with ethanol-saturated rag, and allow surface to dry. If fresh corrosion appears, repeat process.] Apply wax coating to produce uniform appearance without runs or other surface imperfections.

          - Clean and dry surface being waxed.

          - Preheat surface to about 212 deg F (100 deg C); hot enough to melt the wax and remove water vapor and other gases within metal surface, but not hot enough to boil the wax or ignite solvents if any.

          - Apply uniform wax coating to surface, ensuring that wax coverage is complete, including recesses.[ Apply second wax coating following the same process.]

          - Inspect surface and repair holidays by reheating and applying more wax.

          - Buff waxed surface to a slight shine with a lint-free cloth after wax has cooled to a hazy appearance.

        - Protective Organic Coating:[ Pretreat cleaned copper-alloy surfaces with copper-alloy corrosion inhibitor, wipe off excess with ethanol-saturated rag, and allow surface to dry. If fresh corrosion appears, repeat process.] Apply organic coating to produce uniform appearance without runs or other surface imperfections.

          - Clean and dry surface being coated.

          - Apply two uniform coats by air-spray method according to manufacturer's written instructions, with interim drying between coats.

          - Apply coating to a total dry film thickness of 1 mil (0.025 mm).

          - Protect coated surface from contamination until fully cured.

      - REMOVAL, REPAIR, AND REINSTALLATION

Indicate on Drawings or in the Decorative Metal Refinishing Schedule which decorative metal items are to be removed and reinstalled.

        - General: Perform removal, repair, and reinstallation work as required in Section 024119 "Selective Demolition" and Section 050170.61 "Decorative Metal Repair."

      - DECORATIVE METAL REFINISHING SCHEDULE

This schedule demonstrates a method to indicate refinishing and other requirements for decorative metal. A schedule helps to prevent confusion where Project includes several items of varying sizes, characteristics, and complexities; where extensive drawing notations would otherwise be used. The design professional decides what to include in a schedule and what to annotate on Drawings. This schedule is an example only; revise to suit Project and coordinate with decorative metal schedules in Section 050170.51 "Decorative Metal Cleaning" and Section 050170.61 "Decorative Metal Repair" if retained.

Insert drawing designation for each item to be treated, and indicate the methods of treatment that apply to the item. Use these designations on Drawings to identify locations.

        - Treatment of Decorative Handrail [DMR-#] <Insert drawing designation>: Tarnished bronze railing with bronze handrail.

          - General: Perform work [in the shop] [or] [in the field].

          - Cleaning: [Water cleaning] [Detergent cleaning] [Chemical cleaning] [Abrasive blasting] <Insert description>.

          - Bronze Finish: [Satin finish with statuary conversion coating on railing; satin hand-rubbed finish, lacquered, on handrail] <Insert requirement>.

        - Treatment for Bronze Statue Finish [DMS-#] <Insert drawing designation>: Clean, repair patina finish, and coat statue.

          - General: Perform work [in the shop] [or] [in the field].

          - Cleaning: [Water cleaning] [Detergent cleaning] [Chemical cleaning] [Abrasive blasting] <Insert description>.

          - Finish Repair: Selectively patinate the [nose] [foot] [and] [previous metal repairs] <Insert description> to match the rest of the statue.

          - Protective Coating: Protective [hot-wax] [organic] coating.

END OF SECTION 050170.63