Copyright 2022 by The American Institute of Architects (AIA)

Exclusively published and distributed Deltek, Inc. for the AIA

SECTION 062023 - INTERIOR FINISH CARPENTRY

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

MasterSpec includes provisions for LEED 2009, LEED v4, LEED v4.1, IgCC, and Green Globes. Sustainable design requirements may be inserted in the Section Text using the hypertext links.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Interior trim.

          - Paneling.

          - Shelving and clothes rods.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Retain option in first subparagraph below if structural wood is exposed to view.

          - Section 061000 "Rough Carpentry" for furring, blocking, and other carpentry work not exposed to view[ and for framing exposed to view].

          - Section 064023 "Interior Architectural Woodwork" for shop-fabricated carpentry.

          - Section 099123 "Interior Painting" for priming and backpriming of interior finish carpentry.

      - DEFINITIONS

Retain terms that remain after this Section has been edited for a project.

        - MDF: Medium-density fiberboard.

        - MDO: Plywood with a medium-density overlay on the face.

        - PVC: Polyvinyl chloride.

      - ACTION SUBMITTALS

Action submittals are submittals requiring responsive action and return of reviewed documents to Contractor.

        - Product Data:

          - Interior trim.

          - Paneling.

          - Shelving and clothes rods.

        - Product Data Submittals: For each type of process and factory-fabricated product. Indicate component materials, dimensions, profiles, textures, and colors and include construction and application details.

          - Include data for wood-preservative treatment from chemical-treatment manufacturer and certification by treating plant that treated materials comply with requirements. Indicate type of preservative used and net amount of preservative retained. Include chemical-treatment manufacturer's written instructions for finishing treated material.

          - For products receiving a waterborne treatment, include statement that moisture content of treated materials was reduced before shipment to Project site to levels specified.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for regional materials.>

          - <Double click to insert sustainable design text for certified wood.>

          - <Double click to insert sustainable design text for certified wood.>

          - <Double click to insert sustainable design text for composite wood.>

          - <Double click to insert sustainable design text for installation adhesives.>

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples.

        - Samples: For each exposed product and for each color and texture specified.

        - Samples for Initial Selection: For each type of product involving selection of colors, profiles, or textures.

        - Samples for Verification:

          - For each species and cut of lumber and panel products with nonfactory-applied finish, with half of exposed surface finished; 50 sq. in. (300 sq. cm) for lumber and 8 by 10 inches (200 by 250 mm) for panels.

          - For foam-plastic moldings, with half of exposed surface finished; 50 sq. in. (300 sq. cm).

          - For each finish system and color of lumber and panel products with factory-applied finish, 50 sq. in. (300 sq. cm) for lumber and 8 by 10 inches (200 by 250 mm) for panels.

      - QUALITY ASSURANCE

        - <Double click to insert sustainable design text for manufacturer qualifications.>

        - <Double click to insert sustainable design text for vendor qualifications.>

      - DELIVERY, STORAGE, AND HANDLING

        - Stack lumber, plywood, and other panels flat with spacers between each bundle to provide air circulation.

          - Protect materials from weather by covering with waterproof sheeting, securely anchored.

          - Provide for air circulation around stacks and under coverings.

        - Deliver interior finish carpentry materials only when environmental conditions comply with requirements specified for installation areas. If interior finish carpentry materials must be stored in other than installation areas, store only where environmental conditions comply with requirements specified for installation areas.

      - FIELD CONDITIONS

        - Environmental Limitations: Do not deliver or install interior finish carpentry materials until building is enclosed and weatherproof, wet-work in space is completed and nominally dry, and HVAC system is operating and maintaining temperature and relative humidity at occupancy levels during the remainder of the construction period.

        - Do not install finish carpentry materials that are wet, moisture damaged, or mold damaged.

          - Indications that materials are wet or moisture damaged include, but are not limited to, discoloration, sagging, or irregular shape.

          - Indications that materials are mold damaged include, but are not limited to, fuzzy or splotchy surface contamination and discoloration.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - MATERIALS, GENERAL

        - <Double click to insert sustainable design text for regional materials.>

        - <Double click to insert sustainable design text for certified wood.>

        - <Double click to insert sustainable design text for composite wood products.>

        - Lumber: DOC PS 20 and applicable rules of grading agencies indicated. If no grading agency is indicated, comply with applicable rules of any rules-writing agency certified by the American Lumber Standard Committee's (ALSC) Board of Review. Grade lumber by an agency certified by the ALSC's Board of Review to inspect and grade lumber under the rules indicated.

          - Factory mark each piece of lumber with grade stamp of grading agency.

          - For exposed lumber, mark grade stamp on end or back of each piece[, or omit grade stamp and provide certificates of grade compliance issued by grading agency].

        - Softwood Plywood: DOC PS 1.

        - Hardboard: ANSI A135.4.

        - MDF: ANSI A208.2, [Grade 130] <Insert grade>.

        - Particleboard: ANSI A208.1, [Grade M-2] [Grade M-2-Exterior Glue].

Retain "Melamine-Faced Particleboard" Paragraph below if required for shelving. Product below contains urea formaldehyde.

        - Melamine-Faced Particleboard: Particleboard complying with ANSI A208.1, Grade M-2, finished on both faces with thermally fused, melamine-impregnated decorative paper and complying with ISO 4586-3, Grade VGS.

Retain one option in "Color" Subparagraph below.

          - Color: [White] [Black] [Gray] [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range] <Insert color>.

      - WOOD-PRESERVATIVE-TREATED MATERIALS

See the Evaluations for discussion of preservative formulations. In "Preservative Treatment by Pressure Process" Paragraph below, Use Category UC1 is suitable for interior dry locations; Use Category UC2, for interior damp locations.

        - Preservative Treatment by Pressure Process: AWPA U1; Use Category [UC1] [UC2].

Maximum moisture contents specified in first subparagraph below are standard limits for preservative-treated lumber and plywood that are kiln dried after treatment.

          - Kiln dry lumber and plywood after treatment to a maximum moisture content of 19 and 18 percent, respectively.

See the Evaluations for information about treatment chemicals.

          - Preservative Chemicals: Acceptable to authorities having jurisdiction[ and containing no arsenic or chromium].

          - For exposed items indicated to receive transparent finish, do not use chemical formulations that contain colorants or that bleed through or otherwise adversely affect finishes.

          - Do not use material that is warped or does not comply with requirements for untreated material.

          - Mark lumber with treatment-quality mark of an inspection agency approved by the ALSC's Board of Review.

Retain only first option in first subparagraph below if authorities having jurisdiction require classification marking on all materials.

            - For exposed lumber indicated to receive a stained or natural finish, [mark end or back of each piece] [or] [omit marking and provide certificates of treatment compliance issued by inspection agency].

          - Mark plywood with appropriate classification marking of an inspection agency acceptable to authorities having jurisdiction.

            - For exposed plywood indicated to receive a stained or natural finish, mark back of each piece.

          - Application: [Where indicated on Drawings] [All interior lumber and plywood] <Insert application>.

      - INTERIOR TRIM

        - Softwood Lumber Trim for Transparent Finish (Stain or Clear Finish):

          - Species and Grade:

Verify local availability before retaining species and grade in first seven subparagraphs below. Some grades in subparagraphs are considered "knotty." Other species and grades are available.

            - Eastern white pine; NeLMA or NLGA [C Select] [D Select] [Finish or 1 Common] [Premium or 2 Common].

            - Idaho white, lodgepole, ponderosa, radiata, or sugar pine; NLGA or WWPA [C Select (Choice)] [D Select (Quality)] [1 Common (Colonial)] [2 Common (Sterling)].

Grading rules for eastern white pine are not the same as those for western pine, so requirements in first subparagraph below will vary somewhat among species.

            - Eastern white, Idaho white, lodgepole, ponderosa, radiata, or sugar pine; NeLMA, NLGA, or WWPA [C Select (Choice)] [D Select (Quality)] [Finish or 1 Common (Colonial)] [Premium or 2 Common (Sterling)].

            - White woods; WWPA [C Select] [D Select] [1 Common] [2 Common].

            - Douglas fir-larch or Douglas fir south; NLGA, WCLIB, or WWPA [Superior or C & Btr] [Prime or D] finish.

            - Southern pine; SPIB [B & B] [C & Btr] finish.

            - Western red cedar; NLGA, WCLIB, or WWPA [Clear Heart] [Grade A] [Grade B].

Maximum moisture content for seasoned or kiln-dried, board-size lumber varies, depending on species, grade, and grading agency. See the Evaluations.

          - Maximum Moisture Content: [19] [15] percent[ with at least 85 percent of shipment at 12 percent or less].

          - Finger Jointing: [Allowed] [Not allowed].

          - Face Surface: [Surfaced (smooth)] [Saw textured].

        - Hardwood Lumber Trim for Transparent Finish (Stain or Clear Finish):

Fourth option in "Species and Grade" Subparagraph below includes light-colored, closed-grain species that will take stain; if retaining, delete undesirable species, if any, from list.

          - Species and Grade: [Red oak] [White maple] [Alder] [Aspen, basswood, cottonwood, sap gum, sycamore, white maple, or yellow poplar] <Insert species>; NHLA [Clear] [A Finish] [B Finish].

NHLA does not define any maximum moisture content values for kiln-dried hardwood lumber; purchaser must specify the value. Percentages in "Maximum Moisture Content" Subparagraph below are based on ranges given for optimum moisture content in AWI's "Architectural Woodwork Standards." First option applies to damp coastal areas of the southern United States and the Maritime Provinces. Second option applies to Ontario, Quebec, and most of the United States. Third option applies to the dry southwestern United States and to Alberta, Manitoba, and Saskatchewan.

          - Maximum Moisture Content: [13] [10] [9] <Insert number> percent.

          - Finger Jointing: Not allowed.

          - Gluing for Width: [Allowed] [Not allowed] [Use for lumber trim wider than 6 inches (150 mm)].

          - Veneered Material: [Allowed] [Not allowed] [Use for lumber trim wider than 6 inches (150 mm)].

          - Face Surface: [Surfaced (smooth)] [Saw textured].

          - Matching: Selected for compatible grain and color.

        - Lumber Trim for Opaque Finish (Painted Finish):

          - Species and Grade:

Verify local availability before retaining species and grade in first seven subparagraphs below.

            - Eastern white pine; NeLMA or NLGA [D Select] [Finish or 1 Common] [Premium or 2 Common].

            - Idaho white, lodgepole, ponderosa, radiata, or sugar pine; NLGA or WWPA [D Select (Quality)] [1 Common (Colonial)] [2 Common (Sterling)].

Grading rules for eastern white pine are not the same as those for western pine, so requirements in first subparagraph below will vary somewhat among species.

            - Eastern white, Idaho white, lodgepole, ponderosa, radiata, or sugar pine; NeLMA, NLGA, or WWPA [D Select (Quality)] [Finish or 1 Common (Colonial)] [Premium or 2 Common (Sterling)].

            - White woods; WWPA [D Select] [1 Common] [2 Common].

            - Douglas fir-larch or Douglas fir south; NLGA, WCLIB, or WWPA [Superior or C & Btr] [Prime or D] finish.

            - Spruce-pine-fir; NeLMA, NLGA, WCLIB, or WWPA [1 Common] [2 Common].

            - Alder, aspen, basswood, cottonwood, gum, magnolia, soft maple, sycamore, tupelo, or yellow poplar; NHLA [A Finish] [B Finish].

"Maximum Moisture Content for Softwoods" Subparagraph below is for softwood boards. Maximum moisture content for seasoned or kiln-dried, board-size lumber varies, depending on species, grade, and grading agency. See the Evaluations.

          - Maximum Moisture Content for Softwoods: [19] [15] percent[ with at least 85 percent of shipment at 12 percent or less].

"Maximum Moisture Content for Hardwoods" Subparagraph below is for hardwood boards. NHLA does not define any maximum moisture content values for kiln-dried hardwood lumber; purchaser must specify the value. Percentages in subparagraph are based on ranges given for optimum moisture content in AWI's "Architectural Woodwork Standards." First option applies to damp coastal areas of the southern United States and the Maritime Provinces. Second option applies to Ontario, Quebec, and most of the United States. Third option applies to the dry southwestern United States and to Alberta, Manitoba, and Saskatchewan.

          - Maximum Moisture Content for Hardwoods: [13] [10] [9] <Insert number> percent.

          - Finger Jointing: [Allowed] [Not allowed].

          - Face Surface: [Surfaced (smooth)] [Saw textured].

          - Optional Material: Primed MDF of same actual dimensions as lumber indicated may be used in lieu of lumber.

        - Softwood Moldings for Transparent Finish (Stain or Clear Finish): MMPA WM 4, N-grade wood moldings. Made to patterns included in MMPA's "WM/Series Softwood Moulding Patterns."

          - Species: [Eastern white, Idaho white, lodgepole, ponderosa, radiata, or sugar pine] [Southern pine] [Western red cedar] [Douglas fir] <Insert species>.

Requirement in "Maximum Moisture Content" Subparagraph below is typical requirement of grading agencies for kiln-dried softwood moldings and molding stock.

          - Maximum Moisture Content: 15 percent with at least 85 percent of shipment at 12 percent or less.

          - Finger Jointing: Not allowed.

          - Matching: Selected for compatible grain and color.

Six subparagraphs below are examples of molding patterns that might be specified. Delete all if moldings are sufficiently detailed on Drawings. See MMPA's "WM/Series Softwood Moulding Patterns" for additional patterns.

          - Base Pattern: [WM 623, 9/16-by-3-1/4-inch (14-by-83-mm) ogee] [WM 713, 9/16-by-3-1/4-inch (14-by-83-mm) ranch] [WM 753, 9/16-by-3-1/4-inch (14-by-83-mm) beaded-edge] [WM 620, 9/16-by-4-1/4-inch (14-by-108-mm) ogee] [WM 750, 9/16-by-4-1/4-inch (14-by-108-mm) beaded-edge] base.

          - Shoe-Mold Pattern: [WM 129, 7/16-by-11/16-inch (11-by-17-mm) quarter-round] [WM 126, 1/2-by-3/4-inch (13-by-19-mm) quarter-round] [WM 131, 1/2-by-3/4-inch (13-by-19-mm) ogee] shoe mold.

          - Casing Pattern: [WM 327, 11/16-by-2-1/4-inch (17-by-57-mm) clamshell] [WM 366, 11/16-by-2-1/4-inch (17-by-57-mm) featheredge] [WM 376, 11/16-by-2-1/4-inch (17-by-57-mm) beaded-edge] casing.

          - Mull-Casing Pattern: [WM 957, 3/8-by-1-3/4-inch (9.5-by-44-mm) beaded-edge] [WM 973, 3/8-by-1-3/4-inch (9.5-by-44-mm) bullnose] [WM 983, 3/8-by-1-3/4-inch (9.5-by-44-mm) featheredge] casing.

          - Stop Pattern: [WM 856, 3/8-by-1-3/8-inch (9.5-by-35-mm) ranch] [WM 946, 3/8-by-1-3/8-inch (9.5-by-35-mm) ogee] [WM 886, 3/8-by-1-3/8-inch (9.5-by-35-mm) bullnose] stop.

          - Chair-Rail Pattern: WM 297, 11/16-by-3-inch (17-by-76-mm) chair rail.

        - Hardwood Moldings for Transparent Finish (Stain or Clear Finish): MMPA WM 4, N-grade wood moldings made to patterns included in MMPA's "HWM/Series Hardwood Moulding Patterns."

Third option in "Species" Subparagraph below includes light-colored, closed-grain hardwood species that will take stain; if retaining, delete undesirable species, if any, from list.

          - Species: [Red oak] [White maple] [Aspen, basswood, cottonwood, sap gum, sycamore, white maple, or yellow poplar] <Insert species>.

          - Maximum Moisture Content: 9 percent.

          - Finger Jointing: Not allowed.

          - Matching: Selected for compatible grain and color.

          - Optional Material: Kiln-dried softwood or MDF, with exposed surfaces veneered with species indicated, may be used in lieu of solid wood.

Six subparagraphs below are examples of molding patterns that might be specified. Delete all if moldings are sufficiently detailed on Drawings. See MMPA's "HWM/Series Hardwood Moulding Patterns" for additional patterns.

          - Base Pattern: [HWM 633, 7/16-by-3-1/4-inch (11-by-83-mm) ogee] [HWM 713, 7/16-by-3-1/4-inch (11-by-83-mm) ranch] [HWM 753, 7/16-by-3-1/4-inch (11-by-83-mm) beaded-edge] [WM 620, 7/16-by-4-1/4-inch (11-by-108-mm) ogee] base.

          - Shoe-Mold Pattern: [HWM 129, 7/16-by-11/16-inch (11-by-17-mm) quarter-round] [HWM 126, 1/2-by-3/4-inch (13-by-19-mm) quarter-round] [HWM 131, 1/2-by-3/4-inch (13-by-19-mm) ogee] shoe mold.

          - Casing Pattern: [HWM 328, 1/2-by-2-1/4-inch (13-by-57-mm) clamshell] [HWM 366, 1/2-by-2-1/4-inch (13-by-57-mm) featheredge] [HWM 376, 1/2-by-2-1/4-inch (13-by-57-mm) beaded-edge] casing.

          - Mull-Casing Pattern: [HWM 989, 3/16-by-2-inch (5-by-51-mm) square-edge] [HWM 988, 3/8-by-1-1/2-inch (9.5-by-38-mm) featheredge] [HWM 987, 3/8-by-2-inch (9.5-by-51-mm) featheredge] casing.

          - Stop Pattern: [HWM 856, 3/8-by-1-3/8-inch (9.5-by-35-mm) ranch] [HWM 946, 3/8-by-1-3/8-inch (9.5-by-35-mm) ogee] [HWM 886, 3/8-by-1-3/8-inch (9.5-by-35-mm) bullnose] stop.

          - Chair-Rail Pattern: HWM 297, 11/16-by-3-inch (17-by-76-mm) chair rail.

        - Moldings for Opaque Finish (Painted Finish): Made to patterns included in MMPA's "WM/Series Softwood Moulding Patterns."

          - Softwood Moldings: MMPA WM 4, P grade.

            - Species: [Eastern white, Idaho white, lodgepole, ponderosa, radiata, or sugar pine] <Insert species>.

Requirement in "Maximum Moisture Content" Subparagraph below is typical requirement of grading agencies for kiln-dried softwood moldings and molding stock.

            - Maximum Moisture Content: 15 percent with at least 85 percent of shipment at 12 percent or less.

          - Hardwood Moldings: MMPA WM 4, P-grade.

            - Species: [Aspen, basswood, cottonwood, gum, magnolia, soft maple, tupelo, or yellow poplar] <Insert species>.

            - Maximum Moisture Content: 9 percent.

          - Finger Jointing: [Allowed] [Not allowed].

          - Optional Material: Primed MDF.

Six subparagraphs below are examples of molding patterns that might be specified. Delete all if moldings are sufficiently detailed on Drawings. See MMPA's "WM/Series Softwood Moulding Patterns" or MMPA's "HWM/Series Hardwood Moulding Patterns" for additional patterns.

          - Base Pattern: [WM 623, 9/16-by-3-1/4-inch (14-by-83-mm) ogee] [WM 713, 9/16-by-3-1/4-inch (14-by-83-mm) ranch] [WM 753, 9/16-by-3-1/4-inch (14-by-83-mm) beaded-edge] [WM 620, 9/16-by-4-1/4-inch (14-by-108-mm) ogee] [WM 750, 9/16-by-4-1/4-inch (14-by-108-mm) beaded-edge] base.

          - Shoe-Mold Pattern: [WM 129, 7/16-by-11/16-inch (11-by-17-mm) quarter-round] [WM 126, 1/2-by-3/4-inch (13-by-19-mm) quarter-round] [WM 131, 1/2-by-3/4-inch (13-by-19-mm) ogee] shoe mold.

          - Casing Pattern: [WM 327, 11/16-by-2-1/4-inch (17-by-57-mm) clamshell] [WM 366, 11/16-by-2-1/4-inch (17-by-57-mm) featheredge] [WM 376, 11/16-by-2-1/4-inch (17-by-57-mm) beaded-edge] casing.

          - Mull-Casing Pattern: [WM 957, 3/8-by-1-3/4-inch (9.5-by-44-mm) beaded-edge] [WM 973, 3/8-by-1-3/4-inch (9.5-by-44-mm) bullnose] [WM 983, 3/8-by-1-3/4-inch (9.5-by-44-mm) featheredge] casing.

          - Stop Pattern: [WM 856, 3/8-by-1-3/8-inch (9.5-by-35-mm) ranch] [WM 946, 3/8-by-1-3/8-inch (9.5-by-35-mm) ogee] [WM 886, 3/8-by-1-3/8-inch (9.5-by-35-mm) bullnose] stop.

          - Chair-Rail Pattern: WM 297, 11/16-by-3-inch (17-by-76-mm) chair rail.

        - PVC-Wrapped Moldings: MMPA WM 2 and made to patterns included in MMPA's "WM/Series Softwood Moulding Patterns."

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

First six subparagraphs below are examples of molding patterns that might be specified; verify availability before retaining. Delete all if moldings are sufficiently detailed on Drawings. See MMPA's "WM/Series Softwood Moulding Patterns" for additional patterns.

          - Base Pattern: [WM 623, 9/16-by-3-1/4-inch (14-by-83-mm) ogee] [WM 713, 9/16-by-3-1/4-inch (14-by-83-mm) ranch] base.

          - Shoe-Mold Pattern: [WM 129, 7/16-by-11/16-inch (11-by-17-mm) quarter-round] [WM 126, 1/2-by-3/4-inch (13-by-19-mm) quarter-round] shoe mold.

          - Casing Pattern: [WM 327, 11/16-by-2-1/4-inch (17-by-57-mm) clamshell] [WM 366, 11/16-by-2-1/4-inch (17-by-57-mm) featheredge] casing.

          - Mull-Casing Pattern: [WM 973, 3/8-by-1-3/4-inch (9.5-by-44-mm) bullnose] [WM 983, 3/8-by-1-3/4-inch (9.5-by-44-mm) featheredge] casing.

          - Stop Pattern: [WM 856, 3/8-by-1-3/8-inch (9.5-by-35-mm) ranch] [WM 886, 3/8-by-1-3/8-inch (9.5-by-35-mm) bullnose] stop.

          - Chair-Rail Pattern: WM 297, 11/16-by-3-inch (17-by-76-mm) chair rail.

Retain one of three options in "Colors, Textures, and Grain Patterns" Subparagraph below; if retaining first, indicate colors, textures, and patterns in additional subparagraphs.

          - Colors, Textures, and Grain Patterns: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

        - Foam-Plastic Moldings: Molded product of shapes indicated, with a tough outer skin on exposed surfaces; factory primed. Exposed surfaces are not to be shaped after molding.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Requirements in "Density," "Flame-Spread Index," "Thickness," and "Width" subparagraphs below are based on requirements in the IBC for foam-plastic trim. Note that the IBC restricts such trim to not more than 10 percent of the wall and ceiling area of room or space in which it is installed.

          - Density: Not less than 20 lb/cu. ft. (320 kg/cu. m).

          - Flame-Spread Index: Not more than [75] <Insert number> when tested according to ASTM E84.

          - Thickness: Not more than 1/2 inch (12.7 mm).

          - Width: Not more than 8 inches (204 mm).

Retain "Patterns" Subparagraph below or insert subparagraphs for various types of moldings required (such as crown molding, picture molding, and so forth). If retaining first option, include patterns in additional subparagraphs.

          - Patterns: [As indicated by manufacturer's designations] [Match Architect's samples].

      - PANELING

Revise "Hardwood Veneer Plywood Paneling" Paragraph below for softwood veneer if required.

        - Hardwood Veneer Plywood Paneling: Manufacturer's stock hardwood plywood panels complying with HPVA HP-1.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

First six subparagraphs below are examples only. Revise to suit Project.

          - Face Veneer Species and Cut: [Rotary-cut white birch] [Plain-sliced red oak] [Plain-sliced hickory] <Insert species and cut>.

          - Veneer Matching: [Random match] [Selected for similar color and grain].

          - Backing Veneer Species: [Same species as face veneer] [Any hardwood compatible with face species].

          - Construction: Veneer core.

          - Thickness: [1/8 inch (3.2 mm)] [5/32 inch (4 mm)] [3/16 inch (5 mm)] [1/4 inch (6.4 mm)] [5/16 inch (7.9 mm)] [7/16 inch (11 mm)].

          - Panel Size:

            - [48 by 96 inches (1219 by 2438 mm)] [48 by 120 inches (1219 by 3048 mm)].

Options in first subparagraph below are true SI (metric) sizes; verify availability before specifying. Panel width must be coordinated with stud spacing and will affect groove spacing.

            - [1200 by 2400 mm] [1200 by 3000 mm].

          - Glue Bond: Type II (interior).

Patterns in "Face Pattern" Subparagraph below are typical; others are available. Retain either option or revise to suit product.

          - Face Pattern: Manufacturer's standard [V] [channel]-grooved pattern, with grooves at edges, center, and third points of panels, and at other locations to provide pattern resembling random-width boards.

Retain one of four options in "Finish" Subparagraph below or revise if unfinished paneling is required. If retaining second, indicate finishes in additional subparagraphs.

          - Finish: [Manufacturer's standard, transparent, UV-resistant, protective finish] [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

        - Hardboard Paneling: Interior factory-finished hardboard paneling complying with ANSI A135.5.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Thickness: [1/8 inch (3.2 mm)] [5/32 inch (4 mm)] [1/4 inch (6.4 mm)].

Class I finishes have greater resistance to abrasion, fading, heat, humidity, scrape adhesion, and steam than Class II.

          - Finish: [Class I] [Class II].

"Surface-Burning Characteristics" Subparagraph below is an example only. Retain or revise to suit finish class and products.

          - Surface-Burning Characteristics: As follows, tested according to ASTM E84:

            - Flame-Spread Index: 25 or less.

            - Smoke-Developed Index: 450 or less.

Retain one of three options in "Colors, Textures, and Patterns" Subparagraph below; if retaining first, indicate colors, textures, and patterns in additional subparagraphs.

          - Colors, Textures, and Patterns: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

"Board Paneling, MMPA" Paragraph below is a generic specification for wood-board paneling. Delete and retain "Board Paneling" Paragraph below if other grades and patterns, such as SPIB's or WWPA's, are used.

        - Board Paneling, MMPA: Interior wood-board paneling complying with MMPA WM 9.

Retain one of four options in "Species" Subparagraph below or revise to suit Project.

          - Species: [Eastern white, Idaho white, lodgepole, ponderosa, radiata, or sugar pine] [Southern pine] [Western red cedar] [Figured red gum] <Insert species>.

Retain one of five options in "Grade" Subparagraph below.

          - Grade: [Clear No. 1] [Clear No. 2] [Knotty No. 1] [Knotty No. 2] [Finger jointed].

First option in "Maximum Moisture Content" Subparagraph below is typical requirement of grading agencies for kiln-dried softwood moldings and molding stock. Second option is based on MMPA requirement for hardwood moldings.

          - Maximum Moisture Content: [15 percent with at least 85 percent of shipment at 12 percent or less] [9 percent].

Retain one of four options in "Pattern" Subparagraph below or revise to suit Project. See MMPA WM 9.

          - Pattern: [V-joint, tongue and groove, PT 82] [Beaded ceiling, PT 85] [Beveled-edge channel, shiplapped, PT 82] [As indicated].

Sizes in "Net Coverage Width" Subparagraph below represent 6-, 8-, and 10-inch (150-, 200-, 254-mm) nominal widths.

          - Net Coverage Width: Not less than [5-1/16 inches (128 mm)] [6-3/4 inches (171 mm)] [8-3/4 inches (222 mm)].

Retain "Board Paneling" Paragraph below for softwood paneling graded according to, and made to, patterns of lumber-grading agencies.

        - Board Paneling:

          - Species and Grade:

            - Eastern white pine; NeLMA or NLGA [C Select] [D Select] [Finish or 1 Common] [Premium or 2 Common].

            - Idaho white, lodgepole, ponderosa, radiata, or sugar pine; NLGA or WWPA [C Select (Choice)] [D Select (Quality)] [1 Common (Colonial)] [2 Common (Sterling)].

Grading rules for eastern white pine are not the same as those for western pine, so requirements in first subparagraph below will vary somewhat among species.

            - Eastern white, Idaho white, lodgepole, ponderosa, radiata, or sugar pine; NeLMA, NLGA, or WWPA [C Select (Choice)] [D Select (Quality)] [Finish or 1 Common (Colonial)] [Premium or 2 Common (Sterling)].

            - Southern pine; SPIB [B & B] [C & Btr] [No. 2] Paneling.

            - Western red cedar; NLGA, WCLIB, or WWPA [Clear Heart] [Grade A] [Grade B].

Maximum moisture content for seasoned or kiln-dried, board-size lumber varies, depending on species, grade, and grading agency. See the Evaluations.

          - Maximum Moisture Content: [19] [15] percent[ with at least 85 percent of shipment at 12 percent or less].

          - Pattern:

Retain one of first four subparagraphs below or revise to suit Project.

            - V-joint, tongue and groove, [NeLMA EWP 4] [SPIB SPP 54] [or] [WWPA WP 4].

            - Pickwick, tongue and groove, [NeLMA EWP 2] [SPIB SPP 52] [or] [WWPA WP 2].

            - Rounded-edge channel groove, tongue and groove, [SPIB SPP 60] [or] [WWPA WP 6].

            - Edge and center bead, tongue and groove, [NeLMA E & CB] [or] [WWPA E & CB Ceiling].

Sizes in "Net Coverage Width" Subparagraph below represent 6-, 8-, and 10-inch (150-, 200-, 254-mm) nominal widths.

          - Net Coverage Width: Not less than [5-1/16 inches (128 mm)] [6-3/4 inches (171 mm)] [8-3/4 inches (222 mm)].

      - SHELVING AND CLOTHES RODS

Copy "Shelving" Paragraph below and re-edit as needed to describe different categories of shelving required. Consider specifying only wood-board or plywood shelving instead of particleboard or MDF as a way of eliminating urea formaldehyde.

        - Shelving: [Exposed] [Closet] [Utility] shelving, made from [the following material] [one of the following materials], 3/4 inch (19 mm) thick:

          - Particleboard with [radiused and filled] [or] [solid-wood] front edge.

          - MDF with [radiused] [or] [solid-wood] front edge.

          - MDO softwood plywood with solid-wood edge.

          - Melamine-faced particleboard with [radiused and filled] [applied-PVC] front edge.

          - Wood boards as specified above for [lumber trim for opaque] [softwood lumber trim for transparent] [hardwood lumber trim for transparent] finish.

If not retaining lumber trim paragraphs in "Interior Trim" Article, "Softwood Boards" Subparagraph below can be used to specify board shelving. Revise species and grade below, if required, by copying from lumber trim paragraphs in "Interior Trim" Article.

          - Softwood Boards:

            - Kiln-dried eastern white, Idaho white, lodgepole, ponderosa, radiata, or sugar pine; NeLMA, NLGA, or WWPA [C Select (Choice)] [D Select (Quality)] [Finish or 1 Common (Colonial)] [Premium or 2 Common (Sterling)].

            - Kiln-dried Douglas fir-larch, Douglas fir south, or hem-fir; SPIB [Superior or C & Btr] [Prime or D] finish; NLGA, WCLIB, or WWPA; or southern pine; [B & B] [C] finish.

        - Shelf Cleats: [3/4-by-3-1/2-inch (19-by-89-mm) boards] [3/4-by-5-1/2-inch (19-by-140-mm) boards] [3/4-by-5-1/2-inch (19-by-140-mm) boards with hole and notch to receive clothes rods], as specified above for [shelving] [lumber trim for opaque finish] [softwood lumber trim for transparent finish] [hardwood lumber trim for transparent finish].

        - Shelf Brackets with Rod Support: BHMA A156.16, B04051; prime-painted formed steel.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Shelf Brackets without Rod Support: BHMA A156.16, B04041; prime-painted formed steel.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Standards for Adjustable Shelf Brackets: BHMA A156.9, B04102; [powder-coat-finished] [brass-finished] [zinc-plated] steel.

        - Adjustable Shelf Brackets: BHMA A156.9, B04112; [powder-coat-finished steel] [brass-finished steel] [zinc-plated steel] [bronze-anodized aluminum] [black-anodized aluminum] [natural aluminum].

        - Standards for Adjustable Shelf Supports: BHMA A156.9, B04071; [powder-coat-finished] [brass-finished] [zinc-plated] steel.

        - Adjustable Shelf Supports: BHMA A156.9, B04081 or B04091; [powder-coat-finished] [brass-finished] [zinc-plated] steel.

        - Wood Clothes Rods: 1-1/2-inch- (38-mm-) diameter, clear, kiln-dried [hardwood] [Douglas fir or southern pine].

        - Metal Clothes Rods: 1-5/16-inch- (33-mm-) diameter, [aluminum tubes] [chrome-plated-steel tubes] [color-coated-steel tubes] [stainless steel tubes] [chrome-plated-steel telescoping tubes with end brackets for mounting on shelf cleats].

Retain "Wood Rod Flanges" or "Metal Rod Flanges" Paragraph below if applicable.

        - Wood Rod Flanges: Clear, kiln-dried, [Douglas fir or southern pine] [eastern white, Idaho white, lodgepole, ponderosa, radiata, or sugar pine] [red oak] [white maple] [aspen, basswood, cottonwood, sap gum, white maple, or yellow poplar] <Insert species> turnings[ with clear finish].

        - Metal Rod Flanges: [Aluminum] [Chrome-plated steel] [Stainless steel].

      - MISCELLANEOUS MATERIALS

Retain materials in this article to suit Project.

        - Fasteners for Interior Finish Carpentry: Nails, screws, and other anchoring devices of type, size, material, and finish required for application indicated to provide secure attachment, concealed where possible.

Aliphatic-resin glues in "Glue" Paragraph below are sold as "carpenter's wood glue"; polyurethane, as "gorilla glue"; and resorcinol glues, as "waterproof plastic resin glue."

        - Glue: Aliphatic-resin, polyurethane, or resorcinol wood glue recommended by manufacturer for general carpentry use.

          - <Double click to insert sustainable design text for low emitting adhesives.>

          - <Double click to insert sustainable design text for VOC content of Wood Glue.>

Retain "Installation Adhesive for Foam-Plastic Moldings" Paragraph below if required.

        - Installation Adhesive for Foam-Plastic Moldings: Product recommended for indicated use by foam-plastic molding manufacturer.

          - <Double click to insert sustainable design text for VOC content of plastic foam adhesive.>

          - <Double click to insert sustainable design text for low emitting adhesives.>

        - Paneling Adhesive: Comply with paneling manufacturer's written instructions for adhesives.

          - <Double click to insert sustainable design text for VOC content of adhesive.>

          - <Double click to insert sustainable design text for low emitting adhesives.>

Retain "Multipurpose Construction Adhesive" Paragraph below if required.

        - Multipurpose Construction Adhesive: Formulation, complying with ASTM D3498, that is recommended for indicated use by adhesive manufacturer.

          - <Double click to insert sustainable design text for VOC content of adhesive.>

          - <Double click to insert sustainable design text for low emitting adhesives.>

      - FABRICATION

        - Back out or kerf backs of the following members, except those with ends exposed in finished work:

          - Interior standing and running trim, except shoe and crown molds.

          - Wood-board paneling.

Revise paragraph below to describe conditions where eased edges are required. Delete if eased edges are not required.

        - Ease edges of lumber less than 1 inch (25 mm) in nominal thickness to 1/16-inch (1.5-mm) radius and edges of lumber 1 inch (25 mm) or more in nominal thickness to 1/8-inch (3-mm) radius.

- EXECUTION

      - EXAMINATION

        - Examine substrates, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of the Work.

        - Examine finish carpentry materials before installation. Reject materials that are wet, moisture damaged, and mold damaged.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Clean substrates of projections and substances detrimental to application.

        - Before installing interior finish carpentry, condition materials to average prevailing humidity in installation areas for a minimum of 24 hours[ unless longer conditioning is recommended by manufacturer].

      - INSTALLATION, GENERAL

        - Do not use materials that are unsound; warped; improperly treated or finished; inadequately seasoned; too small to fabricate with proper jointing arrangements; or with defective surfaces, sizes, or patterns.

        - Install interior finish carpentry level, plumb, true, and aligned with adjacent materials.

          - Use concealed shims where necessary for alignment.

          - Scribe and cut interior finish carpentry to fit adjoining work. Refinish and seal cuts as recommended by manufacturer.

          - Where face fastening is unavoidable, countersink fasteners, fill surface flush, and sand unless otherwise indicated.

Revise tolerances in first subparagraph below to suit Project.

          - Install to tolerance of 1/8 inch in 96 inches (3 mm in 2438 mm) for level and plumb. Install adjoining interior finish carpentry with 1/32-inch (0.8-mm) maximum offset for flush installation and 1/16-inch (1.5-mm) maximum offset for reveal installation.

          - Coordinate interior finish carpentry with materials and systems in or adjacent to it. Provide cutouts for mechanical and electrical items that penetrate interior finish carpentry.

      - INSTALLATION OF INTERIOR TRIM

        - Install trim with minimum number of joints as is practical, using full-length pieces from maximum lengths of lumber available.

          - Do not use pieces less than 24 inches (610 mm) long, except where necessary.

          - Stagger joints in adjacent and related standing and running trim.

          - [Cope] [Miter] at returns, miter at outside corners, and cope at inside corners to produce tight-fitting joints with full-surface contact throughout length of joint.

          - Use scarf joints for end-to-end joints.

          - Plane backs of casings to provide uniform thickness across joints where necessary for alignment.

Consider deleting first subparagraph below. Match of color and grain is subject to interpretation; below may be difficult to enforce.

          - Match color and grain pattern of trim for transparent finish (stain or clear finish) across joints.

          - Install trim after gypsum-board joint finishing operations are completed.

          - Install without splitting; drill pilot holes before fastening where necessary to prevent splitting.

          - Fasten to prevent movement or warping.

          - Countersink fastener heads on exposed carpentry work and fill holes.

      - INSTALLATION OF PANELING

Retain paneling types in this article to suit Project.

        - Plywood Paneling: Select and arrange panels on each wall to minimize noticeable variations in grain character and color between adjacent panels.

          - Leave 1/4-inch (6-mm) gap to be covered with trim at top, bottom, and openings.

          - Install with uniform tight joints between panels.

          - Attach panels to supports with manufacturer's recommended panel adhesive and fasteners.

          - Space fasteners and adhesive as recommended by panel manufacturer.

          - Conceal fasteners to greatest practical extent.

Retain subparagraph below if using grooved panels.

          - Arrange panels with grooves and joints over supports.

            - Fasten to supports with nails of type and at spacing recommended by panel manufacturer.

            - Use fasteners with prefinished heads matching groove color.

        - Hardboard Paneling: Install according to manufacturer's written instructions.

          - Leave 1/4-inch (6-mm) gap to be covered with trim at top, bottom, and openings.

          - Butt adjacent panels with moderate contact.

          - Use fasteners with prefinished heads matching paneling color.

Retain "Wood Stud or Furring Substrate" and "Plaster or Gypsum-Board Substrate" subparagraphs below if required.

          - Wood Stud or Furring Substrate: Install with 1-inch (25-mm) annular-ring shank hardboard nails.

          - Plaster or Gypsum-Board Substrate: Install with 1-5/8-inch (41-mm) annular-ring shank hardboard nails.

          - Nailing: Space nails 4 inches (100 mm) o.c. at panel perimeter and 8 inches (200 mm) o.c. at intermediate supports unless otherwise required by manufacturer.

        - Board Paneling: Install according to manufacturer's written instructions.

          - Arrange in random-width pattern suggested by manufacturer unless boards or planks are of uniform width.

Retain first subparagraph below if end joints are unacceptable; second subparagraph, if acceptable.

          - Install in full lengths without end joints.

          - Stagger end joints in random pattern to uniformly distribute joints on each wall.

Retain one of first two subparagraphs below if retaining last subparagraph above. First below is for tongue-and-groove pattern; second, for other patterns.

          - Install with uniform end joints with only end-matched (tongue-and-groove) joints within each field of paneling.

          - Install with uniform end joints. Locate end joints only over furring or blocking.

          - Select and arrange boards on each wall to minimize noticeable variations in grain character and color between adjacent boards.

          - Install with uniform tight joints between boards.

Retain one of five subparagraphs below.

          - Fasten paneling by face nailing, setting nails, and filling over nail heads.

          - Fasten paneling with trim screws, set below face and filled.

          - Fasten paneling by blind nailing through tongues.

          - Fasten paneling with paneling system manufacturer's concealed clips.

          - Fasten paneling to gypsum wallboard with panel adhesive.

      - INSTALLATION OF SHELVING AND CLOTHES RODS

        - Cut shelf cleats at ends of shelves about 1/2 inch (13 mm) less than width of shelves and sand exposed ends smooth.

          - Install shelf cleats by fastening to framing or backing with finish nails or trim screws, set below face and filled.

          - Space fasteners not more than 16 inches (400 mm) o.c.[ Use two fasteners at each framing member or fastener location for cleats 4 inches nominal (89 mm actual) in width and wider.]

Retain first subparagraph below if required.

          - Apply a bead of multipurpose construction adhesive to back of shelf cleats before installing.

          - Remove adhesive that is squeezed out after fastening shelf cleats in place.

        - Install shelf brackets according to manufacturer's written instructions, spaced not more than [32 inches (800 mm)] [36 inches (900 mm)] o.c. Fasten to framing members, blocking, or metal backing, or use toggle bolts or hollow wall anchors.

        - Install standards for adjustable shelf supports according to manufacturer's written instructions. Fasten to framing members, blocking, or metal backing, or use toggle bolts or hollow wall anchors. Space fasteners not more than 12 inches (300 mm) o.c.

        - Install standards for adjustable shelf brackets according to manufacturer's written instructions, spaced not more than 36 inches (900 mm) o.c. and within 6 inches (150 mm) of ends of shelves. Fasten to framing members, blocking, or metal backing, or use toggle bolts or hollow wall anchors.

        - Cut shelves to neatly fit openings with only enough gap to allow shelves to be removed and reinstalled.

          - Install shelves, fully seated on cleats, brackets, and supports.

Retain first subparagraph below if shelves do not need to be removed for painting.

          - Fasten shelves to cleats with finish nails or trim screws, set flush.

Usually retain subparagraph below so shelves provide lateral support for shelf brackets.

          - Fasten shelves to brackets to comply with bracket manufacturer's written instructions.

        - Install rod flanges for rods as indicated.

          - Fasten to shelf cleats, framing members, blocking, or metal backing, or use toggle bolts or hollow wall anchors.

          - Install rods in rod flanges.

      - ADJUSTING

        - Replace interior finish carpentry that is damaged or does not comply with requirements.

          - Interior finish carpentry may be repaired or refinished if work complies with requirements and shows no evidence of repair or refinishing.

        - Adjust joinery for uniform appearance.

      - CLEANING

        - Clean interior finish carpentry on exposed and semiexposed surfaces.

        - Restore damaged or soiled areas and touch up factory-applied finishes if any.

      - PROTECTION

        - Protect installed products from damage from weather and other causes during construction.

        - Remove and replace finish carpentry materials that are wet, moisture damaged, and mold damaged.

          - Indications that materials are wet or moisture damaged include, but are not limited to, discoloration, sagging, or irregular shape.

          - Indications that materials are mold damaged include, but are not limited to, fuzzy or splotchy surface contamination and discoloration.

END OF SECTION 062023