Copyright 2021 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 064400 - ORNAMENTAL WOODWORK

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

MasterSpec includes provisions for LEED 2009, LEED v4, LEED v4.1, IgCC, and Green Globes. Sustainable design requirements may be inserted in the Section Text using the hypertext links.

Review requirements of the Architectural Woodwork Institute (AWI), Architectural Woodwork Manufacturers Association of Canada (AWMAC), and Woodwork Institute's (WI) Architectural Woodwork Standards before revising this Section.

- GENERAL

      - SUMMARY

        - Section Includes:

Revise list below to suit Project.

          - Exterior ornamental woodwork for transparent finish.

          - Exterior ornamental woodwork for opaque finish.

          - Interior ornamental woodwork for transparent finish.

          - Interior ornamental woodwork for opaque finish.

          - Wood furring, blocking, shims, and hanging strips for installing ornamental woodwork items that are not concealed within other construction.

          - Shop priming of exterior ornamental woodwork.

          - Shop priming of interior ornamental woodwork.

          - Shop finishing of exterior ornamental woodwork.

          - Shop finishing of interior ornamental woodwork.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - [Section 061000 "Rough Carpentry"] [Section 061052 "Miscellaneous Rough Carpentry"] for wood furring, blocking, shims, and hanging strips required for installing ornamental woodwork that are concealed within other construction before ornamental woodwork installation.

          - Section 062013 "Exterior Finish Carpentry" for exterior carpentry exposed to view that is not specified in this Section.

          - Section 062023 "Interior Finish Carpentry" for interior carpentry exposed to view that is not specified in this Section.

      - COORDINATION

        - Coordinate sizes and locations of framing, blocking, furring, reinforcements, and other related units of Work specified in other Sections, to ensure that interior ornamental woodwork can be supported and installed as indicated.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

      - ACTION SUBMITTALS

Action submittals are submittals requiring responsive action and return of reviewed documents to Contractor.

        - Product Data: For the following:

          - Composite wood products.

          - Fire-retardant-treated materials.

          - Finishing materials and processes.

Retain "Wood-Preservative Treatment" Subparagraph below if required.

          - Wood-Preservative Treatment:

            - Include data and warranty from chemical-treatment manufacturer and certification by treating plant that treated materials to comply with requirements.

            - Indicate type of preservative used and net amount of preservative retained.

            - Include chemical-treatment manufacturer's written instructions for finishing treated material and manufacturer's written warranty.

Retain "Fire-Retardant Treatment" Subparagraph below if required.

          - Fire-Retardant Treatment: Include data and warranty information from chemical-treatment manufacturer and certification by treating plant that treated materials to comply with requirements.

          - Waterborne Treatments: For products receiving a waterborne treatment, Include statement that moisture content of treated materials was reduced to levels specified before shipment to Project site.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for recycled content.>

          - <Double click to insert sustainable design text for regional materials.>

          - <Double click to insert sustainable design text for certified wood.>

          - <Double click to insert sustainable design text for adhesives.>

          - <Double click to insert sustainable design text for composite wood.>

        - Shop Drawings: Show location of each item, including the following:

          - Dimensioned plans, elevations, and sections.

          - Attachment devices, and other components.

Retain first subparagraph below only for ornate, complex, or very high-quality work.

          - Show [large-scale] [full-size] details.

          - Show locations and sizes of furring, blocking, and hanging strips, including blocking and reinforcement concealed by construction and specified in other Sections.

          - Show veneer leaves with dimensions, grain direction, exposed face, and identification numbers indicating the flitch and sequence within the flitch for each leaf.

Retain subparagraph below and applicable option if retaining other requirements for AWI's or WI's quality certification programs.

          - Apply [AWI Quality Certification] [WI Certified Compliance] Program label to Shop Drawings.

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples.

        - Samples: For each exposed product and for each shop-applied color and finish specified.

          - Size:

            - Panel Products: 12 inches by 12 inches (300 mm by 300 mm).

            - Lumber Products: Not less than [5 inches (125 mm) wide by 12 inches (300 mm) long] [5 inches (125 mm) wide by 24 inches (600 mm) long], for each species and cut, finished on one side and one edge.

        - Samples for Initial Selection: For each type of shop-applied exposed finish.

          - Size:

            - Panel Products: 12 inches by 12 inches (300 mm by 300 mm).

            - Lumber Products: Not less than [5 inches (125 mm) wide by 12 inches (300 mm) long] [5 inches (125 mm) wide by 24 inches (600 mm) long], for each species and cut, finished on one side and one edge.

        - Samples for Verification:

Retain "Lumber for Exterior Wood-Stain Finish," "Lumber for Transparent Finish," "Veneer Leaves," and "Lumber and Panel Products with Shop-Applied Opaque Finish" subparagraphs below to control grain character, color, and finish, or insert other subparagraphs to suit Project. The Architectural Woodwork Standards require samples to be "as wide as practical" by 12 inches (300 mm) long for lumber and 12 by 12 inches (300 by 300 mm) for panel products.

          - Lumber for Exterior Wood-Stain Finish: Not less than 5 inches (125 mm) wide by 12 inches (300 mm) long, for each species, with one-half of exposed surface finished.

          - Lumber for Transparent Finish: Not less than [5 inches (125 mm) wide by 12 inches (300 mm) long] [5 inches (125 mm) wide by 24 inches (600 mm) long], for each species and cut, finished on one side and one edge.

          - Veneer Leaves: Representative of and selected from flitches to be used for transparent-finished ornamental woodwork.

          - Lumber and Panel Products with Shop-Applied Opaque Finish: 5 inches (125 mm) wide by 12 inches (300 mm) long for lumber and [8 by 10 inches (200 by 250 mm)] [12 by 12 inches (300 by 300 mm)] for panels, for each finish system and color, with[ one-half of] exposed surface finished.

            - Finish [entire] [one-half of] exposed surface.

      - INFORMATIONAL SUBMITTALS

Informational submittals are submittals that require review by Architect, but they do not require Architect's responsive action and return of reviewed documents to Contractor, provided submittals comply with requirements. If rejected, submittals with responsive action must be returned to Contractor.

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

        - Qualification Data: For [ornamental woodwork manufacturer] [and] [Installer].

        - Product Certificates: For [each type of product.] [the following:]

          - Composite wood products.

          - Adhesives.

Retain "Evaluation Reports" Paragraph below for preservative-treated or fire-retardant-treated wood materials.

        - Evaluation Reports: For [wood-preservative-treated] [and] [fire-retardant-treated] wood materials, from ICC-ES.

Retain "Field quality-control reports" Paragraph below if AWI or WI field inspection are retained under Part 3 "Field Quality Control" Article. Typically, AWI and WI do not perform inspections for every "certified" project. If field inspection is required, the Architect and Contractor have the option to request these inspections at any time, at no cost to the Owner or Architect.

        - Field quality-control reports.

      - CLOSEOUT SUBMITTALS

Retain "Quality Standard Compliance Certificates" Paragraph below only if retaining requirements for AWI's Quality Certification Program or WI's Certified Compliance Program.

        - Quality Standard Compliance Certificates: [AWI Quality Certification Program] [WI Certified Compliance Program] certificates.

      - QUALITY ASSURANCE

        - Manufacturer's Qualifications: Employs skilled workers who custom fabricate products similar to those required for this Project and whose products have a record of successful in-service performance.

Retain "Manufacturer's Certification" Subparagraph below if AWI Quality Certification Program or WI Certified Compliance Program is required. Both AWI and WI will inspect work and provide certification for work that passes inspection if manufacturer is not licensed under their respective programs.

          - Manufacturer's Certification: Licensed participant in [AWI's Quality Certification Program] [WI's Certified Compliance Program].

Retain "Installer Qualifications" Paragraph below if required. If AWI Quality Certification Program labels or certificates are required for installation, Installer must be a certified participant. If woodwork must be FSC certified, ornamental woodwork manufacturer must either install woodwork or be FSC certified for chain of custody.

        - Installer Qualifications: [Manufacturer of products] [and] [Licensed participant in AWI's Quality Certification Program] [Licensed participant in WI's Certified Compliance Program].

        - Mockups: Build mockups to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for materials and execution.

          - Build mockups of <Insert description>.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Owner specifically approves such deviations by Change Order.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Comply with Architectural Woodwork Standards, Section 2.

        - Do not deliver interior ornamental woodwork until painting and similar operations that could damage woodwork have been completed in installation areas.

        - Store woodwork in installation areas or in areas where environmental conditions comply with requirements specified in "Field Conditions" Article.

          - Handle and store fire-retardant-treated wood to comply with chemical-treatment manufacturer's written instructions.

      - FIELD CONDITIONS

Requirements in "Weather Limitations for Exterior Work" Paragraph below may not be realistic for Project location. Consider deleting and including requirement in Part 2 for shop priming to protect ornamental woodwork until it can be finished.

        - Weather Limitations for Exterior Work: Proceed with installation of exterior ornamental woodwork only when existing and forecasted weather conditions permit work to be performed and at least one coat of specified finish is to be applied without exposure to rain, snow, or dampness.

Retain "Environmental Limitations for Interior Work without Humidity Control" Paragraph below if relative humidity will not be controlled after building is occupied.

        - Environmental Limitations for Interior Work without Humidity Control: Do not deliver or install interior ornamental woodwork until building is enclosed, wet work is complete, and HVAC system is operating and maintaining temperature and relative humidity at levels designed for building occupancy for the remainder of the construction period.

Retain "Environmental Limitations for Interior Work with Humidity Control" Paragraph below if relative humidity will be controlled after building is occupied, and retain one of three options or insert another range based on local climatological data. Three ranges given are for painted or finished woodwork. First applies to Ontario, Quebec, and most of the United States. Second applies to damp coastal areas of southern United States and the Maritime Provinces. Third applies to dry southwestern United States and to Alberta, Manitoba, and Saskatchewan. For unfinished woodwork, narrower ranges will be required to maintain optimum moisture content. See relative-humidity and moisture-content map in the Architectural Woodwork Standards.

        - Environmental Limitations for Interior Work with Humidity Control: Do not deliver or install interior ornamental woodwork until building is enclosed, wet-work is complete, and HVAC system is operating and maintaining temperature between 60 and 90 deg F (16 and 32 deg C) and relative humidity between [25 and 55] [43 and 70] [20 and 50] <Insert humidity range> percent during the remainder of the construction period.

Retain "Field Measurements" or "Established Dimensions" Paragraph below. Establishing dimensions allows woodwork fabrication to begin before installation areas are complete.

        - Field Measurements: Where ornamental woodwork is indicated to fit to other construction, verify dimensions of other construction by field measurements before fabrication, and indicate measurements on Shop Drawings.

          - Locate concealed framing, blocking, and reinforcements that support woodwork by field measurements before being concealed by construction, and indicate measurements on Shop Drawings.

        - Established Dimensions: Where ornamental woodwork is indicated to fit to other construction, establish dimensions for areas where woodwork is to fit. Provide allowance for trimming at site, and coordinate construction to ensure that actual dimensions correspond to established dimensions.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - ORNAMENTAL WOODWORK MANUFACTURERS

Retain this article if a list of preapproved ornamental woodwork manufacturers is used as a quality-control procedure. See the Evaluations. See AWI's or WI's member list for names of woodworking firms.

        - Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

          - <Insert in separate subparagraphs, names of preapproved ornamental woodworking firms>.

      - ORNAMENTAL WOODWORK, GENERAL

The Section Text is based on the AWI Architectural Woodwork Standards. The Section Text can be revised to incorporate the North American Architectural Woodwork Standards. See the Evaluations.

        - Quality Standard: Unless otherwise indicated, comply with the Architectural Woodwork Standards for grades of ornamental woodwork indicated for construction, finishes, installation, and other requirements.

If retaining first subparagraph below, verify applicability of certification for Project's geographic location. AWI has licensed manufacturers throughout the United States. WI primarily has licensed manufacturers in California and other west coast states. Certification programs of AWI and WI are available to member and nonmember firms. Both AWI and WI will inspect work and provide certification for work that passes inspection if ornamental woodwork manufacturer is not licensed. Contact either organization for a list of licensed manufacturers in Project's location.

          - Provide [labels] [and] [certificates] from [AWI] [WI] certification program indicating that woodwork[, including installation,] complies with requirements of grades specified.

Retain one of first two subparagraphs below if Project is to be certified under AWI Quality Certification Program.

            - This project has been registered with AWI as AWI Quality Certification Program Number <Insert number>.

            - Contractor is to register the Work under this Section with the AWI Quality Certification Program at www.awiqcp.org or by calling 800-345-0991.

Retain subparagraph below only if Drawings and Specifications are more restrictive than Architectural Woodwork Standards.

          - The Contract Documents contain requirements that are more stringent than the Architectural Woodwork Standards. Comply with Contract Documents and Architectural Woodwork Standards.

        - <Double click to insert sustainable design text for regional wood materials.>

        - <Double click to insert sustainable design text for certified wood.>

      - EXTERIOR ORNAMENTAL WORK FOR TRANSPARENT FINISH

The term "exterior ornamental work" refers to miscellaneous items of woodwork not included in other categories.

        - Exterior ornamental work for transparent finish includes the following:

Revise list below to suit Project.

          - Balustrades.

          - Columns.

          - Cupolas.

          - Pediment heads.

          - Pilasters.

          - <Insert description>.

        - Architectural Woodwork Standards Grade: [Premium] [Custom] [Economy].

        - <Double click to insert sustainable design text for regional wood materials.>

        - <Double click to insert sustainable design text for certified wood.>

Options in "Wood Species" Paragraph below are examples only. Revise to suit Project. See the Evaluations.

        - Wood Species: [Teak] [African mahogany] [All-heart redwood] [Western red cedar] [Ponderosa pine or sugar pine] <Insert species>.

Usually retain subparagraph below if using softwood lumber.

          - Do not use plain-sawn softwood lumber with exposed, flat surfaces more than 3 inches (76 mm) wide.

Retain one of three options in "Wood Moisture Content" Paragraph below. First range applies to Ontario, Quebec, and most of the United States. Second applies to damp coastal areas of southern United States and Maritime Provinces. Third applies to dry southwestern United States, Alberta, Manitoba, and Saskatchewan. See relative-humidity and moisture-content map in the Architectural Woodwork Standards. Some locations have microclimates that differ from the surrounding region.

        - Wood Moisture Content: [9 to 15] [10 to 15] [7 to 12] percent.

      - EXTERIOR ORNAMENTAL WORK FOR OPAQUE FINISH

The term "exterior ornamental work" refers to miscellaneous items of woodwork not included in other categories.

        - Exterior ornamental work for opaque finish includes the following:

Revise list below to suit Project.

          - Balustrades.

          - Columns.

          - Cupolas.

          - Pediment heads.

          - Pilasters.

          - <Insert description>.

        - Architectural Woodwork Standards Grade: [Premium] [Custom] [Economy].

        - <Double click to insert sustainable design text for regional wood materials.>

        - <Double click to insert sustainable design text for certified wood.>

Options in "Wood Species" Paragraph below are examples only. Revise to suit Project. See the Evaluations.

        - Wood Species: [All-heart redwood] [Western red cedar] [Ponderosa pine] [Ponderosa pine or sugar pine] [Eastern white pine, sugar pine, or western white pine] [Any closed-grain hardwood] [Softwood plywood] <Insert species>.

Usually retain subparagraph below if using softwood lumber.

          - Do not use plain-sawn softwood lumber with exposed, flat surfaces more than 3 inches (76 mm) wide.

Retain one of three options in "Wood Moisture Content" Paragraph below. First range applies to Ontario, Quebec, and most of the United States. Second applies to damp coastal areas of southern United States and Maritime Provinces. Third applies to dry southwestern United States, Alberta, Manitoba, and Saskatchewan. See relative-humidity and moisture-content map in the Architectural Woodwork Standards. Some locations have microclimates that differ from the surrounding region.

        - Wood Moisture Content: [9 to 15] [10 to 15] [7 to 12] percent.

      - INTERIOR ORNAMENTAL WORK FOR TRANSPARENT FINISH

        - Interior ornamental work for transparent finish includes the following:

Revise list below to suit Project.

          - Altar.

          - Balustrades.

          - Columns.

          - Grilles.

          - Judge's bench.

          - Lectern.

          - Mantels.

          - Pediment heads.

          - Pilasters.

          - Pulpit.

          - Witness stand.

          - <Insert description>.

        - Architectural Woodwork Standards Grade: [Premium] [Custom] [Economy].

        - <Double click to insert sustainable design text for regional wood materials.>

        - <Double click to insert sustainable design text for certified wood.>

Retain option in "Wood Species and Cut" Paragraph below if ornamental work must match other wood surfaces, such as cabinets or paneling.

        - Wood Species and Cut:[ Match species and cut indicated for other types of transparent-finished ornamental woodwork located in same area of building unless otherwise indicated.]

Options in "Species" and "Cut" subparagraphs below are examples only. Retain one option in each subparagraph, or insert others.

          - Species: [Red oak] [White oak] [White ash] [Hickory] <Insert species>.

          - Cut: [Plain sliced/plain sawn] [Rift cut/rift sawn] [Quarter cut/quarter sawn] [Any cut].

Retain one of three options in "Wood Moisture Content" Paragraph below. First range applies to Ontario, Quebec, and most of the United States. Second applies to damp coastal areas of southern United States and Maritime Provinces. Third applies to dry southwestern United States, Alberta, Manitoba, and Saskatchewan. See relative-humidity and moisture-content map in the Architectural Woodwork Standards. Some locations have microclimates that differ from the surrounding region.

        - Wood Moisture Content: [5 to 10] [8 to 13] [4 to 9] percent.

      - INTERIOR ORNAMENTAL WORK FOR OPAQUE FINISH

        - Interior ornamental work for opaque finish includes the following:

Revise list below to suit Project.

          - Altar.

          - Balustrades.

          - Columns.

          - Grilles.

          - Lectern.

          - Mantels.

          - Pediment heads.

          - Pilasters.

          - Pulpit.

          - <Insert description>.

        - Architectural Woodwork Standards Grade: [Premium] [Custom] [Economy].

        - <Double click to insert sustainable design text for regional wood materials.>

        - <Double click to insert sustainable design text for certified wood.>

For opaque-finished woodwork, closed-grain hardwood is generally a better choice than softwood except for Economy grade.

        - Wood Species: [Any closed-grain hardwood] [Eastern white pine, sugar pine, or western white pine] <Insert species>.

Retain one of three options in "Wood Moisture Content" Subparagraph below. First range applies to Ontario, Quebec, and most of the United States. Second applies to damp coastal areas of southern United States and Maritime Provinces. Third applies to dry southwestern United States, Alberta, Manitoba, and Saskatchewan. See relative-humidity and moisture-content map in Architectural Woodwork Standards. Some locations have microclimates that differ from the surrounding region.

        - Wood Moisture Content: [5 to 10] [8 to 13] [4 to 9] percent.

      - WOOD MATERIALS

        - Composite Wood Products: Provide materials that comply with requirements of the Architectural Woodwork Standards for each type of ornamental woodwork and quality grade specified unless otherwise indicated.

          - <Double click to insert sustainable design text for recycled content.>

        - <Double click to insert sustainable design text for composite wood products.>

          - Medium-Density Fiberboard (MDF): ANSI A208.2, [Grade 130] <Insert grade>.

          - Particleboard: ANSI A208.1, [Grade M-2] [Grade M-2-Exterior Glue].

          - Softwood Plywood: DOC PS 1[, exterior] [, medium-density overlay].

The term "plywood" in "Veneer-Faced Panel Products (Hardwood Plywood)" Subparagraph below refers to a wood-based panel with veneers applied to both faces; core may be made up of veneers (either hardwood or softwood), particleboard, MDF, hardboard, or glued-up lumber.

          - Veneer-Faced Panel Products (Hardwood Plywood): HPVA HP-1.

      - PRESERVATIVE-TREATED WOOD MATERIALS

See the Evaluations for discussion of formulations and requirements of the Architectural Woodwork Standards for preservative treatment. Verify compatibility of preservative treatments with specified finishes.

        - Preservative-Treated Wood Materials: Provide with water-repellent preservative treatment complying with AWPA N1 (dip, spray, flood, or vacuum-pressure treatment).

If necessary, revise "Preservative Chemicals" Subparagraph below after verifying availability and compliance with environmental and regulatory controls in effect at Project location. Retain option if resistance to wood-destroying insects is required.

          - Preservative Chemicals: 3-iodo-2-propynyl butyl carbamate (IPBC)[, combined with a compatible EPA registered insecticide].

          - Use chemical formulations that do not bleed through or otherwise adversely affect finishes. Do not use colorants in solution to distinguish treated material from untreated material.

        - Extent of Preservative Treated Wood Materials: Treat [exterior ornamental woodwork indicated on Drawings] [exterior ornamental woodwork unless otherwise indicated on Drawings] [interior ornamental woodwork in contact with concrete or masonry] <Insert requirements>.

Decay-resistant wood can benefit from treatment with water-repellent preservative. Where subject to termites, decay-resistant wood can also benefit from treatment with an insecticide.

          - Items fabricated from the following wood species need not be treated:

            - [Redwood] [All-heart redwood].

            - [Western red cedar] [All-heart western red cedar].

            - White oak.

            - African mahogany.

            - Honduras mahogany.

            - Ipe.

            - Dark red meranti.

            - Teak.

      - FIRE-RETARDANT-TREATED MATERIALS

If fire-retardant materials are required, verify requirements and acceptability of various materials with authorities having jurisdiction. Verify compatibility of fire-retardant treatments with specified finishes.

        - Fire-Retardant-Treated Materials: Where fire-retardant-treated materials are indicated, use materials complying with requirements in this article that are acceptable to authorities having jurisdiction and with fire-test-response characteristics specified as determined by testing identical products in accordance with test method indicated by a qualified testing agency.

          - Use treated materials that comply with requirements of Architectural Woodwork Standards for the grade specified. Do not use materials that are warped, discolored, or otherwise defective.

          - Use fire-retardant-treatment formulations that do not bleed through or otherwise adversely affect finishes. Do not use colorants to distinguish treated materials from untreated materials.

          - Identify fire-retardant-treated materials with appropriate classification marking of qualified testing agency in the form of removable paper label or imprint on surfaces that will be concealed from view after installation.

        - Fire-Retardant-Treated Lumber and Plywood: Products with a flame-spread index of 25 or less when tested in accordance with ASTM E84, with no evidence of significant progressive combustion when the test is extended an additional 20 minutes, and with the flame front not extending more than 10.5 feet (3.2 m) beyond the centerline of the burners at any time during the test.

          - For exterior applications, use materials that comply with testing requirements after being subjected to accelerated weathering in accordance with ASTM D2898.

          - Kiln-dry lumber and plywood after treatment to a maximum moisture content of 19 and 15 percent, respectively.

Retain first subparagraph below if items are to receive a stained or natural finish. Organic resin treatments are more expensive than salt treatments but helps ensure better stained, transparent, or natural finishes.

          - For items indicated to receive a stained, transparent or natural finish, use organic resin chemical formulation.

Retain one of two subparagraphs below. Before retaining first subparagraph, verify that wood species and treatment process specified are approved for milling after treatment.

          - Mill lumber after treatment within limits set for wood removal that do not affect listed fire-test-response characteristics, using a woodworking shop certified by testing and inspecting agency.

          - Mill lumber before treatment, and implement procedures during treatment and drying processes that prevent lumber from warping and developing discolorations from drying sticks or other causes, marring, and other defects affecting appearance of treated woodwork.

Fire-retardant particleboard contains urea formaldehyde. It complies with requirements for Class I (Class A) finish but not requirements of model codes for use where noncombustible materials are required.

        - Fire-Retardant Particleboard: Made from softwood particles and fire-retardant chemicals mixed together at time of panel manufacture, to achieve flame-spread index of 25 or less and smoke-developed index of 25 or less in accordance with ASTM E84.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - For panels 3/4 inch (19 mm) thick and less, comply with ANSI A208.1 for Grade M-2, except for the following minimum properties: modulus of rupture, 1600 psi (11 MPa); modulus of elasticity, 300,000 psi (2070 MPa); internal bond, 80 psi (550 kPa); and screw-holding capacity on face and edge, 250 and 225 lbf (1100 and 1000 N), respectively.

          - For panels 13/16 to 1-1/4 inches (20 to 32 mm) thick, comply with ANSI A208.1 for Grade M-1, except for the following minimum properties: modulus of rupture, 1300 psi (9 MPa); modulus of elasticity, 250,000 psi (1720 MPa); linear expansion, 0.50 percent; and screw-holding capacity on face and edge, 250 and 175 lbf (1100 and 780 N), respectively.

Fiberboard in "Fire-Retardant Fiberboard" Paragraph below complies with requirements for Class I (Class A) finish but not requirements of model codes for use where noncombustible materials are required.

        - Fire-Retardant Fiberboard: Medium-density fiberboard (MDF) panels complying with ANSI A208.2, made from softwood fibers, synthetic resins, and fire-retardant chemicals mixed together at time of panel manufacture to achieve flame-spread index of 25 or less and smoke-developed index of 200 or less in accordance with ASTM E84.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

      - FASTENERS

        - General: Provide fasteners of size and type indicated, acceptable to authorities having jurisdiction, and that comply with requirements specified in this article for material and manufacture. Provide nails or screws, in sufficient length, to penetrate not less than 1-1/2 inches (38 mm) into wood substrate.

          - Use [stainless steel] [fasteners with hot-dip zinc coating complying with ASTM A153/A153M or ASTM F2329/F2329M] unless otherwise indicated.

          - For pressure-preservative-treated wood, use stainless steel fasteners.

California Redwood Association recommends stainless steel fasteners or hot-dip galvanized-steel fasteners.

          - For redwood, use [brass/bronze] [stainless steel] [hot-dip galvanized-steel] fasteners.

        - Nails: ASTM F1667.

        - Power-Driven Fasteners: ICC-ES AC70.

        - Wood Screws and Lag Screws: ASME B18.2.1, ASME B18.6.1, or ICC-ES AC233.

        - Carbon-Steel Bolts: ASTM A307 with ASTM A563 (ASTM A563M) hex nuts and, where indicated, flat washers all hot-dip zinc coated.

        - Stainless Steel Bolts: ASTM F593, Alloy Group 1 or 2; with ASTM F594, Alloy Group 1 or 2 (ASTM F836M, Grade A1 or Grade A4) hex nuts and, where indicated, flat washers.

        - Postinstalled Anchors: Stainless steel, [chemical] [or] [torque-controlled expansion] anchors with capability to sustain, without failure, a load equal to 6 times the load imposed when installed in unit masonry assemblies and equal to 4 times the load imposed when installed in concrete as determined by testing in accordance with ASTM E488/E488M conducted by a qualified independent testing and inspecting agency.

          - Stainless steel bolts and nuts complying with ASTM F593 and ASTM F594, Alloy Group 1 or 2 (ASTM F738M and ASTM F836M, Grade A1 or Grade A4).

      - MISCELLANEOUS MATERIALS

Retain "Furring, Blocking, Shims, Hanging Strips, and Nailers" Paragraph below if not included in a carpentry Section. If retaining, retain one of two options or delete both if not required. Revise moisture content to suit regional requirements and local availability.

        - Furring, Blocking, Shims, Hanging Strips, and Nailers: Softwood or hardwood lumber[, pressure-preservative treated] [, fire-retardant treated], kiln dried to less than 15 percent moisture content.

Retain "Wood Preservative Treatment" or "Fire-Retardant Treatment" Subparagraph below, or indicate locations of each treatment on the Drawings or in the "Preservative-Treated Wood Materials" and "Fire-Retardant-Treated Materials" articles. Treatments cannot be used together.

          - Wood-Preservative Treatment: By pressure process, AWPA U1; Use Category UC3b.

Maximum moisture content specified in first subparagraph below is standard limit for preservative-treated lumber that is kiln dried after treatment.

            - Kiln-dry lumber after treatment to a maximum moisture content of 19 percent.

See the Evaluations for information about treatment chemicals.

            - Preservative Chemicals: Acceptable to authorities having jurisdiction[ and containing no arsenic or chromium].

            - Mark lumber with treatment quality mark of an inspection agency approved by the American Lumber Standards Committee's (ALSC) Board of Review.

          - Fire-Retardant Treatment: Complying with requirements; provide [where indicated on Drawings] <Insert requirements>.

        - <Double click to insert sustainable design text for adhesives.>

        - Installation Adhesive: Product recommended by fabricator for each substrate for secure anchorage.

          - <Double click to insert sustainable design text for VOC content of adhesive.>

          - <Double click to insert sustainable design text for adhesives.>

      - FABRICATION

Retain first paragraph below if fire-retardant-treat wood is applicable.

        - Sand fire-retardant-treated wood lightly to remove raised grain on exposed surfaces before fabrication.

        - Fabricate ornamental woodwork to dimensions, profiles, and details indicated.

          - Ease edges to radius indicated for the following:

            - Edges of Solid-Wood (Lumber) Members: 1/16 inch (1.5 mm) unless otherwise indicated.

Retain "Edges of Rails and Similar Members More Than 3/4 Inch (19 mm) Thick" Subparagraph below if required.

            - Edges of Rails and Similar Members More Than 3/4 Inch (19 mm) Thick: 1/8 inch (3 mm).

If applicable, insert subparagraph here to describe conditions where eased edges are not required.

        - Complete fabrication, including assembly[ and finishing], to maximum extent possible before shipment to Project site.

          - Disassemble components only as necessary for shipment and installation.

          - Where necessary for fitting at site, provide ample allowance for scribing, trimming, and fitting.

Retain first subparagraph below if Architect will examine work in woodwork shop before it is shipped to Project site.

          - Notify Architect seven days in advance of the dates and times ornamental woodwork fabrication will be complete.

Retain first subparagraph below for high-quality and large or complex work.

          - Trial fit assemblies at fabrication shop that cannot be shipped completely assembled.

            - Install dowels, screws, bolted connectors, and other fastening devices that can be removed after trial fitting.

            - Verify that parts fit as intended, and check measurements of assemblies against field measurements indicated on approved Shop Drawings before disassembling for shipment.

      - SHOP PRIMING

Retain this article if shop priming is required and if shop finishing is not specified. Shop priming or shop finishing is recommended to seal woodwork. See the Evaluations.

        - Preparations for Finishing: Comply with the Architectural Woodwork Standards for sanding, filling countersunk fasteners, sealing concealed surfaces, and similar preparations for finishing ornamental woodwork, as applicable to each unit of work.

Retain "Backpriming," "Exterior Ornamental Woodwork for Opaque Finish," or "Exterior Ornamental Woodwork for Opaque Finish" Paragraph below for exterior ornamental woodwork. First paragraph is for shop priming only surfaces that will be concealed after installation. Second paragraph is for shop priming all surfaces. Third paragraph is for transparent finishes.

        - Backpriming: Apply one coat of sealer or primer, compatible with finish coats, to concealed surfaces of ornamental woodwork.[ Apply two coats to surfaces installed in contact with concrete or masonry and to end-grain surfaces.]

        - Exterior Ornamental Woodwork for Opaque Finish: Shop prime all surfaces with one coat of wood primer specified in Section 099113 "Exterior Painting."

        - Exterior Ornamental Woodwork for Transparent Finish:

          - Shop seal surfaces to be concealed.

          - Shop seal exposed surfaces with stain (if specified), other required pretreatments, and first coat of finish as specified in Section 099300 "Staining and Transparent Finishing."

        - Interior Ornamental Woodwork for Opaque Finish: Shop prime with one coat of wood primer specified in Section 099123 "Interior Painting."

Usually retain "Backpriming" Subparagraph below; backpriming may prolong life of interior ornamental woodwork by retarding moisture absorption.

          - Backpriming: Apply one coat of primer, compatible with finish coats, to concealed surfaces of woodwork.[ Apply two coats to surfaces installed in contact with concrete or masonry and to end-grain surfaces.]

        - Interior Ornamental Woodwork for Transparent Finish: Shop seal with stain (if required), other required pretreatments, and first coat of finish as specified in Section 099300 "Staining and Transparent Finishing."

Usually retain "Backpriming" Subparagraph below; backpriming may prolong life of interior ornamental woodwork by retarding moisture absorption.

          - Backpriming: Apply one coat of sealer, compatible with finish coats, to concealed surfaces of woodwork.[ Apply two coats to surfaces installed in contact with concrete or masonry and to end-grain surfaces.]

      - SHOP FINISHING

Retain one of first three paragraphs below to indicate extent of shop finishing required. First paragraph requires all work to be shop finished.

        - Finish ornamental woodwork at fabrication shop as specified in this Section. Defer only final touchup, cleaning, and polishing until after installation.

Retain first paragraph below if both painted and transparent finishes are used and only transparent finish is shop applied.

        - Shop finish transparent-finished ornamental woodwork at fabrication shop as specified in this Section. Refer to [Section 099113 "Exterior Painting"] [and] [Section 099123 "Interior Painting"] for field finishing opaque-finished ornamental woodwork.

Retain first paragraph below if both shop-finished and field-finished ornamental woodwork is required and Drawings indicate which items are required to be shop finished.

        - Drawings indicate items that are required to be shop finished. Finish such items at fabrication shop as specified in this Section. Refer to [Section 099113 "Exterior Painting"] [Section 099123 "Interior Painting"] [and] [Section 099300 "Staining and Transparent Finishing"] for field finishing ornamental woodwork not indicated to be shop finished.

        - Transparent Finish for Exterior Items: Comply with Section 099300 "Staining and Transparent Finishing."

        - Opaque Finish for Exterior Items: Comply with Section 099113 "Exterior Painting."

        - Transparent Finish for Interior Items:

          - Architectural Woodwork Standards Grade: [Premium] [Custom] [Economy] [Same as item to be finished].

          - Finish System - 1: Lacquer, Nitrocellulose.

          - Finish System - 2: Lacquer, Pre Catalyzed.

          - Finish System - 3: Lacquer, Post Catalyzed.

Finish System - 4 has best resistance to yellowing.

          - Finish System - 4: Latex Acrylic, Water-Based.

Finish System - 5 is a durable, repairable, and good general-purpose fine finish.

          - Finish System - 5: Varnish, Conversion.

          - Finish System - 6: Oil, Synthetic Penetrating.

Finish System - 7 is durable and has good chemical resistance.

          - Finish System - 7: Vinyl, Catalyzed.

          - Finish System - 8: Acrylic Cross Linking, Water-Based.

          - Finish System - 9: UV Curable, Acrylated Epoxy, Polyester, or Urethane.

          - Finish System - 10: UV curable, Water-Based.

Finish System - 11 is very durable but not easily repaired.

          - Finish System - 11: Polyurethane, Catalyzed.

          - Finish System - 12: Polyurethane, Water-Based.

Finish System - 13 can have high gloss (wet look), requires special care in applying, and is not generally repairable.

          - Finish System - 13: Polyester, Catalyzed.

Wash coat helps prevent blotchiness with wiping stains.

          - Wash Coat for Closed-Grain Woods: Apply wash-coat sealer to woodwork made from closed-grain wood before staining and finishing.

          - Staining: [None required] [Match approved sample for color] [Match Architect's sample].

Retain "Open Finish for Open-Grain Woods" or "Filled Finish for Open-Grain Woods" Subparagraph below if using open-grain wood.

          - Open Finish for Open-Grain Woods: Do not apply filler to open-grain woods.

Retain option in "Filled Finish for Open-Grain Woods" Subparagraph below for highest-quality work to prevent solvent in filler from smearing stain.

          - Filled Finish for Open-Grain Woods:[ After staining, apply wash-coat sealer and allow to dry.] Apply paste wood filler and wipe off excess. Tint filler to match stained wood.

Numerical values for gloss ratings are those published in the Architectural Woodwork Standards; coordinate with effect and finish system required. Retain flat sheen with oil finish.

          - Sheen: [Flat, 8-14] [Satin, 15-25] [Satin Gloss, 26-49] [Semigloss, 50-70] [Gloss, 71-90] gloss units measured on 60-degree gloss meter in accordance with ASTM D523.

        - Opaque Finish for Interior Items:

          - Architectural Woodwork Standards Grade: [Premium] [Custom] [Economy] [Same as item to be finished].

Retain one or more of 12 finish system subparagraphs below. Review the Architectural Woodwork Standards for general performance characteristics of finishing systems.

          - Finish System - 1: Lacquer, Nitrocellulose.

          - Finish System - 2: Lacquer, Pre Catalyzed.

          - Finish System - 3: Lacquer, Post Catalyzed Lacquer.

          - Finish System - 4: Latex Acrylic, Water-Based.

          - Finish System - 5: Varnish, Conversion.

          - Finish System - 7: Vinyl, Catalyzed.

          - Finish System - 8: Acrylic Cross Linking, Water-Based.

          - Finish System - 9: UV Curable, Acrylated Epoxy, Polyester, or Urethane.

          - Finish System - 10: UV Curable, Water-Based.

          - Finish System - 11: Polyurethane, Catalyzed.

          - Finish System - 12: Polyurethane, Water-Based.

          - Finish System - 13: Polyester, Catalyzed.

Retain one of three options in "Color" Subparagraph below. If retaining first, indicate colors in a separate subparagraph.

          - Color: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range].

Numerical values for gloss ratings are those published in the Architectural Woodwork Standards.

          - Sheen: [Flat, 8-14] [Satin, 15-25] [Satin Gloss, 26-49] [Semigloss, 50-70] [Gloss, 71-90] gloss units measured on 60-degree gloss meter in accordance with ASTM D523.

- EXECUTION

      - PREPARATION

        - Before installation, condition ornamental woodwork to average prevailing humidity conditions in installation areas for not less than 72 hours prior to beginning of installation.

        - Before installing ornamental woodwork, examine shop-fabricated work for completion, and complete work as required, including removing packing and backpriming concealed surfaces.

      - INSTALLATION

Revise "Grade" Paragraph below if installation grade is different from fabrication grade.

        - Grade: Install ornamental woodwork to comply with same grade as item to be installed.

        - Assemble ornamental woodwork, and complete fabrication at Project site to the extent that it was not completed during shop fabrication.

        - Install ornamental woodwork level, plumb, true in line, and without distortion.

          - Shim as required with concealed shims.

          - Install level and plumb to a tolerance of 1/8 inch in 96 inches (3 mm in 2400 mm).

        - Scribe and cut ornamental woodwork to fit adjoining work, refinish cut surfaces, and repair damaged finish at cuts.

        - Preservative-Treated Wood: Where cut or drilled, treat cut ends and drilled holes in accordance with AWPA M4.

        - Fire-Retardant-Treated Wood: Install fire-retardant-treated wood to comply with chemical treatment manufacturer's written instructions, including those for adhesives used to install woodwork.

        - Anchor ornamental woodwork to anchors or blocking built in or directly attached to substrates.

          - Secure with countersunk, concealed fasteners and blind nailing.

          - Use fine finishing nails[ or finishing screws] for exposed fastening, countersunk and filled flush with ornamental woodwork.

          - For exposed work, arrange fasteners in straight rows parallel with edges of members, with fasteners evenly spaced and with adjacent rows staggered.

          - For shop-finished items, use filler matching finish of items being installed.

      - FIELD QUALITY CONTROL

Retain "Inspections" Paragraph below to require inspection of installed Work by either AWI or WI. Under both AWI and WI quality programs, the Architect has the right to request an inspection at any time during the Project.

        - Inspections: Provide inspection of installed Work through [AWI's Quality Certification Program] [WI's Certified Compliance Program] certifying that woodwork, including installation, complies with requirements of the Architectural Woodwork Standards for the specified grade.

          - Inspection entity is to prepare and submit report of inspection.

      - REPAIR

        - Repair damaged and defective ornamental woodwork, where possible, to eliminate functional and visual defects[ and to result in interior ornamental woodwork being in compliance with requirements of Architectural Woodwork Standards for the specified grade].

        - Where not possible to repair, replace defective Work.

Retain "Shop Finish" or "Field Finish" paragraphs below; coordinate with selections made in "Shop Finishing" Article.

        - Shop Finish: Touch up finishing work specified in this Section after installation of ornamental woodwork.

          - Fill nail holes with matching filler where exposed.

          - Apply specified finish coats, including stains and paste fillers if any, to exposed surfaces where only sealer/prime coats are shop applied.

        - Field Finish: See [Section 099123 "Interior Painting"] [and] [Section 099300 "Staining and Transparent Finishing"] for final finishing of installed ornamental woodwork not indicated to be shop finished.

END OF SECTION 064400