Copyright 2022 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 073126 - SLATE SHINGLES

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

MasterSpec includes provisions for LEED 2009, LEED v4, LEED v4.1, IgCC, and Green Globes. Sustainable design requirements may be inserted in the Section Text using the hypertext links.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Slate shingles.

          - Underlayment materials.

          - Ridge accessories.

          - Metal flashing and trim.

        - Related Requirements:

Retain subparagraph below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections. Retain if snow guards are not inserted in this Section.

          - Section 077253 "Snow Guards" for snow guards.

      - ALLOWANCES

Retain this article if products and Work included in this Section are covered by lump-sum, unit-cost, or quantity allowances.

        - See Section 012100 "Allowances" for description of allowances affecting items specified under this Section.

      - UNIT PRICES

Retain this article if products and Work specified in this Section are measured and paid for under the provisions of unit prices.

        - See Section 012200 "Unit Prices" for description of unit prices affecting items specified under this Section.

      - ALTERNATES

Retain this article if products and Work specified in this Section are to be added to or deducted from the base bid amount under the provisions of alternates.

        - See Section 012300 "Alternates" for description of alternates affecting items specified under this Section.

      - DEFINITIONS

        - Roofing Terminology: See ASTM D1079 for definitions of terms related to roofing Work in this Section.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

          - <Insert participant requirements>.

      - ACTION SUBMITTALS

        - Product Data:

          - Slate shingles.

          - Underlayment materials.

          - Ridge accessories.

          - Metal flashing and trim.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for regional materials.>

Retain "Shop Drawings" Paragraph below if Drawings do not fully detail metal flashing and trim specified in Part 2 or to verify requirements specified in Part 2.

        - Shop Drawings: For metal flashing and trim.

Retain "Samples" Paragraph below for single-stage Samples. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples.

        - Samples: For each exposed product and for each color and texture specified, in sizes indicated.

          - Slate Shingles: Full size, of each color, size, texture, and shape.

          - Metal Ridge Cap: 12-inch- (305-mm-) long Sample.

          - Rigid-Plastic Ridge Vent: 12-inch- (305-mm-) long Sample.

Retain "Metal Valley Flashing" Subparagraph below if open valleys are required.

          - Metal Valley Flashing: 12 inches (305 mm) square.

        - Samples for Initial Selection:

          - For each type of slate shingle.

          - For each type of accessory involving color selection.

        - Samples for Verification: For the following products, in sizes indicated:

          - Slate Shingle: Full size, of each color, size, texture, and shape.

          - Metal Ridge Cap: 12-inch- (305-mm-) long Sample.

          - Rigid-Plastic Ridge Vent: 12-inch- (305-mm-) long Sample.

Retain "Metal Valley Flashing" Subparagraph below if open valleys are required.

          - Metal Valley Flashing: 12 inches (305 mm) square.

      - INFORMATIONAL SUBMITTALS

Retain "Material Test Reports" Paragraph below for material test reports that are Contractor's responsibility.

        - Material Test Reports: For each slate variety, by a qualified testing agency.

Retain "Research Reports" Paragraph below for polymer-modified bitumen sheet and synthetic underlayment if required.

        - Research Reports: From [an agency acceptable to authorities having jurisdiction] [ICC-ES] <Insert evaluation agency>, indicating that product is suitable for intended use under applicable building codes for the following:

Retain applicable subparagraphs below to suit Project. The IBC and the IRC do not address polymer-modified bitumen sheet and synthetic underlayments.

          - Polymer-modified bitumen sheet underlayment.

          - Synthetic underlayment.

      - MAINTENANCE MATERIAL SUBMITTALS

        - Furnish extra materials that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

Revise "Slate Shingles" Subparagraph below if different quantities of different types of shingles are required; for example, special shapes or colors.

          - Slate Shingles: [100 sq. ft. (9.3 sq. m)] <Insert area> of each size, type, and color, in unbroken bundles.

      - MOCKUPS

        - Build mockups to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for materials and execution.

          - Build mockups for slate shingles including related roofing materials.

            - Size: [48 inches (1219 mm) long by 48 inches (1219 mm) wide] <Insert dimensions>.

Retain first subparagraph below if required; insert other mockup requirements to suit Project.

            - Include gutter and downspout complying with requirements in [Section 076200 "Sheet Metal Flashing and Trim."] [Section 077100 "Roof Specialties."]

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Store underlayment rolls in a dry, well-ventilated location protected from weather, sunlight, and moisture in accordance with manufacturer's written instructions.

          - Store on end, on pallets or other raised surfaces.

          - Do not double-stack rolls.

        - Protect unused underlayment from weather, sunlight, and moisture when left overnight or when roofing work is not in progress.

        - Handle, store, and place roofing materials in a manner to prevent damage to roof deck or structural supporting members.

      - FIELD CONDITIONS

        - Environmental Limitations: Proceed with installation only when existing and forecasted weather conditions permit product installation and related Work to be performed in accordance with manufacturer's written instructions and warranty requirements.

Retain subparagraph below for self-adhering, polymer-modified bitumen sheet used as water protection, an ice barrier, or underlayment.

          - Install self-adhering, polymer-modified bitumen sheet underlayment within the range of ambient and substrate temperatures recommended in writing by manufacturer.

      - WARRANTY

When warranties are required, verify with Owner's counsel that warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

Retain "Roofing Installer's Warranty" Paragraph below, with "Roofing Installer's Warranty" Article, if required.

        - Roofing Installer's Warranty: On warranty form at end of this Section, signed by Installer, in which Installer agrees to repair or replace components of slate-shingle roofing that fail in materials or workmanship within specified warranty period.

          - Warranty Period: [Two] [Five] <Insert number> years from date of Substantial Completion.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - SOURCE LIMITATIONS

        - Obtain each type of product from single source from single manufacturer.

      - PERFORMANCE REQUIREMENTS

Retain this article for classified roof assemblies. If retaining, revise "Exterior Fire-Test Exposure" Paragraph below to suit Project. Slate shingles are exempt from testing for Class A fire resistance if installed on noncombustible roof decks under the IBC and the IRC. Using ASTM D226/D226M Type II underlayment over combustible decks also satisfies the IBC and the IRC requirements for Class A roof assemblies. See "Fire Resistance" Article in the Evaluations and verify requirements of authorities having jurisdiction for roof assembly.

        - Exterior Fire-Test Exposure: Provide slate shingles and related roofing materials identical to those of assemblies tested for Class A fire resistance in accordance with ASTM E108 or UL 790 by Underwriters Laboratories or another testing and inspecting agency acceptable to authorities having jurisdiction. Identify products with appropriate markings of applicable testing agency.

      - SLATE SHINGLES

For roofing longevity, NRCA recommends Grade S1, the highest grade for slate shingles, instead of Grade S2. See "Slate Product Standard" Article in the Evaluations.

        - Slate Shingles: ASTM C406/C406M, [Grade S1] [Grade S2]; hard, dense, and sound; with chamfered edges and nail holes machine punched or drilled and countersunk; with no broken or cracked slates, no broken exposed corners, and no broken corners on covered ends that could sacrifice nailing strength or laying of a watertight roof.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Standard slate roofs use smooth-textured slate shingles that are nominal 1/4 inch (6 mm) thick.

For graduated slate roofing, revise "Thickness and Surface Texture," "Length," and "Width" subparagraphs below to include range of thicknesses and sizes; use the thickest, widest, and longest shingles at the eaves and progressively reduce these dimensions toward the ridge.

          - Thickness and Surface Texture: Nominal [1/4 inch (6 mm), smooth] [1/4 to 3/8 inch (6 to 10 mm), rough] [3/8 to 1/2 inch (10 to 13 mm), rough] <Insert dimension and surface texture>.

Typical shingle lengths are 12, 14, 16, 18, 20, 22, and 24 inches (305, 356, 406, 457, 508, 559, and 610 mm), although shorter lengths are available. Commonly produced lengths include 16, 18, and 20 inches (406, 457, and 508 mm).

          - Length: [16 inches (406 mm)] [18 inches (457 mm)] [20 inches (508 mm)] <Insert dimension>.

The narrowest width for a shingle length equals one-half of the length. The widest shingle width is typically 14 inches (356 mm), although widths of 16 inches (406 mm) are available. Traditionally, 13-inch (330-mm) widths are unavailable. For 16-inch- (406-mm-) long shingles, common uniform widths are 8, 10, and 12 inches (203, 254, and 305 mm). For 18- and 20-inch- (457- and 508-mm) long shingles, common uniform widths are 10 and 12 inches (254 and 305 mm).

          - Width: [14 inches (356 mm)] [12 inches (305 mm)] [11 inches (279 mm)] [10 inches (254 mm)] [9 inches (229 mm)] [8 inches (203 mm)] [random widths, but not less than one-half-length] <Insert dimension>.

Two prepunched holes per shingle are standard for slate shingles. For roofs subject to high winds and for 3/4-inch- (19-mm-) thick or thicker slate shingles, four holes may be required.

          - Nail Holes: [Two] [Four] per shingle.

Specify uniform width, rather than random widths, with special butt shapes (shapes other than standard square cut). Descriptions of special butt shapes may vary regionally. Indicate shape on Drawings if descriptions are insufficient.

          - Butt Shape: [Standard square cut] [Pointed] [Deep bevel] [Shallow bevel] [Deep scallop] [Shallow scallop] [Round] <Insert shape>.

Retain color option in "Color" Subparagraph below after verifying availability. Colors available in one region may not be available in another.

          - Color: [Black] [Gray] [Purple] [Green] [Blue-black] [Blue-gray] [Mottled purple and green] [Red] [Match Architect's samples] [As selected by Architect from manufacturer's full range] <Insert color>.

Retain "Unfading" option in "Weather-Exposure Color Change" Subparagraph below for minimal color change; retain "Weathering" option for moderate or obvious color change. Because color change is an inherent slate property, verify availability with manufacturers.

          - Weather-Exposure Color Change: [Unfading] [Weathering].

        - Starter Slate: Slate shingles with chamfered nail holes front-side punched.

          - Length: Exposure of slate shingle plus headlap.

Retain "Ridge Slate" Paragraph below if ridge slate requires special fabrication during manufacture. Slate shingles for valleys, hips, finish course, and roof penetrations are field cut to shape and hole punched.

        - Ridge Slate: Slate shingles fabricated with [vertical] [horizontal] grain orientation.

      - UNDERLAYMENT MATERIALS

See "Underlayment," "Model-Code Underlayment Requirements," "NRCA Underlayment Recommendations," "Asphalt-Saturated Organic Felt Underlayment," "Synthetic Underlayment," "Polymer-Modified Bitumen Sheet Underlayment," and "Self-Adhering, Polymer-Modified Bitumen Sheet Underlayment" articles in the Evaluations for a discussion of various underlayment options.

Retain one of four options in "Asphalt-Saturated Organic Felt" Paragraph below to suit Project. NRCA no longer recommends felt underlayment for use with slate shingles. ASTM D226/D226M Type II and ASTM D4869/D4869M Type IV felt, both weighing 26 lb/100 sq. ft. (1270 g/sq. m), are most commonly used. The IBC requires one layer of ASTM D226/D226M Type II or ASTM D4869/D4869M Type III or IV felt where basic design wind speeds (three-second gusts per ASCE/SEI 7) are less than 140 mph (63 m/s). For greater basic design wind speeds, the IBC requires one layer of ASTM D226/D226M Type II or ASTM D4869/D4869M Type IV felt. The IRC has less stringent requirements. See "Model-Code Underlayment Requirements" and "Asphalt-Saturated Organic Felt Underlayment" articles in the Evaluations.

        - Asphalt-Saturated Organic Felt: [ASTM D226/D226M Type I] [ASTM D226/D226M Type II] [ASTM D4869/D4869M Type III] [ASTM D4869/D4869M Type IV] <Insert requirements>, unperforated.

If retaining "Synthetic Underlayment" Paragraph below, verify that products comply with requirements of authorities having jurisdiction and are recommended for use under slate shingles. NRCA only recommends using synthetic underlayment as a top layer installed over an anchor layer of mechanically fastened or self-adhering, polymer-modified bitumen sheet. See "NRCA Underlayment Recommendations" Article in the Evaluations.

        - Synthetic Underlayment: UV-resistant polypropylene, polyolefin, or polyethylene polymer fabric with surface coatings or treatments to improve traction underfoot and abrasion resistance; recommended, in writing, by manufacturer for use under slate shingles; and evaluated and documented to be suitable for use as a roof underlayment under applicable codes by a testing and inspecting agency acceptable to authorities having jurisdiction.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Retain "Polymer-Modified Bitumen Sheet" Paragraph below for products marketed as underlayment or valley flashing. Revise to suit Project. NRCA recommends using polymer-modified bitumen sheet, including products used as base sheets in low-slope membrane roof systems and products marketed as underlayment, for slate-shingle underlayment. Sheets are mechanically fastened or, where used as an adhered top layer in a two-layer installation, set in a continuous layer of hot roofing asphalt or cold adhesive. See "NRCA Underlayment Recommendations" and "Polymer-Modified Bitumen Sheet Underlayment" articles in the Evaluations.

        - Polymer-Modified Bitumen Sheet: Styrene-butadiene-styrene- (SBS) modified asphalt, glass-fiber-mat-reinforced sheet; minimum [55-mil (1.4-mm)] [40-mil (1.0-mm)] <Insert dimension> nominal thickness; recommended in writing by manufacturer and acceptable to authorities having jurisdiction for use as underlayment in slate steep-slope roofing systems; and designed for mechanical fastening or adhesive attachment using roofing asphalt or cold-applied adhesive.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

If required, insert specific testing requirements for polymer-modified bitumen sheet products here. Product testing varies among manufacturers.

          - <Insert testing requirements>.

Retain "Self-Adhering, Polymer-Modified Bitumen Sheet" or "Self-Adhering, Polymer-Modified Bitumen Sheet, High Temperature" Paragraph below to suit Project. Self-adhering, polymer-modified bitumen sheet commonly covers the entire roof deck for slate roofs and is also used for water and ice-dam protection in roof areas vulnerable to leakage. NRCA and the National Slate Association recommend covering self-adhering sheet with a top layer of a different type of underlayment. See "Self-Adhering, Polymer-Modified Bitumen Sheet Underlayment" Article in the Evaluations.

Retain one of first three options in "Self-Adhering, Polymer-Modified Bitumen Sheet" Paragraph below to suit Project. ASTM D1970/D1970M requires a minimum thickness of 40 mils (1.0 mm); however, product thicknesses vary.

        - Self-Adhering, Polymer-Modified Bitumen Sheet: ASTM D1970/D1970M, minimum [55-mil- (1.4-mm-)] [50-mil- (1.3-mm-)] [40-mil- (1.0-mm-)] <Insert dimension> thick sheet; glass-fiber-mat-reinforced, polymer-modified asphalt; with slip-resistant top surface and release backing; cold applied.[ Provide primer for adjoining concrete, masonry, and metal surfaces to receive underlayment.]

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Retain "Top Surface" Subparagraph below if a specific surface is required. Polymer-film- and polyester-surfaced products cost more and might form better-quality laps than sand- and granule-surfaced products. Shingles will stick to sand- and granule-surfaced products, which makes roof repairs more difficult. To prevent this problem, cover self-adhering sheet with another type of underlayment. Installer preference based on experience and the slip-resistance characteristics of the various surface options might be a good reason to choose one type of surface over another.

          - Top Surface: [Sand] [Granule] [Textured polymer film] [Polyester].

        - Self-Adhering, Polymer-Modified Bitumen Sheet, High Temperature: ASTM D1970/D1970M, minimum [55-mil- (1.4-mm-)] [50-mil- (1.3-mm-)] [40-mil- (1.0-mm-)] <Insert thickness> thick sheet; glass-fiber-mat-reinforced, polymer-modified asphalt; with slip-resistant top surface and release backing; cold applied.[ Provide primer for adjoining concrete, masonry, and metal surfaces to receive underlayment.]

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Thermal Stability: Stable after testing at 240 deg F (116 deg C) in accordance with ASTM D1970/D1970M.

Retain "Top Surface" Subparagraph below if a specific surface is required. Polymer-film- and polyester-surfaced products cost more and might form better-quality laps than granule-surfaced products. Shingles will stick to granule-surfaced products, which makes roof repairs more difficult. To prevent this problem, cover self-adhering sheet with another type of underlayment. Installer preference based on experience and the slip-resistance characteristics of the various surface options might be a good reason to choose one type of surface over another.

          - Top Surface: [Granule] [Textured polymer film] [Polyester].

      - RIDGE ACCESSORIES

"Metal Ridge Cap" Paragraph below is an example of a proprietary slate-covered ridge cap that must be fastened into a wood ridge beam. The cap can be installed over a ventilating base.

        - Metal Ridge Cap: Metal covers with noncorrosive components complete with internal anchoring lag screws, compression plates, and snap-on caps, fabricated for slate roof system indicated.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Type: [Exposed-metal] [Slate-covered] legs.

Retain "Venting" Subparagraph below if required.

          - Venting:

            - Continuous, low-profile, compression-resistant ventilating base that provides a net free area of [18 sq. in./ft. (380 sq. cm/m)] <Insert requirements> of ridge.

            - [With] [Without] external baffles.

          - Metal Components: [Copper, 20-oz./sq. ft.- (0.7-mm-) thick sheet] [Aluminum, 0.050-inch- (1.3-mm-) thick sheet, with manufacturer's standard two-coat, thermocured system consisting of specially formulated inhibitive primer and fluoropolymer color topcoat containing not less than 70 percent polyvinylidene fluoride (PVDF) resin by weight on exposed surfaces] <Insert requirements>.

          - Accessories:

            - Splices, end caps, and other accessories of matching metal and finish.

If retaining "Rigid-Plastic Ridge Vent" Paragraph below, verify that products can withstand the weight of slate over several decades.

        - Rigid-Plastic Ridge Vent: Manufacturer's standard, rigid section high-density polypropylene or other UV-stabilized plastic ridge vent for use under slate ridge shingles.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Minimum Net Free Area: <Insert area>.

          - Width: <Insert dimension>.

          - Thickness: <Insert dimension>.

      - ACCESSORIES

        - Asphalt Roofing Cement: ASTM D4586/D4586M Type II, asbestos free.

        - Butyl Sealant: ASTM C1311, single-component, solvent-release butyl rubber sealant; polyisobutylene plasticized; heavy bodied.

Revise "Elastomeric Sealant" Paragraph below if a specific polymer, class, and use are required.

        - Elastomeric Sealant: ASTM C920, Type S, Grade NS, one-part, non-sag, elastomeric polymer sealant; of class and use classifications required to seal joints in slate-shingle roofing and remain watertight; recommended in writing by manufacturer for applications indicated.

Retain "Roofing Asphalt" Paragraph below if adhering top layer of polymer-modified bitumen sheet to the anchor layer of polymer-modified bitumen sheet with hot asphalt.

        - Roofing Asphalt: ASTM D312/D312M Type IV.

Retain "Cold-Applied Adhesive" Paragraph below if adhering top layer of polymer-modified bitumen sheet to anchor layer of polymer-modified bitumen sheet with cold-applied adhesive.

        - Cold-Applied Adhesive: Manufacturer's standard asphalt-based, one- or two-part, asbestos-free, cold-applied adhesive specially formulated for compatibility and use with underlayments.

Retain one of four options in "Slating Nails" Paragraph below. NRCA recognizes the use of all options, but suggests using copper slating nails.

        - Slating Nails: ASTM F1667, [copper] [stainless steel] [silicon-bronze] [cut-brass], smooth-shanked, wire nails; 0.135-inch- (3.4-mm-) minimum thickness; sharp pointed; with 3/8-inch- (10-mm-) minimum diameter flat head; of sufficient length to penetrate a minimum of 3/4 inch (19 mm) into sheathing or extend at least 1/8 inch (3 mm) through sheathing less than 3/4 inch (19 mm) thick.

          - Where nails are in contact with metal flashing, use nails made from same metal as flashing.

        - Underlayment Nails: Aluminum, stainless steel, or hot-dip galvanized-steel wire nails with low-profile metal or plastic caps, 1-inch- (25-mm-) minimum diameter.

Retain subparagraph below to comply with IBC requirements for locations where the basic design wind speed is equal to or greater than 140 mph (63 m/s) or with IRC requirements for locations where the ultimate design wind speed (as defined in the IRC) is equal to or greater than 140 mph (63 m/s).

          - Provide with minimum 0.0134-inch- (0.34-mm-) thick metal cap, 0.010-inch- (0.25-mm-) thick power-driven metal cap, or 0.035-inch- (0.89-mm-) thick plastic cap; and with minimum 0.083-inch- (2.11-mm-) thick ring shank or 0.091-inch- (2.31-mm-) thick smooth shank of length to penetrate at least 3/4 inch (19 mm) into roof sheathing or to penetrate through roof sheathing less than 3/4 inch (19 mm) thick.

Retain "Nailer Strips" Paragraph below if eave cants and wood nailer strips at ridges and hips are required. Revise to insert material requirements for wood if preferred.

        - Nailer Strips: Comply with requirements in Section 061000 "Rough Carpentry."

        - Nails for Wood Strips: ASTM F1667; common or box, steel wire, flat head, and smooth shank; hot-dip galvanized.

      - METAL FLASHING AND TRIM

        - Comply with requirements in Section 076200 "Sheet Metal Flashing and Trim."

          - Sheet Metal: [Copper] [Stainless steel] [Zinc-tin alloy coated copper] [Anodized aluminum] [Aluminum, mill finished] <Insert requirements>.

        - Fabricate sheet metal flashing and trim to comply with recommendations in SMACNA's "Architectural Sheet Metal Manual" for design, dimensions, metal, and other characteristics of the item unless otherwise specified in this Section or indicated on Drawings.

Retain "Apron Flashings," "Step Flashings," "Cricket and Backer Flashings," "Counterflashings," "Hip Flashings," "Open-Valley Flashings," "Closed-Valley Flashings," "Interwoven Closed-Valley Flashings," and "Drip Edges" subparagraphs below if Drawings do not fully detail these flashing conditions. Review recommendations in SMACNA's "Architectural Sheet Metal Manual" and NRCA's "The NRCA Roofing Manual: Steep-Slope Roof Systems"; revise to suit Project.

          - Apron Flashings: Fabricate with lower flange extending a minimum of [4 inches (102 mm)] [6 inches (152 mm)] <Insert dimension> over and [4 inches (102 mm)] <Insert dimension> beyond each side of downslope slate shingles and [6 inches (152 mm)] <Insert dimension> up the vertical surface.

Retain "Step Flashings" Subparagraph below for interweaving metal step flashings between succeeding courses of slate shingles that abut vertical surfaces such as chimneys, sidewalls, and skylights.

          - Step Flashings: Fabricate with a headlap of 3 inches (76 mm) and a minimum extension of [4 inches (102 mm)] [5 inches (127 mm)] <Insert dimension> both horizontally and vertically.

Retain "Cricket and Backer Flashings" Subparagraph below if required.

          - Cricket and Backer Flashings: Fabricate with concealed flange extending a minimum of [24 inches (610 mm)] <Insert dimension> beneath upslope slate shingles, [6 inches (152 mm)] <Insert dimension> beyond each side of [chimney] [skylight], and [6 inches (152 mm)] <Insert dimension> above the roof plane.

Retain "Counterflashings" Subparagraph below to protect top edges of apron, step, channel, cricket, and backer flashings from water intrusion.

          - Counterflashings: Fabricate to cover [4 inches (102 mm)] <Insert dimension> of base flashing measured vertically; and in lengths required so that no step exceeds [8 inches (203 mm)] <Insert dimension> and overall length is no more than [10 feet (3 m)] <Insert dimension>.

            - Provide metal [reglets] [receivers] for installation.

Retain "Hip Flashings" Subparagraph below if interwoven hip flashings are required for mitered or fantail hips.

          - Hip Flashings: Fabricate to length of slate shingle and to extend [3 inches (76 mm)] <Insert dimension> beyond joint of hip shingle with adjoining roof shingle.

Retain "Open-Valley Flashings," "Closed-Valley Flashings," or "Interwoven Closed-Valley Flashings" Subparagraph below to suit Project. NRCA recommends using closed valleys only on roofs with slopes of 8:12 or greater. The IBC and the IRC include prescriptive requirements for valley flashings; verify requirements of authorities having jurisdiction.

Options in "Open-Valley Flashings" Subparagraph below reflect NRCA recommendation for using minimum 18-inch- (457-mm-) wide sheet metal. SMACNA recommends minimum 10-inch- (254-mm-) wide flanges. SMACNA also recommends a minimum 1-inch- (25-mm-) high, inverted-V profile and a 2-inch- (51-mm-) high, inverted-V profile for slopes greater than 6:12 and for where dissimilar slopes join. Revise subparagraph to suit Project.

          - Open-Valley Flashings: Fabricate from metal sheet not less than [18 inches (457 mm)] <Insert dimension> wide in lengths not exceeding [10 feet (3 m)] <Insert dimension>, with [1-inch- (25-mm-)] <Insert dimension> high, inverted-V profile water diverter at center of valley and equal flange widths of not less than [8 inches (203 mm)] <Insert dimension>.

Retain first subparagraph below if securing flange edges with cleats.

            - Hem flange edges for fastening with metal cleats.

          - Closed-Valley Flashings: Fabricate in lengths not exceeding [10 feet (3 m)] <Insert dimension> and equal flange widths of [9 inches (229 mm)] [10 inches (254 mm)] [12 inches (305 mm)] <Insert dimension>.

Retain first subparagraph below if securing flange edges with cleats.

            - Hem flange edges for fastening with metal cleats.

          - Interwoven Closed-Valley Flashings: Fabricate in lengths [equal to shingle exposure plus headlap plus 2 inches (51 mm)] <Insert dimension> and equal flange widths of [9 inches (229 mm)] [10 inches (254 mm)] [12 inches (305 mm)] <Insert dimension>.

Retain "Drip Edges" Subparagraph below if required at eave or rake edges.

          - Drip Edges: Fabricate in lengths not exceeding [10 feet (3 m)] <Insert dimension> with roof-deck flange and 1-1/2-inch (38-mm) fascia flange with 3/8-inch (10-mm) drip at lower edge.

            - Roof-Deck Flange at Eaves: [Form to cover cant strip and fasten to roof deck] <Insert description>.

            - Roof-Deck Flange at Rakes: Form to extend minimum of [2 inches (51 mm)] <Insert dimension> onto roof deck.

Retain "Vent-Pipe Flashings" Paragraph below for plumbing vents that penetrate roof. Revise if another flashing material is required, or delete paragraph and include requirements in Section 076200 "Sheet Metal Flashing and Trim."

        - Vent-Pipe Flashings: ASTM B749, Type L51121, at least 1/16 inch (1.6 mm) thick. Provide lead sleeve sized to slip over and turn down into pipe, soldered to skirt at slope of roof and extending at least 4 inches (102 mm) from pipe onto roof.

Insert requirements for snow guards using Section 077253 "Snow Guards" as a basis if not specifying them in that Section.

        - <Insert snow-guard requirements>.

- EXECUTION

      - EXAMINATION

        - Examine substrates, areas, and conditions, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of the Work.

          - Examine roof sheathing to verify that sheathing joints are supported by framing and blocking or metal clips and that installation is within flatness tolerances.

          - Verify that substrate is sound, dry, smooth, clean, sloped for drainage, and completely anchored and that provisions have been made for flashings and penetrations through roofing.

          - Verify that vent stacks and other penetrations through roofing are installed and securely fastened.

        - Prepare written report, endorsed by Installer, listing conditions detrimental to performance of the Work.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - INSTALLATION OF SLATE SHINGLES

        - Beginning at eaves, install slate shingles in accordance with manufacturer's written instructions and with details and recommendations in NRCA's "The NRCA Roofing Manual: Steep-Slope Roof Systems."

          - Install wood strip cant at eave edges [under underlayment materials] <Insert description>.

          - Install shingle starter course chamfered face down.

        - Install first and succeeding shingle courses chamfered face up. Install full-width first course at rake edge.

          - Offset joints of uniform-width slate shingles by half the shingle width in succeeding courses.

          - Offset joints of random-width slate shingles a minimum of 3 inches (76 mm) in succeeding courses.

The IBC and the IRC require a minimum 4-inch (102-mm) headlap for roof slopes less than 8:12, a minimum 3-inch (76-mm) headlap for slopes of 8:12 to slopes less than 20:12, and a 2-inch (51-mm) headlap for slopes of 20:12 or greater.

        - Maintain a [4-inch- (102-mm-)] [3-inch- (76-mm-)] <Insert dimension> minimum headlap between succeeding shingle courses.

Retain one option in first paragraph below or revise paragraph if required to describe a graduated slate roof where shingle length and exposure gradually reduce between eaves and ridge.

        - Maintain uniform exposure of shingle courses [between eaves and ridge] [midway between eaves and ridge, and increase headlap of succeeding shingle courses to ensure uniform exposure on remaining shingle courses].

        - At eaves, extend shingle starter course and first course 1 inch (25 mm) over fasciae.

        - At rakes, extend shingle starter course and succeeding courses [1 inch (25 mm)] [2 inches (51 mm)] over fasciae.

        - Cut and fit slate neatly around roof vents, pipes, ventilators, and other projections through roof.

        - Hang slate with [two] [four] slating nails for each shingle, with nail heads lightly touching slate.

          - Do not drive nails home, which draws slates downward, and do not leave nail heads protruding enough to interfere with the overlapping shingle above.

          - At vented ridges, terminate slate shingles to produce a uniform airspace on each side of ridge apex.

Retain one of three options in "Ridges" Paragraph below for traditional treatment at uncapped or unvented ridges.

        - Ridges: Install ridge slate in [saddle] [strip saddle] [combed] configuration.

Retain first subparagraph below for saddle ridges; delete for strip saddle or combed ridges.

          - Install and anchor wood nailer strips of thicknesses to match abutting courses of slate shingles, terminating nailer strip 3 to 4 inches (76 to 102 mm) from the eave. Cover with [self-adhering, polymer-modified bitumen sheet] <Insert requirement>, extending to underlying slate but concealed by ridge slate.

Retain first subparagraph below for saddle and combed ridges.

          - Lay ridge slate in bed of [asphalt roofing cement] [butyl sealant].

Retain first option in first subparagraph below for saddle ridge and strip saddle ridge; retain second option for combed ridge.

          - Anchor ridge slate to supporting wood nailer strip with [two] [four] <Insert number> nails for each slate shingle, without nails penetrating underlying slate.

Retain first subparagraph below for combed ridge.

          - Extend combed-ridge slate over leeward ridge slate by 1/8 to 1/4 inch (3 to 6 mm). Seal ridge joint with elastomeric sealant.

Retain subparagraph below for strip saddle and combed ridges.

          - Cover heads of exposed nails at final ridge shingle with [asphalt roofing cement] [butyl sealant].

        - Hips: Install and anchor slate hips in [saddle] [mitered] [fantail] configuration.

Retain first subparagraph below for saddle hip; delete for mitered and fantail hips.

          - Install and anchor wood nailer strips of thickness to match abutting courses of slate shingles.

            - Cover nailer strip with [self-adhering, polymer-modified bitumen sheet] <Insert requirement>, extending on to underlying slate but concealed by hip slate.

            - Anchor hip slate to nailer strip with [two] <Insert number> nails located in upper third of hip-slate length.

Retain first subparagraph below for saddle hips.

          - Notch starter shingle and first shingle course at hip to fit around nailer strips so no wood is exposed at ridge eave.

          - Lay hip slate in bed of [asphalt roofing cement] [butyl sealant].

Retain subparagraph below for mitered and fantail hips.

          - Seal hip centerline joint with elastomeric sealant.

        - Open Valleys: Cut slate shingles to form straight lines at open valleys, trimming upper concealed corners of shingles. [Maintain uniform width of exposed open valley] [Widen exposed portion of open valley 1/8 inch in 12 inches (1:96)] from highest to lowest point.

          - Do not nail shingles to valley metal flashings.

NRCA recommends using closed valleys only on roofs with slopes of 8:12 or greater.

        - Closed Valleys: Cut slate shingles to form straight lines at closed valleys, trimming upper concealed corners of shingles.

          - Maintain uniform gap at centerline of valley of [1/2 to 3/4 inch (13 to 19 mm)] [3/4 to 1 inch (19 to 25 mm)].

          - Do not nail shingles to valley metal flashings.

          - Wire-tie shingles to roof deck on either side of flashing as required to secure shingles.

        - Remove and replace damaged or broken slate shingles.

      - INSTALLATION OF UNDERLAYMENT MATERIALS

Underlayments installed parallel to eaves are installed perpendicular to sloped roof deck. Underlayments installed parallel to the rake are installed parallel to sloped roof deck.

        - Comply with slate-shingle and underlayment manufacturers' written installation instructions and with recommendations in NRCA's "The NRCA Roofing Manual: Steep-Slope Roof Systems" applicable to products and applications indicated unless more stringent requirements are specified in this Section or indicated on Drawings.

Retain "Asphalt-Saturated Organic Felt" Paragraph below if required. Because of slate shingles' long service lives, NRCA recommends using polymer-modified bitumen sheet instead of felt underlayment. Verify recommendations of local installers and slate-shingle manufacturers.

        - Asphalt-Saturated Organic Felt: Install on roof deck parallel with and starting at eaves and fasten with underlayment nails.

Retain "Single-Layer Installation" or "Double-Layer Installation" Subparagraph below to suit Project. Some shingle manufacturers recommend a double-layer installation. The National Slate Association recommends using double layer for roof slopes from 4:12 to 8:12, for 3/8-inch- (10-mm-) thick or thicker slates, and for slates smaller than 12 by 9 inches (305 by 229 mm).

          - Single-Layer Installation:

Usually, retain first option in first subparagraph below for 2-inch- (51-mm-) minimum side laps, except for where the limiting design wind speed is equal to or greater than 140 mph (63 m/s). In that case, the IBC and the IRC require at least 4-inch (102-mm) side laps. Verify requirements of authorities having jurisdiction.

            - Lap sides a minimum of [2 inches (51 mm)] [4 inches (102 mm)] over underlying course.

            - Lap ends a minimum of 4 inches (102 mm).

            - Stagger end laps between succeeding courses at least 72 inches (1829 mm).

Side lap and starter course dimensions in "Double-Layer Installation" Subparagraph below are based on 36-inch- (914-mm-) wide rolls of felt underlayment and are needed to maintain double-layer felt underlayment coverage with 2 inches (51 mm) to spare. Verify requirements of authorities having jurisdiction.

          - Double-Layer Installation:

            - Install a 19-inch- (483-mm-) wide starter course at eaves and completely cover with a 36-inch- (914-mm-) wide second course.

            - Install succeeding 36-inch- (914-mm-) wide courses lapping previous courses 19 inches (483 mm) in shingle fashion.

            - Lap ends a minimum of 4 inches (102 mm).

            - Stagger end laps between succeeding courses at least 72 inches (1829 mm).

Retain first subparagraph below if cemented double layers of felt serve as water and ice-dam membranes or if required for additional protection. Some slate-shingle manufacturers recommend using cemented double layers. Self-adhering, polymer-modified bitumen sheet has largely replaced cemented double layers of felt as water and ice-dam protection.

            - Apply a continuous layer of asphalt roofing cement over starter course and on felt surface to be concealed by succeeding courses as each felt course is installed. Apply [over entire roof] [at locations indicated on Drawings].

Retain first subparagraph below for areas subject to high wind speeds. The IBC requires fastening of underlayment in grid pattern described below where the basic design wind speed is equal to or greater than 140 mph (63 m/s). The IRC requires the same fastening pattern where the ultimate design wind speed is equal to or greater than 140 mph (63 m/s).

          - Install fasteners in a grid pattern of 12 inches (305 mm) between side laps with 6-inch (152-mm) spacing at side and end laps.

Retain first subparagraph below if combining felt with self-adhering, polymer-modified bitumen sheet. NRCA recommends covering water and ice-dam protection with the roof-field underlayment.

          - Install felt over areas protected by self-adhering, polymer-modified bitumen sheet.

Retain first option in subparagraph below if desired for areas where roof deck is covered by self-adhering, polymer-modified bitumen sheet against walls and other roof projections. Verify requirements of authorities having jurisdiction for cap and base flashing at masonry or stucco walls and chimneys and revise subparagraph to suit Project.

          - Terminate felt [flush] [extended up not less than 4 inches (102 mm)] <Insert requirements> against sidewalls, curbs, chimneys, and other roof projections.

Retain "Synthetic-Underlayment Top Layer" Paragraph below if required as a top layer over an anchor layer of mechanically fastened, polymer-modified bitumen sheet or an anchor layer of self-adhering, polymer-modified bitumen sheet.

        - Synthetic-Underlayment Top Layer: Install in accordance with manufacturer's written installation instructions and as second layer over anchor-layer underlayment.

          - Completely cover anchor-layer underlayment and install parallel with and starting at the eaves, with side laps offset halfway between side laps of underlying anchor layer.

Usually, retain first option in first subparagraph below for 2-inch- (51-mm-) minimum side laps, except for where the limiting design wind speed is equal to or greater than 140 mph (63 m/s). In that case, the IBC and the IRC require at least 4-inch (102-mm) side laps. Verify requirements of manufacturers and authorities having jurisdiction.

          - Lap sides and ends as recommended in writing by manufacturer, but not less than [2 inches (51 mm)] [4 inches (102 mm)] for side laps and 6 inches (152 mm) for end laps.

          - Stagger end laps from anchor-layer end laps and between succeeding top courses at interval recommended in writing by manufacturer, but not less than 72 inches (1829 mm).

          - Fasten with underlayment nails.

Retain subparagraph below for areas subject to high wind speeds. The IBC requires fastening of underlayment in grid pattern described below where the basic design wind speed is equal to or greater than 140 mph (63 m/s). The IRC requires the same fastening pattern where the ultimate design wind speed is equal to or greater than 140 mph (63 m/s).

          - Install fasteners in a grid pattern of 12 inches (305 mm) between side laps with 6-inch (152-mm) spacing at side and end laps.

Retain "Polymer-Modified Bitumen Sheet" Paragraph below if required. NRCA's "The NRCA Roofing Manual: Steep-Slope Roof Systems" recommends using polymer-modified bitumen sheet in single-, double-, and two-layer installations. In two-layer installations, NRCA recommends using it as an anchor layer under a top layer of mechanically fastened, polymer-modified bitumen sheet or synthetic underlayment; as an anchor layer under a top layer of polymer-modified bitumen sheet adhered using hot bitumen or cold adhesive or a top layer of self-adhering, polymer-modified bitumen sheet; and as a top layer over an anchor layer of self-adhering, polymer-modified bitumen sheet.

        - Polymer-Modified Bitumen Sheet: Install parallel with and starting at eaves.

Retain one of first three installation subparagraphs below to suit Project.

Retain "Single- or Anchor-Layer Installation" Subparagraph below with "Top-Layer Installation" Subparagraph for both methods of two-layer installation recommended by NRCA. NRCA also recommends using self-adhering, polymer-modified bitumen sheet for the anchor layer. Delete both subparagraphs and retain "Double-Layer Installation" Subparagraph for another installation method recommended by NRCA.

          - Single- or Anchor-Layer Installation:

            - Install on roof deck.

Usually, retain first option in first subparagraph below for 2-inch- (51-mm-) minimum side laps, except for where the limiting design wind speed is equal to or greater than 140 mph (63 m/s). In that case, the IBC and the IRC require at least 4-inch (102-mm) side laps. Verify requirements of authorities having jurisdiction.

            - Lap sides a minimum of [2 inches (51 mm)] [4 inches (102 mm)] over underlying course.

            - Lap ends a minimum of 6 inches (152 mm).

            - Stagger end laps between succeeding courses at least 72 inches (1829 mm).

            - Fasten with underlayment nails.

          - Top-Layer Installation:

            - Install as a second layer over anchor-layer underlayment.

            - Completely cover anchor layer, with side laps offset halfway between side laps of underlying anchor layer.

Usually, retain first option in first subparagraph below for 2-inch- (51-mm-) minimum side laps, except for where the limiting design wind speed is equal to or greater than 140 mph (63 m/s). In that case, the IBC and the IRC require at least 4-inches (102-mm) side laps. Verify requirements of authorities having jurisdiction.

            - Lap sides a minimum of [2 inches (51 mm)] [4 inches (102 mm)].

            - Lap ends a minimum of 6 inches (152 mm).

            - Stagger end laps from anchor-layer end laps and between succeeding top-layer courses at least 72 inches (1829 mm).

            - [Fasten with underlayment nails] [Adhere to anchor layer in a solid mopping of hot roofing asphalt, applied within plus or minus 25 deg F (14 deg C) of equiviscous temperature] [Adhere to anchor layer in uniform coating of cold-applied adhesive].

          - Double-Layer Installation:

            - Install on roof deck in overlapping layers with a half-width plus 1-inch- (25-mm-) wide starter course at eaves completely covered by full-width second course.

            - Install succeeding courses lapping previous courses by a half-width plus 1 inch (25 mm) in shingle fashion.

            - Lap ends a minimum of 6 inches (152 mm).

            - Stagger end laps between succeeding courses at least 72 inches (1829 mm).

            - Fasten with underlayment nails.

Retain first subparagraph below for areas subject to high wind speeds. The IBC requires fastening of underlayment in grid pattern described below where the basic design wind speed is equal to or greater than 140 mph (63 m/s). The IRC requires the same fastening pattern where the ultimate design wind speed is equal to or greater than 140 mph (63 m/s).

          - Install fasteners in a grid pattern of 12 inches (305 mm) between side laps with 6-inch (152-mm) spacing at side and end laps.

Retain first subparagraph below if combining polymer-modified bitumen sheet with self-adhering, polymer-modified bitumen sheet used for water and ice-dam protection. NRCA recommends covering water and ice-dam protection with the roof-field underlayment.

          - Install sheets over areas protected by self-adhering, polymer-modified bitumen sheet.

Retain first option in subparagraph below if desired for areas where roof deck is covered by self-adhering, polymer-modified bitumen sheet against walls and other roof projections.

          - Terminate sheets [flush] [extended up not less than 4 inches (102 mm)] <Insert requirements> against sidewalls, curbs, chimneys, and other roof projections.

Retain "Self-Adhering, Polymer-Modified Bitumen Sheet" Paragraph below if required. NRCA's "The NRCA Roofing Manual: Steep-Slope Roof Systems" recommends using a single layer of self-adhering, polymer-modified bitumen sheet over the entire roof deck, although NRCA suggests covering it with a layer of another type of underlayment. NRCA recommends using it as an anchor layer for a top layer of mechanically fastened, polymer-modified bitumen sheet or synthetic underlayment and using it for a top layer over mechanically fastened, polymer-modified bitumen sheet.

        - Self-Adhering, Polymer-Modified Bitumen Sheet: Install, wrinkle free.

          - Comply with low-temperature installation restrictions of underlayment manufacturer.

          - Install lapped in direction that sheds water. Lap sides not less than 4 inches (102 mm).

          - Lap ends not less than 6 inches (152 mm), staggered 24 inches (610 mm) between succeeding courses.

          - Roll laps with roller.

Retain first subparagraph below if primer is required to enhance adhesion to concrete and masonry surfaces, such as chimneys or walls, and metal surfaces, such as valley flashing.

          - Prime concrete, masonry, and metal surfaces to receive self-adhering, polymer-modified bitumen sheet.

Retain "Single- or Anchor-Layer Installation" Subparagraph below if self-adhering, polymer-modified bitumen sheet covers the entire roof deck. NRCA suggests installing a second layer of another type of underlayment over self-adhering, polymer-modified bitumen sheet.

          - Single- or Anchor-Layer Installation: Install over entire roof deck.

Retain "Top-Layer Installation" Subparagraph below if required. Slates might stick to granule-surfaced top layers. Verify manufacturers' written instructions for top-layer installation and revise to suit Project.

          - Top-Layer Installation: Install as second layer over anchor-layer underlayment.

            - Completely cover anchor-layer underlayment.

            - Offset side laps halfway between side laps of underlying anchor layer and offset end laps from those of underlying anchor layer at least 72 inches (1829 mm).

Retain "Water and Ice-Dam Protection Installation" Subparagraph below if a layer of self-adhering, polymer-modified bitumen sheet partially covers roof deck in areas vulnerable to moisture penetration; revise to suit Project. Because of slate's long service life, NRCA recommends extending the underlayment covering the roof field over the water and ice-dam protection layer.

          - Water and Ice-Dam Protection Installation: Install on roof deck where indicated [below] [on Drawings].

Retain one or more of first eight subparagraphs below if locations are not indicated on Drawings. Revise to suit Project.

            - Eaves: Extend from edges of eaves [24 inches (610 mm)] [36 inches (914 mm)] <Insert dimension> beyond interior face of exterior wall.

            - Rakes: Extend from edges of rakes [24 inches (610 mm)] [36 inches (914 mm)] <Insert dimension> beyond interior face of exterior wall.

Verify requirements of authorities having jurisdiction for valley underlayment.

            - Valleys: Extend from lowest to highest point [18 inches (457 mm)] <Insert dimension> on each side of centerline.

            - Hips: Extend [18 inches (457 mm)] <Insert dimension> on each side.

            - Ridges: Extend [36 inches (914 mm)] <Insert dimension> on each side[ without obstructing continuous ridge vent slot].

            - Sidewalls: Extend [18 inches (457 mm)] <Insert dimension> beyond sidewalls and return vertically against sidewalls not less than [4 inches (102 mm)] <Insert dimension>.

            - Dormers, Chimneys, Skylights, and Other Roof-Penetrating Elements: Extend [18 inches (457 mm)] <Insert dimension> beyond penetrating elements and return vertically against penetrating elements not less than [4 inches (102 mm)] <Insert dimension>.

            - Roof-Slope Transitions: Extend [18 inches (457 mm)] <Insert dimension> on each roof slope.

          - Cover underlayment within seven days.

Retain "Valley Underlayment" Paragraph below if required and if installing self-adhering, polymer-modified bitumen sheet is not specified for water and ice-dam protection at valleys. Paragraph is applicable if using felt or polymer-modified bitumen sheet underlayment; synthetic-underlayment manufacturers recommend using self-adhering, polymer-modified bitumen sheet for valley underlayment. Paragraph is based on NRCA recommendations. Verify requirements of authorities having jurisdiction and revise to suit Project.

        - Valley Underlayment: Install one layer of 36-inch- (914-mm-) wide underlayment centered in valley, running full length of valley, and on top of underlayment on field of roof that is woven through valley. Install all layers of underlayment in and through valley tight with no bridging.

Revise first subparagraph below to suit Project.

          - Use [same underlayment as installed on field of roof] <Insert requirements>.

          - Lap ends at least 12 inches (305 mm) in direction that sheds water, and seal with asphalt roofing cement.

          - Fasten to roof deck with underlayment nails located as far from valley center as possible and only to extent necessary to hold underlayment in place until installation of valley flashing.

      - INSTALLATION OF RIDGE ACCESSORIES

Retain this article if manufactured ridge caps or ridge vents are required.

        - Metal Ridge Caps: Install units in accordance with manufacturer's written instructions.

Retain subparagraph below if covering ridge cap with slate shingles.

          - Install slate shingles into retention channels, butting adjacent shingles.

        - Rigid-Plastic Ridge Vents: Install continuous ridge vents in accordance with manufacturer's written instructions. Fasten with slating nails of sufficient length to penetrate sheathing.

      - INSTALLATION OF METAL FLASHING AND TRIM

        - Install metal flashings and other sheet metal to comply with requirements in Section 076200 "Sheet Metal Flashing and Trim."

          - Install metal flashings in accordance with recommendations in NRCA's "The NRCA Roofing Manual: Steep-Slope Roof Systems."

Retain "Apron Flashings" Paragraph below to provide a weatherproofing transition material where a roof area intersects a head wall. Common locations for apron flashings include the front downslope side of a dormer or chimney, curbed roof penetrations, and clerestory transitions.

        - Apron Flashings: Extend lower flange over and beyond each side of downslope slate shingles and up the vertical surface.

Retain "Step Flashings" Paragraph below for interweaving metal step flashings between succeeding courses of slate shingles that abut vertical surfaces such as chimneys, sidewalls, and skylights.

        - Step Flashings: Install with a headlap of 3 inches (76 mm) and extend both horizontally and vertically. Install with lower edge of flashing just upslope of, and concealed by, butt of overlying slate shingle. Fasten to roof deck only.

Retain "Cricket and Backer Flashings" Paragraph below if required.

        - Cricket and Backer Flashings: Install against roof-penetrating elements, extending concealed flange beneath upslope slate shingles and beyond each side.

        - Counterflashings: Coordinate with installation of base flashing and fit tightly to base flashing. Lap joints a minimum of 4 inches (102 mm) secured in a waterproof manner.

          - Install in reglets or receivers.

Retain "Hip Flashings" Paragraph below if interwoven hip flashings are required for mitered or fantail hips.

        - Hip Flashings: Install centered over hip with lower edge of flashing concealed by butt of overlying slate shingle. Fasten to roof deck.

        - Open-Valley Flashings: Install centered in valleys, lapping ends at least [8 inches (203 mm)] <Insert dimension> in direction that sheds water.

          - Fasten upper end of each length to roof deck beneath overlap.

Retain one of first two subparagraphs below, or both, if required. NRCA recommends using cleats and stripping-in flashing using self-adhering, polymer-modified bitumen sheet strips adhered to metal flanges and similar valley underlayment in climates prone to heavy accumulations of snow and ice or regular freeze-thaw cycling.

          - Secure hemmed flange edges into metal cleats spaced [12 inches (305 mm)] [24 inches (610 mm)] <Insert dimension> apart and fastened to roof deck.

          - Adhere minimum [9-inch- (229-mm-)] <Insert dimension> wide strips of self-adhering, polymer-modified bitumen sheet to metal flanges and to [underlying self-adhering, polymer-modified bitumen sheet] <Insert requirements>. Place strips parallel to and over flanges so that they will be just concealed by installed shingles.

Retain subparagraph below for climates prone to heavy accumulations of snow and ice or regular freeze-thaw cycling.

          - Provide a closure at the end of the inverted-V profile of the valley metal to minimize water and ice infiltration.

        - Closed-Valley Flashings: Install centered in valleys, lapping ends at least [8 inches (203 mm)] <Insert dimension> in direction that sheds water. Fasten upper end of each length to roof deck beneath overlap.

Retain first or second subparagraph below, or both, if required. NRCA recommends using cleats and stripping-in flashing using self-adhering, polymer-modified bitumen sheet strips adhered to metal flanges and similar underlayment in climates prone to heavy accumulations of snow and ice or regular freeze-thaw cycling.

          - Secure hemmed flange edges into metal cleats spaced [12 inches (305 mm)] [24 inches (610 mm)] <Insert dimension> apart and fastened to roof deck.

          - Adhere minimum [9-inch- (229-mm-)] <Insert dimension> wide strips of self-adhering, polymer-modified bitumen sheet to metal flanges and to [underlying self-adhering, polymer-modified bitumen] <Insert requirements> valley underlayment.

        - Interwoven Closed-Valley Flashings: Install centered in valleys at every shingle course overlapping the shingles in the preceding course similar to a step flashing treatment so that the butts just conceal the end of the flashing after installing the course. Fasten to roof approximately 8 inches (203 mm) away from center of the valley.

Retain "Rake Drip Edges" and "Eave Drip Edges" paragraphs below if applicable.

        - Rake Drip Edges: Install over underlayment materials and fasten to roof deck.

        - Eave Drip Edges: [Install over wood cant strip and under underlayment materials; fasten to roof deck] <Insert description>.

        - Pipe Flashings: Form flashing around pipe penetrations and slate shingles. Fasten and seal to slate shingles.

      - ROOFING INSTALLER'S WARRANTY

Retain this article if required. Revise to include another Roofing Installer's Warranty form or as advised by Owner's counsel. Coordinate with "Warranty" Article.

        - WHEREAS <Insert name> of <Insert address>, herein called the "Roofing Installer," has performed roofing and associated work ("the work") on the following project:

          - Owner: <Insert name of Owner>.

          - Owner Address: <Insert address>.

          - Building Name/Type: <Insert information>.

          - Building Address: <Insert address>.

          - Area of the Work: <Insert information>.

          - Acceptance Date: <Insert date>.

          - Warranty Period: <Insert time>.

          - Expiration Date: <Insert date>.

        - AND WHEREAS Roofing Installer has contracted (either directly with Owner or indirectly as a subcontractor) to warrant the work against leaks and faulty or defective materials and workmanship for designated Warranty Period,

        - NOW THEREFORE Roofing Installer hereby warrants, subject to terms and conditions herein set forth, that, during Warranty Period, Roofing Installer will, at Roofing Installer's own cost and expense, make or cause to be made such repairs to or replacements of the work as are necessary to correct faulty and defective work and as are necessary to maintain the work in a watertight condition.

        - This Warranty is made subject to the following terms and conditions:

          - Specifically excluded from this Warranty are damages to the work and other parts of the building, and to building contents, caused by:

            - Lightning;

Insert required wind speed in first subparagraph below.

            - Peak gust wind speed exceeding <Insert mph (m/s)>;

            - Fire;

            - Failure of roofing system substrate, including cracking, settlement, excessive deflection, deterioration, and decomposition;

            - Faulty construction of copings, chimneys, skylights, vents, equipment supports, and other edge conditions and penetrations of the work;

            - Vapor condensation on bottom of roofing; and

            - Activity on roofing by others, including construction contractors, maintenance personnel, other persons, and animals, whether authorized or unauthorized by Owner.

          - When the work has been damaged by any of foregoing causes, Warranty shall be null and void until such damage has been repaired by Roofing Installer and until cost and expense thereof have been paid by Owner or by another responsible party so designated.

          - Roofing Installer is responsible for damage to the work covered by this Warranty but is not liable for consequential damages to building or building contents resulting from leaks or faults or defects of the work.

          - During Warranty Period, if Owner allows alteration of the work by anyone other than Roofing Installer, including cutting, patching, and maintenance in connection with penetrations, attachment of other work, and positioning of anything on roof, this Warranty shall become null and void on date of the alterations, but only to the extent the alterations affect the work covered by this Warranty. If Owner engages Roofing Installer to perform the alterations, Warranty shall not become null and void unless Roofing Installer, before starting the alterations, notified Owner in writing, showing reasonable cause for claim, that the alterations would likely damage or deteriorate the work, thereby reasonably justifying a limitation or termination of this Warranty.

          - During Warranty Period, if original use of roof is changed and it becomes used for, but was not originally specified for, a use or service more severe than originally specified, this Warranty shall become null and void on date of the change, but only to the extent the change affects the work covered by this Warranty.

          - Owner shall promptly notify Roofing Installer of observed, known, or suspected leaks, defects, or deterioration and shall afford reasonable opportunity for Roofing Installer to inspect the work and to examine evidence of such leaks, defects, or deterioration.

          - This Warranty is recognized to be the only warranty of Roofing Installer on the work and shall not operate to restrict or cut off Owner from other remedies and resources lawfully available to Owner in cases of roofing failure. Specifically, this Warranty shall not operate to relieve Roofing Installer of responsibility for performance of the work according to requirements of the Contract Documents, regardless of whether Contract was a contract directly with Owner or a subcontract with Owner's General Contractor.

        - IN WITNESS THEREOF, this instrument has been duly executed this <Insert day> day of <Insert month>, <Insert year>.

          - Authorized Signature: <Insert signature>.

          - Name: <Insert name>.

          - Title: <Insert title>.

END OF SECTION 073126