Copyright 2022 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 074646 - FIBER-CEMENT SIDING

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Access Manufacturer-Provided, AIA MasterSpec-Based Sections:

<Double click here for this Section based on specific manufacturer’s products set as Basis-of-Design at ProductMasterSpec.com.>

Revise this Section by inserting or deleting text to meet Project-specific requirements.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Fiber-cement siding.

          - Fiber-cement soffit.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 061000 "Rough Carpentry" for wood furring, grounds, nailers, and blocking.

          - Section 062013 "Exterior Finish Carpentry" for exterior [cellular PVC] [and] [foam-plastic] trim.

          - Section 072500 "Weather Barriers" for weather-resistive barriers.

      - COORDINATION

        - Coordinate siding installation with flashings and other adjoining construction to ensure proper sequencing.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

      - ACTION SUBMITTALS

        - Product Data:

          - Fiber-cement siding.

          - Fiber-cement soffit.

        - Product Data Submittals: For each type of fiber-cement [siding] [and] [soffit].[ Include construction details, material descriptions, dimensions of individual components and profiles, and finishes.]

        - Samples for Initial Selection: For fiber-cement [siding] [and] [soffit] including related accessories.

        - Samples for Verification:[ For each type, color, texture, and pattern required.]

Retain one of first two subparagraphs below.

          - 12-inch- (300-mm-) long-by-actual-width Sample of siding.

          - 24-inch- (600-mm-) wide-by-36-inch- (900-mm-) high Sample panel of siding assembled on plywood backing.

Retain one or both subparagraphs below if required.

          - 12-inch- (300-mm-) long-by-actual-width Sample of soffit.

          - 12-inch- (300-mm-) long-by-actual-width Samples of trim and accessories.

      - INFORMATIONAL SUBMITTALS

        - Product Certificates: For each type of fiber-cement [siding] [and] [soffit].

        - Product Test Reports: Based on evaluation of comprehensive tests performed by a qualified testing agency, for fiber-cement siding.

        - Research/Evaluation Reports: For each type of fiber-cement siding required, from ICC-ES.

        - Sample Warranty: For special warranty.

      - CLOSEOUT SUBMITTALS

        - Maintenance Data: For each type of fiber-cement [siding] [and] [soffit], including related accessories, to include in maintenance manuals.

      - MAINTENANCE MATERIAL SUBMITTALS

        - Furnish extra materials that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

          - Furnish full lengths of fiber-cement [siding] [and] [soffit] including related accessories, in a quantity equal to 2 percent of amount installed.

      - MOCKUPS

        - Build mockups to verify selections made under Sample submittals and to demonstrate aesthetic effects and to set quality standards for fabrication and installation.

Retain first subparagraph below for large-scale mockup. Indicate portion of wall represented by mockup on Drawings or draw mockup as separate element.

          - Build mockup of typical wall area as shown on Drawings.

Retain first subparagraph below for limited mockups.

          - Build mockups for fiber-cement [siding] [and] [soffit] including accessories.

            - Size: [48 inches (1200 mm) long by 60 inches (1800 mm) high] <Insert dimensions>.

            - Include outside corner on one end of mockup[ and inside corner on other end].

Retain first subparagraph below if mockups are not only for establishing appearance factors.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver and store packaged materials in original containers with labels intact until time of use.

        - Store materials on elevated platforms, under cover, and in a dry location.

      - WARRANTY

When warranties are required, verify with Owner's counsel that warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

        - Special Warranty: Manufacturer agrees to repair or replace products that fail in materials or workmanship within specified warranty period.

          - Failures include, but are not limited to, the following:

            - Structural failures including cracking and deforming.

            - Deterioration of materials beyond normal weathering.

            - <Insert failure modes>.

Verify available warranties and warranty periods for fiber-cement siding and soffit.

          - Warranty Period: [10] [25] [50] <Insert number> years from date of Substantial Completion.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - SOURCE LIMITATIONS

        - Obtain products, including related accessories, from single source from single manufacturer.

      - FIBER-CEMENT SIDING

        - Fiber-Cement Siding: ASTM C1186, Type A, Grade II, fiber-cement board, noncombustible when tested in accordance with ASTM E136; with a flame-spread index of 25 or less when tested in accordance with ASTM E84.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

The International Building Code requires fiber-cement siding to be third-party tested and labeled in accordance with ASTM C1186.

        - Labeling: Provide fiber-cement siding that is tested and labeled in accordance with ASTM C1186 by a qualified testing agency acceptable to authorities having jurisdiction.

        - Nominal Thickness: Not less than 5/16 inch (8 mm).

Retain one or more of first four paragraphs below or revise to suit Project. "Horizontal Pattern" Subparagraph includes some sizes advertised by manufacturers listed; verify availability before retaining. Widths are board sizes; exposure is 1-1/4 to 1-1/2 inches (32 to 38 mm) less.

        - Horizontal Pattern: Boards [5-1/4 inches (133 mm)] [6-1/4 to 6-1/2 inches (159 to 165 mm)] [7-1/4 to 7-1/2 inches (184 to 190 mm)] [8-1/4 to 8-1/2 inches (210 to 216 mm)] [9-1/4 to 9-1/2 inches (235 to 241 mm)] <Insert dimensions> wide in [plain] [beaded-edge] <Insert requirement> style.

          - Texture: [Smooth] [Rough sawn] [Wood grain] <Insert requirement>.

        - Vertical Pattern: 48-inch- (1200-mm-) wide sheets with wood-grain texture and grooves [8 inches (203 mm)] [12 inches (300 mm)] <Insert dimension> o.c.

        - Shingle Pattern: 48-inch- (1200-mm-) wide, [straight-edge notched] [staggered-edge notched] <Insert requirement> sheets with wood-grain texture.

        - Panel Texture: 48-inch- (1200-mm-) wide sheets with [smooth] [stucco] [wood-grain] <Insert requirement> texture.

Factory priming is generally offered as an optional feature by manufacturers listed.

        - Factory Priming: Manufacturer's standard acrylic primer.

      - FIBER-CEMENT SOFFIT

        - Fiber-Cement Soffit: ASTM C1186, Type A, Grade II, fiber-cement board, noncombustible when tested in accordance with ASTM E136; with a flame-spread index of 25 or less when tested in accordance with ASTM E84.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Nominal Thickness: Not less than 5/16 inch (8 mm).

        - Pattern: [12-inch- (300-mm-)] [16-inch- (400-mm-)] [24-inch- (600-mm-)] <Insert dimension> wide sheets with [smooth] [wood-grain] <Insert requirement> texture.

Perforated panels are offered by James Hardie.

        - Ventilation: Provide [perforated] [unperforated] soffit[ unless otherwise indicated].

Factory priming is generally offered as an optional feature by manufacturers listed.

        - Factory Priming: Manufacturer's standard acrylic primer.

      - ACCESSORIES

        - Siding Accessories, General: Provide starter strips, edge trim, outside and inside corner caps, and other items as recommended by siding manufacturer for building configuration.

          - Provide accessories matching color and texture of adjacent siding unless otherwise indicated.

Retain "Decorative Accessories" Paragraph below if decorative accessories are required for Project. Verify availability with manufacturers.

        - Decorative Accessories: Provide the following fiber-cement decorative accessories as indicated:

Retain decorative accessories in subparagraphs below and revise to suit Project. Indicate locations and details on Drawings.

          - Corner posts.

          - Door and window casings.

          - Fasciae.

          - Moldings and trim.

          - <Insert accessories>.

        - Flashing: Provide [aluminum] [stainless steel] <Insert metal> flashing complying with Section 076200 "Sheet Metal Flashing and Trim" at window and door heads and where indicated.

          - Finish for Aluminum Flashing: [Siliconized polyester coating] [High-performance organic finish] [Factory-prime coating] <Insert finish>.

        - Fasteners:

          - For fastening to wood, use [siding nails] [ribbed bugle-head screws] of sufficient length to penetrate a minimum of 1 inch (25 mm) into substrate.

          - For fastening to metal, use ribbed bugle-head screws of sufficient length to penetrate a minimum of 1/4 inch (6 mm), or three screw-threads, into substrate.

          - For fastening fiber cement, use [hot-dip galvanized] [stainless steel] fasteners.

        - Insect Screening for Soffit Vents: [Aluminum, 18-by-16 (1.4-by-1.6-mm) mesh] [PVC-coated, glass-fiber fabric, 18-by-14 or 18-by-16 (1.4-by-1.8- or 1.4-by-1.6-mm) mesh] [Stainless steel, 18-by-18 (1.4-by-1.4-mm) mesh] <Insert requirement>.

        - Continuous Soffit Vents: Aluminum, hat-channel shape, with [stamped louvers] [perforations]; 2 inches (51 mm) wide and not less than 96 inches (2438 mm) long.

          - Net-Free Area: [4 sq. in./linear ft. (280 sq. cm/m)] [6 sq. in./linear ft. (420 sq. cm/m)] [8 sq. in./linear ft. (560 sq. cm/m)] <Insert dimension>.

          - Finish: [Mill finish] [White paint] [Brown paint] <Insert requirement>.

        - Round Soffit Vents: Stamped aluminum louvered vents, [2 inches (51 mm)] [2-1/2 inches (64 mm)] [3 inches (76 mm)] [4 inches (102 mm)] <Insert dimension> in diameter, made to be inserted in round holes cut into soffit.

          - Finish: [Mill finish] [White paint] [Brown paint] <Insert requirement>.

- EXECUTION

      - EXAMINATION

        - Examine substrates for compliance with requirements for installation tolerances and other conditions affecting performance of fiber-cement [siding] [and] [soffit] and related accessories.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Clean substrates of projections and substances detrimental to application.

      - INSTALLATION

        - General: Comply with manufacturer's written installation instructions applicable to products and applications indicated unless more stringent requirements apply.

          - Do not install damaged components.

          - Install fasteners no more than [24 inches (600 mm)] <Insert dimension> o.c.

        - Install joint sealants as specified in Section 079200 "Joint Sealants" and to produce a weathertight installation.

      - ADJUSTING AND CLEANING

        - Remove damaged, improperly installed, or otherwise defective materials and replace with new materials complying with specified requirements.

        - Clean finished surfaces according to manufacturer's written instructions and maintain in a clean condition during construction.

END OF SECTION 074646