Copyright 2022 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 075556 - FLUID-APPLIED PROTECTED MEMBRANE ROOFING

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

MasterSpec includes provisions for LEED v4, LEED v4.1, IgCC/ASHRAE 189.1, and Green Globes. Sustainable design requirements may be inserted in the Section Text using the hypertext links.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Hot fluid-applied, rubberized-asphalt roofing membrane.

          - Base flashing sheet materials.

          - Roof insulation.

          - Electronic leak detection (ELD) materials.

          - Ballast.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 061000 "Rough Carpentry" for wood nailers, curbs, and blocking.

          - Section 076200 "Sheet Metal Flashing and Trim" for metal roof flashings and counterflashings.

          - Section 077129 "Manufactured Roof Expansion Joints" for proprietary manufactured roof expansion-joint assemblies.

          - Section 079200 "Joint Sealants" for joint sealants, joint fillers, and joint preparation.

          - Section 221423 "Storm Drainage Piping Specialties" for roof drains.

      - DEFINITIONS

        - Roofing Terminology: See ASTM D1079 and glossary of NRCA's "The NRCA Roofing and Waterproofing Manual" for definition of terms related to roofing work in this Section.

      - PREINSTALLATION MEETINGS

Consider retaining "Preliminary Roofing Conference" Paragraph below if roofing installation is large and complicated. A preliminary roofing conference precedes a preinstallation conference and focuses on roof deck construction and planning activities of roofing Installer.

        - Preliminary Roofing Conference: Before starting roof deck construction, conduct conference at [Project site] <Insert location>.

Retain subparagraphs below if required. If retaining, revise to include Project-specific requirements. Insert additional requirements to suit Project.

          - Meet with Owner, Architect, Owner's insurer if applicable, testing and inspecting agency representative, roofing Installer, roofing system manufacturer's representative, and installers whose work interfaces with or affects roofing, including installers of roof accessories and roof-mounted equipment.

          - Review methods and procedures related to roofing installation, including manufacturer's written instructions.

          - Review and finalize construction schedule, and verify availability of materials, Installer's personnel, equipment, and facilities needed to make progress and avoid delays.

          - Review substrate requirements for conditions and finishes, including flatness.

          - Review structural loading limitations of roof deck during and after roofing.

          - Review base flashings, special roofing details, roof drainage, roof penetrations, equipment curbs, and condition of other construction that affects roofing system.

          - Review governing regulations and requirements for insurance and certificates if applicable.

          - Review temporary protection requirements for roofing during and after installation.

          - Review roof observation and repair procedures after roofing installation.

Retain "Preinstallation Roofing Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a preinstallation conference. Paragraph is recommended with or without a preliminary roofing conference.

        - Preinstallation Roofing Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

Retain subparagraphs below if required. If retaining, revise to include Project-specific requirements. Insert additional requirements to suit Project.

          - Meet with Owner, Architect, Owner's insurer if applicable, testing and inspecting agency representative, roofing Installer, roofing system manufacturer's representative, and installers whose work interfaces with or affects roofing, including installers of roof accessories and roof-mounted equipment.

          - Review methods and procedures related to roofing installation, including manufacturer's written instructions.

          - Review and finalize construction schedule, and verify availability of materials, Installer's personnel, equipment, and facilities needed to make progress and avoid delays.

          - Review substrate requirements for conditions and finishes, including flatness.

          - Review structural loading limitations of roof deck during and after roofing.

          - Review base flashings, special roofing details, roof drainage, roof penetrations, equipment curbs, and condition of other construction that affects roofing system.

          - Review governing regulations and requirements for insurance and certificates if applicable.

          - Review temporary protection requirements for roofing during and after installation.

          - Review roof observation and repair procedures after roofing installation.

      - ACTION SUBMITTALS

        - Product Data: For the following:

          - Hot fluid-applied, rubberized-asphalt roofing membrane.

          - Base flashing sheet materials.

          - Asphalt primer.

          - Elastomeric sheet.

          - Metal termination bars.

          - Reinforcing fabric.

          - Protection course.

          - Roof insulation.

          - Insulation accessories.

          - Ballast.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for roofing.>

        - Shop Drawings: For roofing system. Include plans, elevations, sections, details, and attachments to other work.

Retain subparagraph below if retaining roof pavers.

          - Show locations, extent, and details of roof pavers.

        - Samples for Verification: For each of the following products:

Samples in subparagraphs below are examples only; retain if required.

          - Flashing material, of color required.

          - Aggregate ballast in gradation[ and color] indicated.

          - Roof paver[, full sized,] in each color and texture required.

      - INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

        - Qualification Data: For [Installer] [and] [testing agency].

Retain "Manufacturer Certificates" Paragraph below if retaining "Roofing System Design," "FM Global Listing," or "Energy Performance" Paragraph in "Performance Requirements" Article.

        - Manufacturer Certificates: Signed by roofing manufacturer certifying that roofing system complies with requirements specified in "Performance Requirements" Article.

          - Submit evidence of compliance with performance requirements.

        - Product Test Reports: For components of roofing system, tests performed by manufacturer and witnessed by a qualified testing agency.

Retain "Field quality-control reports" Paragraph below if Contractor is responsible for field quality-control testing and inspecting. Retain option if submittal of manufacturer's final roof inspection report is required.

        - Field quality-control reports[ and manufacturer's final roof inspection report].

        - Sample Warranties: For manufacturer's special warranties.

      - CLOSEOUT SUBMITTALS

        - Maintenance Data: For roofing system to include in maintenance manuals.

      - QUALITY ASSURANCE

Revise "Installer Qualifications" Paragraph below if placing further limitations on Installer. A roofing manufacturer may approve, license, or otherwise qualify an installer.

        - Installer Qualifications: A qualified firm that is approved, authorized, or licensed by roofing system manufacturer to install manufacturer's product and that is eligible to receive manufacturer's special warranty.

        - Mockups: Install roofing on 100 sq. ft. (9.3 sq. m) of deck to demonstrate surface preparation, joint and crack treatment, thickness of roofing, and execution quality. Install [insulation] [aggregate ballast] [and] [roof pavers] over roofing membrane.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver roofing materials to Project site in original containers with seals unbroken and labeled with manufacturer's name, product brand name and type, date of manufacture, approval or listing agency markings, and directions for storing and mixing with other components.

        - Handle and store roofing materials, and place equipment in a manner to avoid significant or permanent damage to deck or structural supporting members.

        - Protect roof insulation materials from physical damage and from deterioration by sunlight, moisture, soiling, and other sources. Store in a dry location. Comply with insulation manufacturer's written instructions for handling, storing, and protecting during installation.

      - PROJECT CONDITIONS

        - Environmental Limitations: Apply roofing within the range of ambient and substrate temperatures recommended by roofing system manufacturer. Do not apply roofing to a damp or wet substrate or when temperature is below 0 deg F (minus 18 deg C).

          - Do not apply roofing in snow, rain, fog, or mist.

      - WARRANTY

When warranties are required, verify with Owner's counsel that warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

Retain "Special Warranty" Paragraph below if manufacturer's labor-and-materials warranty, covering roofing and base flashing, is required. Manufacturers of hot fluid-applied roofing do not offer "no-dollar-limit" warranties. Verify coverage offered by roofing manufacturers, because roof insulation, fasteners, and other roofing components may be excluded unless part of a roofing manufacturer's roofing system warranty. Board insulation or roof pavers may be the subject of separate warranties or may be excluded unless part of a total-system warranty. Revise below to suit Project. Verify warranty availability, and coordinate with manufacturers accordingly.

        - Special Warranty: Manufacturer agrees to repair or replace components of roofing system that fail in materials or workmanship within specified warranty period.

Retain first subparagraph below if a single-source or total-system warranty is required. Revise below if separate manufacturers' warranties are required for these components.

          - Warranty also includes base flashings, insulation,[ roof pavers,] and other components of roofing system.

Verify available roofing system warranties and warranty periods with manufacturers. Warranty periods of 10 and 15 years predominate, but 20 years may be available. Warranty periods of 15 and 20 years are usually limited to reinforced roofing membranes.

          - Warranty Period: [10] [15] [20] <Insert number> years from date of Substantial Completion.

Usually retain "Special Project Warranty" Paragraph below if deleting "Special Warranty" Paragraph above. Manufacturer's labor-and-materials warranty typically binds Installer for the first two or three years. If retaining below, retain or revise sample roofing Installer's warranty form at end of this Section. Alternatively, insert copy of local roofing contractor association's warranty form, or use another form as advised by Owner's counsel. Revise below to reflect scope of special Project warranty.

        - Special Project Warranty: Submit roofing Installer's warranty, on warranty form at end of this Section, signed by Installer, covering Work of this Section, including all components of roofing system such as base flashing, board insulation, [roof pavers] [and] [aggregate ballast] for the following warranty period:

Verify available warranties and warranty periods.

          - Warranty Period: [Two] <Insert number> years from date of Substantial Completion.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - SOURCE LIMITATIONS

Retain paragraph below if required to comply with FM Global, UL, or another building code, or to comply with provisions of manufacturer's special warranty. Consult manufacturer's literature because requirements vary.

        - Obtain roofing materials [sheet flashings] [protection course] [insulation] [pavers] [and] [pedestals] from single source from single manufacturer.

      - PERFORMANCE REQUIREMENTS

        - General Performance: Installed roofing and base flashings are to withstand specified uplift pressures, thermally induced movement, and exposure to weather without failure due to defective manufacture, fabrication, installation, or other defects in construction. Roofing and base flashings are to remain watertight.

          - Accelerated Weathering: Roofing system is to withstand 2000 hours of exposure when tested in accordance with ASTM G152, ASTM G154, or ASTM G155.

          - Impact Resistance: Roofing system is to resist impact damage when tested in accordance with ASTM D3746 or ASTM D4272.

        - Material Compatibility: Roofing materials are to be compatible with one another and adjacent materials under conditions of service and application required, as demonstrated by roofing manufacturer based on testing and field experience.

Retain "Roofing System Design" Paragraph below if roofing system is to be designed to withstand uplift pressure established by ASCE/SEI 7. Indicate dimensions of corners, perimeter, and field of roof on Drawings.

        - Roofing System Design: Tested by a qualified testing agency to resist the following uplift pressures:

          - Corner Uplift Pressure: <Insert lbf/sq. ft. (kPa)>.

          - Perimeter Uplift Pressure: <Insert lbf/sq. ft. (kPa)>.

          - Field-of-Roof Uplift Pressure: <Insert lbf/sq. ft. (kPa)>.

Retain "FM Global Listing" Paragraph below if Project is FM Global insured or if FM Global requirements set a minimum quality standard. Coordinate requirements in FM Global classification with other requirements in this Section. For further clarification, discuss with FM Global.

        - FM Global Listing: Roofing, base flashings, and component materials are to comply with requirements in FM Global 4450 or FM Global 4470 as part of a roofing system, and are to be listed in FM Global's "RoofNav" for Class 1 or noncombustible construction, as applicable. Identify materials with FM Global markings.

Retain one option in "Fire/Windstorm Classification" Subparagraph below based on windstorm classification of Project. FM Global Loss Prevention Data Sheet 1-28 multiplies the actual field-of-roof uplift pressure by a factor of 2 to obtain the factored pressure, the number that establishes the minimum FM Global approval rating. Verify availability of roofing systems that comply with these classifications. Other options for classifications increase in increments of 15 (e.g., Classes 1A-135, 1A-150, 1A-165, and higher). "Class 1A" signifies complying with ASTM E108, Class A fire performance for FM Approved Class 1 roof covers. For areas having three or more hailstorms annually, FM Global recommends roofing systems rated SH (severe hail) instead of MH (moderate hail).

          - Fire/Windstorm Classification: [Class 1A-60] [Class 1A-75] [Class 1A-90] [Class 1A-105] [Class 1A-120] <Insert class>.

          - Hail Resistance Rating: [MH] [SH].

        - <Double click to insert sustainable design text for solar reflectance index.>

Retain "Energy Star Listing" Paragraph below for roofs that must comply with the DOE's Energy Star requirements. The DOE's Energy Star "Roof Products Qualified Product List" is available in PDF at www.energystar.gov.

        - Energy Star Listing: Roofing system is to be listed on the DOE's Energy Star "Roof Products Qualified Product List" for low-slope roof products.

Usually retain "Energy Performance" Paragraph below for roofs that must comply with California Energy Commission's CEC-Title 24. Options are values required for low-slope roofs by prescriptive approach; revise if other values are required for building-envelope trade-off approach or whole-building performance approach. A list of products tested in accordance with ANSI/CRRC S100 with their test values is available at www.coolroofs.org.

        - Energy Performance: Roofing system is to have an initial solar reflectance not less than [0.70] <Insert value> and an emissivity of not less than [0.75] <Insert value> when tested in accordance with ANSI/CRRC S100.

Retain one of three options in "Exterior Fire-Test Exposure" Paragraph below based on fire classification of roof assembly and roof covering. Delete paragraph if including exterior fire-test exposure in FM Global class designation. Each manufacturer has a roofing system capable of obtaining a Class A UL listing over noncombustible decks. No Class B or Class C listings are reported.

        - Exterior Fire-Test Exposure: ASTM E108 or UL 790, [Class A] [Class B] [Class C]; for application and roof slopes indicated; testing by a qualified testing agency. Identify products with appropriate markings of applicable testing agency.

Retain "Fire-Resistance Ratings" Paragraph below only if products specified are part of a fire-resistance-rated assembly. Indicate rating, testing agency, and testing agency's design designation on Drawings.

        - Fire-Resistance Ratings: Comply with fire-resistance-rated assembly designs indicated. Identify products with appropriate markings of applicable testing agency.

      - ELECTRONIC LEAK DETECTION (ELD) MATERIALS

Retain this article if required for ELD testing. Certain roof assemblies require a conductive medium installed immediately below the roof membrane. Confirm selected materials will not void roofing warranty. See the Evaluations.

        - Conductive Medium: Materials providing less than 104 ohms per square as determined in accordance with ASTM D4496 and approved by roof membrane manufacturer.

          - Electrically Conductive Primer: Water-based, non-flammable, nonmetallic low-VOC primer[, UL listed and FM Global approved].

            - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Grounding Screen: [Welded, stainless steel mesh] [Aluminum screen], for use with vector mapping system[, FM Global approved].

            - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Electrically Conductive Fabric: Non-abrasive felt.

            - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Leak Detection and Moisture-Monitoring System: Permanent, embedded leak detection and moisture-monitoring system.

          - Sensors measuring moisture content[, temperature, and vapor drive], placed [below roof insulation] [over vapor barrier] and connected to a monitoring program, with a notification indicating location of breach.

          - Sensors measuring moisture content[, temperature, and vapor drive], in a conductive fabric placed below roof membrane and connected to a monitoring program, with a notification indicating location of breach.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

      - ROOFING MEMBRANE

        - Hot Fluid-Applied, Rubberized-Asphalt Roofing Membrane: Single component; 100 percent solids; hot fluid-applied, rubberized asphalt.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Insert product physical and performance properties below if required. Manufacturers still report properties according to the withdrawn CAN/CGSB-37.50, "Hot Applied, Rubberized Asphalt for Roofing and Waterproofing." See Evaluations for discussion and a listing of these properties.

          - <Insert requirements>.

      - BASE FLASHING SHEET MATERIALS

Retain one of three paragraphs in this article.

Retain "Elastomeric Flashing Sheet" Paragraph below if elastomeric flashing sheet is required for base sheet flashing. Retain option if an adhesive is bonding the base flashing to parapets and other vertical terminations.

        - Elastomeric Flashing Sheet: 50-mil- (1.3-mm-) thick, minimum, uncured sheet neoprene[ with manufacturer's recommended contact adhesives] as follows:

          - Tensile Strength: 1400 psi (9.6 MPa) minimum; ASTM D412, Die C.

          - Elongation: 300 percent minimum; ASTM D412.

          - Tear Resistance: 125 psi (860 kPa) minimum; ASTM D624, Die C.

          - Brittleness: Does not break at minus 30 deg F (minus 34 deg C); ASTM D2137.

Retain "SBS-Modified Bituminous Flashing Sheet" Paragraph below for granule-surfaced, SBS-modified bituminous flashing sheet. Retain one of three options for color.

        - SBS-Modified Bituminous Flashing Sheet: ASTM D6164/D6164M, Grade G, Type I or Type II, polyester-reinforced, SBS-modified asphalt sheet; granular surfaced; suitable for application method specified, [white] [gray] [tan] <Insert color>.

Retain backer sheet, if required, from "Backer Sheet" Subparagraph below for first ply of two-ply, SBS-modified bituminous flashing.

          - Backer Sheet: ASTM D6164/D6164M, Grade S, Type I or Type II, polyester-reinforced, SBS-modified asphalt sheet; smooth surfaced; suitable for application method specified.

Retain "APP-Modified Bituminous Flashing Sheet" Paragraph below for APP-modified bituminous flashing sheet. Retain one of two options for smooth surfaced or granule surfaced. American Hydrotech uses smooth APP-modified flashing sheets without backer sheet, torch applied. Although smooth APP sheet is considered to have UV resistance, insert protective coating or covering if required.

        - APP-Modified Bituminous Flashing Sheet: ASTM D6222/D6222M, [Grade S, smooth] [Grade G, granular] surfaced, Type I or Type II, polyester-reinforced, APP-modified asphalt sheet; suitable for application method specified.

Retain color from options in "Granule Color" Subparagraph below for granular-surfaced sheet.

          - Granule Color: [White] [Gray] [Tan] <Insert color>.

      - ACCESSORY MATERIALS

        - Accessory materials recommended by roofing manufacturer for intended use and compatible with roofing membrane.

          - Liquid-type accessory materials are to comply with VOC limits of authorities having jurisdiction.

          - <Double click to insert sustainable design text for VOC content of adhesives and sealants.>

          - <Double click to insert sustainable design text for low-emitting adhesives and sealants.>

        - Asphalt Primer: ASTM D41/D41M.

Retain "Elastomeric Sheet" Paragraph below if using elastomeric sheet for treatment of moving joints and cracks as well as joints and cracks exceeding 1/8 inch (3 mm) thick.

        - Elastomeric Sheet: 50-mil- (1.3-mm-) thick, minimum, uncured sheet neoprene[ with manufacturer's recommended contact adhesives] as follows:

          - Tensile Strength: 1400 psi (9.6 MPa) minimum; ASTM D412, Die C.

          - Elongation: 300 percent minimum; ASTM D412.

          - Tear Resistance: 125 psi (860 kPa) minimum; ASTM D624, Die C.

          - Brittleness: Does not break at minus 30 deg F (minus 34 deg C); ASTM D2137.

        - Metal Termination Bars: Manufacturer's standard, predrilled, stainless steel or aluminum termination bars, approximately 1 by 1/8 inch (25 by 3 mm) thick; with stainless steel anchors.

Retain Reinforcing Fabric" Paragraph below if a reinforced roofing membrane is required, or if using reinforcing fabric over joints and cracks not exceeding 1/8 inch (3 mm) thick.

        - Reinforcing Fabric: Manufacturer's recommended, [spun-bonded polyester fabric] [fiberglass mat].

        - Protection Course: Manufacturer's standard, 80-to-90-mil- (2.0-to-2.3-mm-) thick, fiberglass-reinforced rubberized-asphalt or modified bituminous sheet.

      - ROOF INSULATION

Roofing system manufacturers may require use of their own insulations or limit approvals to some insulation manufacturers. Retain second option in first paragraph below if FM Global approval is required.

        - Preformed roof insulation boards manufactured[ or approved] by roofing manufacturer, selected from manufacturer's standard sizes suitable for application, of thicknesses indicated[ and that produce FM Approved roof insulation].

Retain "Extruded-Polystyrene Board Insulation" Paragraph below for extruded-polystyrene board insulation installed above the membrane of a protected membrane roofing system. Usually retain Type VI; limit Type VII to roofs with heavy pedestrian traffic.

        - Extruded-Polystyrene Board Insulation: ASTM C578, [Type VI, 1.8 lb/cu. ft. (29 kg/cu. m)] [Type VII, 2.2 lb/cu. ft. (35 kg/cu. m)], with two or four edges rabbeted.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Retain "Extruded-Polystyrene Drainable Board Insulation" Paragraph below if board insulation with surface drainage ribs is required. Drainage-ribbed insulation is usually limited to heavyweight pavers not elevated on paver pedestals. An air space of at least 3/16 inch (5 mm) is recommended to prevent freeze-thaw spalling of pavers and moisture vapor buildup in insulation.

        - Extruded-Polystyrene Drainable Board Insulation: ASTM C578, [Type VI, 1.8 lb/cu. ft. (29 kg/cu. m)] [Type VII, 2.2 lb/cu. ft. (35 kg/cu. m)], with rabbeted edges and with one side having ribbed drainage channels.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Retain "Mortar-Faced, Extruded-Polystyrene Board Insulation" Paragraph below for mortar-faced, extruded-polystyrene board insulation installed above the membrane of a protected membrane roofing system.

        - Mortar-Faced, Extruded-Polystyrene Board Insulation: ASTM C578, Type VI, 1.8-lb/cu. ft. (29-kg/cu. m) minimum density, with tongue-and-groove edges on long dimension, and latex-modified cement mortar topping, [3/8 inch (9 mm) thick, 4.5 lb/sq. ft. (19.5 kg/sq. m)] [15/16 inch (23 mm) thick, 11 lb/sq. ft. (53.7 kg/sq. m)].

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

      - INSULATION ACCESSORIES

        - General: Roof insulation accessories recommended by insulation manufacturer for intended use and compatibility with membrane roofing.

Protection mats in "Protection Mat" Paragraph below, sometimes called "filter fabrics" or "fabric mats," limit aggregate ballast movement and control insulation flotation in protected membrane roofing systems.

        - Protection Mat: Woven or nonwoven polypropylene, polyolefin, or polyester fabric, water permeable and resistant to UV degradation, type and weight as recommended by roofing system manufacturer for application.

Retain "Metal Securement System" Paragraph below if T. Clear's proprietary metal securement system is required for mortar-faced board insulation. Specify gravel stop or counterflashing in Section 076200 "Sheet Metal Flashing and Trim" or Section 077100 "Roof Specialties," if required.

        - Metal Securement System: Perimeter securement flashing and strapping fabricated from stainless steel, a minimum of 0.031 inch (0.8 mm) thick. Provide fasteners as recommended by mortar-faced insulation manufacturer.

      - BALLAST

        - Aggregate Ballast: Washed, crushed stone or smooth stone that withstands weather exposure without significant deterioration and does not contribute to membrane degradation; of the following size:

Retain one or more of three options in "Size" Subparagraph below to suit Project. Revise descriptions if other sizes are permitted. ANSI/SPRI RP-4 also allows ASTM D448, Sizes 1, 2, 3, or 24 to be used where Size 4 is required, and Size 1 where Size 2 is required. Coordinate size of aggregate with optional paragraphs for ballast weight in Part 3.

          - Size: ASTM D448, [Size 5, ranging in size from 1/2 to 1 inch (13 to 25 mm)] [Size 4, ranging in size from 3/4 to 1-1/2 inches (19 to 38 mm)] [Size 2, ranging in size from 1-1/2 to 2-1/2 inches (38 to 63 mm)].

Retain "Interlocking Roof Pavers" Paragraph below if covering entire roofed area with interlocking, lightweight roof pavers. Verify wind-uplift resistance with interlocking roof-paver manufacturers.

        - Interlocking Roof Pavers: Interlocking, lightweight concrete units; grooved back, with four-way drainage capability; beveled, doweled, or otherwise profiled; and as follows:

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Coordinate size selection in "Size" Subparagraph below with minimum paver coverage required, especially at corners, perimeter, penetrations, and above large wall openings. Paver sizes vary with manufacturers and include 8 by 16, 12 by 12, 12 by 16-1/2, and 12 by 18 inches (200 by 400, 300 by 300, 300 by 420, and 300 by 450 mm).

          - Size: <Insert actual size(s) of pavers>.

Insert weight of roof paver in "Weight" Subparagraph below. SPRI identifies interlocking, lightweight roof pavers as weighing at least 10 lb/sq. ft. (50 kg/sq. m) but not exceeding 18 lb/sq. ft. (90 kg/sq. m). Dow Technote 508 requires a minimum of 11 lb/sq. ft. (55 kg/sq. m) and notes that the wind-resistance warranty is the responsibility of interlocking paver manufacturer. Verify availability with manufacturers.

          - Weight: <Insert weight or weight range>.

Retain one of two options in "Compressive Strength" Subparagraph below.

          - Compressive Strength: [2500 psi (17 MPa)] [5000 psi (34 MPa)] <Insert value>, minimum.

Retain one of three options in "Colors and Textures" Subparagraph below. If retaining first option, indicate colors and textures in a separate schedule.

          - Colors and Textures: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

Retain normal-weight roof pavers in "Roof Pavers" Paragraph below if roof pavers are required to form walkways, cover entire roofed area, or replace aggregate ballast at roof perimeters, corners, and penetrations.

        - Roof Pavers: Heavyweight, hydraulically pressed, concrete units, [square edged] [with top edges beveled 3/16 inch (5 mm)], factory cast for use as roof pavers; absorption not greater than 5 percent, ASTM C140; no breakage and maximum 1 percent mass loss when tested for freeze-thaw resistance, ASTM C67; and as follows:

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Coordinate size selection in "Size" Subparagraph below with minimum paver coverage required, especially at corners, perimeter, penetrations, and above large wall openings. Consider handling of pavers as weight increases. Paver sizes vary among manufacturers and include 12 by 12 and 18 by 18 inches (300 by 300 and 450 by 450 mm).

          - Size: [24 by 24 inches (600 by 600 mm)] <Insert dimensions>. Manufacture pavers to dimensional tolerances of plus or minus 1/16 inch (1.6 mm) in length, height, and thickness.

Insert weight of roof pavers in "Weight" Subparagraph below. SPRI identifies heavyweight roof pavers as weighing 18 lb/sq. ft. (90 kg/sq. m) or more. Dow Technote 508 identifies two roof-paver minimum weights of 18 and 22 lb/sq. ft. (90 and 110 kg/sq. m), respectively; see Dow Technote 508 for details. Roof-paver weights vary; 18, 20, 22, and 24 lb/sq. ft. (90, 100, 110, and 120 kg/sq. m), minimum. Verify availability with manufacturers.

          - Weight: <Insert value>.

Retain one of two options in "Compressive Strength" Subparagraph below.

          - Compressive Strength: [7500 psi (52 MPa)] [6500 psi (45 MPa)] <Insert value>, minimum; ASTM C140.

Retain one of three options in "Colors and Textures" Subparagraph below. If retaining first option, indicate colors and textures in a separate schedule.

          - Colors and Textures: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

          - Paver Supports:

Retain one of two subparagraphs below for paver supports, which are used to elevate pavers and facilitate drainage, if required. Retain first subparagraph if paver supports are integrally cast. Retain second subparagraph if separate pedestal supports, which are used to space, level, and stabilize pavers, are required. Pedestals may be of fixed height or adjustable for leveling pavers over a sloped substrate.

            - Integral Paver Supports: Integral corner pedestals creating a minimum 3/16-inch- (5-mm-) high ventilation air space.

            - Paver Support Assembly: Paver manufacturer's standard SBR rubber, high-density polyethylene, or polyurethane paver support assembly, including [fixed-height] [adjustable or stackable] pedestals, shims, and spacer tabs for joint spacing of [1/8 inch (3 mm)] [3/16 inch (5 mm)] [1/8 to 3/16 inch (3 to 5 mm)].

Retain "Roof-Paver Metal Straps" Paragraph below if strapping roof pavers together with stainless steel straps at roof corners or perimeter.

        - Roof-Paver Metal Straps: Securement strapping fabricated from stainless steel, a minimum of 3 inches (75 mm) wide by 0.031 inch (0.8 mm) thick with stainless steel anchors.

- EXECUTION

      - EXAMINATION

        - Examine substrates, areas, and conditions, with Installer present, for compliance with requirements and other conditions affecting performance of the Work:

          - Verify that roof openings and penetrations are in place, curbs are set and braced, and roof drain bodies are securely clamped in place.

Cants, blocking, curbs, and nailers are required at edges of roof penetrations, area dividers, and terminations.

          - Verify that wood cants, blocking, curbs, and nailers are securely anchored to roof deck at penetrations and terminations.

          - Verify that minimum concrete drying period recommended by roofing system manufacturer has passed.

          - Verify that concrete substrate is visibly dry and free of moisture. Test for capillary moisture by plastic sheet method in accordance with ASTM D4263.

          - Verify that concrete-curing compounds that will impair adhesion of roofing components to roof deck have been removed.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Clean substrate of dust, debris, moisture, and other substances detrimental to roofing installation in accordance with roofing system manufacturer's written instructions.

        - Remove fins, ridges, and other projections and fill honeycomb, aggregate pockets, and other voids.

        - Mask off adjoining surfaces not receiving roofing to prevent spillage from affecting other construction.

        - Prevent materials from entering and clogging roof drains and conductors and from spilling or migrating onto surfaces of other construction. Remove roof-drain plugs when no work is taking place or when rain is forecast.

      - JOINTS, CRACKS, AND TERMINATIONS

        - Prepare and treat substrates to receive roofing, including joints and cracks, roof drains, and penetrations, in accordance with roofing system manufacturer's written instructions.

          - Rout and fill joints and cracks in substrate. Before filling, remove dust and dirt in accordance with ASTM D4258.

Usually retain subparagraphs below. Retain first subparagraph for reinforcing strips over moving or large joints and cracks.

          - Adhere strip of elastomeric sheet to substrate in a layer of hot fluid-applied, rubberized asphalt. Extend elastomeric sheet a minimum of 6 inches (150 mm) on each side of moving joints and cracks or joints and cracks exceeding 1/8 inch (3 mm) thick, and beyond roof drains and penetrations. Apply second layer of hot fluid-applied, rubberized asphalt over elastomeric sheet.

Retain first subparagraph below for reinforcing strips over nonmoving joints and cracks not exceeding 1/8 inch (3 mm) thick.

          - Embed strip of reinforcing fabric into a layer of hot fluid-applied, rubberized asphalt. Extend reinforcing fabric a minimum of 6 inches (150 mm) on each side of nonmoving joints and cracks not exceeding 1/8 inch (3 mm) thick, and beyond roof drains and penetrations.

Retain subparagraph below with fabric-reinforced joints for unreinforced roofing membrane.

            - Apply second layer of hot fluid-applied, rubberized asphalt over reinforcing fabric.

Revise or delete paragraph below if using expansion-joint gaskets or expansion-joint cover assemblies.

        - At expansion joints and discontinuous deck-to-wall or deck-to-deck joints, bridge joints with elastomeric sheet extended a minimum of 6 inches (150 mm) on each side of joints, and adhere to substrates in a layer of hot fluid-applied, rubberized asphalt. Apply second layer of hot fluid-applied, rubberized asphalt over elastomeric sheet.

      - INSTALLATION OF ELD COMPONENTS

Retain first paragraph below if conductive medium will be field installed immediately below roof membrane.

        - Install conductive medium over [cover board] [existing substrate] [and on vertical locations to receive roof membrane] in accordance with manufacturer's written instructions.

Retain paragraph below for embedded ELD and moisture-monitoring systems.

        - Install sensors, [wire loop] [conductive fabric], connections, and accessory items required for complete system in accordance with manufacturer's written instructions.

      - INSTALLATION OF BASE FLASHING

        - Install base flashing at terminations of roofing in accordance with manufacturer's written instructions.

Smooth surfaces of masonry and concrete walls, and parapets usually require priming.

        - Prime substrate with asphalt primer if required by manufacturer.

Retain first paragraph below if base flashing uses elastomeric flashing sheet. Most manufacturers recommend protecting elastomeric flashing sheets with metal counterflashing or a cover layer of rubberized asphalt. Verify with manufacturer and supplement below if required.

        - Bond elastomeric flashing sheet in contact adhesive against wall substrate to within 3 inches (75 mm) of deck. Adhere remaining vertical leg and horizontal leg of flashing sheet in a layer of hot fluid-applied, rubberized asphalt.

Retain first paragraph below if base flashing uses modified bituminous flashing sheet.

        - Bond modified bituminous flashing sheet to substrate as follows:

Retain one of three subparagraphs below. Retain option in first subparagraph below if a two-ply, base flashing assembly is required. Verify attachment method for backer sheet and flashing sheet with roofing manufacturers, and revise descriptions accordingly. Retain third subparagraph if one or other product type is standard with selected roofing manufacturer.

          - Adhere SBS-modified bituminous[ backer sheet and] flashing sheet to substrate in a layer of hot fluid-applied, rubberized asphalt.

          - Torch apply APP-modified bituminous flashing sheet to substrate.

          - Adhere SBS-modified bituminous[ backer sheet and] flashing sheet to substrate in a layer of hot fluid-applied, rubberized asphalt, or torch apply APP-modified bituminous flashing sheet to substrate as standard with manufacturer.

Revise dimensions in first paragraph below if required. Verify minimum and maximum height limits with manufacturers if required.

        - Extend flashing sheet up walls or parapets a minimum of 8 inches (200 mm) above insulation and 6 inches (150 mm) onto roof deck.

        - Install termination bars and mechanically fasten to top of flashing sheet at terminations and perimeter of roofing.

      - INSTALLATION OF ROOFING MEMBRANE

        - Apply primer, at manufacturer's recommended rate, over prepared substrate and allow to dry.

        - Heat and apply rubberized asphalt in accordance with manufacturer's written instructions.

          - Heat rubberized asphalt in an oil- or air-jacketed melter with mechanical agitator specifically designed for heating rubberized asphalt.

Retain first paragraph below if applicable.

        - Start application with manufacturer's authorized representative present.

Retain "Unreinforced Membrane" or "Reinforced Membrane" Paragraph below, or both. If retaining both, indicate location of each system on Drawings.

        - Unreinforced Membrane: Apply hot rubberized asphalt to area to receive roofing. Spread hot rubberized asphalt to form a uniform, unreinforced, seamless membrane, [180-mil (4.5-mm) minimum thickness] [180-mil (4.5-mm) average thickness, but not less than 125 mils (3.2 mm) thick].

        - Reinforced Membrane: Apply hot fluid-applied, rubberized asphalt to area to receive roofing. Spread a 90-mil- (2.3-mm-) thick layer of hot fluid-applied, rubberized asphalt; embed reinforcing fabric, overlapping sheets 2 inches (50 mm); spread another 125-mil- (3.2-mm-) thick layer of hot fluid-applied, rubberized asphalt to form a uniform, reinforced, seamless membrane, 215 mils (5.5 mm) thick.

        - Apply hot fluid-applied, rubberized asphalt over prepared joints and up wall terminations and vertical surfaces to heights indicated or required by manufacturer.

Protection course also prevents insulation from sticking to membrane.

        - Cover membrane with protection course with overlapped joints before membrane is subject to construction traffic.

      - INSTALLATION OF INSULATION

        - Loosely lay board insulation units over roofing membrane, with long joints of insulation in continuous straight lines and with end joints staggered between rows. Abut edges and ends between units.

        - Install one or more layers of insulation to achieve required thickness over roofing membrane. Cut and fit to within 3/4 inch (19 mm) of projections and penetrations.

Retain subparagraph below if required, or revise to suit Project. Revise below if one or more insulation layers are topped with a final layer of mortar-faced board insulation.

          - Where overall insulation thickness is 2 inches (50 mm) or more, install required thickness in two or more layers with joints of each succeeding layer staggered over joints of previous layer a minimum of 6 inches (150 mm) in each direction.

Retain paragraph below for aggregate ballast. Geotextile fabric is usually omitted under roof-paver ballast.

        - Install geotextile fabric over insulation, overlapping edges and ends at least 12 inches (300 mm). Do not lap ends of fabric sheets within 72 inches (1800 mm) of roof perimeter. Extend fabric 2 to 3 inches (50 to 75 mm) above ballast at perimeter and penetrations. Apply additional layer of fabric around penetrations to prevent aggregate from getting between penetration and insulation. Do not cover drains or restrict water flow to drains.

      - INSTALLATION OF BALLAST

Retain this article if aggregate ballast or a combination of roof pavers and aggregate ballast are required, and delete "Roof-Paver Installation" Article. Loads and roof perimeter and corner dimensions below are based on Dow Technote 508. Revise if using ANSI/SPRI RP-4 or another design source, because requirements may vary.

Retain option in first paragraph below if roof paver ballast is required.

        - Install aggregate ballast[ and roof paver ballast] uniformly over protection layer.

        - Spread aggregate to not damage roof membrane or base flashings.

        - Apply ballast as insulation is installed, leaving roof insulated and ballasted at end of workday.

        - Install aggregate ballast at rate required by insulation manufacturer, but not less than the following:

          - Zone 1 (Roof Area Field): [10 lb/sq. ft. (50 kg/sq. m) of Size 5 aggregate] [12 lb/sq. ft. (60 kg/sq. m) of Size 5 aggregate] [13 lb/sq. ft. (65 kg/sq. m) of Size 2 aggregate] <Insert value>.

Retain first option in first three subparagraphs below for insulation thicknesses of less than 3 inches (76 mm). Retain second option for insulation thicknesses of 3 inches (76 mm) and more.

          - Zone 2 (Roof Area Perimeter): [15 lb/sq. ft. (75 kg/sq. m)] [20 lb/sq. ft. (100 kg/sq. m)] [One row of roof pavers] [Two rows of roof pavers] [Three rows of roof pavers] [Four rows of roof pavers] <Insert value> a distance of <Insert dimension> inside roof edge, but not less than 96 inches (2438 mm).

            - Aggregate: [Size 5] [Size 4] [Size 2].

            - Mechanically fasten securement strapping to center of first perimeter row of roof pavers closest to edge of roof, using straps running parallel to parapet wall or roof edge.

          - Zone 3 (Roof Area Corners): [15 lb/sq. ft. (75 kg/sq. m)] [20 lb/sq. ft. (100 kg/sq. m)] [One row of roof pavers] [Two rows of roof pavers] [Three rows of roof pavers] [Four rows of roof pavers] <Insert value> a distance of <Insert dimension> in each direction form a building corner, but not less than 96 inches (2438 mm).

            - Aggregate: [Size 5] [Size 4] [Size 2].

            - Mechanically fasten securement strapping to center of first perimeter row of roof pavers closest to edge of roof, using straps running parallel to parapet wall or roof edge.

          - Within 48 Inches (1219 mm) of Roof Penetrations: [15 lb/sq. ft. (75 kg/sq. m)] [20 lb/sq. ft. (100 kg/sq. m)] [Two rows of roof pavers around perimeter of penetration] <Insert value>. A "penetration" is defined as any object projecting above the roof insulation that measures 48 inches (1219 mm) or more on any side.

            - Aggregate: [Size 5] [Size 4] [Size 2].

Retain "Walkway Pavers" Subparagraph below if required. Roofing manufacturers recommend use of walkway pavers in place of ballast in areas subject to service traffic.

          - Walkway Pavers: Install walkways formed from [one row] [two rows] of roof pavers, loosely laid and butted.

      - INSTALLATION OF ROOF PAVERS

Retain this article if covering roofed area with roof pavers instead of aggregate ballast.

        - Interlocking Roof Pavers: Install interlocking roof pavers over roofed area in accordance with manufacturer's written instructions.

Retain one of first three paragraphs below for roof pavers installed over insulation.

        - Install roof pavers over roofed area in accordance with insulation manufacturer's written instructions.

        - Install roof pavers over roofed area in accordance with insulation manufacturer's written instructions. Mechanically fasten roof-paver metal straps to center of first perimeter and first perimeter corner row of roof pavers.

        - Install roof pavers over roofed area in accordance with insulation manufacturer's written instructions. Mechanically fasten roof-paver metal straps to center of first two perimeters and first two perimeter corner rows of roof pavers.

Retain paragraph below if separate pedestals are required.

        - Install roof pavers on pedestals set in accordance with pedestal manufacturer's written instructions.

      - INSTALLATION OF MORTAR-FACED BOARD INSULATION

Retain this article if using proprietary mortar-faced board insulation over entire roofed area.

        - Install mortar-faced board insulation loosely laid, in accordance with manufacturer's written instructions, with tongue-and-groove joints nested. Stagger end joints of adjoining rows and abut insulation.

Retain one or both subparagraphs below. Retain first if securing mortar-faced board insulation with metal strapping at penetrations and perimeters. Revise below if a more elaborate description of perimeter edge conditions is required. Requirements differ depending on whether a parapet wall or a gravel stop is detailed on Drawings. Coordinate inclusion of gravel stop or counterflashing for parapet with Section 076200 "Sheet Metal Flashing and Trim" or Section 077100 "Roof Specialties," as applicable.

          - Mechanically fasten metal securement strapping at penetrations and at perimeter edges of mortar-faced board insulation.

Retain subparagraph below if securing proprietary mortar-faced board insulation with roof pavers in addition to metal perimeter securement.

          - Over mortar-faced board insulation, install roof pavers on roof perimeter and corners in accordance with manufacturer's written instructions.

Retain paragraph below if securing proprietary mortar-faced board insulation with roof pavers alone, which is manufacturer's preferred method of perimeter securement.

        - Install [one row] [two rows] of 24-inch- (600-mm-) wide roof pavers to roof perimeter, corners, and penetrations in accordance with mortar-faced board insulation manufacturer's written instructions.

      - FIELD QUALITY CONTROL

Retain this article if field inspecting and testing are required. Revise to suit local practices and requirements of authorities having jurisdiction if applicable.

Retain first paragraph below if a manufacturer's site representative is required throughout installation. Manufacturer may also require this as a warranty condition.

        - Engage a full-time site representative qualified by roofing manufacturer to inspect substrate conditions; surface preparation; and application of membrane, base flashings, protection, insulation, and ballast; furnish daily reports.

Retain "Testing Agency" Paragraph below to identify who performs tests and inspections. If retaining second option in "Testing Agency" Paragraph, retain "Field quality-control reports" Paragraph in "Informational Submittals" Article.

        - Testing Agency: [Owner will engage] [Engage] a qualified testing agency to inspect substrate conditions, surface preparation, membrane application, flashings, protection, and drainage components, and to furnish reports to Architect.

        - Perform the following tests:

Retain one or more of "Flood Testing," "Low-Voltage ELD Testing," and "High-Voltage Membrane Testing" subparagraphs below.

Retain "Flood Testing" Subparagraph below if required. Localize testing to flashings or penetrations if preferred. Limit water depth to not more than load capacity of deck as determined by structural engineer. Review procedures in ASTM D5957 for applicability. Note that NRCA does not recommend flood testing.

          - Flood Testing: Flood test each roofing area for leaks, in accordance with recommendations in ASTM D5957, after completing roofing and flashing but before overlying construction is placed. Install temporary containment assemblies, plug or dam drains, and flood with potable water.

            - Perform tests before overlying construction is placed.

            - Flood to an average depth of 2-1/2 inches (65 mm) with a minimum depth of 1 inch (25 mm) and not exceeding a depth of 4 inches (100 mm). Maintain 2 inches (50 mm) of clearance from top of base flashing.

ASTM D5957 sets 24 hours as minimum and 72 hours as maximum duration for flood testing.

            - Flood each area for [24] [48] [72] hours.

            - After flood testing, repair leaks, repeat flood tests, and make further repairs until roofing and flashing installation are watertight.

              - Cost of retesting is Contractor's responsibility.

            - Testing agency will prepare survey report indicating locations of initial leaks, if any, and final survey report.

Retain "Low-Voltage ELD Testing" Subparagraph below if required. First option is for platform-type system; second option is also referred to by the trademark brand name EFVM; third option is a handheld device, often used in conjunction with first option to test vertical areas. All options identify specific leak locations and require a conductive medium directly below the exposed roof membrane.

          - Low-Voltage ELD Testing: Testing agency will survey entire roof area and flashings to locate discontinuities in the roof membrane using low-voltage [horizontal membrane scanning platform] [membrane electric field vector mapping] [or] [vertical membrane scanning] in accordance with ASTM D8231.

            - Perform tests before overlying construction is placed.

            - After testing, repair areas of discontinuities, repeat tests, and make further repairs until roofing and flashing installations are contiguous.

              - Cost of retesting is Contractor's responsibility.

            - Testing agency will prepare survey report indicating locations of initial discontinuities, if any.

Retain "High-Voltage Membrane Testing" Subparagraph below if required. This method requires a dry roof membrane, can be used on vertical surfaces, and identifies specific leak locations.

          - High-Voltage Membrane Testing: Testing agency will survey [entire roof area,] [flashings,] [and] [parapet walls] to locate discontinuity in the roof membrane using an electrically charged metal "broom head."

            - Perform tests before overlying construction is placed.

            - After testing, repair areas of discontinuities, repeat tests, and make further repairs until roofing and flashing installations are contiguous.

              - Cost of retesting is Contractor's responsibility.

            - Testing agency will prepare survey report indicating locations of initial discontinuities, if any.

      - PROTECTING AND CLEANING

        - Protect roofing system from damage and wear during remainder of construction period. When remaining construction does not affect or endanger roofing, inspect roofing for deterioration and damage, describing its nature and extent in a written report, with copies to Architect and Owner.

        - Correct deficiencies in or remove roofing system that does not comply with requirements, repair substrates, and repair or reinstall roofing system to a condition free of damage and deterioration at time of Substantial Completion and in accordance with warranty requirements.

        - Clean spillage and soiling from adjacent construction using cleaning agents and procedures recommended by manufacturer of affected construction.

      - ROOFING INSTALLER'S WARRANTY

Retain this warranty or include another roofing Installer's warranty form if required. Coordinate with "Warranty" Article.

        - WHEREAS _______________________________ of ___________________________, herein called the "Roofing Installer," has performed roofing and associated work ("work") on the following project:

          - Owner: <Insert name of Owner>.

          - Owner Address: <Insert address>.

          - Building Name/Type: <Insert information>.

          - Building Address: <Insert address>.

          - Area of Work: <Insert information>.

          - Acceptance Date: _________________.

          - Warranty Period: <Insert time>.

          - Expiration Date: __________________.

        - AND WHEREAS Roofing Installer has contracted (either directly with Owner or indirectly as a subcontractor) to warrant said work against leaks and faulty or defective materials and workmanship for designated Warranty Period,

        - NOW THEREFORE Roofing Installer hereby warrants, subject to terms and conditions herein set forth, that during Warranty Period he will, at his own cost and expense, make or cause to be made such repairs to or replacements of said work as are necessary to correct faulty and defective work and as are necessary to maintain said work in a watertight condition.

        - This Warranty is made subject to the following terms and conditions:

          - Specifically excluded from this Warranty are damages to work and other parts of the building, and to building contents, caused by:

            - lightning;

Insert required wind speed in first subparagraph below.

            - peak gust wind speed exceeding <Insert mph (m/sec)>;

            - fire;

            - failure of roofing system substrate, including cracking, settlement, excessive deflection, deterioration, and decomposition;

            - faulty construction of parapet walls, copings, chimneys, skylights, vents, equipment supports, and other edge conditions and penetrations of the work;

            - vapor condensation on bottom of roofing; and

            - activity on roofing by others, including construction contractors, maintenance personnel, other persons, and animals, whether authorized or unauthorized by Owner.

          - When work has been damaged by any of foregoing causes, Warranty shall be null and void until such damage has been repaired by Roofing Installer and until cost and expense thereof have been paid by Owner or by another responsible party so designated.

          - Roofing Installer is responsible for damage to work covered by this Warranty but is not liable for consequential damages to building or building contents resulting from leaks or faults or defects of work.

          - During Warranty Period, if Owner allows alteration of work by anyone other than Roofing Installer, including cutting, patching, and maintenance in connection with penetrations, attachment of other work, and positioning of anything on roof, this Warranty shall become null and void on date of said alterations, but only to the extent said alterations affect work covered by this Warranty. If Owner engages Roofing Installer to perform said alterations, Warranty shall not become null and void unless Roofing Installer, before starting said work, shall have notified Owner in writing, showing reasonable cause for claim, that said alterations would likely damage or deteriorate work, thereby reasonably justifying a limitation or termination of this Warranty.

          - During Warranty Period, if original use of roof is changed and it becomes used for, but was not originally specified for, a promenade, work deck, spray-cooled surface, flooded basin, or other use or service more severe than originally specified, this Warranty shall become null and void on date of said change, but only to the extent said change affects work covered by this Warranty.

          - Owner shall promptly notify Roofing Installer of observed, known, or suspected leaks, defects, or deterioration and shall afford reasonable opportunity for Roofing Installer to inspect work and to examine evidence of such leaks, defects, or deterioration.

          - This Warranty is recognized to be the only warranty of Roofing Installer on said work and shall not operate to restrict or cut off Owner from other remedies and resources lawfully available to Owner in cases of roofing failure. Specifically, this Warranty shall not operate to relieve Roofing Installer of responsibility for performance of original work according to requirements of the Contract Documents, regardless of whether Contract was a contract directly with Owner or a subcontract with Owner's General Contractor.

        - IN WITNESS THEREOF, this instrument has been duly executed this ___________ day of ___________________, ________________.

          - Authorized Signature: _______________________________________.

          - Name: ______________________________________.

          - Title: _______________________________________.

END OF SECTION 075556