Copyright 2022 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 077253 - SNOW GUARDS

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Access Manufacturer-Provided, AIA MasterSpec-Based Sections:

<Double click here for this Section based on specific manufacturer’s products set as Basis-of-Design at ProductMasterSpec.com.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Pad-type, flat-mounted metal snow guards.

          - Pad-type, flat-mounted plastic snow guards.

          - Pad-type, seam-mounted cast-metal snow guards.

          - Pad-type, seam-mounted plastic snow guards.

          - Rail-type, flat-mounted snow guards.

          - Rail-type, seam-mounted snow guards.

      - ACTION SUBMITTALS

        - Product Data: Include construction details, material descriptions, dimensions of individual components and profiles, and finishes.

          - Pad-type, flat-mounted metal snow guards.

          - Pad-type, flat-mounted plastic snow guards.

          - Pad-type, seam-mounted cast-metal snow guards.

          - Pad-type, seam-mounted plastic snow guards.

          - Rail-type, flat-mounted snow guards.

          - Rail-type, seam-mounted snow guards.

        - Shop Drawings: Include roof plans showing layouts and attachment details of snow guards.

Retain subparagraph below for rail-type snow guards.

          - Include details of rail-type snow guards.

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable.

        - Samples:

          - Pad-Type Snow Guards: Full-size unit with installation hardware.

            - For units with factory-applied finishes, submit [manufacturer's standard color selections] [specified color].

          - Rail-Type Snow Guards: Bracket, 12-inch- (300-mm-) long rail, and installation hardware.

            - For units with factory-applied finishes, submit [manufacturer's standard color selections] [specified color].

Retain "Delegated Design Submittals" Paragraph below if design services have been delegated to Contractor.

        - Delegated Design Submittals: For snow guards, include analysis reports signed and sealed by the qualified professional engineer responsible for their preparation.

          - Include calculation of number and location of snow guards.

      - INFORMATIONAL SUBMITTALS

Retain "Qualification Data" Paragraph below if design services have been delegated to Contractor. Coordinate with qualification requirements in Section 014000 "Quality Requirements."

        - Qualification Data: For professional engineer's experience with providing delegated design engineering services of the kind indicated, including documentation that the engineer is licensed in the [jurisdiction] [state] in which the Project is located.

Retain "Product Test Reports" Paragraph below if retaining "Structural Performance" Paragraph in "Performance Requirements" Article.

        - Product Test Reports: For each type of snow guard, for tests performed by a qualified testing agency, indicating load at failure of attachment to roof system identical to roof system used on this Project.

      - FIELD CONDITIONS

        - Weather Limitations: Proceed with installation only when existing and forecasted weather conditions permit adhesive-mounted snow guards to be installed, and adhesive cured, according to adhesive manufacturer's written instructions.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - PERFORMANCE REQUIREMENTS

Retain "Delegated Design" Paragraph below if Contractor is required to assume responsibility for design.

        - Delegated Design: Engage a qualified professional engineer, as defined in Section 014000 "Quality Requirements," to design snow guards, including attachment to roofing material and roof deck, as applicable for attachment method, based on the following:

          - Roof snow load.

          - Snow drifting

          - Roof slope.

          - Roof type.

          - Roof dimensions.

          - Roofing substrate type and thickness.

          - Snow guard type.

          - Snow guard fastening method and strength.

          - Snow guard spacing.

          - Coefficient of Friction Between Snow and Roof Surface: 0.

          - Factor of Safety: [2] [3] <Insert factor of safety>.

        - Performance Requirements: Provide snow guards that withstand exposure to weather and resist thermally induced movement without failure, rattling, or fastener disengagement due to defective manufacture, fabrication, installation, or other defects in construction.

Differential values in "Temperature Change" Subparagraph below (for aluminum in particular) are suitable for most of the United States.

          - Temperature Change: [120 deg F (67 deg C), ambient; 180 deg F (100 deg C), material surfaces] <Insert temperature change>.

Retain "Structural Performance" Paragraph below if detailed design is assigned to manufacturer.

        - Structural Performance: Snow guards to withstand the effects of gravity loads and the following loads and stresses within limits and under conditions indicated.

          - Snow Loads: [As indicated on Drawings] <Insert loading requirements>.

      - PAD-TYPE SNOW GUARDS

Flat-mounted metal systems may be recommended by manufacturers for slate, clay, or concrete tile; wood shake; asphalt shingle; and metal roofing. Consult manufacturer's literature for specific applications.

        - Pad-Type, Flat-Mounted Metal Snow Guards:

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Material:

Retain one or more of eight subparagraphs below. Verify material and finish availability with manufacturers.

            - Aluminum Sheet: ASTM B209 (ASTM B209M), not less than [0.032 inch (0.81 mm)] [0.040 inch (1.02 mm)] [0.050 inch (1.27 mm)] [0.063 inch (1.60 mm)] thick.

              - Finish: [Mill] [Black epoxy coating] [Powder coat finish complying with AAMA 2603, with a minimum dry film thickness of 1.5 mils (0.04 mm)] [High-performance organic two-coat fluoropolymer finish complying with AAMA 2605 and containing not less than 70 percent PVDF resin by weight in color coat] <Insert finish>.

                - Color: [As selected by Architect from manufacturer's full range] [Match sheet metal roofing] <Insert color>.

            - Cast Aluminum: ASTM B26/B26M.

            - Cast Bronze: ASTM B584.

            - Copper Sheet: ASTM B370, not less than 16 oz./sq. ft. (0.55 mm thick).

            - Metallic-Coated Steel Sheet: ASTM A653/A653M, with G90 (Z275) coating, not less than [0.022 inch (0.56 mm)] <Insert dimension> thick.

              - Finish: [Powder coat finish complying with AAMA 2603, with a minimum dry film thickness of 1.5 mils (0.04 mm)] [High-performance organic two-coat fluoropolymer finish complying with AAMA 2605 and containing not less than 70 percent PVDF resin by weight in color coat] <Insert finish>.

                - Color: [As selected by Architect from manufacturer's full range] [Match sheet metal roofing] <Insert color>.

            - Aluminum-Zinc Alloy-Coated Steel Sheet: ASTM A792/A792M, Class AZ50 (Class AZM150), Grade 40 (Grade 275), not less than [0.022 inch (0.56 mm)] <Insert dimension> thick.

              - Finish: [High-performance organic two-coat fluoropolymer finish complying with AAMA 2605 and containing not less than 70 percent PVDF resin by weight in color coat] <Insert finish>.

                - Color: [As selected by Architect from manufacturer's full range] [Match sheet metal roofing] <Insert color>.

"Steel Sheet" Subparagraph below is the current version of "Cor-Ten" sheet weathering steel.

            - Steel Sheet: ASTM A606/A606M, not less than [0.022 inch (0.56 mm)] <Insert dimension> thick.

            - Stainless Steel Sheet: ASTM A240/A240M, [Type 304] [Type 316], not less than [0.0156 inch (0.396 mm)] <Insert dimension> thick.

              - Finish: ASTM A480/A480M, [No. 2D] [No. 2B] [No. 3] [No. 4].

          - Attachment: Manufacturer's tested system, capable of resisting design loads.

        - Pad-Type, Flat-Mounted Plastic Snow Guards:

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Polycarbonate: ASTM D6098.

            - Color: [As selected by Architect from manufacturer's full range] <Insert color>.

          - Attachment: Manufacturer's tested system, capable of resisting design loads.

        - Pad-Type, Seam-Mounted Cast-Metal Snow Guards:

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Material:

Retain one or more of "Cast Aluminum," "Cast Bronze," and "Cast Brass" subparagraphs below. Verify material and finish availability with manufacturers.

            - Cast Aluminum: ASTM B26/B26M; [mill] [factory black epoxy] finish.

            - Cast Bronze: ASTM B584; polished finish.

            - Cast Brass: ASTM B584; polished finish.

          - Attachment: Manufacturer's tested system, capable of resisting design loads.

        - Pad-Type, Seam-Mounted Plastic Snow Guards:

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Material: Clear UV-stabilized polycarbonate.

          - Attachment: Manufacturer's tested system, capable of resisting design loads.

      - RAIL-TYPE SNOW GUARDS

        - Rail-Type, Flat-Mounted Snow Guards:

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Description: Units fabricated from metal baseplate anchored to [adjustable] [fixed] bracket and equipped with [one] [two] [three] [four] bar(s), rail(s), or pipe(s).

Retain applicable options in "Brackets and Baseplate" and "Bars" subparagraphs below. Verify material and finish availability with manufacturers.

          - Brackets and Baseplate: [ASTM B209 (ASTM B209M) aluminum; mill finished] [ASTM B209 (ASTM B209M) aluminum; clear anodized] [ASTM B584 bronze or brass] [ASTM A240/A240M, Type 304 stainless steel; mill finish] [Galvanized steel, G90 coating] [Galvanized steel, G60 (Z180) coating] <Insert material and finish>.

          - Bars: [ASTM B221 (ASTM B221M) aluminum; mill finish] [ASTM B221 (ASTM B221M) aluminum; clear anodized] [ASTM B584 bronze or brass] [ASTM A240/A240M, Type 304 stainless steel; mill finish] <Insert material and finish>.

            - Profile: [Round] [Square] [with integral track to accept color-matching inserts of material and finish used for metal roof].

          - Seam Clamps: ASTM B221 (ASTM B221M) aluminum extrusion or ASTM B85/B85M aluminum casting with stainless steel set screws incorporating round nonpenetrating point; designed for use with applicable roofing system to which clamp is attached.

        - Rail-Type, Seam-Mounted Snow Guards:

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Description: Snow guard rails fabricated from metal pipes, bars, or extrusions, anchored to brackets and equipped with [one rail] [two rails] [three rails] [one rail with integral track to accept color-matching inserts of material and finish used for metal roof] [two rails with integral track to accept color-matching inserts of material and finish used for metal roof] [three rails with integral track to accept color-matching inserts of material and finish used for metal roof].

Retain applicable options in "Brackets and Baseplate" and "Bars" subparagraphs below. Verify material and finish availability with manufacturers.

          - Brackets and Baseplate: [ASTM B209 (ASTM B209M) aluminum; mill finished] [ASTM B209 (ASTM B209M) aluminum; clear anodized] [ASTM A240/A240M, Type 304 stainless steel; mill] [ASTM A240/A240M, Type 304 stainless steel; 180-grit polished finish, uniform, directionally textured finish] [ASTM A240/A240M, Type 304 stainless steel; 320-grit polished finish, oil-ground, uniform, fine, directionally textured finish] [ASTM B584 brass; polished] <Insert material and finish>.

          - Bars: [ASTM B221 (ASTM B221M) aluminum; mill finish] [ASTM B221 (ASTM B221M) aluminum, clear anodized] [ASTM A240/A240M, Type 304 stainless steel; mill finish] [ASTM A240/A240M, Type 304 stainless steel; 180-grit polished finish, uniform, directionally textured finish] [ASTM A240/A240M, Type 304 stainless steel; 320-grit polished finish, oil-ground, uniform, fine, directionally textured finish] [ASTM B584 brass; polished] [Galvanized steel, G90 (Z275) coating] [Galvanized steel, G60 (Z180) coating] <Insert material and finish>.

            - Profile: [Round] [Square] [with integral track to accept color-matching inserts of material and finish used for metal roof].

          - Seam Clamps: ASTM B221 (ASTM B221M) aluminum extrusion or ASTM B85/B85M aluminum casting with stainless steel set screws incorporating round nonpenetrating point; designed for use with applicable roofing system to which clamp is attached.

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Installer present, for compliance with requirements for installation tolerances, snow guard attachment, and other conditions affecting performance of the Work.

          - Verify compatibility with and suitability of substrates, including compatibility with existing finishes or primers.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

Retain this article for adhesively attached snow guards.

        - Clean and prepare substrates for bonding snow guards.

        - Prime substrates according to snow guard manufacturer's written instructions.

      - INSTALLATION

        - Install snow guards according to manufacturer's written instructions.

Retain one of two subparagraphs below as applicable to Project.

          - Space rows as indicated on [Drawings] [Shop Drawings].

          - Space rows as recommended by manufacturer.

Retain paragraph(s) below for roofing and snow guard types used for Project.

        - Attachment for Asphalt Shingle Roofing:

          - Pad-Type, Flat-Mounted Snow Guards: [Mechanically anchored through each factory-prepared hole with fasteners concealed by the shingles] [Retrofit mechanical anchor and counterflashing sleeve system] <Insert attachment>.

          - Rail-Type, Flat-Mounted, Snow Guards: [Mounting plates bolted or screwed to the roof framing or roof deck] <Insert requirement>.

        - Attachment for Wood Shingle and Shake Roofing:

          - Pad-Type, Flat-Mounted Snow Guards: [Mechanically anchored through each factory-prepared hole with fasteners concealed by the shingles] [Retrofit mechanical anchor and counterflashing sleeve system] [Hook and mechanically anchored through each factory-prepared hole, concealed by shingles and shakes] <Insert attachment>.

          - Rail-Type, Flat-Mounted Snow Guards: [Mounting plates bolted or screwed to the roof framing or roof deck] <Insert requirement>.

        - Attachment for Slate Shingle Roofing:

          - Pad-Type, Flat-Mounted Snow Guards: [Mechanically anchored through each factory-prepared hole with fasteners concealed by the shingles] [Retrofit strap-and-hook system] [Retrofit mechanical anchor and counterflashing sleeve system] [Hook and mechanically anchored through each factory-prepared hole, concealed by shingles] <Insert attachment>.

          - Rail-Type, Flat-Mounted Snow Guards: [Mounting plates bolted or screwed to the roof framing or roof deck] <Insert requirement>.

        - Attachment for Metal Shingle Roofing:

          - Pad-Type, Flat-Mounted Snow Guards: [Mechanically anchored through each factory-prepared hole with fasteners concealed by the shingles] [Mechanical anchor and counterflashing sleeve system] <Insert attachment>.

          - Rail Type, Flat-Mounted Snow Guards: [Mounting plates bolted or screwed to the roof framing or roof deck] <Insert requirement>.

        - Attachment for Tile Roofing:

          - Pad-Type, Flat-Mounted Snow Guards: [Hooked to tile and roof batten with head of snow guard positioned over headlap of tile] [Hook and mechanically anchored through each factory-prepared hole, concealed by roof tiles] <Insert attachment>.

          - Rail-Type, Flat-Mounted Snow Guards: [Mounting plates bolted or screwed to the roof framing or roof deck] <Insert requirement>.

        - Attachment for Standing-Seam Metal Roofing:

          - Do not use fasteners that will penetrate metal roofing or fastening methods that void metal roofing finish warranty.

          - Pad-Type, Flat-Mounted Snow Guards:

Second option in first subparagraph below may void finish warranty for metal roofing. Verify with metal roofing manufacturer.

            - [Mechanically attach] [Adhere] to metal roofing in accordance with manufacturer's written instructions.

Retain first subparagraph below for copper roof material.

            - Solder to copper roofing in accordance with manufacturer's written instructions.

          - Pad-Type, Seam-Mounted Snow Guards:

            - Install snow guards in straight rows.

            - Secure in place using stainless steel set screws, incorporating round nonpenetrating point.

            - Torque set screw in accordance with manufacturer's written instructions.

          - Rail-Type, Seam-Mounted Snow Guards:

            - Install brackets to vertical ribs in straight rows.

            - Secure with stainless steel set screws, incorporating round nonpenetrating point, on same side of standing seam.

            - Torque set screw in accordance with manufacturer's written instructions.

            - Install cross members to brackets.

        - Attachment for Exposed Fastened Metal Roofing:

          - Do not use fasteners that will void metal roofing finish warranty.

          - Pad-Type, Flat-Mounted Snow Guards:

Retain one of first three subparagraphs below. First subparagraph may void finish warranty for metal roofing. Verify with metal roofing manufacturer.

            - Adhere to metal roofing in accordance with manufacturer's written instructions.

            - Mechanically fasten to metal roofing, using fasteners identical to those used to secure metal roofing to substrate.

Retain first subparagraph below for copper roof material.

            - Solder to copper roofing in accordance with manufacturer's written instructions.

          - Rail-Type, Flat-Mounted Snow Guards:

            - Install brackets in straight rows.

            - Mechanically fasten to metal roofing, using sealant and mechanical fasteners identical to those used to secure metal roofing to substrate.

            - Install cross members to brackets.

        - Attachment for <Insert roofing type> Roofing:

          - <Insert requirements>.

END OF SECTION 077253