Copyright 2020 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 081816.19 - SLIDING WOOD-FRAMED GLASS DOORS

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Aluminum-clad sliding wood-framed glass doors.

          - Vinyl-clad sliding wood-framed glass doors.

          - Unclad sliding wood-framed glass doors.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 085200 "Wood Windows" for related wood-framed transom and sidelite windows and mullions.

          - [Section 087100 "Door Hardware"] [Section 087111 "Door Hardware (Descriptive Specification)"] for hardware not specified in Section 081816.19.

          - Section 099300 "Staining and Transparent Finishing" for on-site finishing of unfinished sliding wood-framed glass doors.

          - [Section 099113 "Exterior Painting"] [and] [Section 099123 "Interior Painting"] for on-site finishing of [unfinished] [and] [factory-primed] sliding wood-framed glass doors.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

          - Include construction details, material descriptions, fabrication methods, dimensions of individual components and profiles, hardware, finishes, and operating instructions.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for certified wood.>

          - <Double click to insert sustainable design text for certified wood.>

        - Shop Drawings: For sliding wood-framed glass doors.

          - Include plans, elevations, sections, and details.

          - Detail attachments to other work, and between units, if any.

          - Include hardware and required clearances.

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples.

        - Samples: For each exposed product and for each color specified, 12-inch-long (300-mm-long) section with weather stripping, glazing bead, and factory-applied color finish.

        - Samples for Initial Selection: For units with factory-applied color finishes.

          - Include Samples of hardware and accessories involving color selection.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled. Retain "Samples for Verification" Paragraph below with or without above.

        - Samples for Verification: For sliding wood-framed glass doors and components required, prepared on Samples of size indicated below:

Retain "Main Framing Member" Subparagraph below with vinyl- or aluminum-clad doors. Delete if doors are not clad and are to be finished on-site. Retain and edit if Sample is required for verification of framing member profile for doors finished on-site.

          - Main Framing Member: 12-inch-long (300-mm-long) section with weather stripping, glazing bead, and factory-applied color finish.

          - Hardware: Full-size units with factory-applied finish.

          - <Insert component>: <Insert description>.

        - Product Schedule: For sliding wood-framed glass doors.[ Use same designations indicated on Drawings.]

      - INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article. Retain "testing agency" option if Contractor is providing testing in "Field Quality Control" Article.

        - Qualification Data: For [Installer] [and] [testing agency].

Retain option in "Product Test Reports" Paragraph below if manufacturers verify and their product literature indicates that sliding doors were tested according to AAMA/WDMA/CSA procedures.

        - Product Test Reports: For each sliding wood-framed glass door, for tests performed by [manufacturer and witnessed by a qualified testing agency] [a qualified testing agency], and for each class and performance grade indicated, tested at AAMA gateway size.

Retain "Field quality-control reports" Paragraph below if Contractor is responsible for field quality-control testing and inspecting in "Field Quality Control" Article.

        - Field quality-control reports.

        - Sample Warranty: For manufacturer's special warranty.

      - CLOSEOUT SUBMITTALS

Delete option in "Maintenance Data" Paragraph below if sliding wood-framed doors are unfinished or prime-coated for site finishing.

        - Maintenance Data: For [finishes, ]weather stripping, operable panels, and operating hardware to include in maintenance manuals.

      - QUALITY ASSURANCE

        - <Double click to insert sustainable design text for manufacturer qualifications.>

        - <Double click to insert sustainable design text for vendor qualifications.>

        - Installer Qualifications: An installer acceptable to sliding wood-framed glass door manufacturer for installation of units required for this Project.

        - Mockups: Build mockups to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for materials and execution.

          - Build mockup for sliding wood-framed glass doors, as shown on Drawings.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

      - WARRANTY

When warranties are required, verify with Owner's counsel that warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

        - Manufacturer's Special Warranty: Manufacturer agrees to repair or replace sliding wood-framed glass doors that fail in materials or workmanship within specified warranty period.

          - Failures include, but are not limited to, the following:

            - Failure to meet performance requirements.

            - Structural failures including excessive deflection.

Most manufacturers exclude condensation from their warranties. Add to first subparagraph below if available.

            - Excessive water leakage or air infiltration.

            - Faulty operation of movable panels and hardware.

            - Deterioration of wood, metals, finishes, vinyl, and other materials beyond normal weathering.

            - Failure of insulating glass[ and laminated glass].

            - <Insert failure modes>.

Verify available warranties and warranty periods for units and components; retain or insert numbers in remaining subparagraphs below.

          - Warranty Period:

            - Sliding Door: [Two] [Three] [Five] <Insert number> years from date of Substantial Completion.

Warranty period for glazing units varies by type. Insulating-glass units typically have longer warranties than laminated glass. Some manufacturers may insist that warranties begin on date of manufacture or sale.

            - Insulating Glass: [10] [20] <Insert number> years from date of Substantial Completion.

            - Laminated Glass: [Five] <Insert number> years from date of Substantial Completion.

Warranty period for metal finish depends on type of finish. Baked-on enamel finishes often have 10-year warranties; high-performance fluoropolymer finishes often have 20-year warranties.

            - Metal Finish: [Five] [10] [20] <Insert number> years from date of Substantial Completion.

Insert requirements for warranties on finishes for wood or vinyl cladding offered by some manufacturers.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - MANUFACTURERS

Revise "Source Limitations" Paragraph to require sliding wood-framed glass doors to be provided by same manufacturer as wood windows specified in Section 085200 "Wood Windows."

        - Source Limitations: Obtain sliding wood-framed glass doors from single source from single manufacturer.

      - PERFORMANCE REQUIREMENTS

See the Evaluations for discussion of establishing performance requirements using AAMA/WDMA/CSA 101/I.S.2/A440.

        - Product Standard: Comply with AAMA/WDMA/CSA 101/I.S.2/A440 for minimum standards of performance, materials, components, accessories, and fabrication unless more stringent requirements are indicated.

Retain "Product Certification" Subparagraph below if AAMA certification and labeling is needed. Not all manufacturers that test products according to AAMA/WDMA/CSA 101/I.S.2/A440 requirements participate in AAMA's third-party certification program for listing and labeling sliding wood-framed glass doors.

          - Product Certification: AAMA certified with label attached to each door.

Coordinate performance class and grade with available options and features. Some options, such as thresholds, affect door performance, or may not be available for doors meeting selected performance class and grade.

        - Performance Class and Grade: AAMA/WDMA/CSA 101/I.S.2/A440 as follows:

          - Minimum Performance Class: [Class R] [Class LC] [Class CW] [As indicated on Drawings] <Insert class>.

AAMA/WDMA/CSA 101/I.S.2/A440 establishes a gateway Performance Grade for sliding doors to qualify for each Performance Class. The gateway Performance Grade is 15 for Class R, 25 for Class LC, 30 for Class CW, and 40 for Class AW. For a particular project, the minimum Performance Grade for sliding doors is typically based on the design pressure.

          - Minimum Performance Grade: [Grade 15] [Grade 20] [Grade 25] [Grade 30] [Grade 35] [Grade 40] [Grade 45] [Grade 50] [As indicated on Drawings] <Insert grade>.

Retain "Thermal Transmittance" Paragraph below if required to comply with requirements of authorities having jurisdiction. First option is the Energy Star Requirement for sliding entry doors with 1/2-lite or larger (29.8 percent of door area by Energy Star definition) and applies in the entire United States. Requirements of authorities having jurisdiction may exceed the Energy Star minimum. Second and third options are examples; confirm availability with manufacturers.

        - Thermal Transmittance: NFRC 100 maximum total fenestration product U-factor of [0.32 Btu/sq. ft. x h x deg F (1.83 W/sq. m x K)] [0.54 Btu/sq. ft. x h x deg F (3.06 W/sq. m x K)] [0.56 Btu/sq. ft. x h x deg F (3.17 W/sq. m x K)] <Insert value>.

Options in "Solar Heat-Gain Coefficient (SHGC)" Paragraph below are based on Energy Star requirements effective January 2010. First option is the Energy Star Requirement for sliding entry doors with glazing and applies in the entire United States. Requirements of authorities having jurisdiction may exceed the Energy Star minimum.

        - Solar Heat-Gain Coefficient (SHGC): NFRC 200 maximum total fenestration product SHGC of [0.30] [0.27] <Insert value>.

Retain "Sound Transmission Class (STC)" or "Outside-Inside Transmission Class (OITC)" Paragraph below after verifying availability of test data. STC evaluates construction subject to interior, spoken-voice frequencies, while OITC evaluates using a sound-frequency range with lower frequencies more representative of transportation noise, which building envelopes are more likely to experience. OITC is generally a better evaluation method for exterior fenestration, but fewer manufacturers have OITC test data available. Some manufacturers can provide special glazing to improve acoustical performance.

        - Sound Transmission Class (STC): Rated for not less than [28] [32] <Insert rating> STC when tested for laboratory sound transmission loss according to ASTM E90 and determined by ASTM E413.

        - Outside-Inside Transmission Class (OITC): Rated for not less than [23] [27] [29] <Insert rating> OITC when tested for laboratory sound transmission loss according to ASTM E90 and determined by ASTM E1332.

Retain "Windborne-Debris Impact Resistance" Paragraph below to suit Project. The IBC establishes criteria for buildings in hurricane-prone locations. In paragraph, "enhanced" option applies to essential facilities and has additional requirements. Verify requirements of authorities having jurisdiction. Verify which manufacturers have tested products and can demonstrate compliance.

        - Windborne-Debris Impact Resistance: Passes ASTM E1886 missile-impact and cyclic-pressure tests in accordance with ASTM E1996 for Wind Zone [1] [2] [3] [4] for [basic] [enhanced] protection.

Insert increased heights if different from those in "Large-Missile Test" and "Small-Missile Test" subparagraphs below. For enhanced protection, delete "Small-Missile Test" Subparagraph.

          - Large-Missile Test: For glazing located within [30 feet (9.1 m)] <Insert dimension> of grade.

          - Small-Missile Test: For glazing located between 30 feet (9.1 m) and [60 feet (18.3 m)] <Insert dimension> above grade.

      - ALUMINUM-CLAD SLIDING WOOD-FRAMED GLASS DOORS

A broad range of quality exists among manufacturers and among product lines of individual manufacturers. Consider specifying specific models from acceptable manufacturers. Refer to Evaluations.

Lists below include some sliding wood-framed glass door manufacturers that certify their products comply with AAMA/WDMA performance standards. Retain manufacturers that produce types required and whose products correspond with performance requirements specified. Insert other manufacturers if required.

        - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Exterior Surfaces: Aluminum cladding with [manufacturer's standard baked-on enamel finish] [manufacturer's standard high-performance organic finish] [manufacturer's standard fluoropolymer two-coat system with fluoropolymer color topcoat containing not less than 70 percent polyvinylidene fluoride resin by weight and complying with AAMA 2605] <Insert finish>.

          - Color: [As selected by Architect from manufacturer's full range] <Insert color>.

        - Interior Surfaces: [Unfinished] [Manufacturer's standard factory-applied primer] [Manufacturer's standard factory-applied color finish] [Manufacturer's standard stain-and varnish-finish] <Insert finish>.

Retain "Wood Species" Subparagraph below for unfinished or varnished wood.

          - Wood Species: [Manufacturer's standard species] [Pine] [Mahogany] [Fir] [Alder] [Oak] [Cherry] <Insert species>.

Retain "Color" Subparagraph below for color-coated or stain-and-varnish finish.

          - Color: [As selected by Architect from manufacturer's full range] <Insert color>.

Retain profile option in "Frames and Door Panels" Paragraph below, or edit to require nominal dimensions. Door styles often referred to as "French doors" typically have wider stiles and rails and false or true muntins. Products often referred to as "builder's" lines tend to have narrower profiles. A broad range of quality exists between manufacturers, and within various product lines of individual manufacturers. Refer to Evaluations. Some manufacturers provide knocked-down frames for field assembly. Larger units with multiple door panels may require field assembly due to shipping limitations. Consult manufacturers.

        - Frames and Door Panels: Fabricate from wood components complying with indicated requirements. Provide factory-assembled [narrow-profile] [standard-profile] [wide-profile] door panels and [factory-assembled] [or] [field-assembled] frames.

Delete "True Divided Lites" Subparagraph if muntins are not required, or if applied grilles (false muntins) are used. Applied grilles are specified in the "Grilles (False Muntins)" Paragraph in the "Accessories" Article.

          - True Divided Lites: Provide glazing with true muntins resulting in individually glazed lites, in pattern indicated.

        - <Double click to insert sustainable design text for certified wood.>

        - Wood Components: Manufacturer's standard LVL or fine-grained wood lumber complying with AAMA/WDMA/CSA 101/I.S.2/A440; kiln dried to a moisture content of not more than 12 percent at time of fabrication; free of visible finger joints, blue stain, knots, pitch pockets, and surface checks larger than 1/32 inch (0.8 mm) deep by 2 inches (51 mm) wide; water-repellent preservative treated.

Some manufacturers offer multiple profiles for glazing stops and trim. Casing profiles include brick mold, flat, and stucco receptor. Jamb extensions are also available. Revise "Trim and Glazing Stops" Paragraph below if specific members and profiles are not indicated on Drawings. Retain first option for wood trim members; retain second option for trim component materials to match cladding material.

        - Trim and Glazing Stops: Material and finish to match [frame members] [cladding].

Retain "Mullions" Paragraph below if required. Coordinate with similar requirements for mullions in Section 085200 "Wood Windows" for installations with door and window unit combinations where units are joined by independent or integral mullions.

        - Mullions: Provide mullions and mullion casing and cover plates as shown, matching door units, complete with anchors for support to structure and installation of sliding wood-framed glass door units. Allow for erection tolerances and provide for movement of door units due to thermal expansion and building deflections, as indicated. Provide mullions and cover plates capable of withstanding design loads of door units.

"Integral Nailing Fin" Paragraph below is typically used with sliding wood-framed glass doors. Integral fins may also be part of water-/weather-resistive barrier assemblies. Some manufacturers provide nailing fins as an option. Verify availability and function with manufacturers.

        - Integral Nailing Fin: Aluminum nailing fins for securing frame to structure; provide sufficient strength to withstand design pressure indicated.

Some manufacturers provide drip caps as an accessory for installations that do not use a nailing fin.

        - Drip Caps: Extruded aluminum, factory fabricated and finished to match door frame; designed to direct water away from building when installed horizontally at head of sliding wood-framed glass doors.

Revise "Threshold and Sill Cap/Track" Paragraph below for thermally broken threshold or for another finish. Insert requirements for wood, polycarbonate, stainless steel, or composite threshold and track. Some manufacturers may use other materials. Coordinate with performance requirements for air infiltration and water penetration. Verify requirements of authorities having jurisdiction.

        - Threshold and Sill Cap/Track: Provide [pultruded fiberglass threshold with polycarbonate track] [extruded-aluminum threshold and track] [extruded-aluminum threshold and track with nonmagnetic stainless steel cover] [manufacturer's standard threshold and track] <Insert description of threshold and track> of thickness, dimensions, and profile indicated; designed to comply with performance requirements indicated and to drain to exterior.

          - Color: [Bronze] [Black] [Beige] [Mill finish] [Manufacturer's standard].

Retain "Low-Profile Floor Track" Subparagraph below for ADA-ABA compliant track offered by some manufacturers and that may be permitted or required by authorities having jurisdiction. Low-profile tracks may have lower water-infiltration resistance than standard height tracks. Coordinate available AAMA performance grade with manufacturers when using low-profile track.

          - Low-Profile Floor Track: ADA-ABA compliant.

      - VINYL-CLAD SLIDING WOOD-FRAMED GLASS DOORS

A broad range of quality exists among manufacturers and among product lines of individual manufacturers. Consider specifying specific models from acceptable manufacturers. Refer to Evaluations.

Lists below include some sliding wood-framed glass door manufacturers that certify their products comply with AAMA/WDMA performance standards. Retain manufacturers that produce types required and whose products correspond with performance requirements specified. Insert other manufacturers if required.

        - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Weather Shield uses vinyl cladding on door panels and frames; Andersen uses a high-performance coating on door panels and vinyl cladding on door frames.

        - Exterior Surfaces: Vinyl-clad frames; vinyl-clad or high performance color-coated finish door panels.

          - Color: [As selected by Architect from manufacturer's full range] <Insert color>.

        - Interior Surfaces: [Unfinished] [Manufacturer's standard factory-applied primer] [Manufacturer's standard factory-applied color finish] [Manufacturer's standard stain-and-varnish finish] <Insert finish>.

Retain "Wood Species" Subparagraph below for unfinished wood or varnished wood.

          - Wood Species: [Manufacturer's standard species] [Pine] [Mahogany] [Fir] [Alder] [Oak] [Cherry] <Insert species>.

Retain "Color" Subparagraph below for color-coated or stain-and-varnish finish.

          - Color: [As selected by Architect from manufacturer's full range] <Insert color>.

Retain profile option in "Frames and Door Panels" Paragraph below, or edit to require nominal dimensions. Door styles often referred to as "French doors" typically have wider stiles and rails and false or true muntins. Products often referred to as "builder's" lines tend to have narrower profiles. A broad range of quality exists between manufacturers, and within various product lines of individual manufacturers. Refer to Evaluations. Some manufacturers provide knocked-down frames for field assembly. Larger units with multiple door panels may require field assembly due to shipping limitations. Consult manufacturers.

        - Frames and Door Panels: Fabricate from wood components complying with indicated requirements. Provide factory-assembled [narrow-profile] [standard-profile] [wide-profile] door panels and [factory-assembled] [or] [field-assembled] frames.

Delete "True Divided Lites" Subparagraph if muntins are not required, or if applied grilles (false muntins) are used. Applied grilles are specified in the "Grilles (False Muntins)" Paragraph in the "Accessories" Article.

          - True Divided Lites: Provide glazing with true muntins resulting in individually glazed lites, in pattern indicated.

        - <Double click to insert sustainable design text for certified wood.>

        - Wood Components: Manufacturer's standard LVL or fine-grained wood lumber complying with AAMA/WDMA/CSA 101/I.S.2/A440; kiln dried to a moisture content of not more than 12 percent at time of fabrication; free of visible finger joints, blue stain, knots, pitch pockets, and surface checks larger than 1/32 inch (0.8 mm) deep by 2 inches (51 mm) wide; water-repellent preservative treated.

Some manufacturers offer multiple profiles for glazing stops and trim. Casing profiles include brick mold, flat, and stucco receptor. Jamb extensions are also available. Revise "Trim and Glazing Stops" Paragraph below if specific members and profiles are not indicated on Drawings. Retain first option for wood trim members; retain second option for trim component materials to match cladding material.

        - Trim and Glazing Stops: Material and finish to match [frame members] [cladding].

Retain "Mullions" Paragraph below if required. Coordinate with similar requirements for mullions in Section 085200 "Wood Windows" for installations with door and window unit combinations where units are joined by independent or integral mullions.

        - Mullions: Provide mullions and mullion casing and cover plates as shown, matching door units, complete with anchors for support to structure and installation of sliding wood-framed glass door units. Allow for erection tolerances and provide for movement of door units due to thermal expansion and building deflections, as indicated. Provide mullions and cover plates capable of withstanding design loads of door units.

"Integral Nailing Fin" Paragraph below is typically used with sliding wood-framed glass doors. Integral fins may also be part of water-/weather-resistive barrier assemblies. Some manufacturers provide nailing fins as an option. Verify availability and function with manufacturers.

        - Integral Nailing Fin: PVC nailing fins for securing frame to structure; provide sufficient strength to withstand design pressure indicated.

Some manufacturers provide drip caps as an accessory for installations that do not use a nailing fin.

        - Drip Caps: Extruded aluminum, factory fabricated and finished to match door frame; designed to direct water away from building when installed horizontally at head of sliding wood-framed glass doors.

Revise "Threshold and Sill Cap/Track" Paragraph below for thermally broken threshold or for another finish. Insert requirements for wood, polycarbonate, stainless steel, or composite threshold and track. Some manufacturers may use other materials. Coordinate with performance requirements for air infiltration and water penetration. Verify requirements of authorities having jurisdiction.

        - Threshold and Sill Cap/Track: Provide [pultruded fiberglass threshold with polycarbonate track] [extruded-aluminum threshold and track] [extruded-aluminum threshold and track with nonmagnetic stainless steel cover] [manufacturer's standard threshold and track] <Insert description of threshold and track> of thickness, dimensions, and profile indicated; designed to comply with performance requirements indicated and to drain to exterior.

          - Color: [Bronze] [Black] [Beige] [Mill finish] [Manufacturer's standard].

Retain "Low-Profile Floor Track" Subparagraph below for ADA-ABA compliant track offered by some manufacturers and that may be permitted or required by authorities having jurisdiction. Low-profile tracks may have lower water-infiltration resistance than standard height tracks. Coordinate available AAMA performance grade with manufacturers when using low-profile track.

          - Low-Profile Floor Track: ADA-ABA compliant.

      - UNCLAD SLIDING WOOD-FRAMED GLASS DOORS

A broad range of quality exists among manufacturers and among product lines of individual manufacturers. Consider specifying specific models from acceptable manufacturers. Refer to Evaluations.

Lists below include some sliding wood-framed glass door manufacturers that certify their products comply with AAMA/WDMA performance standards. Retain manufacturers that produce types required and whose products correspond with performance requirements specified. Insert other manufacturers if required.

        - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Exterior Surfaces: [Manufacturer's standard factory-applied primer] [Manufacturer's standard factory-applied color finish] [Unfinished].

Retain "Wood Species" Subparagraph below for unfinished wood.

          - Wood Species: [Manufacturer's standard paint-grade species] [Pine] [Mahogany] <Insert species>.

Retain "Color" Subparagraph below for factory-applied color finish.

          - Color: [As selected by Architect from manufacturer's full range] <Insert color>.

        - Interior Surfaces: [Unfinished] [Manufacturer's standard factory-applied primer] [Manufacturer's standard factory-applied color finish] [Manufacturer's standard stain-and-varnish finish] <Insert finish>.

Retain "Wood Species" Subparagraph below for unfinished or varnished wood.

          - Wood Species: [Pine] [Mahogany] [Fir] [Alder] [Oak] [Cherry] [Manufacturer's standard paint-grade species] <Insert species>.

Retain "Color" Subparagraph below for color-coated or stain-and-varnish finish.

          - Color: [As selected by Architect from manufacturer's full range] <Insert color>.

Retain profile option in "Frames and Door Panels" Paragraph below, or edit to require nominal dimensions. Door styles often referred to as "French doors" typically have wider stiles and rails and false or true muntins. Products often referred to as "builder's" lines tend to have narrower profiles. A broad range of quality exists between manufacturers, and within various product lines of individual manufacturers. Refer to Evaluations. Some manufacturers provide knocked-down frames for field assembly. Larger units with multiple door panels may require field assembly due to shipping limitations. Consult manufacturers.

        - Frames and Door Panels: Fabricate from wood components complying with indicated requirements. Provide factory-assembled [narrow-profile] [standard-profile] [wide-profile] door panels and [factory-assembled] [or] [field-assembled] frames.

Delete "True Divided Lites" Subparagraph if muntins are not required, or if applied grilles (false muntins) are used. Applied grilles are specified in the "Grilles (False Muntins)" Paragraph in the "Accessories" Article.

          - True Divided Lites: Provide glazing with true muntins resulting in individually glazed lites, in pattern indicated.

        - <Double click to insert sustainable design text for certified wood.>

        - Wood Components: Manufacturer's standard LVL or fine-grained wood lumber complying with AAMA/WDMA/CSA 101/I.S.2/A440; kiln dried to a moisture content of not more than 12 percent at time of fabrication; free of visible finger joints, blue stain, knots, pitch pockets, and surface checks larger than 1/32 inch (0.8 mm) deep by 2 inches (51 mm) wide; water-repellent preservative treated.

Some manufacturers offer multiple profiles for glazing stops and trim. Casing profiles include brick mold, flat, and stucco receptor. Jamb extensions are also available. Revise "Trim and Glazing Stops" Paragraph below if specific members and profiles are not indicated on Drawings. Retain first option for wood trim members; retain second option for trim component materials to match cladding material.

        - Trim and Glazing Stops: Material and finish to match [frame members] [cladding].

Retain "Mullions" Paragraph below if required. Coordinate with similar requirements for mullions in Section 085200 "Wood Windows" for installations with door and window unit combinations where units are joined by independent or integral mullions.

        - Mullions: Provide mullions and mullion casing and cover plates as shown, matching door units, complete with anchors for support to structure and installation of sliding wood-framed glass door units. Allow for erection tolerances and provide for movement of door units due to thermal expansion and building deflections, as indicated. Provide mullions and cover plates capable of withstanding design loads of door units.

"Integral Nailing Fin" Paragraph below is typically used with sliding wood-framed glass doors. Integral fins may also be part of water-/weather-resistive barrier assemblies. Some manufacturers provide nailing fins as an option. Verify availability and function with manufacturers.

        - Integral Nailing Fin: [PVC] [Aluminum] nailing fins for securing frame to structure; provide sufficient strength to withstand design pressure indicated.

Some manufacturers provide drip caps as an accessory for installations that do not use a nailing fin.

        - Drip Caps: Extruded aluminum, factory fabricated and finished to match door frame; designed to direct water away from building when installed horizontally at head of sliding wood-framed glass doors.

Revise "Threshold and Sill Cap/Track" Paragraph below for thermally broken threshold or for another finish. Insert requirements for wood, polycarbonate, stainless steel, or composite threshold and track. Some manufacturers may use other materials. Coordinate with performance requirements for air infiltration and water penetration. Verify requirements of authorities having jurisdiction.

        - Threshold and Sill Cap/Track: Provide [pultruded fiberglass threshold with polycarbonate track] [extruded-aluminum threshold and track] [extruded-aluminum threshold and track with nonmagnetic stainless steel cover] [manufacturer's standard threshold and track] <Insert description of threshold and track> of thickness, dimensions, and profile indicated; designed to comply with performance requirements indicated and to drain to exterior.

          - Color: [Bronze] [Black] [Beige] [Mill finish] [Manufacturer's standard].

Retain "Low-Profile Floor Track" Subparagraph below for ADA-ABA compliant track offered by some manufacturers and that may be permitted or required by authorities having jurisdiction. Low-profile tracks may have lower water-infiltration resistance than standard height tracks. Coordinate available AAMA performance grade with manufacturers when using low-profile track.

          - Low-Profile Floor Track: ADA-ABA compliant.

      - GLAZING

Revise "Glass and Glazing" Paragraph below for custom glass or glazing requirements if available from selected manufacturers.

        - Glass and Glazing: Manufacturer's standard glazing system that produces weathertight seal.[ Comply with requirements for windborne-debris resistance.] <Insert glazing requirements.>

          - Glass: ASTM C1036, Type 1, q3, Category II safety glass complying with testing requirements in 16 CFR 1201.

Retain "Safety Glazing Labeling" Subparagraph below if applicable and if labeling is required. Not all manufacturers participate in third-party testing programs.

          - Safety Glazing Labeling: Permanently mark safety glazing with certification label of [the SGCC] [the SGCC or another certification agency acceptable to authorities having jurisdiction] [or] [the manufacturer]. Label shall indicate manufacturer's name, type of glass, thickness, and safety glazing standard with which glass complies.

          - Tint: [Clear] [Gray] [Bronze] [Green] <Insert tint>.

Delete "Insulating-Glass Units" Subparagraph below if using monolithic glazing. Retain option in "Insulating-Glass Units" Subparagraph below after verifying that manufacturers obtain glass units from glass manufacturers that participate in the Insulating Glass Certification Council program.

          - Insulating-Glass Units: ASTM E2190[, certified through IgCC as complying with requirements of IgCC].

            - Filling: Fill space between glass lites with [air] [argon].

            - Lites: [Two] [Three].

            - Low-E Coating: [Manufacturer's standard] [Pyrolytic on second surface] [Sputtered on second surface] [Sputtered on third surface] [Sputtered on second or third surface] <Insert coating>.

Retain "Integral Louver Blinds" Subparagraph below if required. Verify availability with manufacturers.

            - Integral Louver Blinds: Glass manufacturer's standard horizontal louver blinds with aluminum slats and polyester fiber cords, located in space between glass lites, and operated by hardware located on inside face of door panel.

              - Operation: [Tilt only] [Tilt, raising, and lowering].

              - Color: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color>.

          - Dual Glazing:

            - Interior Lite: [Glass] <Insert type>.

            - Exterior Lite: [Glass] [Insulating-glass unit] <Insert type>.

      - HARDWARE

Nonmagnetic stainless steel, Series 300, or a superior corrosion-resistant-coated metal may be required to meet specific customer or regional needs and for protection against corrosive environments, such as in urban, coastal, or industrial areas.

        - General: Provide manufacturer's standard hardware, fabricated from a corrosion-resistant material compatible with wood[ and aluminum cladding] complying with AAMA 907; designed to smoothly operate, tightly close, and securely lock sliding wood-framed glass doors; and sized to accommodate panel weight and dimensions.

Revise "Door Pulls" Paragraph below if optional, better-quality door pulls are available from manufacturer and are required to suit Project.

        - Door Pulls: Provide manufacturer's standard [metal] [wood] [metal or wood] pull grips.

Revise "Lock" Paragraph below to suit Project's locking requirements, or insert others. Multipoint locking devices improve security and performance. Include key-operated cylinders here or in Section 087100 "Door Hardware."

        - Lock: Install manufacturer's keyed cylinder lock and [multipoint] locking device on each movable panel, lockable from the inside [only] [and outside]. Adjust locking device to allow unobstructed movement of the panel across adjacent panel in the direction indicated.

          - Keying System: [All cylinders keyed alike] [Keyed to match other building entrances] <Insert instructions>.

Retain "Security Foot Bolt" Paragraph below if security foot bolt is required or available. Some manufacturers offer a foot bolt as standard hardware; for others, it is an option. If retaining, revise to suit selected manufacturers' standard equipment (such as bolt attached to track or frame instead of bottom rail).

        - Security Foot Bolt: Provide security foot-operated dead bolt attached to bottom rail of movable sliding door panels to lock the panel when fully closed and when partially open to permit ventilation.

        - Limit Stops: Resilient rubber.

      - INSECT SCREENS

Manufacturers' designs may incorporate screens on inside or outside of door. Review availability and revise "General" Paragraph below if limiting screen location.

        - General: Design sliding wood-framed glass doors to accommodate screens in a tight-fitting, removable arrangement fully integrated with door frame. Locate screens on the [inside] [outside] of door and provide for each operable door panel. Comply with SMA 1201.

Retain first option in "Insect Screen Frames" Paragraph below if only heavy-duty, extruded-aluminum frames are suitable for Project. Extruded-aluminum frames may be standard or optional with each manufacturer; revise paragraph accordingly. Screens that roll away are available from some manufacturers.

        - Insect Screen Frames: Manufacturer's standard [extruded-aluminum] [or] [formed-tubular-aluminum] members, with mitered or coped joints, concealed fasteners, adjustable rollers, and removable PVC or PE spline/anchor concealing edge of mesh. Provide finish to match door frame.

Retain "Glass-Fiber Mesh Fabric" or "Aluminum Wire Fabric" Paragraph below or insert another. Glass-fiber mesh is standard with most manufacturers. Usually retain first option in first paragraph for most locations. Second option is suitable for areas plagued by small insects such as no-see-ums. Second option is also suitable for use as a solar screen that blocks up to 65 percent of incident solar heat and glare. Some manufacturers offer a screen that uses a finer mesh that transmits more light; confirm availability and revise paragraph if required.

        - Glass-Fiber Mesh Fabric: ASTM D3656, [18-by-14 or 18-by-16] [20-by-20 or 20-by-30] count per sq. in. (645-sq.-mm) mesh of PVC-coated, glass-fiber threads; woven and fused to form a fabric mesh resistant to corrosion, shrinkage, stretch, impact damage, and weather deterioration. Comply with ASTM D3656.

          - Mesh Color: [Manufacturer's standard] [Charcoal gray] [Silver gray] <Insert color>.

        - Aluminum Wire Fabric: 18-by-16 (1.1-by-1.3-mm) mesh of 0.011-inch-diameter (0.28-mm-diameter) coated aluminum wire.

          - Wire-Fabric Finish: [Manufacturer's standard] [Natural bright] [Charcoal gray] [Black].

        - Hardware: Manufacturer's standard noncorrosive metal.

          - Lock: Manufacturer's standard pull and keyless locking device on each movable panel, lockable from inside only designed to allow unobstructed movement of panel across adjacent panel.

      - ACCESSORIES

Retain "Grilles (False Muntins)" Paragraph below if grilles are required; delete if using muntins (true divided lites) specified in "True Divided Lites" subparagraphs above. Some manufacturers have a limited range of options for grilles; confirm availability.

        - Grilles (False Muntins): Provide grilles in designs indicated, for removable application to inside of each panel lite.

Retain one of first three options in "Type" Subparagraph below. Retain fourth option with any of first three, if applicable.

          - Type: [Interior, removable] [Exterior and interior, removable] [Exterior and interior, adhered to glass] [with between-glass grille].

          - Material: To match adjacent finish of door panel.

          - Design: [Rectangular] [Diamond] [as indicated on Drawings] <Insert design>.

          - Bar Width: Not less than [3/4 inch (19 mm)] [7/8 inch (22 mm)] [1-1/8 inches (28 mm)] <Insert dimension> wide.

          - Bar Profile: [Beveled] [Ovolo] [Square].

          - Color: [White] [Bronze] [As selected by Architect from manufacturer's full range] <Insert color>.

        - Fasteners: Noncorrosive and compatible with door members, trim, hardware, anchors, and other components.

Generally, retain "Exposed Fasteners" Subparagraph below. Revise if exposed fasteners are permitted.

          - Exposed Fasteners: Do not use exposed fasteners to the greatest extent possible. For application of hardware, use fasteners that match finish hardware being fastened.

        - Anchors, Clips, and Accessories: Provide anchors, clips, and accessories of aluminum, nonmagnetic stainless steel, or zinc-coated steel or iron for sliding wood-framed glass doors, complying with ASTM B456 or ASTM B633 for SC 3 severe service conditions; provide sufficient strength to withstand design pressure indicated.

          - Windborne-Debris Resistance: Provide anchors of same design used in windborne-debris resistance testing.

      - FABRICATION

        - Fabricate sliding wood-framed glass doors in sizes indicated. Include a complete system for assembling components and anchoring doors.

        - Fabricate sliding wood-framed glass doors that are reglazable without dismantling panel framing.

        - Weather Stripping: Provide full-perimeter weather stripping for each door panel unless otherwise indicated.

        - Factory-machine sliding wood-framed glass doors for openings and hardware that is not surface applied.

        - Complete fabrication, assembly, finishing, hardware application, and other work in the factory to greatest extent possible. Disassemble components only as necessary for shipment and installation. Allow for scribing, trimming, and fitting at Project site.

        - Factory-Glazed Fabrication: Glaze sliding wood-framed glass doors in the factory.

      - WOOD FINISHES

Delete this article if finished, aluminum-clad sliding wood-framed glass doors without primed interior surfaces or if unfinished sliding wood-framed glass doors are required.

        - Factory-Applied Primer: Provide manufacturer's standard factory-applied prime coat complying with WDMA T.M. 11. <Insert specific requirements for factory-applied prime coat if any> on exposed [exterior] [and] [interior] wood surfaces.

First option in "Factory-Applied Color Finish" Paragraph below is for pigmented (paint) coatings suitable for exterior exposure. Retain this paragraph for factory-applied color finishes or if Andersen vinyl-clad sliding wood-framed glass doors are used because that product uses a high-performance urethane coating on the exterior of door panels.

        - Factory-Applied Color Finish: Provide manufacturer's standard factory-applied finish [complying with WDMA T.M. 12] <Insert manufacturer's standard finish>. Apply finish to exposed [exterior] [and] [interior] wood surfaces.

          - Color: [White] [Brown] [Gray] [As selected by Architect from manufacturer's full range] <Insert color>.

      - ALUMINUM FINISHES

If retaining more than one finish in paragraphs below, indicate location of each on Drawings or by inserts.

"Baked-Enamel or Powder-Coat Finish" Paragraph below references AAMA standard for pigmented organic coating on extrusions and panels.

        - Baked-Enamel or Powder-Coat Finish: AAMA 2603 except with a minimum dry film thickness of 1.5 mils (0.04 mm). Comply with coating manufacturer's written instructions for cleaning, conversion coating, and applying and baking finish.

          - Color and Gloss: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color and gloss>.

Retain "High-Performance Organic Finish" Paragraph below. Retain AAMA 2604 or AAMA 2605 for high- or superior-performance organic coatings, respectively, on extrusions and panels. If specific products are required, name coating manufacturers and products.

        - High-Performance Organic Finish: Two-coat fluoropolymer finish complying with [AAMA 2604] [AAMA 2605] and containing not less than [50] [70] percent PVDF resin by weight in color coat. Prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturers' written instructions.

          - Color and Gloss: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color and gloss>.

- EXECUTION

      - EXAMINATION

        - Examine openings, substrates, structural support, anchorage, and conditions, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of the Work.

        - Verify rough opening dimensions, levelness of threshold substrate, and operational clearances.

        - Examine wall flashings, vapor retarders, water and weather barriers, and other built-in components to ensure a coordinated, weathertight sliding door installation.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - INSTALLATION

        - Comply with Drawings, Shop Drawings, and manufacturer's written instructions for installing sliding doors, hardware, accessories, and other components.

Retain "Windborne-Debris Resistance" Paragraph below for installations requiring windborne-debris resistance. Proper anchorage of units is necessary to maintain performance as tested.

        - Windborne-Debris Resistance: Anchor sliding wood-framed glass doors that have been tested for windborne-debris resistance to structure using anchoring method, fastener type, and fastening frequency identical to that used in windborne-debris resistance testing.

        - Install sliding wood-framed glass doors level, plumb, square, true to line, without distortion, without warp or rack of frames and panels, and without impeding thermal movement; anchored securely in place to structural support; and in proper relation to wall flashing, vapor retarders, air barriers, water/weather barriers, and other adjacent construction. Comply with ASTM E2112.

        - Set sill members in bed of sealant or with gaskets, as indicated, to provide weathertight construction.

Retain paragraph below only for aluminum-clad sliding wood-framed glass doors.

        - Separate aluminum and other corrodible surfaces from sources of corrosion or electrolytic action at points of contact with other materials according to ASTM E2112, Section 5.12, "Dissimilar Materials."

Insert article for field testing if required by Project.

      - FIELD QUALITY CONTROL

Retain this article if field tests are required. Small projects may not need testing. If retaining, indicate number of doors to be tested. Field tests for air and water leakage should be specified for significant projects.

Retain "Testing Agency" Paragraph below to identify who shall perform tests and inspections. If retaining second option in "Testing Agency" Paragraph, retain "Field quality-control reports" Paragraph in "Informational Submittals" Article.

        - Testing Agency: [Owner will engage] [Engage] a qualified testing agency to perform tests and inspections.

          - Testing and inspecting agency will interpret tests and state in each report whether tested work complies with or deviates from requirements.

Revise "Testing Services" Paragraph below if more stringent testing is required. AAMA 502 Test Method A is default unless otherwise indicated.

        - Testing Services: Test and inspect installed sliding wood-framed glass doors as follows:

          - Testing Methodology: Test sliding wood-framed glass doors for air infiltration and water resistance according to AAMA 502.

          - Air-Infiltration Testing:

            - Test Pressure: That required to determine compliance with AAMA/WDMA/CSA 101/I.S.2/A440 performance class indicated.

            - Allowable Air-Leakage Rate: [1.5] <Insert number> times the applicable AAMA/WDMA/CSA 101/I.S.2/A440 rate for product type and performance class rounded down to one decimal place.

          - Water-Resistance Testing:

            - Test Pressure: [Two-thirds] <Insert number> times test pressure required to determine compliance with AAMA/WDMA/CSA 101/I.S.2/A440 performance grade indicated.

            - Allowable Water Infiltration: No water penetration.

          - Testing Extent: [Three] [Three mockup] <Insert number or description> sliding wood-framed glass doors of each type as selected by Architect and a qualified independent testing and inspecting agency. Conduct tests after perimeter sealants have cured.

          - Test Reports: Prepared according to AAMA 502.

See Section 014000 "Quality Requirements" for retesting and reinspecting requirements and Section 017300 "Execution" for requirements for correcting the Work.

        - Sliding wood-framed glass door will be considered defective if it does not pass tests and inspections.

      - ADJUSTING, CLEANING, AND PROTECTION

        - Lubricate hardware and moving parts.

        - Adjust operating panels and screens to provide a tight fit at contact points and weather stripping for smooth operation, without binding, and weathertight closure.

        - Adjust hardware for proper alignment, smooth operation, and proper latching without unnecessary force or excessive clearance.

        - Clean exposed surfaces immediately after installing sliding wood-framed glass doors. Avoid damaging protective coatings and finishes. Remove nonpermanent labels, excess sealants, glazing materials, dirt, and other substances.

        - Remove and replace glass that has been broken, chipped, cracked, abraded, or damaged during construction period.

        - Protect sliding wood-framed glass door surfaces from contact with contaminating substances resulting from construction operations. If contaminating substances contact sliding wood-framed glass door surfaces, remove contaminants immediately according to manufacturer's written instructions.

Retain first paragraph below if sliding doors are factory finished.

        - Refinish or replace sliding doors with damaged finishes.

        - Replace damaged components.

END OF SECTION 081816.19