Copyright 2017 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 096466 - WOOD ATHLETIC FLOORING

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - This Section includes wood athletic flooring.

        - Related Requirements:

Retain subparagraph below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 096400 "Wood Flooring" for traditional solid-wood and engineered-wood, strip, plank, and parquet flooring.

      - COORDINATION

Retain "Coordination" Article if Project includes concrete-slab depressions or floor inserts for volleyball post standards or other gymnasium equipment. Floor inserts are specified in Section 116623 "Gymnasium Equipment."

        - Coordinate layout and installation of slab depressions to accommodate layout and height of wood athletic flooring assembly.

        - Coordinate layout and installation of flooring with floor inserts for gymnasium equipment.

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

          - Include construction details, material descriptions, dimensions of individual components and profiles, and finishes for wood athletic flooring.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for certified wood.>

          - <Double click to insert sustainable design text for certified wood.>

          - <Double click to insert sustainable design text for adhesives.>

          - <Double click to insert sustainable design text for composite wood.>

          - <Double click to insert sustainable design text for low-emitting floor finish system.>

        - Shop Drawings: For each type of floor assembly, include the following:

          - Plans, sections, and attachment details.

Retain first subparagraph below if concrete-slab depressions are required.

          - Details of concrete-slab depressions.

Retain first subparagraph below if various grades of wood floor are required.

          - Locations of different grades of wood flooring.

          - Expansion provisions and trim details.

          - Layout, colors, widths, and dimensions of game lines and markers.

          - Locations of floor inserts for athletic equipment installed through flooring assembly.

          - <Insert requirements>.

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples.

        - Samples: For each exposed product and for each color and texture specified, approximately [12 inches (300 mm) long] <Insert dimension> in size.

          - Include Sample sets showing the full range of normal color and texture variations expected in wood flooring.

          - Include Sample sets showing finishes[ and game-line and marker paints] applied to wood flooring.

        - Samples for Initial Selection: For each type of wood athletic flooring and accessory in each type of exposed color and finish.

          - Include manufacturer's color charts showing colors and glosses available for the following:

            - Floor finishes.

            - Game-line and marker paints.

        - Samples for Verification: For each type of wood athletic flooring and accessory required; approximately [12 inches (300 mm) long] <Insert dimension> and of same thickness and material indicated for the Work.

          - Include Sample sets showing the full range of normal color and texture variations expected in wood flooring.

          - Include Sample sets showing finishes[ and game-line and marker paints] applied to wood flooring.

      - INFORMATIONAL SUBMITTALS

Manufacturers measure assembly performance differently. See "Measuring Assembly Performance" Article in the Evaluations. "Product Test Reports" Paragraph below assumes manufacturer's standard tests are acceptable unless specific requirements are added to the "Performance Requirements" Article.

        - Product Test Reports: For each wood athletic flooring system, for tests performed by a qualified testing agency.

      - CLOSEOUT SUBMITTALS

        - Maintenance Data: For wood athletic flooring and finish systems to include in maintenance manuals.

      - QUALITY ASSURANCE

        - <Double click to insert sustainable design text for manufacturer qualifications.>

        - <Double click to insert sustainable design text for vendor qualifications.>

Retain "Installer Qualifications" Paragraph below to require an MFMA-accredited Installer. Verify that installers are available to perform work in Project location using list of accredited installers available online through MFMA.

        - Installer Qualifications: A firm or individual that has been approved by MFMA as an accredited Installer according to the MFMA Accreditation Program.

          - Installer responsibilities include installation and field finishing of wood athletic flooring components and accessories, and application of game lines and markers.

        - Mockups: Build mockups to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for installation.

Indicate portion of floor represented by mockup on Drawings or draw mockup as separate element.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver floor assembly materials in unopened cartons or bundles.

        - Protect wood from exposure to moisture. Do not deliver wood components until after concrete, masonry, plaster, ceramic tile, and similar wet-work is complete and dry.

        - Store wood components in a dry, warm, well-ventilated, weathertight location and in a horizontal position.

      - FIELD CONDITIONS

        - Conditioning period begins not less than seven days before wood athletic flooring installation, is continuous through installation, and continues not less than seven days after installation.

          - Environmental Conditioning: Maintain ambient temperature between 65 and 75 deg F (18 and 24 deg C) and relative humidity planned for building occupants, but not less than 35 percent or more than 50 percent, in spaces to receive wood athletic flooring during the conditioning period.

          - Wood Conditioning: Move wood components into spaces where they will be installed, no later than beginning of the conditioning period.

            - Do not install wood athletic flooring until wood components adjust to relative humidity of, and are at same temperature as, spaces where they are to be installed.

            - Open sealed packages to allow wood components to acclimatize immediately on moving wood components into spaces in which they will be installed.

        - After conditioning period, maintain relative humidity and ambient temperature planned for building occupants.

        - Install wood athletic flooring after other finishing operations, including painting, have been completed.

- PRODUCTS

Manufacturers and products listed in SpecAgent and MasterWorks Paragraph Builder are neither recommended nor endorsed by the AIA or Deltek. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - MANUFACTURERS

        - <Double click here to find, evaluate, and insert list of manufacturers and products.>

      - SYSTEM DESCRIPTION

Retain "System Type" Paragraph below if generic description is required. First option indicates systems not fastened to the concrete substrate; second option indicates systems mechanically attached to the concrete substrate; third option indicates systems with resilient pads that are mechanically restrained by channels and clips; fourth option indicates removable flooring systems used in multipurpose arenas.

        - System Type: [Floating] [Fixed] [Anchored resilient] [Portable] <Insert system>.

Options in "Overall System Height" Paragraph below are examples only. Systems are available in various heights; coordinate system heights with slab depressions.

        - Overall System Height: [As indicated on Drawings] [2-1/8 inches (54 mm)] [2-1/4 inches (57 mm)] [2-1/2 inches (64 mm)] <Insert height>.

      - PERFORMANCE REQUIREMENTS

Before inserting performance requirements according to ASTM, MFMA, or European standards for wood athletic flooring, see "Measuring Assembly Performance" Article in the Evaluations.

        - <Double click to insert sustainable design text for certified wood.>

        - <Double click to insert sustainable design text for composite wood products.>

      - FLOORING MATERIALS

        - Maple Flooring: Comply with MFMA grading rules for species, grade, and cut.

Retain "Certification" Subparagraph below if required. Only MFMA members can use mark; however, nonmembers may comply with grading rules. Manufacturers listed in Part 2 provide flooring that carries MFMA mark.

          - Certification: Provide flooring that carries MFMA mark on each bundle or piece.

Retain "Random-Length Strip Flooring" Paragraph below to coordinate with products required.

        - Random-Length Strip Flooring: Northern hard maple (Acer saccharum), kiln dried, random length, tongue and groove, and end matched.

          - Grade: MFMA-RL [First] [Second and Better] [Third and Better].

If applicable, retain "Exception" Subparagraph below.

            - Exception: For areas under stacked portion of telescoping bleachers that are normally concealed from view, provide Third and Better Grade.

Unless otherwise specified, MFMA permits flat grain. Edge grain is more resistant to effects of moisture and is more durable than flat grain.

          - Cut: [Edge] [Flat].

Usually retain first option in "Thickness" Subparagraph below. Retain second option only if required for heavy-duty applications such as roller-skating rinks. Other thicknesses, including 27/32 inch (21 mm), are available.

          - Thickness: [25/32 inch (20 mm)] [33/32 inch (26 mm)] <Insert dimension>.

Face width of 2-1/4 inches (57 mm) is most common. Face width of 3-1/4 inches (83 mm) is also available.

          - Face Width: [2-1/4 inches (57 mm)] [1-1/2 inches (38 mm)] <Insert dimension>.

Retain "Finger-Jointed Strip Flooring" Paragraph below to coordinate with products required.

        - Finger-Jointed Strip Flooring: Northern hard maple (Acer saccharum), kiln dried, random length, tongue and groove, and end matched.

          - Grade: MFMA-FJ [First] [Second and Better] [Third and Better].

If applicable, retain "Exception" Subparagraph below.

            - Exception: For areas under stacked portion of telescoping bleachers that are normally concealed from view, provide Third and Better Grade.

Unless otherwise specified, MFMA permits flat grain. Edge grain is more resistant to effects of moisture and is more durable than flat grain.

          - Cut: [Edge] [Flat].

Usually retain first option in "Thickness" Subparagraph below. Retain second option only if required for heavy-duty applications such as roller-skating rinks. Other thicknesses, including 27/32 inch (21 mm), are available.

          - Thickness: [25/32 inch (20 mm)] [33/32 inch (26 mm)] <Insert dimension>.

Face width of 2-1/4 inches (57 mm) is most common. Face width of 3-1/4 inches (83 mm) is also available.

          - Face Width: [2-1/4 inches (57 mm)] [1-1/2 inches (38 mm)] <Insert dimension>.

Retain "Parquet Flooring" Paragraph below to coordinate with products required.

        - Parquet Flooring: Northern hard maple (Acer saccharum), kiln dried, edge grain, and square edge.

          - Grade: MFMA-PQ [Second and Better] [Third and Better].

          - Thickness: Not less than [5/16 inch (8 mm)] [3/8 inch (10 mm)] [7/16 inch (11 mm)] [1/2 inch (13 mm)] [11/16 inch (17 mm)] <Insert dimension>.

          - Picket Dimensions:

Generally, 7/8-inch (22-mm) width is more readily available than 1-1/8-inch (29-mm) width. Retaining first option in "Width" Subparagraph below allows manufacturer to use stock that is most readily available.

            - Width: [7/8 inch (22 mm)] [or] [1-1/8 inches (29 mm)].

            - Length: [6 inches (152 mm)] [9 inches (229 mm)] <Insert dimension>.

      - SUBFLOOR MATERIALS

Retain subfloor system components in this article to suit Project, and insert others to coordinate with products required.

        - Board Underlayment: Nominal 1-by-6-inch (25-by-150-mm) graded boards; of SPIB No. 2 Southern pine, WCLIB Construction grade (any species), or WWPA No. 3 (any species), dried to 15 percent moisture content.

        - Plywood Underlayment: APA rated, C-D plugged, exterior glue, tongue and groove, [15/32 inch (12 mm)] [23/32 inch (18 mm)] thick.

        - Wood Sleepers: Standard grade; 48 inches (1200 mm) long; kiln-dried Eastern hemlock, fir, pine, or spruce.

          - Size: Nominal [2 by 3 inches (50 by 75 mm)] [2 by 4 inches (50 by 100 mm)].

Revise "Sleeper Anchors" Subparagraph below if greater pullout strength is required.

          - Sleeper Anchors: Manufacturer's standard drive pins recommended by anchor manufacturer to achieve minimum 900-lbf (4000-N) pullout strength in 3000-psi (20.7-MPa) concrete.

          - Sleeper Shims: In size and type recommended in writing by flooring manufacturer for application indicated.

Retain "Asphalt Primer" and "Asphalt Mastic" subparagraphs below for fixed-sleeper systems without pads. If retaining, coordinate with installation in Part 3.

          - Asphalt Primer: ASTM D41/D41M.

          - Asphalt Mastic: ASTM D312, Type I, cold-applied dead-level asphalt or Type III, hot-applied steep asphalt, as recommended in writing by manufacturer.

        - Channels: [Manufacturer's standard as indicated by product designation above] <Insert description>.

          - Channel Anchors: Manufacturer's standard, but not less than modified steel drive pins recommended by anchor manufacturer to achieve minimum 900-lbf (4000-N) pullout strength.

Retain "Clips" Subparagraph below if required.

          - Clips: [Manufacturer's standard as indicated by product designation above] <Insert description or proprietary product name>.

        - Resilient Pads: With air voids for resiliency and installed at manufacturer's standard spacing for product designation indicated above.

Revise "Type," "Material," and "Thickness" subparagraphs below to suit specific products required and to ensure differentiation among similar products. Different pads may be required for different installation areas; see "Subfloor Systems" Article in the Evaluations.

          - Type: <Insert description>.

          - Material: [PVC] [Rubber] [Neoprene] <Insert requirements>.

          - Thickness: [3/8 inch (10 mm)] [7/16 inch (11 mm)] [5/8 inch (16 mm)] [3/4 inch (19 mm)] <Insert dimension>.

        - Resilient Underlayment: Flexible, multicellular, closed-cell, expanded polyethylene-foam sheet; nominal 2-lb/cu. ft. (32-kg/cu. m) density.

          - Thickness: [1/4 inch (6 mm)] [1/2 inch (13 mm)] [3/4 inch (19 mm)] [1 inch (25 mm)] <Insert dimension>.

      - FINISHES

        - Floor-Finish System: System of compatible components recommended in writing by flooring manufacturer, and MFMA approved.

          - Floor-Sealer Formulation: Pliable, penetrating type. MFMA Group 1, Sealers.

          - Finish-Coat Formulation: Formulated for gloss finish indicated and multicoat application.

Verify finishes available through manufacturers and revise "Type" Subparagraph below to suit Project. Consider inserting specific finish products using MFMA's "Athletic Flooring Sealer and Finish Specifications and Conformance List #31" as a guide (available online). Retain Group 5 if low-VOC products are required. Groups 3 and 5 are high gloss; revise to include low-gloss finish groups if required.

            - Type: [MFMA Group 3, Gymnasium-Type Surface Finishes] [MFMA Group 5, Water-Based Finishes] <Insert finish>.

          - Game-Line and Marker Paint: Industrial enamel compatible with finish coats and recommended in writing by manufacturers of finish coats, and paint for this use.

          - <Double click to insert sustainable design text for floor treatment products.>

      - ACCESSORIES

Generally, retain "Vapor Retarder" Paragraph below for floors installed over concrete slabs. Delete if using asphalt primer and mastic for fixed-sleeper system without pads.

        - Vapor Retarder: ASTM D4397, polyethylene sheet not less than 6 mils (0.15 mm) thick.

        - Resilient Wall Base: Molded, vented, rubber or vinyl cove base; 4 by 3 by 48 inches (100 by 75 by 1200 mm); with premolded outside corners.

          - Color: [Black] [Brown].

In "Wood Wall Base" Paragraph below, wood base in first option will not conceal expansion voids at perimeters of installation.

        - Wood Wall Base: [Nominal 1-by-3-inch (25-by-75-mm) wood base] [Built-up wood base as indicated on Drawings] <Insert description> matching species, grade, and cut of wood flooring.

        - Thresholds: [As specified in Section 087100 "Door Hardware."] <Insert requirements.>

If concealed spaces between wood athletic flooring and fire-resistance-rated floor assemblies are fireblocked or filled with noncombustible material, insert requirements here. See "Code Requirements" Article in the Evaluations.

If sound-deadening underlayment is needed, insert requirements here. Sound-deadening underlayment may affect initial performance of wood athletic flooring, but it may have little effect on long-term performance; consult manufacturers for recommendations.

        - Fasteners: Type and size recommended by manufacturer, but not less than those recommended by MFMA for application indicated.

        - Trowelable Leveling and Patching Compound: Latex-modified, hydraulic-cement-based formulation approved by wood athletic flooring manufacturer.

        - Adhesives: Manufacturer's standard for application indicated.

          - <Double click to insert sustainable design text for VOC content of adhesive.>

          - <Double click to insert sustainable design text for adhesives.>

- EXECUTION

      - EXAMINATION

        - Examine substrates, areas, and conditions, with Installer present, for compliance with requirements for maximum moisture content, installation tolerances, and other conditions affecting performance of the Work.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

        - Concrete Slabs: Verify that concrete substrates are dry and moisture-vapor emissions are within acceptable levels according to manufacturer's written instructions.

Retain "Moisture Testing" Subparagraph below; excessive moisture vapor can cause failure of systems installed on slabs-on-grade. ASTM F1869 (anhydrous calcium chloride test) and ASTM F2170 (relative humidity test) both recommend one test per 1000 sq. ft. (304.8 sq. m), but no fewer than three tests per test area.

          - Moisture Testing: Perform tests so that each test area does not exceed [200 sq. ft. (18.6 sq. m)] [1000 sq. ft. (304.8 sq. m)] <Insert area>, and perform no fewer than three tests in each installation area and with test areas evenly spaced in installation areas.

Retain "Anhydrous Calcium Chloride Test" or "Relative Humidity Test" Subparagraph below, or both.

First option in "Anhydrous Calcium Chloride Test" Subparagraph below is based on NWFA recommendations and on floor-covering industry practices for adhered floor coverings to avoid adhesive failures; second option is based on MFMA recommendations. Consider retaining the lower value if assembly components are adhered to slab; consult manufacturers for recommendations.

            - Anhydrous Calcium Chloride Test: ASTM F1869. Proceed with installation only after substrates have maximum moisture-vapor-emission rate of [3 lb of water/1000 sq. ft. (1.36 kg of water/92.9 sq. m)] [4.5 lb of water/1000 sq. ft. (2.04 kg of water/92.9 sq. m)] <Insert emission> in 24 hours.

MFMA recommends a maximum relative humidity level of 80 percent for concrete slabs before installation of non-adhered systems and 75 percent for adhered systems.

            - Relative Humidity Test: Using in situ probes, ASTM F2170. Proceed with installation only after substrates have a maximum [80] [75] <Insert number> percent relative humidity level measurement.

            - Perform additional moisture tests recommended by manufacturer. Proceed with installation only after substrates pass testing.

If products are installed on other substrates, including existing concrete, insert examination requirements here and revise "Preparation" Article.

      - PREPARATION

        - Concrete Slabs:

          - Grind high spots and fill low spots on concrete substrates to produce a maximum 1/8-inch (3-mm) deviation in any direction when checked with a 10-foot (3-m) straight edge.

          - Use trowelable leveling and patching compounds, according to manufacturer's written instructions, to fill cracks, holes, and depressions in substrates.

Retain subparagraph below if products are adhered to concrete substrates.

          - Remove coatings including curing compounds and other substances on substrates that are incompatible with installation adhesives and that contain soap, wax, oil, or silicone; use mechanical methods recommended by manufacturer. Do not use solvents.

        - Broom and vacuum clean substrates to be covered immediately before product installation. After cleaning, examine substrates for moisture, alkaline salts, carbonation, or dust. Proceed with installation only after unsatisfactory conditions have been corrected.

      - INSTALLATION

        - Comply with wood athletic flooring manufacturer's written instructions, but not less than written recommendations of MFMA applicable to flooring type indicated.

Generally, retain "Pattern" Paragraph below. Indicate special patterns on Drawings or by inserts.

        - Pattern: Lay flooring parallel with long dimension of space to be floored unless otherwise indicated.

        - Expansion Spaces: Provide as indicated, but not less than that required by manufacturer's written instructions and MFMA's written recommendations at walls and other obstructions, and at interruptions and terminations of flooring.

Indicate how expansion spaces are covered on Drawings, or insert requirements in subparagraph below.

          - Cover expansion spaces with base molding, trim, and saddles, as indicated on Drawings.

Retain "Vapor Retarder" Paragraph below if required. Delete if using asphalt primer and mastic for fixed-sleeper system without pads.

        - Vapor Retarder: Cover entire slab area beneath wood flooring. Install with joints lapped a minimum of 6 inches (150 mm) and sealed.

Retain "Underlayment" Paragraph below if required.

        - Underlayment: Install perpendicular to direction of flooring, staggering end joints in adjacent rows.

Retain "Sleepers" Paragraph below if required.

        - Sleepers:

Retain first subparagraph below for fixed-sleeper systems without pads. If retaining, delete "Vapor Retarder" Paragraph in this article and in "Accessories" Article. Verify specific system requirements with manufacturer.

          - Prime entire slab beneath wood floor area with asphalt primer at coverage rate recommended by manufacturer.

          - Install sleepers perpendicular to direction of flooring, staggering end joints a minimum of [24 inches (610 mm)] <Insert dimension>.

Generally, retain 12-inch (305-mm) spacing in first subparagraph below if assembly includes subfloor. If subfloor is not required, retain 12-inch (305-mm) spacing for 33/32-inch- (26-mm-) thick flooring and 9-inch (229-mm) spacing for 25/32-inch- (20-mm-) thick flooring. For Third and Better or Third Grade, always space sleepers at 8 inches (203 mm) o.c.

          - Space [at spacing recommended by manufacturer for system components indicated] [12 inches (305 mm) o.c.] [9 inches (229 mm) o.c.] [8 inches (203 mm) o.c.] <Insert requirements>.

Retain first subparagraph below if sleepers are anchored directly to concrete.

          - Shim and level sleepers and install anchors at spacing recommended by manufacturer, but not less than 30 inches (760 mm) o.c.

Retain first subparagraph below for fixed-sleeper systems without pads. If retaining, delete "Vapor Retarder" Paragraph in this article and in "Accessories" Article. Verify specific system requirements with manufacturer.

          - Pour asphalt mastic to 1/8 inch (3 mm) above the level of shims.

Retain subparagraph below if sleepers are anchored through resilient pads.

          - Anchor predrilled sleepers through resilient pads.

Retain "Channels" Paragraph below if required.

        - Channels: Anchor channels to substrate according to manufacturer's written instructions.

          - Install wood strip flooring across channels.

Retain subparagraph below if clips are required.

          - Insert steel clip at each intersection of a flooring strip with a channel.

Retain "Strip Flooring" and "Parquet Flooring" paragraphs below to coordinate with products specified in Part 2.

        - Strip Flooring: Mechanically fasten perpendicular to supports.

        - Parquet Flooring: Adhere to substrates according to manufacturer's written instructions.

        - Installation Tolerances: 1/8 inch in 10 feet (3 mm in 3 m) of variance from level.

If sleeper spaces are fireblocked or filled, insert requirements here. See "Code Requirements" Article in the Evaluations.

      - SANDING AND FINISHING

        - Allow installed flooring to acclimate to ambient conditions before sanding.

        - Follow applicable recommendations in MFMA's "Industry Recommendations for Sanding, Sealing, Court Lining, Finishing, and Resurfacing of Maple Gym Floors."

        - Machine sand with coarse, medium, and fine grades of sandpaper to achieve a level, smooth, uniform surface without ridges or cups. Remove sanding dust by tack or vacuum.

        - Finish: Apply seal and finish coats of finish system according to finish manufacturer's written instructions. Provide no fewer than [four] <Insert number> coats total and no fewer than [two] <Insert number> finish coats.

Retain "Water-Based Finishes" Subparagraph below if required.

          - Water-Based Finishes: Use finishing methods recommended by finish manufacturer to reduce grain raise and sidebonding effect.

          - Game-Line and Marker Paint: Apply game-line and marker paint between final seal coat and first finish coat according to paint manufacturer's written instructions.

            - Mask flooring at game lines and markers, and apply paint to produce lines and markers with sharp edges.

Excessive wear of finishes can result in areas where game-line and marker paint buildup is heavy. Game lines should not overlap. Where game lines cross, minor game line should break at intersection.

            - Where game lines cross, break minor game line at intersection; do not overlap lines.

            - Apply game lines and markers in widths and colors according to [requirements indicated on Drawings] <Insert name of sport association publication>.

            - Apply finish coats after game-line and marker paint is fully cured.

      - PROTECTION

        - Protect wood athletic flooring during remainder of construction period to allow finish to cure and to ensure that flooring and finish are without damage or deterioration at time of Substantial Completion.

          - Do not cover flooring after finishing until finish reaches full cure and not before seven days after applying last finish coat.

          - Do not move heavy and sharp objects directly over flooring. Protect fully cured floor finishes and surfaces with plywood or hardboard panels to prevent damage from storing or moving objects over flooring.

END OF SECTION 096466