Copyright 2019 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 099113 - EXTERIOR PAINTING

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Access Manufacturer-Provided, AIA MasterSpec-Based Sections:

<Double click here for this Section based on specific manufacturer’s products set as Basis-of-Design at ProductMasterSpec.com.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - Primers.

          - Finish coatings.

          - Floor sealers and paints.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Primers in other Sections must be coordinated for compatibility with finish coats specified in this Section. Review other Sections for shop-primed exterior products, and insert references to this Section to establish primer requirements.

          - [Section 051200 "Structural Steel Framing"] [Section 051213 "Architecturally Exposed Structural Steel Framing"] for shop priming of metal substrates.

          - Section 055000 "Metal Fabrications" for shop priming metal fabrications.

          - Section 055116 "Metal Floor Plate Stairs" for shop priming metal floor plate stairs.

          - Section 055119 "Metal Grating Stairs" for shop priming metal grating stairs.

          - Section 055213 "Pipe and Tube Railings" for shop [priming] [painting] pipe and tube railings.

          - [Section 055313 "Bar Gratings"] [Section 055316 "Plank Gratings"] [Section 055319 "Expanded Metal Gratings"] for shop priming metal gratings.

          - Section 099300 "Staining and Transparent Finishing" for surface preparation and application of wood stains and transparent finishes on exterior wood substrates.

          - Section 099600 "High-Performance Coatings" for tilelike coatings.

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

          - Include preparation requirements and application instructions.

          - Indicate VOC content.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for VOC content of paints.>

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples. Delete "Samples" and "Samples for Initial Selection" paragraphs if colors and other characteristics are preselected and specified or scheduled and only verification Samples are required.

        - Samples: For each type of topcoat product.

        - Samples for Initial Selection: For each type of topcoat product.

        - Samples for Verification: For each type of paint system and each color and gloss of topcoat.

Color and gloss of Samples change as they age; seven-day-old Samples appear different from freshly dried Samples.

          - Submit Samples on rigid backing, 8 inches (200 mm) square.

          - Apply coats on Samples in steps to show each coat required for system.

          - Label each coat of each Sample.

          - Label each Sample for location and application area.

        - Product Schedule: Use same designations indicated on Drawings and in the Exterior Painting Schedule to cross-reference paint systems specified in this Section. Include color designations.

      - MAINTENANCE MATERIAL SUBMITTALS

        - Furnish extra materials that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

If necessary, replace percentage in "Paint Products" Subparagraph below with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

          - Paint Products: [5] <Insert number> percent, but not less than [1 gal. (3.8 L)] <Insert value> of each material and color applied.

      - QUALITY ASSURANCE

        - Mockups: Apply mockups of each paint system indicated and each color and finish selected to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for materials and execution.

          - Architect will select one surface to represent surfaces and conditions for application of each paint system.

            - Vertical and Horizontal Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

            - Other Items: Architect will designate items or areas required.

          - Final approval of color selections will be based on mockups.

            - If preliminary color selections are not approved, apply additional mockups of additional colors selected by Architect at no added cost to Owner.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

If necessary, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site in paragraph below.

        - Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

          - Maintain containers in clean condition, free of foreign materials and residue.

          - Remove rags and waste from storage areas daily.

      - FIELD CONDITIONS

        - Apply paints only when temperature of surfaces to be painted and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

        - Do not apply paints in snow, rain, fog, or mist; when relative humidity exceeds 85 percent; at temperatures less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

- PRODUCTS

Manufacturers and products listed in SpecAgent and MasterWorks Paragraph Builder are neither recommended nor endorsed by the AIA or Deltek. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

See the "Writing Guide" Article in the Evaluations before editing Part 2.

      - MANUFACTURERS

        - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Source Limitations: Obtain each paint product from single source from single manufacturer.

      - PAINT PRODUCTS, GENERAL

Generally, retain "Material Compatibility" Paragraph below. Systems could fail if paints used for individual coats are incompatible.

        - Material Compatibility:

          - Provide materials for use within each paint system that are compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer based on testing and field experience.

          - For each coat in a paint system, provide products recommended in writing by topcoat manufacturer for use in paint system and on substrate indicated.

        - <Double click to insert sustainable design text for VOC content of paints.>

        - Colors: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule] <Insert requirements>.

          - [10] [20] [30] <Insert number> percent of surface area will be painted with deep tones.

      - PRIMERS

        - Exterior, Alkali-Resistant, Water-Based Primer: Pigmented, water-based primer formulated for use on alkaline surfaces, such as exterior plaster, vertical concrete, and masonry.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Exterior Wood Preservative: Solvent-based, zinc or copper napthenate, penetrating antifungal treatment for exterior wood.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Exterior, Latex Wood Primer: White, waterborne-emulsion primer formulated for resistance to extractive bleeding, mold, and microbials; for hiding stains; and for use on exterior wood subject to extractive bleeding.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Exterior, Alkyd/Oil Wood Primer: Alkyd/oil-based primer that is resistant to extractive bleeding when applied to wood substrates with less than 15 percent moisture content; formulated for sag, mold, and microbial resistance; for hiding stains; and for use on exterior wood subject to extractive bleeding.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Exterior, Latex Block Filler: Water-based, pigmented, high-solids, emulsion coating formulated to bridge and fill porous surfaces of exterior concrete masonry units in preparation for specified subsequent coatings.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Minimum Solids Content: [Manufacturer's standard percentage] [50 percent] <Insert requirements> solids by volume.

        - Water-Based Bonding Primer: Pigmented, water-based-emulsion primer formulated for exterior use and to promote adhesion of subsequent specified coatings.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Solvent-Based Bonding Primer: Pigmented, solvent-based primer formulated for exterior use and to seal substrates and promote adhesion of specified subsequent coatings.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Water-Based, Rust-Inhibitive Primer: Corrosion-resistant, water-based-emulsion primer formulated for resistance to flash rusting when applied to cleaned, exterior ferrous metals subject to mildly corrosive environments.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>.

        - Zinc-Rich, Inorganic Primer: Corrosion-resistant, inorganic-based, zinc-rich primer formulated for use on prepared steel subject to severe industrial or marine environments.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Surface-Tolerant Metal Primer: Corrosion-resistant, solvent-based metal primer formulated for use on structural steel and metal fabrications that have been minimally prepared.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Quick-Drying, Alkyd Metal Primer: Corrosion-resistant, solvent-based, modified-alkyd primer; lead and chromate free; formulated for quick-drying capabilities and for use on cleaned, exterior steel surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Alkyd Metal Primer: Corrosion-resistant, solvent-based, alkyd primer formulated for use on prepared ferrous metals subject to industrial and light marine environments.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Water-Based, Galvanized-Metal Primer: Corrosion-resistant, pigmented, acrylic primer; formulated for use on cleaned/etched, exterior, galvanized metal to prepare it for subsequent water-based coatings.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>.

        - Epoxy Metal Primer: Corrosion-resistant, solvent-based, two-component epoxy primer formulated for use on prepared, exterior ferrous- and galvanized-metal surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Vinyl Wash Primer: Two-component, vinyl butyral/phosphoric acid, wash primer formulated for use over cleaned metal surfaces and zinc-rich primers as a tie coat for subsequent corrosion-resistant primers or finish coatings.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Quick-Drying Aluminum Primer: Corrosion-resistant, solvent-based, alkyd or modified-alkyd primer formulated for quick-drying capabilities and for use on prepared exterior aluminum.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

      - FINISH COATINGS

        - Exterior Latex Paint, Flat: Water-based, pigmented coating; formulated for alkali, mold, microbial, and water resistance and for use on exterior surfaces, such as portland cement plaster, concrete, and primed wood.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss and Sheen" Subparagraph below corresponds with MPI Gloss Level 1.

          - Gloss and Sheen: [Manufacturer's standard flat finish] [Maximum gloss of 5 units at 60 degrees and maximum sheen of 10 units at 85 degrees when tested in accordance with ASTM D523] <Insert requirements>.

        - Exterior Latex Paint, Low Sheen: Water-based, pigmented coating; formulated for alkali, mold, microbial, and water resistance and for use on exterior surfaces, such as portland cement plaster, concrete, and primed wood.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss and Sheen Level" Subparagraph below corresponds with MPI Gloss Level 3 or Level 4.

          - Gloss and Sheen Level: [Manufacturer's standard low-sheen finish] [Gloss of 10 to 35 units at 60 degrees and minimum sheen of 10 units at 85 degrees when tested in accordance with ASTM D523] <Insert requirements>.

        - Exterior Latex Paint, Semigloss: Water-based, pigmented emulsion coating formulated for alkali, mold, microbial, and water resistance and for use on exterior surfaces, such as masonry, portland cement plaster, and primed wood and metal.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss Level" Subparagraph below corresponds with MPI Gloss Level 5.

          - Gloss Level: [Manufacturer's standard semigloss finish] [Gloss of 35 to 70 units at 60 degrees when tested in accordance with ASTM D523] <Insert requirements>.

        - Exterior Latex Paint, Gloss: Water-based, pigmented, acrylic-copolymer-emulsion coating formulated for alkali, mold, microbial, scrub, blocking (sticking of two painted surfaces), and water resistance and for use on exterior, primed, wood and metal trim, sashes, frames, and doors.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss Level" Subparagraph below corresponds with MPI Gloss Level 6.

          - Gloss Level: [Manufacturer's standard gloss finish] [Gloss of 70 to 85 units at 60 degrees when tested in accordance with ASTM D523] <Insert requirements>.

        - Exterior, High-Build Latex Paint: Water-based, high-build, pigmented, emulsion coating; high-solids content improves filling, uniformity, and film build on concrete masonry surfaces. Formulated for abrasion, mold, microbial, and wind-driven rain resistance and for use on exterior masonry, concrete masonry unit, and concrete surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss and Sheen Level" Subparagraph below corresponds with MPI Gloss Level 1, 2, or 3.

          - Gloss and Sheen Level: [Manufacturer's standard low-gloss finish] [Maximum gloss of 20 units at 60 degrees and maximum sheen of 10 units at 85 degrees when tested in accordance with ASTM D523] <Insert requirements>.

          - Minimum Solids Content: [Manufacturer's standard percentage] [47 percent] <Insert requirements> solids by volume.

        - Textured Latex Coating, Flat: Water-based, pigmented coating that contains sand or other hard aggregate and is formulated for use on exterior masonry, concrete masonry unit, and concrete surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss and Sheen Level" Subparagraph below corresponds with MPI Gloss Level 1.

          - Gloss and Sheen Level: [Manufacturer's standard flat finish] [Maximum gloss of 5 units at 60 degrees and maximum sheen of 10 units at 85 degrees when tested in accordance with ASTM D523] <Insert requirements>.

          - Aggregate Size: [Manufacturer's standard] [Fine] [Medium] [Coarse] <Insert requirements>.

        - Textured Latex Coating, Low Sheen: Water-based, pigmented coating that contains sand or other hard aggregate and is formulated for use on exterior masonry, concrete masonry unit, and concrete surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss and Sheen Level" Subparagraph below corresponds with MPI Gloss Level 2 or Level 3.

          - Gloss and Sheen Level: [Manufacturer's standard low-sheen finish] [Gloss of 5 to 25 units at 60 degrees and sheen of 10 to 35 units at 85 degrees when tested in accordance with ASTM D523] <Insert requirements>.

          - Aggregate Size: [Manufacturer's standard] [Fine] [Medium] [Coarse] <Insert requirements>.

        - Exterior Alkyd Enamel, Flat: Solvent-based, pigmented, alkyd enamel formulated for mold, microbial, and water resistance and for use on exterior, primed, wood and metal surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss and Sheen Level" Subparagraph below corresponds with MPI Gloss Level 1.

          - Gloss and Sheen Level: [Manufacturer's standard flat finish] [Maximum gloss of 5 units at 60 degrees and maximum sheen of 10 units at 85 degrees when tested in accordance with ASTM D523] <Insert requirements>.

        - Exterior Alkyd Enamel, Semigloss: Solvent-based, pigmented, alkyd enamel formulated for mold, microbial, and water resistance and for use on exterior, primed, wood and metal surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss Level" Subparagraph below corresponds with MPI Gloss Level 5.

          - Gloss Level: [Manufacturer's standard semigloss finish] [Gloss of 35 to 70 units at 60 degrees when tested in accordance with ASTM D523] <Insert requirements>.

        - Exterior Alkyd Enamel, Gloss: Solvent-based, pigmented, alkyd enamel formulated for mold, microbial, and water resistance and for use on exterior, primed, wood and metal surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss Level" Subparagraph below corresponds with MPI Gloss Level 6.

          - Gloss Level: [Manufacturer's standard gloss finish] [Gloss of 70 to 85 units at 60 degrees when tested in accordance with ASTM D523] <Insert requirements>.

          - Fineness of Grind: [Manufacturer's standard] [Maximum fineness of pigment dispersion of 6 units when tested in accordance with ASTM D1210] <Insert requirements>.

        - Quick-Drying Alkyd Enamel, Semigloss: Solvent-based, alkyd or modified-alkyd enamel formulated for quick-drying capabilities and for use on exterior, primed, metal and dimensionally stable wood surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss Level" Subparagraph below corresponds with MPI Gloss Level 5.

          - Gloss Level: [Manufacturer's standard semigloss finish] [Gloss of 35 to 70 units at 60 degrees when tested in accordance with ASTM D523] <Insert requirements>.

        - Quick-Drying Alkyd Enamel, Gloss: Solvent-based, alkyd or modified-alkyd enamel formulated for quick-drying capabilities and for use on exterior, primed, metal and dimensionally stable wood surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss Level" Subparagraph below corresponds with MPI Gloss Level 7.

          - Gloss Level: [Manufacturer's standard gloss finish] [Minimum gloss of 85 units at 60 degrees when tested in accordance with ASTM D523] <Insert requirements>.

        - Aluminum Paint: Aliphatic, solvent-based coating consisting of varnish or alkyd binder combined with aluminum pigment that is formulated for use as a stain-blocking coating and sealer on exterior wood, metal, bituminous-coated, and prepared masonry surfaces and to be able to be recoated with conventional alkyd and latex paints.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - High-Build Epoxy Paint, Low Gloss: High-solids, two-component epoxy; formulated for use on exterior concrete, masonry, and primed-metal surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss and Sheen Level" Subparagraph below corresponds with MPI Gloss Level 1, 2, or 3.

          - Gloss and Sheen Level: [Manufacturer's standard low-gloss finish] [Maximum gloss of 25 units at 60 degrees and sheen of 10 to 35 units at 85 degrees when tested in accordance with ASTM D523] <Insert requirements>.

        - Exterior, Water-Based, Light Industrial Coating, Low Sheen: Corrosion-resistant, water-based, pigmented, emulsion coating formulated for resistance to blocking (sticking of two painted surfaces), water, alkalis, moderate abrasion, and mild chemical exposure and for use on exterior, primed, wood and metal surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss and Sheen" Subparagraph below corresponds with MPI Gloss Level 3.

          - Gloss and Sheen Level: [Manufacturer's standard low-sheen finish] [Gloss of 10 to 25 units at 60 degrees and sheen of 10 to 35 units at 85 degrees when tested in accordance with ASTM D523] <Insert requirements>.

        - Exterior, Water-Based, Light Industrial Coating, Semigloss: Corrosion-resistant, water-based, pigmented, emulsion coating formulated for resistance to blocking (sticking of two painted surfaces), water, alkalis, moderate abrasion, and mild chemical exposure and for use on exterior, primed, wood and metal surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss Level" Subparagraph below corresponds with MPI Gloss Level 5.

          - Gloss Level: [Manufacturer's standard semigloss finish] [Gloss of 35 to 70 units at 60 degrees when tested in accordance with ASTM D523] <Insert requirements>.

        - Exterior, Water-Based, Light Industrial Coating, Gloss: Corrosion-resistant, water-based, pigmented, emulsion coating formulated for resistance to blocking (sticking of two painted surfaces), water, alkalis, moderate abrasion, and mild chemical exposure and for use on exterior, primed, wood and metal surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss Level" Subparagraph below corresponds with MPI Gloss Level 6.

          - Gloss Level: [Manufacturer's standard gloss finish] [Gloss of 70 to 85 units at 60 degrees when tested in accordance with ASTM D523] <Insert requirements>.

      - FLOOR SEALERS AND PAINTS

        - Latex Floor Paint, Low Gloss: Water-based, pigmented coating formulated to hide stains, for alkali and incidental water resistance, and for use on exterior, concrete and primed-wood surfaces subject to low to medium foot traffic.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss and Sheen Level" Subparagraph below corresponds with MPI Gloss Level 1, 2, or 3.

          - Gloss and Sheen Level: [Manufacturer's standard low-gloss finish] [Maximum gloss of 25 units at 60 degrees and sheen of 10 to 35 units at 85 degrees when tested in accordance with ASTM D523] <Insert requirements>.

Retain "Slip-Resistant Aggregate" Subparagraph below if required.

          - Slip-Resistant Aggregate: [Manufacturer's standard additive] <Insert requirements>.

        - Latex Deck Coating: Water-based, high-solids, acrylic-emulsion coating; formulated for use on exterior, concrete and wood-board traffic surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Revise "Gloss Level" Subparagraph below to suit Project. Gloss levels are typically indicated by manufacturers' product designations and range from flat to gloss.

          - Gloss Level: [Manufacturer's standard] <Insert requirements>.

          - Minimum Solids Content: [Manufacturer's standard percentage] [25 percent] <Insert requirements> solids by volume.

          - Surface Texture: [Smooth] [Slip resistant].

        - Alkyd Floor Enamel, Gloss: Solvent-based, alkyd enamel; self-priming where applied to bare wood; formulated to hide stains, for durability, for microbial and abrasion resistance, and for use on exterior, wood-board, traffic surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Second option in "Gloss Level" Subparagraph below corresponds with MPI Gloss Level 6.

          - Gloss Level: [Manufacturer's standard gloss finish] [Gloss of 70 to 85 units at 60 degrees when tested in accordance with ASTM D523] <Insert requirements>.

Retain "Slip-Resistant Aggregate" Subparagraph below if required.

          - Slip-Resistant Aggregate: [Manufacturer's standard additive] <Insert requirements>.

        - Water-Based, Concrete-Floor Sealer: Clear, water-based, acrylic-copolymer-emulsion sealer formulated for oil, gasoline, alkali, and water resistance and for use on exterior, concrete traffic surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

        - Solvent-Based, Concrete-Floor Sealer: Clear, acrylic, solvent-based sealer formulated for oil, gasoline, alkali, and water resistance and for use on exterior, concrete traffic surfaces.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

        - Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows:

Percentages in "Concrete," "Fiber-Cement Board," "Masonry (Clay and Concrete Masonry Units)," "Wood," "Portland Cement Plaster," and Gypsum Board" subparagraphs below are based on MPI recommendations.

          - Concrete: 12 percent.

          - Fiber-Cement Board: 12 percent.

          - Masonry (Clay and Concrete Masonry Units): 12 percent.

          - Wood: 15 percent.

          - Portland Cement Plaster: 12 percent.

          - Gypsum Board: 12 percent.

        - Portland Cement Plaster Substrates: Verify that plaster is fully cured.

        - Exterior Gypsum Board Substrates: Verify that finishing compound is dry and sanded smooth.

        - Verify suitability of substrates, including surface conditions and compatibility, with finishes and primers.

        - Proceed with coating application only after unsatisfactory conditions have been corrected.

          - Application of coating indicates acceptance of surfaces and conditions.

      - PREPARATION

For renovation or maintenance projects where repainting is required, consult manufacturers for recommendations and revise first paragraph below and paint systems specified in the Exterior Painting Schedule.

        - Comply with manufacturer's written instructions applicable to substrates and paint systems indicated.

        - Remove hardware, covers, plates, and similar items already in place that are removable and are not to be painted. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

          - After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection.

        - Clean substrates of substances that could impair bond of paints, including dust, dirt, oil, grease, and incompatible paints and encapsulants.

Coordination of shop-applied prime coats with topcoats is critical.

          - Remove incompatible primers and reprime substrate with compatible primers or apply tie coat as required to produce paint systems specified in this Section.

        - Concrete Substrates: Remove release agents, curing compounds, efflorescence, and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces to be painted exceeds that permitted in manufacturer's written instructions.

        - Masonry Substrates: Remove efflorescence and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces or mortar joints exceeds that permitted in manufacturer's written instructions.

Retain "Steel Substrates" Paragraph below if steel is not shop primed or if shop primer is removed in the field.

        - Steel Substrates: Remove rust, loose mill scale, and shop primer if any. Clean using methods recommended in writing by paint manufacturer[.][ but not less than the following:]

Usually, retain one of first two subparagraphs below. SSPC-SP 2 and SSPC-SP 3 remove loose rust, mill scale, and paint. SSPC-SP 2 is minimum surface preparation accepted by AISC for painted steel.

          - SSPC-SP 2.

          - SSPC-SP 3.

SSPC-SP 7/NACE No. 4 permits tight residues of rust, mill scale, and coatings to remain. Blast cleaning methods specified in SSPC-SP 6/NACE No. 3 may be impractical for use at Project site and may not be allowed by authorities having jurisdiction.

          - SSPC-SP 7/NACE No. 4.

SSPC-SP 11 requires complete removal of rust, mill scale, and paint by power tools. SSPC-SP 11 uses nonabrasive methods and is more thorough than SSPC-SP 2, SSPC-SP 3, and SSPC-SP 7/NACE No. 4.

          - SSPC-SP 11.

Retain "Shop-Primed Steel Substrates" Paragraph below if primers are shop applied and are not removed in the field.

        - Shop-Primed Steel Substrates: Clean field welds, bolted connections, and areas where shop paint is abraded. Paint exposed areas with the same material as used for shop priming to comply with SSPC-PA 1 for touching up shop-primed surfaces.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

        - Galvanized-Metal Substrates: Remove grease and oil residue from galvanized sheet metal by mechanical methods to produce clean, lightly etched surfaces that promote adhesion of subsequently applied paints.

        - Aluminum Substrates: Remove loose surface oxidation.

        - Wood Substrates:

If necessary, insert requirements for power or pressure washing.

          - Scrape and clean knots. Before applying primer, apply coat of knot sealer recommended in writing by topcoat manufacturer for exterior use in paint system indicated.

          - Sand surfaces that will be exposed to view, and remove sanding dust.

          - Prime edges, ends, faces, undersides, and backsides of wood.

          - After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dried.

        - Plastic Trim Fabrication Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

      - INSTALLATION

        - Apply paints in accordance with manufacturer's written instructions.

If Project requires restricted application method (for example, using only spray or rollers), revise first subparagraph below accordingly.

          - Use applicators and techniques suited for paint and substrate indicated.

          - Paint surfaces behind movable items same as similar exposed surfaces. Before final installation, paint surfaces behind permanently fixed items with prime coat only.

          - Paint [both sides] [exterior side] and edges of exterior doors and entire exposed surface of exterior door frames.

Retain first subparagraph below if required for steel windows.

          - Paint entire exposed surface of window frames and sashes.

          - Do not paint over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

          - Primers specified in the Exterior Painting Schedule may be omitted on items that are factory primed or factory finished if compatible with intermediate and topcoat coatings and acceptable to intermediate and topcoat paint manufacturers.

If tinting is not required, delete first paragraph below. Different tints show through as topcoat erodes.

        - Tint undercoats same color as topcoat, but tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of same material are to be applied. Provide sufficient difference in shade of undercoats to distinguish each separate coat.

        - If undercoats or other conditions show through topcoat, apply additional coats until cured film has a uniform paint finish, color, and appearance.

        - Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections. Cut in sharp lines and color breaks.

        - Painting Fire Suppression, Plumbing, HVAC, Electrical, Communication, and Electronic Safety and Security Work:

First subparagraph below is for use where items are to be painted to blend in with surroundings; revise if painting is required to protect items from corrosion. Consider indicating painted items on Drawings or delineating extent of "exposed to view" for complex situations.

          - Paint the following work where exposed to view:

List below contains items that are often field painted, plus others that are often not. Revise list to suit Project.

            - Equipment, including panelboards[ and switch gear].

            - Uninsulated metal piping.

            - Uninsulated plastic piping.

            - Pipe hangers and supports.

            - Metal conduit.

            - Plastic conduit.

            - Tanks that do not have factory-applied final finishes.

            - <Insert requirements>.

      - FIELD QUALITY CONTROL

        - Dry Film Thickness Testing: Owner may engage the services of a qualified testing and inspecting agency to inspect and test paint for dry film thickness.

          - Contractor shall touch up and restore painted surfaces damaged by testing.

          - If test results show that dry film thickness of applied paint does not comply with paint manufacturer's written instructions, Contractor shall pay for testing and apply additional coats as needed to provide dry film thickness that complies with paint manufacturer's written instructions.

      - CLEANING AND PROTECTION

        - At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

          - Do not clean equipment with free-draining water and prevent solvents, thinners, cleaners, and other contaminants from entering into waterways, sanitary and storm drain systems, and ground.

          - Dispose of contaminants in accordance with requirements of authorities having jurisdiction.

          - Allow empty paint cans to dry before disposal.

Retain subparagraph below if paint recycling or collection facilities are available in vicinity of Project.

          - Collect waste paint by type and deliver to recycling or collection facility.

        - After completing paint application, clean spattered surfaces. Remove spattered paints by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

        - Protect work of other trades against damage from paint application. Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

        - At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

      - EXTERIOR PAINTING SCHEDULE

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each ceiling.

Retain "Intermediate Coat" subparagraphs for high-quality systems; delete if not required.

        - Concrete Substrates, Nontraffic Surfaces:

          - Latex System <Insert drawing designation>:

            - Prime Coat: [Exterior, alkali-resistant, water-based primer] [Matching topcoat].

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex over Latex Aggregate System <Insert drawing designation>:

            - Prime Coat: Textured latex coating, flat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex Aggregate System <Insert drawing designation>:

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Textured latex coating, [flat] [low sheen].

          - High-Build Latex System <Insert drawing designation>: Dry film thickness of not less than 10 mils (0.25 mm).

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Exterior, high-build latex paint.

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: Exterior, alkali-resistant, water-based primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

        - Concrete Substrates, Traffic Surfaces:

          - Latex Floor Paint System <Insert drawing designation>:

            - Prime Coat: Matching topcoat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Latex floor paint, low gloss.

          - Latex Deck Coating System <Insert drawing designation>:

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Latex deck coating.

          - Alkyd Floor Enamel System <Insert drawing designation>:

            - Prime Coat: Matching topcoat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Alkyd floor enamel, gloss.

          - Clear, Water-Based Sealer System <Insert drawing designation>:

            - Prime Coat: Matching topcoat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Water-based, concrete-floor sealer.

          - Clear, Solvent-Based Sealer System <Insert drawing designation>:

            - Prime Coat: Matching topcoat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Solvent-based, concrete-floor sealer.

        - Clay Masonry Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: Exterior, alkali-resistant, water-based primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex Aggregate System <Insert drawing designation>:

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Textured latex coating, [flat] [low sheen].

          - High-Build Latex System <Insert drawing designation>: Dry film thickness of not less than 10 mils (0.25 mm).

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Exterior, high-build latex paint.

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: Exterior, alkali-resistant, water-based primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

        - Concrete Masonry Unit Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: Exterior, latex block filler.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex over Alkali-Resistant Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, alkali-resistant, water-based primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex Aggregate System <Insert drawing designation>:

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Textured latex coating, [flat] [low sheen].

          - High-Build Latex System <Insert drawing designation>: Dry film thickness of not less than 10 mils (0.25 mm).

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Exterior, high-build latex paint.

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: Exterior, latex block filler.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

        - Steel and Iron Substrates:

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: [Zinc-rich, inorganic primer] [Alkyd metal primer] [Epoxy metal primer] [Shop primer specified in Section in which substrate is specified].

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

          - Water-Based, Light Industrial Coating over Epoxy System <Insert drawing designation>:

            - Prime Coat: Epoxy metal primer.

            - Intermediate Coat: High-build epoxy paint, low gloss.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: [Alkyd metal primer] [Surface-tolerant metal primer] [Shop primer specified in Section in which substrate is specified].

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

          - Quick-Drying Enamel System <Insert drawing designation>:

            - Prime Coat: Quick-drying, alkyd metal primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Quick-drying alkyd enamel, [semigloss] [gloss].

          - Aluminum Paint System <Insert drawing designation>:

            - Prime Coat: [Alkyd metal primer] [Shop primer specified in Section in which substrate is specified].

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Aluminum paint.

        - Galvanized-Metal Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: Water-based, galvanized-metal primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: [Water-based, galvanized-metal primer] [Epoxy metal primer].

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

        - Aluminum Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: Quick-drying aluminum primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: Quick-drying aluminum primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Pretreatment Coat: Vinyl wash primer.

            - Prime Coat: Quick-drying aluminum primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Copper Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: Quick-drying aluminum primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: Quick-drying aluminum primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Pretreatment Coat: [Vinyl wash] [Quick-drying aluminum] primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Stainless Steel Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: Solvent-based bonding primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: Quick-drying aluminum primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Vinyl wash primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Glue-Laminated Wood Substrates:

          - Latex over Latex Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, latex wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex over Alkyd/Oil Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Exposed Wood-Framing Substrates:

          - Latex over Latex Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, latex wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex over Alkyd Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Dressed-Lumber Substrates: [Trim] [Architectural woodwork] [Doors] [Windows] [Board siding] [Railings] [Fences] <Insert requirements>.

          - Latex over Latex Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, latex wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex over Alkyd Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Wood Shingle and Shake Siding Substrates:

          - Latex over Latex Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, latex wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex over Alkyd Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Wood-Based Panel Substrates:

          - Latex over Latex Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, latex wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex over Alkyd Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Wood-Board, Traffic-Surface Substrates:

          - Latex Floor Paint over Latex Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, latex wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Latex floor paint, low gloss.

          - Latex Floor Paint over Alkyd Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, alkyd/oil wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Latex floor paint, low gloss.

          - Latex Deck Coating System <Insert drawing designation>: For plywood decks.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommending in writing by topcoat manufacturer.

            - Topcoat: Latex deck coating.

          - Alkyd Floor Enamel System <Insert drawing designation>:

            - Prime Coat: Matching topcoat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Alkyd floor enamel, gloss.

          - Alkyd Floor Enamel over Wood Preservative System <Insert drawing designation>:

            - Preservative Coat: Exterior wood preservative.

            - Prime Coat: Matching topcoat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Alkyd floor enamel, gloss.

        - Cementitious Composition Board Substrates: [Siding] [Trim] [Panels] <Insert requirements>.

          - Latex System <Insert drawing designation>:

            - Prime Coat: Matching topcoat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex over Alkyd Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, alkali-resistant, water-based primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Alkyd System over Latex Wood Primer System <Insert drawing designation>:

            - Prime Coat: Exterior, latex wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

          - High-Build Latex System <Insert drawing designation>: Dry film thickness of not less than 10 mils (0.25 mm).

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Exterior, high-build latex paint.

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: Exterior, alkali-resistant, water-based primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Exterior, latex wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Fiberglass Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: Solvent-based bonding primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: Solvent-based bonding primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Solvent-based bonding primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Plastic-Trim-Fabrication Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: [Solvent] [Water]-based bonding primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: [Solvent] [Water]-based bonding primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Solvent-based bonding primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Portland Cement Plaster Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: [Matching topcoat] [Exterior, alkali-resistant, water-based primer].

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - High-Build Latex System <Insert drawing designation>: Dry film thickness of not less than 10 mils (0.25 mm).

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Exterior, high-build latex paint.

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: Exterior, alkali-resistant, water-based primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

        - Exterior Gypsum Board Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: Exterior, latex wood primer, reduced in accordance with manufacturer's written instructions for substrate and topcoat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex Aggregate System <Insert drawing designation>:

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Textured latex coating, [flat] [low sheen].

          - High-Build Latex System <Insert drawing designation>: Dry film thickness of not less than 10 mils (0.25 mm).

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Exterior, high-build latex paint.

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Exterior, latex wood primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

        - Exterior Canvas Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: Matching topcoat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Water-Based, Light Industrial Coating System <Insert drawing designation>:

            - Prime Coat: Matching topcoat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Exterior latex paint, flat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

          - Aluminum Paint System <Insert drawing designation>:

            - Prime Coat: Exterior latex paint, flat.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Aluminum paint.

        - Bituminous-Coated Substrates:

          - Latex System <Insert drawing designation>:

            - Prime Coat: Water-based, rust-inhibitive primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

          - Latex Aggregate System <Insert drawing designation>:

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Textured latex coating, [flat] [low sheen].

          - Alkyd System <Insert drawing designation>:

            - Prime Coat: Water-based, rust-inhibitive primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Exterior alkyd enamel, [flat] [semigloss] [gloss].

          - Aluminum Paint System <Insert drawing designation>:

            - Prime Coat: Water-based, rust-inhibitive primer.

            - Intermediate Coat: Matching topcoat.

            - Topcoat: Aluminum paint.

END OF SECTION 099113