Copyright 2019 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 099114 - EXTERIOR PAINTING (MPI STANDARDS)

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Access Manufacturer-Provided, AIA MasterSpec-Based Sections:

<Double click here for this Section based on specific manufacturer’s products set as Basis-of-Design at ProductMasterSpec.com.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - Surface preparation and application of paint systems on[ exterior substrates.][ the following exterior substrates:]

            - Concrete.

            - Fiber-cement board.

            - Clay masonry.

            - Concrete masonry units (CMUs).

            - Steel and iron.

            - Galvanized metal.

            - Aluminum (not anodized or otherwise coated).

            - Copper.

            - Stainless steel.

            - Wood.

            - Fiberglass.

            - Plastic.

            - Portland cement plaster (stucco).

            - Gypsum board.

            - Cotton or canvas insulation covering.

            - Bituminous-coated surfaces.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Primers in other Sections must be coordinated for compatibility with finish coats specified in this Section. Review other Sections for shop-primed exterior products, and insert references to this Section to establish primer requirements.

          - [Section 051200 "Structural Steel Framing"] [Section 051213 "Architecturally Exposed Structural Steel Framing"] for shop priming of metal substrates.

          - Section 055000 "Metal Fabrications" for shop priming metal fabrications.

          - Section 055116 "Metal Floor Plate Stairs" for shop priming metal floor plate stairs.

          - Section 055119 "Metal Grating Stairs" for shop priming metal grating stairs.

          - Section 055213 "Pipe and Tube Railings" for shop [priming] [painting] pipe and tube railings.

          - [Section 055313 "Bar Gratings"] [Section 055316 "Plank Gratings"] [Section 055319 "Expanded Metal Gratings"] for shop priming metal gratings.

          - Section 099300 "Staining and Transparent Finishing" for surface preparation and application of wood stains and transparent finishes on exterior wood substrates.

          - [Section 099600 "High-Performance Coatings"] [099611 "High-Performance Coatings (Proprietary Specification)"] for tilelike coatings.

      - DEFINITIONS

Retain this article if paints are specified by manufacturers' trade names rather than by MPI paint numbers. Definitions of MPI Gloss Levels below are from "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual").

Retain terms that remain after this Section has been edited for a project.

        - MPI Gloss Level 1: Not more than five units at 60 degrees and 10 units at 85 degrees, according to ASTM D523.

        - MPI Gloss Level 3: 10 to 25 units at 60 degrees and 10 to 35 units at 85 degrees, according to ASTM D523.

        - MPI Gloss Level 4: 20 to 35 units at 60 degrees and not less than 35 units at 85 degrees, according to ASTM D523.

        - MPI Gloss Level 5: 35 to 70 units at 60 degrees, according to ASTM D523.

        - MPI Gloss Level 6: 70 to 85 units at 60 degrees, according to ASTM D523.

        - MPI Gloss Level 7: More than 85 units at 60 degrees, according to ASTM D523.

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

          - Include preparation requirements and application instructions.

See "Writing Guide" Article in the Evaluations for discussion of first subparagraph below.

          - Include printout of current "MPI Approved Products List" for each product category specified, with the proposed product highlighted.

          - Indicate VOC content.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for VOC content of paints.>

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples. Delete "Samples" and "Samples for Initial Selection" paragraphs if colors and other characteristics are preselected and specified or scheduled and only verification Samples are required.

        - Samples: For each type of topcoat product.

        - Samples for Initial Selection: For each type of topcoat product.

        - Samples for Verification: For each type of paint system and each color and gloss of topcoat.

Color and gloss of Samples change as they age; seven-day old Samples appear different from freshly dried Samples.

          - Submit Samples on rigid backing, 8 inches (200 mm) square.

          - Apply coats on Samples in steps to show each coat required for system.

          - Label each coat of each Sample.

          - Label each Sample for location and application area.

        - Product List: Cross-reference to paint system and locations of application areas. Use same designations indicated on Drawings and in the Exterior Painting Schedule to cross-reference paint systems specified in this Section. Include color designations.

      - MAINTENANCE MATERIAL SUBMITTALS

        - Furnish extra materials that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

If necessary, replace percentage in "Paint" Subparagraph below with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

          - Paint: [5] <Insert number> percent, but not less than [1 gal. (3.8 L)] <Insert value> of each material and color applied.

      - QUALITY ASSURANCE

        - Mockups: Apply mockups of each paint system indicated and each color and finish selected to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for materials and execution.

          - Architect will select one surface to represent surfaces and conditions for application of each paint system.

            - Vertical and Horizontal Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

            - Other Items: Architect will designate items or areas required.

          - Final approval of color selections will be based on mockups.

            - If preliminary color selections are not approved, apply additional mockups of additional colors selected by Architect at no added cost to Owner.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

If necessary, in paragraph below, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site.

        - Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

          - Maintain containers in clean condition, free of foreign materials and residue.

          - Remove rags and waste from storage areas daily.

      - FIELD CONDITIONS

        - Apply paints only when temperature of surfaces to be painted and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

        - Do not apply paints in snow, rain, fog, or mist; when relative humidity exceeds 85 percent; at temperatures less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

- PRODUCTS

Manufacturers and products listed in SpecAgent and MasterWorks Paragraph Builder are neither recommended nor endorsed by the AIA or Deltek. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - MANUFACTURERS

        - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Retain "Products" Paragraph below and insert lists of manufacturers and products in the Exterior Painting Schedule to require specific products or a comparable product from other manufacturers.

See lists of products currently approved by MPI in its "MPI Approved Products List." See "Writing Guide" Article in the Evaluations for further discussion.

        - Products: Subject to compliance with requirements, [provide product] [provide one of the products] [available products that may be incorporated into the Work include, but are not limited to products] listed in the Exterior Painting Schedule for the paint category indicated.

        - Source Limitations: Obtain paint from single source from single manufacturer.

      - PAINT PRODUCTS

        - MPI Standards: Provide products complying with MPI standards indicated and listed in its "MPI Approved Products List."

Generally, retain "Material Compatibility" Paragraph below.

        - Material Compatibility:

Systems could fail if paints used for individual coats are incompatible. MPI's paint systems match primers and topcoats and take compatibility into consideration.

          - Provide materials for use within each paint system that are compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

          - For each coat in a paint system, provide products recommended in writing by topcoat manufacturers for use in paint system and on substrate indicated.

        - <Double click to insert sustainable design text for VOC content of paints.>

        - Colors: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule] <Insert requirements>.

          - [10] [20] [30] <Insert number> percent of surface area will be painted with deep tones.

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

        - Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows:

Percentages in "Concrete," "Fiber-Cement Board," "Masonry (Clay and CMUs)," "Wood," "Portland Cement Plaster," and Gypsum Board" subparagraphs below are based on "MPI Manual."

          - Concrete: 12 percent.

          - Fiber-Cement Board: 12 percent.

          - Masonry (Clay and CMUs): 12 percent.

          - Wood: 15 percent.

          - Portland Cement Plaster: 12 percent.

          - Gypsum Board: 12 percent.

        - Portland Cement Plaster Substrates: Verify that plaster is fully cured.

        - Exterior Gypsum Board Substrates: Verify that finishing compound is sanded smooth.

        - Verify suitability of substrates, including surface conditions and compatibility, with existing finishes and primers.

        - Proceed with coating application only after unsatisfactory conditions have been corrected.

          - Application of coating indicates acceptance of surfaces and conditions.

      - PREPARATION

For renovation projects, consult "MPI Maintenance Repainting Manual" and revise first paragraph below and paint systems specified in the Exterior Painting Schedule.

        - Comply with manufacturer's written instructions and recommendations in "MPI Manual" applicable to substrates and paint systems indicated.

        - Remove hardware, covers, plates, and similar items already in place that are removable and are not to be painted. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

          - After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection.

        - Clean substrates of substances that could impair bond of paints, including dust, dirt, oil, grease, and incompatible paints and encapsulants.

Coordination of shop-applied prime coats with topcoats is critical.

          - Remove incompatible primers and reprime substrate with compatible primers or apply tie coat as required to produce paint systems indicated.

        - Concrete Substrates: Remove release agents, curing compounds, efflorescence, and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces to be painted exceeds that permitted in manufacturer's written instructions.

        - Masonry Substrates: Remove efflorescence and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces or mortar joints exceeds that permitted in manufacturer's written instructions.

Retain "Steel Substrates" Paragraph below if steel is not shop primed or if shop primer is removed in the field.

        - Steel Substrates: Remove rust, loose mill scale, and shop primer if any. Clean using methods recommended in writing by paint manufacturer[.][ but not less than the following:]

Usually, retain one of first two subparagraphs below. SSPC-SP 2 and SSPC-SP 3 remove loose rust, mill scale, and paint. SSPC-SP 2 is minimum surface preparation accepted by AISC for painted steel.

          - SSPC-SP 2.

          - SSPC-SP 3.

SSPC-SP 7/NACE No. 4 permits tight residues of rust, mill scale, and coatings to remain. Blast cleaning methods specified in SSPC-SP 6/NACE No. 3 may be impractical for use at Project site and may not be allowed by authorities having jurisdiction.

          - SSPC-SP 7/NACE No. 4.

SSPC-SP 11 requires complete removal of rust, mill scale, and paint by power tools. SSPC-SP 11 uses nonabrasive methods and is more thorough than SSPC-SP 2, SSPC-SP 3, and SSPC-SP 7/NACE No. 4.

          - SSPC-SP 11.

Retain "Shop-Primed Steel Substrates" Paragraph below if primers are shop applied and are not removed in the field.

        - Shop-Primed Steel Substrates: Clean field welds, bolted connections, and areas where shop paint is abraded. Paint exposed areas with the same material as used for shop priming to comply with SSPC-PA 1 for touching up shop-primed surfaces.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

        - Galvanized-Metal Substrates: Remove grease and oil residue from galvanized sheet metal by mechanical methods to produce clean, lightly etched surfaces that promote adhesion of subsequently applied paints.

        - Aluminum Substrates: Remove loose surface oxidation.

        - Wood Substrates:

If necessary, insert requirements for power or pressure washing.

          - Scrape and clean knots. Before applying primer, apply coat of knot sealer recommended in writing by topcoat manufacturer for exterior use in paint system indicated.

          - Sand surfaces that will be exposed to view, and remove sanding dust.

          - Prime edges, ends, faces, undersides, and backsides of wood.

          - After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dried.

        - Plastic Trim Fabrication Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

      - INSTALLATION

        - Apply paints in accordance with manufacturer's written instructions and recommendations in "MPI Manual."

If Project requires restricted application method (e.g., using only spray or rollers), revise first subparagraph below accordingly.

          - Use applicators and techniques suited for paint and substrate indicated.

          - Paint surfaces behind movable items same as similar exposed surfaces. Before final installation, paint surfaces behind permanently fixed items with prime coat only.

          - Paint [both sides] [exterior side] and edges of exterior doors and entire exposed surface of exterior door frames.

Retain first subparagraph below if required for steel windows.

          - Paint entire exposed surface of window frames and sashes.

          - Do not paint over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

          - Primers specified in the Exterior Painting Schedule may be omitted on items that are factory primed or factory finished if compatible with intermediate and topcoat coatings and acceptable to intermediate and topcoat paint manufacturers.

If tinting is not required, delete first paragraph below. Different tints show through as topcoat erodes.

        - Tint undercoats same color as topcoat, but tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of same material are to be applied. Provide sufficient difference in shade of undercoats to distinguish each separate coat.

        - If undercoats or other conditions show through topcoat, apply additional coats until cured film has a uniform paint finish, color, and appearance.

        - Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections. Cut in sharp lines and color breaks.

        - Painting Fire Suppression, Plumbing, HVAC, Electrical, Communication, and Electronic Safety and Security Work:

First subparagraph below is for use where items are to be painted to blend in with surroundings; revise if painting is required to protect items from corrosion. Consider indicating painted items on Drawings or delineating extent of "exposed to view" for complex situations.

          - Paint the following work where exposed to view:

List below contains items that are often field painted, plus others that are often not. Revise list to suit Project.

            - Equipment, including panelboards[ and switch gear].

            - Uninsulated metal piping.

            - Uninsulated plastic piping.

            - Pipe hangers and supports.

            - Metal conduit.

            - Plastic conduit.

            - Tanks that do not have factory-applied final finishes.

            - <Insert requirements>.

      - FIELD QUALITY CONTROL

        - Dry Film Thickness Testing: Owner may engage the services of a qualified testing and inspecting agency to inspect and test paint for dry film thickness.

          - Contractor shall touch up and restore painted surfaces damaged by testing.

          - If test results show that dry film thickness of applied paint does not comply with paint manufacturer's written instructions, Contractor shall pay for testing and apply additional coats as needed to provide dry film thickness that complies with paint manufacturer's written instructions.

      - CLEANING AND PROTECTION

        - At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

          - Do not clean equipment with free-draining water and prevent solvents, thinners, cleaners, and other contaminants from entering into waterways, sanitary and storm drain systems, and ground.

          - Dispose of contaminants in accordance with requirements of authorities having jurisdiction.

          - Allow empty paint cans to dry before disposal.

Retain subparagraph below if paint recycling or collection facilities are available in vicinity of Project.

          - Collect waste paint by type and deliver to recycling or collection facility.

        - After completing paint application, clean spattered surfaces. Remove spattered paints by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

        - Protect work of other trades against damage from paint application. Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

        - At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

      - EXTERIOR PAINTING SCHEDULE

Paint systems in this article are based on "MPI Manual." For renovation projects, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

        - Concrete Substrates, Nontraffic Surfaces:

          - Latex System [MPI EXT 3.1A] [MPI EXT 3.1K]:

Retain "Prime Coat" or "Prime Coat, Latex" Subparagraph below. First corresponds to MPI EXT 3.1A; second corresponds to MPI EXT 3.1K.

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat, Latex: Exterior, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Latex Aggregate System[ MPI EXT 3.1B]:

            - Prime Coat: Textured coating, latex, flat[, MPI #42].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex Aggregate System[ MPI EXT 3.1N]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

Retain "Nonflat Topcoat" or "Flat Topcoat" Subparagraph below.

            - Nonflat Topcoat: Textured coating, latex, nonflat[, MPI #41].

              - <Insert manufacturer's name; product name or designation>.

            - Flat Topcoat: Textured coating, latex, flat[, MPI #42].

              - <Insert manufacturer's name; product name or designation>.

          - High-Build Latex System[ MPI EXT 3.1L]: Dry film thickness of not less than 10 mils (0.25 mm).

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Latex, exterior, high build[, MPI #40].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 3.1C]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

        - Concrete Substrates, Traffic Surfaces:

          - Latex Floor Paint System[ MPI EXT 3.2A]:

            - Prime Coat: Floor paint, latex, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Floor paint, latex, matching topcoat.

            - Topcoat: Floor paint, latex, low gloss (maximum MPI Gloss Level 3)[, MPI #60].

              - <Insert manufacturer's name; product name or designation>.

          - Latex Deck Coating System[ MPI EXT 3.2B]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Deck coating, latex[, MPI #127].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Floor Enamel System[ MPI EXT 3.2D]:

            - Prime Coat: Floor enamel, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Floor enamel, matching topcoat.

            - Topcoat: Floor enamel, alkyd, gloss (MPI Gloss Level 6)[, MPI #27].

              - <Insert manufacturer's name; product name or designation>.

            - Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

          - Clear Water-Based Sealer System[ MPI EXT 3.2H]:

            - Prime Coat: Sealer, water based, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Sealer, water based, matching topcoat.

            - Topcoat: Sealer, water based, for concrete floors[, MPI #99].

              - <Insert manufacturer's name; product name or designation>.

          - Clear Sealer System[ MPI EXT 3.2G]:

            - Prime Coat: Sealer, solvent based, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Sealer, solvent based, matching topcoat.

            - Topcoat: Sealer, solvent based, for concrete floors[, MPI #104].

              - <Insert manufacturer's name; product name or designation>.

        - Cement Board Substrates:

          - Latex System [MPI EXT 3.3A] [MPI EXT 3.3J]:

Retain "Latex Prime Coat" or "Alkali-Resistant Prime Coat" Subparagraph below. First corresponds to MPI EXT 3.3A; second corresponds to MPI EXT 3.3J.

            - Latex Prime Coat: Exterior, matching topcoat.

            - Alkali-Resistant Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex Aggregate System[ MPI EXT 3.3G]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

Retain "Nonflat Topcoat" or "Flat Topcoat" Subparagraph below.

            - Nonflat Topcoat: Textured coating, latex, nonflat[, MPI #41].

              - <Insert manufacturer's name; product name or designation>.

            - Flat Topcoat: Textured coating, latex, flat[, MPI #42].

              - <Insert manufacturer's name; product name or designation>.

          - High-Build Latex System[ MPI EXT 3.3H]: Dry film thickness of not less than 10 mils (0.25 mm).

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Latex, exterior, high build[, MPI #40].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 3.3C]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," "or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 3.3B]:

            - Prime Coat: Primer, latex for exterior wood[, MPI #6].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Clay Masonry Substrates:

          - Latex System[ MPI EXT 4.1A]:

            - Prime Coat: Latex, exterior, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex Aggregate System[ MPI EXT 4.1B]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

Retain "Nonflat Topcoat" or "Flat Topcoat" Subparagraph below.

            - Nonflat Topcoat: Textured coating, latex, nonflat[, MPI #41].

              - <Insert manufacturer's name; product name or designation>.

            - Flat Topcoat: Textured coating, latex, flat[, MPI #42].

              - <Insert manufacturer's name; product name or designation>.

          - High-Build Latex System[ MPI EXT 4.1H]: Dry film thickness of not less than 10 mils (0.25 mm).

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Latex, exterior, high build[, MPI #40].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 4.1C]:

            - Prime Coat: Light industrial coating, exterior, water based, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

        - CMU Substrates:

          - Latex System[ MPI EXT 4.2A]:

            - Prime Coat: Block filler, latex, interior/exterior[, MPI #4].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkali-Resistant Primer System[ MPI EXT 4.2L]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex Aggregate System[ MPI EXT 4.2B]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

Retain "Nonflat Topcoat" or "Flat Topcoat" Subparagraph below.

            - Nonflat Topcoat: Textured coating, latex, nonflat[, MPI #41].

              - <Insert manufacturer's name; product name or designation>.

            - Flat Topcoat: Textured coating, latex, flat[, MPI #42].

              - <Insert manufacturer's name; product name or designation>.

          - High-Build Latex System[ MPI EXT 4.2K]: Dry film thickness of not less than 10 mils (0.25 mm).

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Latex, exterior, high build[, MPI #40].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 4.2C]:

            - Prime Coat: Block filler, latex, interior/exterior[, MPI #4].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

        - Steel and Iron Substrates:

          - Water-Based Light Industrial Coating System[ MPI EXT 5.1B] [MPI EXT 5.1C] [MPI EXT 5.1M] [MPI EXT 5.1N]:

Retain "Zinc-Rich Prime Coat," "Alkyd Prime Coat," "Acrylic Prime Coat," "Epoxy Prime Coat," or "Shop Prime Coat" Subparagraph below. First corresponds to MPI EXT 5.1B; second and fifth correspond to MPI EXT 5.1C; third corresponds to MPI EXT 5.1M; and fourth corresponds to MPI EXT 5.1N. If retaining fifth, specify primer complying with MPI #79 in Section where substrate is specified.

            - Zinc-Rich Prime Coat: Primer, zinc rich, inorganic[, MPI #19].

              - <Insert manufacturer's name; product name or designation>.

            - Alkyd Prime Coat: Primer, alkyd, anti-corrosive for metal[, MPI #79].

              - <Insert manufacturer's name; product name or designation>.

            - Acrylic Prime Coat: Primer, rust inhibitive, water based[ MPI #107].

              - <Insert manufacturer's name; product name or designation>.

            - Epoxy Prime Coat: Primer, epoxy, anti-corrosive[ MPI #101].

              - <Insert manufacturer's name; product name or designation>.

            - Shop Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating over Epoxy System[ MPI EXT 5.1R]:

            - Prime Coat: Primer, epoxy, anti-corrosive[ MPI #101].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, high build, low gloss[ MPI #108].

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System [MPI EXT 5.1D] [MPI EXT 5.1Q]:

Retain "Alkyd Prime Coat," "Shop Prime Coat," or "Surface-Tolerant Prime Coat" Subparagraph below. First and second correspond to MPI EXT 5.1D; third corresponds to MPI EXT 5.1Q. If retaining second, specify primer complying with MPI #79 in Section where substrate is specified.

            - Alkyd Prime Coat: Primer, alkyd, anticorrosive, for metal[, MPI #79].

              - <Insert manufacturer's name; product name or designation>.

            - Shop Prime Coat: Shop primer specified in Section where substrate is specified.

            - Surface-Tolerant Prime Coat: Primer, metal, surface tolerant[, MPI #23].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

          - Quick-Dry Enamel System[ MPI EXT 5.1A]:

            - Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, quick dry, matching topcoat.

Retain "Semigloss Topcoat" or "Gloss Topcoat" Subparagraph below.

            - Semigloss Topcoat: Alkyd, quick dry, semigloss (MPI Gloss Level 5)[, MPI #81].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, quick dry, gloss (MPI Gloss Level 7)[, MPI #96].

              - <Insert manufacturer's name; product name or designation>.

          - Aluminum Paint System[ MPI EXT 5.1K]:

Retain "Alkyd Prime Coat" or "Shop Prime Coat" Subparagraph below. If retaining second, specify primer complying with MPI #79 in Section where substrate is specified.

            - Alkyd Prime Coat: Primer, alkyd, anti-corrosive, for metal[, MPI #79].

              - <Insert manufacturer's name; product name or designation>.

            - Shop Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Aluminum paint, matching topcoat.

            - Topcoat: Aluminum paint[, MPI #1].

              - <Insert manufacturer's name; product name or designation>.

Galvanized-metal substrates should not be chromate passivated if primer is field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

        - Galvanized-Metal Substrates:

          - Latex System [MPI EXT 5.3A] [MPI EXT 5.3H]:

Retain "Cementitious Prime Coat" or "Water-Based Prime Coat" Subparagraph below. First corresponds to MPI EXT 5.3A; second corresponds to MPI EXT 5.3H.

            - Cementitious Prime Coat: Primer, galvanized, cementitious[, MPI #26].

              - <Insert manufacturer's name; product name or designation>.

            - Water-Based Prime Coat: Primer, galvanized, water based[, MPI #134].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System [MPI EXT 5.3G] [MPI EXT 5.3J] [MPI EXT 5.3K]:

Retain "Cementitious Prime Coat," "Acrylic Prime Coat," or "Epoxy Prime Coat" Subparagraph below. First corresponds to MPI EXT 5.3G; second corresponds to MPI EXT 5.3J; third corresponds to MPI EXT 5.3K.

            - Cementitious Prime Coat: Primer, galvanized, cementitious[, MPI #26].

              - <Insert manufacturer's name; product name or designation>.

            - Acrylic Prime Coat: Primer, galvanized, water based[, MPI #134].

              - <Insert manufacturer's name; product name or designation>.

            - Epoxy Prime Coat: Primer, epoxy, anti-corrosive[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 5.3B]:

            - Prime Coat: Primer, galvanized, cementitious[, MPI #26].

              - <Insert manufacturer's name; product name or designation>.

Retain "Intermediate Coat" Subparagraph below if required.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

          - Aluminum Paint System[ MPI EXT 5.3F]:

            - Prime Coat: Primer, galvanized, cementitious[, MPI #26].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Aluminum paint, matching topcoat.

            - Topcoat: Aluminum paint[, MPI #1].

              - <Insert manufacturer's name; product name or designation>.

        - Aluminum Substrates:

          - Latex System[ MPI EXT 5.4H]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 5.4G]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System [MPI EXT 5.4A] [MPI EXT 5.4F]:

Retain "Pretreatment Prime Coat" and "Prime Coat" subparagraphs below for MPI EXT 5.4A; Retain only "Prime Coat" Subparagraph for MPI EXT 5.4F. Note that vinyl wash primer has a high VOC content and may be unavailable in some localities.

            - Pretreatment Prime Coat: Vinyl wash primer[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Copper Substrates:

          - Latex System[ MPI EXT 5.5H]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 5.5G]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System [MPI EXT 5.5A] [MPI EXT 5.5F]:

Retain "Vinyl Wash Prime Coat" or "Quick-Dry Prime Coat" Subparagraph below. First corresponds to MPI EXT 5.5A; second corresponds to MPI EXT 5.5F. Note that vinyl wash primer has a high VOC content and may be unavailable in some localities.

            - Vinyl Wash Prime Coat: Vinyl wash primer[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Quick-Dry Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Stainless Steel Substrates:

          - Latex System[ MPI EXT 5.6F]:

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 5.6G]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 5.6A]:

Note that vinyl wash primer has a high VOC content and may be unavailable in some localities.

            - Prime Coat: Vinyl wash primer[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: Glued-laminated construction.

          - Latex over Latex Primer System[ MPI EXT 6.1L]:

            - Prime Coat: Primer, latex for exterior wood[, MPI #6].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Primer System[ MPI EXT 6.1A]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 6.1B]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: Exposed framing.

          - Latex over Latex Primer System[ MPI EXT 6.2M]:

            - Prime Coat: Primer, latex for exterior wood[, MPI #6].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Primer System[ MPI EXT 6.2A]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 6.2C]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: [Wood trim] [Architectural woodwork] [Doors] [Windows] [Wood board siding] [and] [wood fences].

          - Latex over Latex Primer System[ MPI EXT 6.3L]:

            - Prime Coat: Primer, latex for exterior wood[, MPI #6].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex System[ MPI EXT 6.3A]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 6.3J]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Semigloss Topcoat" or "Gloss Topcoat" Subparagraph below.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 6.3B]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: Wood-based panel products.

          - Latex over Latex Primer System[ MPI EXT 6.4K]:

            - Prime Coat: Primer, latex for exterior wood[, MPI #6].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Primer System[ MPI EXT 6.4G]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 6.4B]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: Traffic surfaces, including [lumber decking] [and] [stairs].

          - Latex Porch and Floor Paint over Latex Primer System[ MPI EXT 6.5E]:

            - Prime Coat: Primer, latex for exterior wood[, MPI #6].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex floor paint, matching topcoat.

            - Topcoat: Latex floor paint, low gloss[, MPI #60].

              - <Insert manufacturer's name; product name or designation>.

            - Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

          - Latex Porch and Floor Paint over Alkyd Primer System[ MPI EXT 6.5A]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex floor paint, matching topcoat.

            - Topcoat: Latex floor paint, low gloss[, MPI #60].

              - <Insert manufacturer's name; product name or designation>.

            - Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

          - Latex Deck Coating System (for Plywood Decks)[ MPI EXT 6.5G]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Latex Deck Coating[, MPI #127].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Floor Enamel System[ MPI EXT 6.5B]:

            - Prime Coat: Floor enamel, alkyd, gloss, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Floor enamel, alkyd, gloss, matching topcoat.

            - Topcoat: Floor enamel, alkyd, gloss (MPI Gloss Level 6)[, MPI #27].

              - <Insert manufacturer's name; product name or designation>.

            - Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

          - Alkyd Floor Enamel over Wood Preservative System[ MPI EXT 6.5C]:

            - Preservative Coat: Preservative, for exterior wood[, MPI #37].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Floor enamel, alkyd, gloss, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Floor enamel, alkyd, gloss, matching topcoat.

            - Topcoat: Floor enamel, alkyd, gloss (MPI Gloss Level 6)[, MPI #27].

              - <Insert manufacturer's name; product name or designation>.

            - Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

        - Wood Substrates: Wood shingles and shakes (excluding roofs).

          - Latex over Latex Primer System[ MPI EXT 6.6E]:

            - Prime Coat: Primer, latex for exterior wood[, MPI #6].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Primer System[ MPI EXT 6.6A]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 6.6B]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Fiberglass Substrates:

          - Latex System[ MPI EXT 6.7A]:

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 6.7C]:

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 6.7B]:

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Plastic Trim Fabrication Substrates:

          - Latex System[ MPI EXT 6.8A]:

Retain "Water-Based Prime Coat" or "Solvent-Based Prime Coat" Subparagraph below.

            - Water-Based Prime Coat: Primer, bonding, water based[, MPI #17].

              - <Insert manufacturer's name; product name or designation>.

            - Solvent-Based Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 6.8C]:

Retain "Water-Based Prime Coat" or "Solvent-Based Prime Coat" Subparagraph below.

            - Water-Based Prime Coat: Primer, bonding, water based[, MPI #17].

              - <Insert manufacturer's name; product name or designation>.

            - Solvent-Based Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 6.8B]:

Retain "Water-Based Prime Coat" or "Solvent-Based Prime Coat" Subparagraph below.

            - Water-Based Prime Coat: Primer, bonding, water based[, MPI #17].

              - <Insert manufacturer's name; product name or designation>.

            - Solvent-Based Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Portland Cement Plaster Substrates:

          - Latex System [MPI EXT 9.1A] [MPI EXT 9.1J]:

Retain "Latex Prime Coat" or "Alkali-Resistant Prime Coat" Subparagraph below. First corresponds to MPI EXT 9.1A; second corresponds to MPI EXT 9.1J.

            - Latex Prime Coat: Latex, exterior, matching topcoat.

            - Alkali-Resistant Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - High-Build Latex System[ MPI EXT 9.1H]: Dry film thickness of not less than 10 mils (0.25 mm).

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Latex, exterior, high build[, MPI #40].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 9.1B]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

        - Exterior Gypsum Board Substrates:

          - Latex System[ MPI EXT 9.2A]:

            - Prime Coat: Primer, latex for exterior wood (reduced)[, MPI #6].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex Aggregate System[ MPI EXT 9.2C]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

Retain "Nonflat Topcoat" or "Flat Top Coat" Subparagraph below.

            - Nonflat Topcoat: Textured coating, latex, nonflat[, MPI #41].

              - <Insert manufacturer's name; product name or designation>.

            - Flat Topcoat: Textured coating, latex, flat[, MPI #42].

              - <Insert manufacturer's name; product name or designation>.

          - High-Build Latex System[ MPI EXT 9.2D]: Dry film thickness of not less than 10 mils (0.25 mm).

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Latex, exterior, high build[, MPI #40].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 9.2B]:

            - Prime Coat: Primer, latex for exterior wood (reduced)[, MPI #6].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

        - Exterior Canvas Substrates:

          - Latex System[ MPI EXT 10.1A]:

            - Prime Coat: Latex, exterior, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light Industrial Coating System[ MPI EXT 10.1B]:

            - Prime Coat: Light industrial coating, exterior, water based, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Low-Sheen Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level 3)[, MPI #161].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Light industrial coating, exterior, water based, semigloss (MPI Gloss Level 5)[, MPI #163].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6)[, MPI #164].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 10.1C]:

            - Prime Coat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

          - Aluminum Paint System[ MPI EXT 10.1D]:

            - Prime Coat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Aluminum paint, matching topcoat.

            - Topcoat: Aluminum paint[, MPI #1].

              - <Insert manufacturer's name; product name or designation>.

        - Exterior Bituminous-Coated Substrates:

          - Latex System[ MPI EXT 10.2A]:

            - Prime Coat: Primer, rust inhibitive, water based[, MPI #107].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, exterior, matching topcoat.

Retain "Flat Topcoat," "Low-Sheen Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Latex, exterior, flat (MPI Gloss Level 1)[, MPI #10].

              - <Insert manufacturer's name; product name or designation>.

            - Low-Sheen Topcoat: Latex, exterior, low sheen (MPI Gloss Level 3-4)[, MPI #15].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Latex, exterior, semigloss (MPI Gloss Level 5)[, MPI #11].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Latex, exterior, gloss (MPI Gloss Level 6)[, MPI #119].

              - <Insert manufacturer's name; product name or designation>.

          - Latex Aggregate Coating System[ MPI EXT 10.2B]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

Retain "Nonflat Topcoat" or "Flat Topcoat" Subparagraph below.

            - Nonflat Topcoat: Textured coating, latex, nonflat[, MPI #41].

              - <Insert manufacturer's name; product name or designation>.

            - Flat Topcoat: Textured coating, latex, flat[, MPI #42].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[ MPI EXT 10.2C]:

            - Prime Coat: Primer, rust inhibitive, water based[, MPI #107].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Exterior, alkyd enamel, matching topcoat.

Retain "Flat Topcoat," "Semigloss Topcoat," or "Gloss Topcoat" Subparagraph below.

            - Flat Topcoat: Alkyd, exterior, flat (MPI Gloss Level 1)[, MPI #8].

              - <Insert manufacturer's name; product name or designation>.

            - Semigloss Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level 5)[, MPI #94].

              - <Insert manufacturer's name; product name or designation>.

            - Gloss Topcoat: Alkyd, exterior, gloss (MPI Gloss Level 6)[, MPI #9].

              - <Insert manufacturer's name; product name or designation>.

          - Aluminum Paint System[ MPI EXT 10.2D]:

            - Prime Coat: Primer, rust inhibitive, water based[, MPI #107].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Aluminum paint, matching topcoat.

            - Topcoat: Aluminum paint[, MPI #1].

              - <Insert manufacturer's name; product name or designation>.

END OF SECTION 099114