Copyright 2020 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 099124 - INTERIOR PAINTING (MPI STANDARDS)

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Access Manufacturer-Provided, AIA MasterSpec-Based Sections:

<Double click here for this Section based on specific manufacturer’s products set as Basis-of-Design at ProductMasterSpec.com.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section includes surface preparation and the application of paint systems on [interior substrates.] [the following interior substrates:]

          - Concrete.

          - Cement board.

          - Clay masonry.

          - Concrete masonry units (CMUs).

          - Steel and iron.

          - Galvanized metal.

          - Aluminum (not anodized or otherwise coated).

          - Copper.

          - Stainless steel.

          - Wood.

          - Fiberglass.

          - Plastic.

          - Gypsum board.

          - Plaster.

          - Acoustic panels and tiles.

          - Spray-textured ceilings.

          - Cotton or canvas insulation covering.

          - ASJ insulation covering.

          - Bituminous-coated surfaces.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Primers in other Sections must be coordinated for compatibility with finish coats specified in this Section. Review other Sections for shop-primed products, and insert references to this Section to establish primer requirements.

          - [Section 051200 "Structural Steel Framing"] [Section 051213 "Architecturally Exposed Structural Steel Framing"] for shop priming structural steel.

          - Section 055000 "Metal Fabrications" for shop priming metal fabrications.

          - Section 055113 "Metal Pan Stairs" for shop priming metal pan stairs.

          - Section 055116 "Metal Floor Plate Stairs" for shop priming metal floor plate stairs.

          - Section 055119 "Metal Grating Stairs" for shop priming metal grating stairs.

          - Section 055213 "Pipe and Tube Railings" for shop [priming] [painting] pipe and tube railings.

          - [Section 055313 "Bar Gratings"] [Section 055316 "Plank Gratings"] [Section 055319 "Expanded Metal Gratings"] for shop priming metal gratings.

          - Section 099300 "Staining and Transparent Finishing" for surface preparation and the application of wood stains and transparent finishes on interior wood substrates.

          - Section 099600 "High-Performance Coatings" for tile-like coatings.

      - DEFINITIONS

Retain this article if paints are specified by manufacturers' trade names rather than by MPI paint numbers. Definitions of MPI Gloss Levels below are from "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual").

Retain terms that remain after this Section has been edited for a project.

        - MPI Gloss Level 1: Not more than five units at 60 degrees and 10 units at 85 degrees, according to ASTM D523.

        - MPI Gloss Level 2: Not more than 10 units at 60 degrees and 10 to 35 units at 85 degrees, according to ASTM D523.

        - MPI Gloss Level 3: 10 to 25 units at 60 degrees and 10 to 35 units at 85 degrees, according to ASTM D523.

        - MPI Gloss Level 4: 20 to 35 units at 60 degrees and not less than 35 units at 85 degrees, according to ASTM D523.

        - MPI Gloss Level 5: 35 to 70 units at 60 degrees, according to ASTM D523.

        - MPI Gloss Level 6: 70 to 85 units at 60 degrees, according to ASTM D523.

        - MPI Gloss Level 7: More than 85 units at 60 degrees, according to ASTM D523.

      - ACTION SUBMITTALS

        - Product Data: For each type of product. Include preparation requirements and application instructions.

See "Writing Guide" Article in the Evaluations for discussion of first subparagraph below.

          - Include printout of current "MPI Approved Products List" for each product category specified, with the proposed product highlighted.

          - Indicate VOC content.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for paints and coatings.>

          - <Double click to insert sustainable design text for EPDs and HPDs.>

          - <Double click here to insert sustainable design text for manufacturer inventory.>

        - Samples for Initial Selection: For each type of topcoat product.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled. Retain "Samples for Verification" Paragraph below with or without above.

        - Samples for Verification: For each type of paint system and in each color and gloss of topcoat.

Color and gloss of Samples change as they age; seven-day old Samples appear different from freshly dried Samples.

          - Submit Samples on rigid backing, 8 inches (200 mm) square.

          - Apply coats on Samples in steps to show each coat required for system.

          - Label each coat of each Sample.

          - Label each Sample for location and application area.

        - Product List: Use same designations indicated on Drawings and in the Interior Painting Schedule to cross-reference paint systems specified in this Section. Include color designations.

      - MAINTENANCE MATERIAL SUBMITTALS

        - Furnish extra materials[, from the same product run,] that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

If necessary, replace percentage in "Paint" Subparagraph below with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

          - Paint: [5] <Insert number> percent, but not less than [1 gal. (3.8 L)] <Insert number> of each material and color applied.

      - QUALITY ASSURANCE

        - Mockups: Apply mockups of each paint system indicated and each color and finish selected to verify preliminary selections made under Sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

          - Architect will select one surface to represent surfaces and conditions for application of each paint system.

            - Vertical and Horizontal Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

            - Other Items: Architect will designate items or areas required.

          - Final approval of color selections will be based on mockups.

            - If preliminary color selections are not approved, apply additional mockups of additional colors selected by Architect at no added cost to Owner.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

If necessary, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site.

        - Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

          - Maintain containers in clean condition, free of foreign materials and residue.

          - Remove rags and waste from storage areas daily.

      - FIELD CONDITIONS

        - Apply paints only when temperature of surfaces to be painted and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

        - Do not apply paints when relative humidity exceeds 85 percent; at temperatures of less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

- PRODUCTS

Manufacturers and products listed in SpecAgent and MasterWorks Paragraph Builder are neither recommended nor endorsed by the AIA or Deltek. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

See the "Writing Guide" Article in the Evaluations before revising Part 2.

      - MANUFACTURERS

        - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Retain "Products" Paragraph below and insert lists of manufacturers and products in Interior Painting Schedule to require specific products or a comparable product from other manufacturers.

See lists of products currently approved by MPI in its "MPI Approved Products List." See "Writing Guide" Article in the Evaluations for further discussion.

        - Products: Subject to compliance with requirements, [provide product] [provide one of the products] [available products that may be incorporated into the Work include, but are not limited to products] listed in the Interior Painting Schedule for the paint category indicated.

      - PAINT, GENERAL

        - MPI Standards: Products shall comply with MPI standards indicated and shall be listed in its "MPI Approved Products List."

        - Material Compatibility:

Systems could fail if paints used for individual coats are incompatible. MPI's paint systems match primers and topcoats and take compatibility into consideration.

          - Materials for use within each paint system shall be compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

          - For each coat in a paint system, products shall be recommended in writing by topcoat manufacturers for use in paint system and on substrate indicated.

        - <Double click to insert sustainable design text for paints.>

        - Colors: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule] <Insert requirements>.

          - [Ten] [Twenty] [Thirty] <Insert number> percent of surface area will be painted with deep tones.

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

        - Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows:

Percentages in six subparagraphs below are based on "MPI Manual."

          - Concrete: 12 percent.

          - Fiber-Cement Board: 12 percent.

          - Masonry (Clay and CMUs): 12 percent.

          - Wood: 15 percent.

          - Gypsum Board: 12 percent.

          - Plaster: 12 percent.

        - Gypsum Board Substrates: Verify that finishing compound is sanded smooth.

        - Plaster Substrates: Verify that plaster is fully cured.

        - Spray-Textured Ceiling Substrates: Verify that surfaces are dry.

        - Verify suitability of substrates, including surface conditions and compatibility, with existing finishes and primers.

        - Proceed with coating application only after unsatisfactory conditions have been corrected.

          - Application of coating indicates acceptance of surfaces and conditions.

      - PREPARATION

For renovation projects, consult "MPI Maintenance Repainting Manual" and revise first paragraph below and paint systems specified in the Interior Painting Schedule.

        - Comply with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual" applicable to substrates and paint systems indicated.

        - Remove hardware, covers, plates, and similar items already in place that are removable and are not to be painted. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

          - After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection if any.

        - Clean substrates of substances that could impair bond of paints, including dust, dirt, oil, grease, and incompatible paints and encapsulants.

Coordination of shop-applied prime coats with topcoats is critical.

          - Remove incompatible primers and reprime substrate with compatible primers or apply tie coat as required to produce paint systems indicated.

        - Concrete Substrates: Remove release agents, curing compounds, efflorescence, and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces to be painted exceeds that permitted in manufacturer's written instructions.

        - Masonry Substrates: Remove efflorescence and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces or mortar joints exceeds that permitted in manufacturer's written instructions.

Retain "Steel Substrates" Paragraph below if steel is not shop primed or if shop primer is removed in the field.

        - Steel Substrates: Remove rust, loose mill scale, and shop primer, if any. Clean using methods recommended in writing by paint manufacturer[.] [ but not less than the following:]

Usually retain one of first two subparagraphs below. SSPC-SP 2 and SSPC-SP 3 remove loose rust, mill scale, and paint. SSPC-SP 2 is minimum surface preparation accepted by AISC for painted steel.

          - SSPC-SP 2.

          - SSPC-SP 3.

SSPC-SP 7/NACE No. 4 permits tight residues of rust, mill scale, and coatings to remain. Be aware that blast-cleaning methods may not be practical for use at Project site and may not be allowed by authorities having jurisdiction.

          - SSPC-SP 7/NACE No. 4.

SSPC-SP 11 requires complete removal of rust, mill scale, and paint by power tools. SSPC-SP 11 uses nonabrasive methods and is more thorough than SSPC-SP 2, SSPC-SP 3, and SSPC-SP 7/NACE No. 4.

          - SSPC-SP 11.

Retain "Shop-Primed Steel Substrates" Paragraph below if primers are shop applied and are not removed in the field.

        - Shop-Primed Steel Substrates: Clean field welds, bolted connections, and areas where shop paint is abraded. Paint exposed areas with the same material as used for shop priming to comply with SSPC-PA 1 for touching up shop-primed surfaces.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

        - Galvanized-Metal Substrates: Remove grease and oil residue from galvanized sheet metal by mechanical methods to produce clean, lightly etched surfaces that promote adhesion of subsequently applied paints.

        - Aluminum Substrates: Remove loose surface oxidation.

        - Wood Substrates:

          - Scrape and clean knots, and apply coat of knot sealer before applying primer.

          - Sand surfaces that will be exposed to view, and dust off.

          - Prime edges, ends, faces, undersides, and backsides of wood.

          - After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dried.

        - Cotton or Canvas Insulation Covering Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

      - INSTALLATION

        - Apply paints according to manufacturer's written instructions and to recommendations in "MPI Manual."

If Project requires restricted application method (e.g., using only spray or rollers), revise first subparagraph below accordingly.

          - Use applicators and techniques suited for paint and substrate indicated.

          - Paint surfaces behind movable equipment and furniture same as similar exposed surfaces. Before final installation, paint surfaces behind permanently fixed equipment or furniture with prime coat only.

          - Paint front and backsides of access panels, removable or hinged covers, and similar hinged items to match exposed surfaces.

          - Do not paint over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

          - Primers specified in painting schedules may be omitted on items that are factory primed or factory finished if acceptable to topcoat manufacturers.

If tinting is not required, delete first paragraph below. Different tints show through as topcoat erodes.

        - Tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of same material are to be applied. Tint undercoats to match color of topcoat, but provide sufficient difference in shade of undercoats to distinguish each separate coat.

        - If undercoats or other conditions show through topcoat, apply additional coats until cured film has a uniform paint finish, color, and appearance.

        - Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections. Cut in sharp lines and color breaks.

        - Painting Fire-Suppression, Plumbing, HVAC, Electrical, Communication, and Electronic Safety and Security Work:

First subparagraph below is for use where items are to be painted to blend in with surroundings; revise if painting is required to protect items from corrosion. Consider indicating painted items on Drawings or delineating extent of "exposed to view" for complex situations.

          - Paint the following work where exposed in equipment rooms:

List below contains items that are often field painted, plus others that are often not. Revise list to suit Project.

            - Equipment, including panelboards[ and switch gear].

            - Uninsulated metal piping.

            - Uninsulated plastic piping.

            - Pipe hangers and supports.

            - Metal conduit.

            - Plastic conduit.

            - Tanks that do not have factory-applied final finishes.

            - Duct, equipment, and pipe insulation having cotton or canvas insulation covering or other paintable jacket material.

            - <Insert mechanical items to be painted>.

          - Paint the following work where exposed in occupied spaces:

List below contains items that are usually field painted. Revise list to suit Project.

            - Equipment, including panelboards.

            - Uninsulated metal piping.

            - Uninsulated plastic piping.

            - Pipe hangers and supports.

            - Metal conduit.

            - Plastic conduit.

            - Duct, equipment, and pipe insulation having cotton or canvas insulation covering or other paintable jacket material.

            - Other items as directed by Architect.

            - <Insert mechanical items to be painted>.

          - Paint portions of internal surfaces of metal ducts, without liner, behind air inlets and outlets that are visible from occupied spaces.

      - FIELD QUALITY CONTROL

        - Dry-Film Thickness Testing: Owner may engage the services of a qualified testing and inspecting agency to inspect and test paint for dry-film thickness.

          - Contractor shall touch up and restore painted surfaces damaged by testing.

          - If test results show that dry-film thickness of applied paint does not comply with paint manufacturer's written recommendations, Contractor shall pay for testing and apply additional coats as needed to provide dry-film thickness that complies with paint manufacturer's written recommendations.

      - CLEANING AND PROTECTION

        - At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

        - After completing paint application, clean spattered surfaces. Remove spattered paints by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

        - Protect work of other trades against damage from paint application. Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

        - At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

      - INTERIOR PAINTING SCHEDULE

Paint systems in this article are based on "MPI Architectural Painting Specification Manual." For renovation projects, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

        - Concrete Substrates, Nontraffic Surfaces:

          - Latex System[, MPI INT 3.1A] [, MPI INT 3.1E]:

Retain one of two "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 3.1A; second corresponds to MPI INT 3.1E.

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Latex, interior, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Latex Aggregate System[, MPI INT 3.1B]:

            - Prime Coat: Textured coating, latex, flat[, MPI #42].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex Aggregate System[, MPI INT 3.1N]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Textured coating, latex, nonflat[, MPI #41].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Textured coating, latex, flat[, MPI #42].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 3.1M]:

            - Prime Coat: Primer sealer, interior, institutional low odor/VOC[, MPI #149].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 3.1C)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 3.1C]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 3.1L]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 3.1D]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

          - Concrete Stain System[, MPI INT 3.1K]:

For a Premium Grade system, "MPI Manual" requires first coat; delete "First Coat" Subparagraph below for a Budget Grade system.

            - First Coat: Stain, interior, matching topcoat.

            - Topcoat: Stain, interior[, MPI #58].

              - <Insert manufacturer's name; product name or designation>.

        - Concrete Substrates, Traffic Surfaces:

          - Latex Floor Enamel System[, MPI INT 3.2A]:

            - Prime Coat: Floor paint, latex, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Floor paint, latex, matching topcoat.

            - Topcoat: Floor paint, latex, low gloss (maximum MPI Gloss Level 3)[, MPI #60].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Floor Enamel System[, MPI INT 3.2B]:

            - Prime Coat: Floor enamel, alkyd, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Floor enamel, alkyd, matching topcoat.

            - Topcoat: Floor enamel, alkyd, gloss (MPI Gloss Level 6)[, MPI #27].

              - <Insert manufacturer's name; product name or designation>.

          - Concrete Stain System[, MPI INT 3.2E]:

For a Premium Grade system, "MPI Manual" requires first coat; delete "First Coat" Subparagraph below for a Budget Grade system.

            - First Coat: Stain, interior, for concrete floors, matching topcoat.

            - Topcoat: Stain, interior, for concrete floors[, MPI #58].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Concrete Floor Sealer System[, MPI INT 3.2G]:

For a Budget Grade system, "MPI Manual" requires first coat; "MPI Manual" does not include a Premium Grade system.

            - First Coat: Sealer, water based, for concrete floors, matching topcoat.

            - Topcoat: Sealer, water based, for concrete floors[, MPI #99].

          - Solvent-Based Concrete Floor Sealer System[, MPI INT 3.2F]:

For a Budget Grade system, "MPI Manual" requires first coat; "MPI Manual" does not include a Premium Grade system.

            - First Coat: Sealer, solvent based, for concrete floors, matching topcoat.

            - Topcoat: Sealer, solvent based, for concrete floors[, MPI #104].

              - <Insert manufacturer's name; product name or designation>.

        - Cement Board Substrates:

          - Latex System[, MPI INT 3.3A]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 3.3G]:

            - Prime Coat: Primer sealer, interior, institutional low odor/VOC[, MPI #149].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 3.3B)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 3.3B]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 3.3H]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 3.3C]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Clay Masonry Substrates:

          - Latex System[, MPI INT 4.1A]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex Aggregate System[, MPI INT 4.1B]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: Primer for textured coating, latex, flat[, as recommended in writing by topcoat manufacturer].

            - Intermediate Coat: Intermediate coat for textured coating, latex, flat[, as recommended in writing by topcoat manufacturer].

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Textured coating, latex, nonflat[, MPI #41].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Textured coating, latex, flat[, MPI #42].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 4.1M]:

            - Prime Coat: Primer sealer, interior, institutional low odor/VOC[, MPI #149].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 4.1L)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 4.1L]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 4.1C]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 4.1D]:

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

          - Clear (Two-Component) Polyurethane System[, MPI INT 4.1K]:

            - Prime Coat: Two-component polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Two-component polyurethane matching topcoat.

            - Topcoat: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or MPI Gloss Level 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

        - CMU Substrates:

          - Latex System[, MPI INT 4.2A]:

            - Block Filler: Block filler, latex, interior/exterior[, MPI #4].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex Aggregate System[, MPI INT 4.2B]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: Primer for textured coating, latex, flat[, as recommended in writing by topcoat manufacturer].

            - Intermediate Coat: Intermediate coat for textured coating, latex, flat[, as recommended in writing by topcoat manufacturer].

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Textured coating, latex, nonflat[, MPI #41].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Textured coating, latex, flat[, MPI #42].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 4.2E]:

            - Block Filler: Block filler, latex, interior/exterior[, MPI #4].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 4.2D) (, MPI INT 4.2P)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 4.2D] [, MPI INT 4.2P]:

Retain "Block Filler" or "Prime Coat" Subparagraph below. First subparagraph corresponds to MPI INT 4.2D; second corresponds to MPI INT 4.2P.

            - Block Filler: Latex, interior/exterior[, MPI #4].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, alkali resistant, water based[, MPI #3].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 4.2K]:

            - Block Filler: Latex, interior/exterior[, MPI #4].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

For areas subject to wetting, consider using epoxy system MPI INT 4.2G, which is specified in Section 099600 "High-Performance Coatings," instead of alkyd system in "Alkyd System(, MPI INT 4.2C) (, MPI INT 4.2N)" Subparagraph below.

          - Alkyd System[, MPI INT 4.2C] [, MPI INT 4.2N]:

            - Block Filler: Latex, interior/exterior[, MPI #4].

              - <Insert manufacturer's name; product name or designation>.

Retain "Sealer Coat" Subparagraph below for MPI INT 4.2N; delete for MPI INT 4.2C.

            - Sealer Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

          - Clear (Two-Component) Polyurethane System[, MPI INT 4.2Q]:

            - Prime Coat: Two-component polyurethane, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Two-component polyurethane, matching topcoat.

            - Topcoat: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or MPI Gloss Level 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

        - Steel Substrates:

          - Latex System, Alkyd Primer[, MPI INT 5.1Q] [, MPI INT 5.1QQ]:

Retain one of three "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 5.1Q; second corresponds to MPI INT 5.1QQ. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

            - Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, alkyd, anticorrosive, for metal[, MPI #79].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Shop-Applied Quick-Drying Shop Primer System[, MPI INT 5.1X]:

            - Prime Coat: Primer, quick dry, for shop application[, MPI #275].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 5.1S]:

            - Prime Coat: Primer, rust inhibitive, water based[ MPI #107].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 5.1R) (, MPI INT 5.1RR)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 5.1R] [, MPI INT 5.1RR]:

Retain one of three "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 5.1R; second corresponds to MPI INT 5.1RR. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

            - Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, alkyd, anticorrosive, for metal[, MPI #79].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 5.1B]:

            - Prime Coat: Primer, rust inhibitive, water based[ MPI #107].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System over Epoxy Primer System[, MPI INT 5.1N]:

            - Prime Coat: Primer, epoxy, anti-corrosive[ MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Dry-Fall System[, MPI INT 5.1C] [, MPI INT 5.1CC]:

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

Retain one of three "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 5.1C; second corresponds to MPI INT 5.1CC. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

            - Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, alkyd, anticorrosive, for metal[, MPI #79].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Shop primer specified in Section where substrate is specified.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Dry fall, latex, flat[, MPI #118].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, water based, for galvanized steel, flat (MPI Gloss Level 1)[, MPI #133].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, latex (MPI Gloss Level 3)[, MPI #155].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, latex (MPI Gloss Level 5)[, MPI #226].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Dry-Fall over Shop-Applied Quick-Drying Shop Primer System[, MPI INT 5.1CCC]:

            - Prime Coat: Primer, quick dry, for shop application[, MPI #275].

              - <Insert manufacturer's name; product name or designation>.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Dry fall, latex, flat[, MPI #118].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, water based, for galvanized steel, flat (MPI Gloss Level 1)[, MPI #133].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, latex (MPI Gloss Level 3)[, MPI #155].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, latex (MPI Gloss Level 5)[, MPI #226].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 5.1E] [, MPI INT 5.1EE]:

Retain one of three "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 5.1E; second corresponds to MPI INT 5.1EE. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

            - Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, alkyd, anticorrosive, for metal[, MPI #79].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd over Surface-Tolerant Primer System[, MPI INT 5.1T]:

            - Prime Coat: Primer, metal, surface tolerant[ MPI #23].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

          - Alkyd over Shop-Applied Quick-Drying Shop Primer System[, MPI INT 5.1W]:

            - Prime Coat: Primer, quick dry, for shop application[, MPI #275].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

          - Quick-Dry Enamel System[, MPI INT 5.1A]:

            - Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

            - Intermediate Coat: Alkyd, quick dry, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, quick dry, semigloss (MPI Gloss Level 5)[, MPI #81].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, quick dry, gloss (MPI Gloss Level 7)[, MPI #96].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd, Dry-Fall System[, MPI INT 5.1D] [, MPI INT 5.1DD]:

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

Retain one of three "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 5.1D; second corresponds to MPI INT 5.1DD. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

            - Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, alkyd, anticorrosive, for metal[, MPI #79].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Shop primer specified in Section where substrate is specified.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Dry fall, alkyd, flat[, MPI #55].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, alkyd (MPI Gloss Level 3)[, MPI #89].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, alkyd, semigloss (MPI Gloss Level 5)[, MPI #225].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Dry-Fall over Quick-Drying Primer System[, MPI INT 5.1ZZ]:

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

            - Prime Coat: Primer, quick dry, for shop application[, MPI #275].

              - <Insert manufacturer's name; product name or designation>.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Dry fall, alkyd, flat[, MPI #55].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, alkyd (MPI Gloss Level 3)[, MPI #89].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, alkyd, semigloss (MPI Gloss Level 5)[, MPI #225].

              - <Insert manufacturer's name; product name or designation>.

          - Aluminum Paint System[, MPI INT 5.1M] [, MPI INT 5.1MM]:

Retain one of three "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 5.1M; second corresponds to MPI INT 5.1MM. If retaining third, specify primer complying with MPI #76 or MPI #79 in Section where substrate is specified.

            - Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, alkyd, anticorrosive, for metal[, MPI #79].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Budget Grade system.

            - Intermediate Coat: Aluminum paint, matching topcoat.

            - Topcoat: Aluminum paint[, MPI #1].

              - <Insert manufacturer's name; product name or designation>.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate primers.

        - Galvanized-Metal Substrates:

          - Latex System[, MPI INT 5.3A] [, MPI INT 5.3J]:

Retain one of two "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 5.3A; second corresponds to MPI INT 5.3J.

            - Prime Coat: Primer, galvanized, cementitious[, MPI #26].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, galvanized, water based[, MPI #134].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 5.3N]:

            - Prime Coat: Primer, galvanized, water based[, MPI #134].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 5.3M)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 5.3M]:

            - Prime Coat: Primer, galvanized, water based[, MPI #134].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 5.3B] [, MPI INT 5.3K]:

Retain one of two "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 5.3B; second corresponds to MPI INT 5.3K.

            - Prime Coat: Primer, galvanized, cementitious[, MPI #26].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, galvanized, water based[, MPI #134].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Dry-Fall System[, MPI INT 5.3H]:

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

            - Prime Coat: Dry fall, water based, for galvanized steel, matching topcoat.

            - Topcoat: Dry fall, water based, for galvanized steel, flat (MPI Gloss Level 1)[, MPI #133].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd over Cementitious Primer System[, MPI INT 5.3C]:

            - Prime Coat: Primer, galvanized, cementitious[, MPI #26].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Dry-Fall System (Cementitious Primer)[, MPI INT 5.3F]:

For a Budget Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Premium Grade system.

            - Prime Coat: Primer, galvanized, cementitious[, MPI #26].

              - <Insert manufacturer's name; product name or designation>.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Dry fall, alkyd, flat[, MPI #55].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, alkyd (MPI Gloss Level 3) [, MPI #89].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Dry fall, alkyd, semigloss (MPI Gloss Level 5)[, MPI #225].

              - <Insert manufacturer's name; product name or designation>.

          - Aluminum Paint System (Cementitious Primer)[, MPI INT 5.3G]:

            - Prime Coat: Primer, galvanized, cementitious[, MPI #26].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Budget Grade system.

            - Intermediate Coat: Aluminum paint, matching topcoat.

            - Topcoat: Aluminum paint[, MPI #1].

              - <Insert manufacturer's name; product name or designation>.

        - Aluminum (Not Anodized or Otherwise Coated) Substrates:

          - Latex System[, MPI INT 5.4H]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 5.4G]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 5.4F)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 5.4F]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 5.4E]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 5.4A] [, MPI INT 5.4J]:

Retain one of two "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 5.4A; second corresponds to MPI INT 5.4J. Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Copper Substrates:

          - Latex System[, MPI INT 5.5H]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 5.5G]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 5.5F)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 5.5F]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 5.5E]:

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 5.5A]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Stainless Steel Substrates:

          - Latex System[, MPI INT 5.6H]:

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 5.6G)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 5.6G]:

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 5.6A] [, MPI INT 5.6F]:

Retain one of two "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 5.6A; second corresponds to MPI INT 5.6F.

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 5.6B]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: Glued-laminated construction.

          - Latex over Latex Primer System[, MPI INT 6.1M]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Primer System[, MPI INT 6.1A]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 6.1Q]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 6.1N)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 6.1N]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 6.1B]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: Exposed framing.

          - Latex over Latex Primer System[, MPI INT 6.2D]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Primer System[, MPI INT 6.2A]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 6.2L]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 6.2B)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 6.2B]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 6.2C]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: [Wood trim] [Architectural woodwork] [Doors] [Windows] [and] [wood board paneling].

          - Latex over Latex Primer System[, MPI INT 6.3T]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Primer System[, MPI INT 6.3U]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 6.3V]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 6.3A)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 6.3A]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 6.3P]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Alkyd System[, MPI INT 6.3BB]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, water based, matching topcoat.

            - Topcoat: Alkyd, water based, gloss (MPI Gloss Level 6-7)[, MPI #157].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 6.3B]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: [Wood paneling] [and] [casework].

          - Latex over Latex Primer System[, MPI INT 6.4R]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Sealer System[, MPI INT 6.4A]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 6.4T]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 6.4S)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 6.4S]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 6.4N]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 6.4B]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: Traffic surfaces, including [floors] [and] [stairs].

          - Latex Porch and Floor Enamel System[, MPI INT 6.5G]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

            - Intermediate Coat: Floor paint, latex, matching topcoat.

            - Topcoat: Floor paint, latex, low gloss (maximum MPI Gloss Level 3)[, MPI #60].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Floor Enamel System[, MPI INT 6.5A]:

            - Prime Coat: Floor enamel, alkyd, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

            - Intermediate Coat: Floor enamel, alkyd, matching topcoat.

            - Topcoat: Floor enamel, alkyd, gloss (MPI Gloss Level 6)[, MPI #27].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: Wood shingles and shakes.

          - Latex over Latex Primer System[, MPI INT 6.6F]:

            - Prime Coat: Primer, latex, for interior wood[, MPI #39].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Primer System[, MPI INT 6.6A]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 6.6B]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Fiberglass Substrates:

          - Latex System[, MPI INT 6.7AA] [, MPI INT 6.7A]:

Retain one of two "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI INT 6.7AA; second corresponds to MPI INT 6.7A.

            - Prime Coat: Primer, bonding, water based[, MPI #17].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 6.7J]:

Retain one of two "Prime Coat" subparagraphs below.

            - Prime Coat: Primer, bonding, water based[, MPI #17].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

          - High-Performance Architectural Latex System[, MPI INT 6.7H]:

Retain one of two "Prime Coat" subparagraphs below.

            - Prime Coat: Primer, bonding, water based[, MPI #17].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 6.7C]:

Retain one of two "Prime Coat" subparagraphs below.

            - Prime Coat: Primer, bonding, water based[, MPI #17].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 6.7B]:

Retain one of two "Prime Coat" subparagraphs below.

            - Prime Coat: Primer, bonding, water based[, MPI #17].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Plastic Substrates:

          - Latex System[, MPI INT 6.8E]:

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 6.8F]:

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

          - High-Performance Architectural Latex System[, MPI INT 6.8A]:

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 6.8C]:

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 6.8B]:

            - Prime Coat: Primer, bonding, solvent based[, MPI #69].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Spray-Textured Ceiling Substrates:

          - Latex, Flat System[, MPI INT 9.1A]: Spray applied.

For a Premium Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Budget Grade system.

            - Prime Coat: Latex, interior, flat, matching topcoat.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

          - Latex System[, MPI INT 9.1E]: Spray applied.

            - Prime Coat: Latex, interior, matching topcoat.

For Budget and Premium Grade systems, "MPI Manual" requires intermediate coat.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Sealer System[, MPI INT 9.1B]:

For a Premium Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Budget Grade system.

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd, Flat System[, MPI INT 9.1C]:

For a Premium Grade system, "MPI Manual" requires prime coat and topcoat; "MPI Manual" does not include a Budget Grade system.

            - Prime Coat: Alkyd, interior, flat, matching topcoat.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd over Alkyd Sealer System[, MPI INT 9.1D]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - [Gypsum Board] [and] [Plaster] Substrates:

          - Latex over Latex Sealer System[, MPI INT 9.2A]:

Retain one of two "Prime Coat" subparagraphs below. Retain first subparagraph for a Premium Grade system.

            - Prime Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat: Latex, interior, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Primer System (for Plaster Only)[, MPI INT 9.2K]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 9.2M]:

            - Prime Coat: Primer sealer, interior, institutional low odor/VOC[, MPI #149].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

"High-Performance Architectural Latex System(, MPI INT 9.2B)" Subparagraph below is recommended for high-traffic and high-contact areas (e.g., public corridors in institutional buildings).

          - High-Performance Architectural Latex System[, MPI INT 9.2B]:

            - Prime Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Light-Industrial Coating System[, MPI INT 9.2L]:

            - Prime Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Light-industrial coating, interior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

            - Topcoat: Light-industrial coating, interior, water based (MPI Gloss Level 3)[, MPI #151].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, semigloss (MPI Gloss Level 5)[, MPI #153].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Light-industrial coating, interior, water based, gloss (MPI Gloss Level 6)[, MPI #154].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd over Latex Sealer System[, MPI INT 9.2C]:

            - Prime Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

        - Acoustic Panels and Tiles:

          - Latex, Flat System[, MPI INT 9.3A]:

            - Prime Coat: Latex, interior, matching topcoat.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

          - Latex over Alkyd Sealer System[, MPI INT 9.3B]:

            - Prime Coat: Primer sealer, alkyd, interior[, MPI #45].

              - <Insert manufacturer's name; product name or designation>.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 9.3D]:

            - Prime Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

          - High-Performance Architectural Latex System[, MPI INT 9.3E]:

            - Prime Coat: Latex, interior, high performance architectural, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 2)[, MPI #138].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 3)[, MPI #139].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural (MPI Gloss Level 4)[, MPI #140].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, high performance architectural, semigloss (MPI Gloss Level 5)[, MPI #141].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd, Flat System[, MPI INT 9.3C]:

            - Prime Coat: Alkyd, interior, matching topcoat.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

        - [Cotton or Canvas] [and] [ASJ] Insulation-Covering Substrates: Including [pipe and duct coverings] <Insert description>.

          - Latex System[, MPI INT 10.1A]:

            - Prime Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Institutional Low-Odor/VOC Latex System[, MPI INT 10.1D]:

            - Prime Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, institutional low odor/VOC, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, institutional low odor/VOC, flat (MPI Gloss Level 1)[, MPI #143].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 2)[, MPI #144].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 3)[, MPI #145].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC (MPI Gloss Level 4)[, MPI #146].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, semigloss (MPI Gloss Level 5)[, MPI #147].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, institutional low odor/VOC, gloss (MPI Gloss Level 6)[, MPI #148].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 10.1B]:

            - Prime Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

          - Aluminum Paint System[, MPI INT 10.1C]:

            - Prime Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Aluminum paint matching topcoat.

            - Topcoat: Aluminum paint[, MPI #1].

              - <Insert manufacturer's name; product name or designation>.

        - Bituminous-Coated Substrates:

          - Latex System[, MPI INT 10.2A]:

            - Prime Coat: Primer, rust inhibitive, water based[, MPI #107].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Latex, interior, matching topcoat.

Retain one of six "Topcoat" subparagraphs below.

            - Topcoat: Latex, interior, flat (MPI Gloss Level 1)[, MPI #53].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 2)[, MPI #44].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 3)[, MPI #52].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior (MPI Gloss Level 4)[, MPI #43].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, semigloss (MPI Gloss Level 5)[, MPI #54].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Latex, interior, gloss (MPI Gloss Level 6, except minimum gloss of 65 units at 60 degrees)[, MPI #114].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd System[, MPI INT 10.2B]:

            - Prime Coat: Primer, rust inhibitive, water based[, MPI #107].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Alkyd, interior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

            - Topcoat: Alkyd, interior, flat (MPI Gloss Level 1)[, MPI #49].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior (MPI Gloss Level 3)[, MPI #51].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, semigloss (MPI Gloss Level 5)[, MPI #47].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Alkyd, interior, gloss (MPI Gloss Level 6)[, MPI #48].

              - <Insert manufacturer's name; product name or designation>.

          - Aluminum Paint System[, MPI INT 10.2C]:

            - Prime Coat: Primer, rust inhibitive, water based[, MPI #107].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Aluminum paint, matching topcoat.

            - Topcoat: Aluminum paint[, MPI #1].

              - <Insert manufacturer's name; product name or designation>.

END OF SECTION 099124