Copyright 2020 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 099301 - STAINING AND TRANSPARENT FINISHING (MPI STANDARDS)

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Access Manufacturer-Provided, AIA MasterSpec-Based Sections:

<Double click here for this Section based on specific manufacturer’s products set as Basis-of-Design at ProductMasterSpec.com.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

MasterSpec includes provisions for LEED 2009, LEED v4, IgCC, and Green Globes. Sustainable design requirements may be inserted in the Section Text using the hypertext links.

- GENERAL

      - SUMMARY

If this Section specifies only stains or transparent finishes, revise Section title to accurately reflect its content.

        - Section Includes:

          - Staining and transparent finishing of exterior and interior wood surfaces.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 099123 "Interior Painting" for stains and transparent finishes on concrete floors.

          - Section 099600 "High-Performance Coatings" for transparent high-performance coatings on concrete floors and clay masonry.

      - ACTION SUBMITTALS

Action submittals are submittals requiring responsive action and return of reviewed documents to Contractor.

        - Product Data:

          - For each type of product.

          - Include preparation requirements and application instructions.

See "Writing Guide" Article in the Evaluations for discussion of first subparagraph below.

          - Include printout of current "MPI Approved Products List" for each product category specified, with the proposed product highlighted.

          - Indicate VOC content.

Retain "Samples for Initial Selection" or "Samples for Verification" Paragraph below, or both.

        - Samples for Initial Selection: Manufacturer's standard color sheets, showing full range of available colors for each type of product.

        - Samples for Verification: For each type of finish system and in each color and gloss of finish required.

          - Submit Samples on representative samples of actual wood substrates, [8 inches (200 mm) square] [or] [8 inches (200 mm) long].

          - Apply coats on Samples in steps to show each coat required for system.

          - Label each coat of each Sample.

          - Label each Sample for location and application area.

        - Product List: Cross-reference to finish system and locations of application areas. Use same designations indicated on Drawings and in schedules. Include color designations.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for paints and coatings.>

          - <Double click to insert sustainable design text for EPDs and HPDs.>

          - <Double click here to insert sustainable design text for manufacturer inventory.>

      - MAINTENANCE MATERIAL SUBMITTALS

See Section 017700 "Closeout Procedures" for submission of maintenance material items.

        - Extra Stock Material: Furnish extra materials[, from the same product run,] to Owner that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

Retain "Stains and Transparent Finishes" Subparagraph below for projects that require only limited quantities of extra materials. If necessary, replace percentage with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

          - Stains and Transparent Finishes: [5] <Insert number> percent, but not less than [1 gal. (3.8 L)] <Insert number> of each material and color applied.

      - MOCKUPS

        - Apply mockups of each finish system indicated and each color selected [to verify preliminary selections made under Sample submittals] [to demonstrate aesthetic effects] [and] [to set quality standards for materials and execution].

          - Architect will select one surface to represent surfaces and conditions for application of each type of finish system and substrate.

            - Vertical and Horizontal Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

            - Other Items: Architect will designate items or areas required.

          - Final approval of stain color selections will be based on mockups.

            - If preliminary stain color selections are not approved, apply additional mockups of additional stain colors selected by Architect at no added cost to Owner.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

          - Maintain containers in clean condition, free of foreign materials and residue.

          - Remove rags and waste from storage areas daily.

If necessary, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site.

      - FIELD CONDITIONS

        - Apply finishes only when temperature of surfaces to be finished and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

        - Do not apply finishes when relative humidity exceeds 85 percent, at temperatures of less than 5 deg F (3 deg C) above the dew point, or to damp or wet surfaces.

        - Do not apply exterior finishes in snow, rain, fog, or mist.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - MANUFACTURERS

        - <Double click here to find, evaluate, and insert list of manufacturers and products.>

See lists of products currently approved by MPI in its "MPI Approved Products List," www.paintinfo.com. See "Writing Guide" Article in the Evaluations for further discussion. Retain "Products" Paragraph below and insert lists of manufacturers and products in wood finish system schedules to require specific products or a comparable product from other manufacturers.

        - Products: Subject to compliance with requirements, [provide product] [provide one of the products] [available products that may be incorporated into the Work include, but are not limited to products] listed in wood finish systems schedules for the product category indicated.

      - SOURCE LIMITATIONS

Retain this article to limit sources for the entire Section. Source limitations may also be specified in individual articles if desired.

        - Source Limitations: Obtain each coating product from single source from single manufacturer.

      - MATERIALS, GENERAL

        - MPI Standards: Products shall comply with MPI standards indicated and shall be listed in its "MPI Approved Products List."

Generally, retain "Material Compatibility" Paragraph below. Systems could fail if paints used for individual coats are incompatible.

        - Material Compatibility:

          - Materials for use within each coating system that are compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

        - <Double click to insert sustainable design text for finishes.>

        - Stain Colors: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule] <Insert requirements>.

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

        - Maximum Moisture Content of Exterior Wood Substrates: 15 percent, when measured with an electronic moisture meter.

Coordinate requirement in "Maximum Moisture Content of Interior Wood Substrates" Paragraph below with Sections where wood substrates are specified. Maximum moisture content of interior wood substrates will depend on the type of wood substrates that are to be finished. Kiln-dried finish lumber is available with maximum moisture content of 15 percent for some species and 12 percent for others. Kiln-dried softwood moldings are generally limited to 15 percent moisture content and hardwood moldings to 9 percent. For woodwork, the Architectural Woodwork Institute recommends a maximum moisture content of 13 percent for damp coastal areas and 10 percent for the rest of the United States except for dry southwestern states, for which it recommends 9 percent.

        - Maximum Moisture Content of Interior Wood Substrates: [15] [13] [10] [9] percent, when measured with an electronic moisture meter.

        - Verify suitability of substrates, including surface conditions and compatibility with existing finishes and primers.

        - Proceed with finish application only after unsatisfactory conditions have been corrected.

          - Beginning finish application constitutes Contractor's acceptance of substrates and conditions.

      - PREPARATION

For renovation projects, consult "MPI Maintenance Repainting Manual" and revise first paragraph below and finish systems specified in the "Exterior Wood-Finish-System Schedule" and "Interior Wood-Finish-System Schedule" articles.

        - Comply with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual" applicable to substrates indicated.

        - Remove hardware, covers, plates, and similar items already in place that are removable. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and finishing.

          - After completing finishing operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection if any.

        - Clean and prepare surfaces to be finished according to manufacturer's written instructions for each substrate condition and as specified.

          - Remove dust, dirt, oil, and grease by washing with a detergent solution; rinse thoroughly with clean water and allow to dry. Remove grade stamps and pencil marks by sanding lightly. Remove loose wood fibers by brushing.

          - Remove mildew by scrubbing with a commercial wash formulated for mildew removal and as recommended by stain manufacturer.

        - Exterior Wood Substrates:

          - Scrape and clean knots, and apply coat of knot sealer before applying primer.

          - Prime edges, ends, faces, undersides, and backsides of wood.

            - For solid hide stained wood, stain edges and ends after priming.

            - For varnish-coated stained wood, stain edges and ends and prime with varnish. Prime undersides and backsides with varnish.

Avoid using steel nails under a stain because of rust. Revise subparagraph below if noncorrosive nails are specified in other Sections; delete if not required.

          - Countersink steel nails, if used, and fill with putty or plastic wood filler tinted to final color. Sand smooth when dried.

        - Interior Wood Substrates:

          - Scrape and clean knots, and apply coat of knot sealer before applying primer.

          - Apply wood filler paste to open-grain woods, as defined in "MPI Architectural Painting Specification Manual," to produce smooth, glasslike finish.

          - Sand surfaces exposed to view and dust off.

          - After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dry.

      - APPLICATION

        - Apply finishes according to manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual."

          - Use applicators and techniques suited for finish and substrate indicated.

          - Finish surfaces behind movable equipment and furniture same as similar exposed surfaces.

          - Do not apply finishes over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

        - Apply finishes to produce surface films without cloudiness, holidays, lap marks, brush marks, runs, ropiness, or other surface imperfections.

      - CLEANING AND PROTECTION

        - At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

        - After completing finish application, clean spattered surfaces. Remove spattered materials by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

        - Protect work of other trades against damage from finish application. Correct damage by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

        - At completion of construction activities of other trades, touch up and restore damaged or defaced finished wood surfaces.

      - EXTERIOR WOOD-FINISH-SYSTEM SCHEDULE

Finish systems in this article are based on "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual"). For renovation projects, consult "MPI Maintenance Repainting Manual" and revise finish systems accordingly.

        - Wood Substrates, Glued-Laminated Construction:

          - Solid-Color, Solvent-Based Stain System[ MPI EXT 6.1C]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat. "MPI Manual" does not include a Budget Grade system.

            - Intermediate Coat: Stain, exterior, solvent based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, solid hide[, MPI #14].

              - <Insert manufacturer's name; product name or designation>.

          - Varnish over Semitransparent Stain System[ MPI EXT 6.1D]:

            - Stain Coat: Stain, exterior, solvent based, semitransparent[, MPI #13].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Semigloss," "Topcoat, Gloss," or "Topcoat, High Gloss" Subparagraph below.

            - Topcoat, Semigloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 5)[, MPI #30].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 6)[, MPI #29].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, High Gloss: Varnish, marine spar, exterior (MPI Gloss Level 7)[, MPI #28].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Varnish System[ MPI EXT 6.1M]:

            - Prime Coat: Water-based varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Water-based varnish matching topcoat.

Retain one of first seven subparagraphs below. Verify availability of products with desired MPI Gloss Level before retaining.

            - Topcoat, Flat: Water-based varnish (MPI Gloss Level 1)[, MPI #191].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Velvet: Water-based varnish (MPI Gloss Level 2)[, MPI #192].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Eggshell: Water-based varnish (MPI Gloss Level 3)[, MPI #193].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Satin: Water-based varnish (MPI Gloss Level 4)[, MPI #194].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Water-based varnish (MPI Gloss Level 5)[, MPI #195].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Water-based varnish (MPI Gloss Level 6)[, MPI #196].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, High Gloss: Water-based varnish (MPI Gloss Level 7)[, MPI #197].

              - <Insert manufacturer's name; product name or designation>.

          - Varnish System[ MPI EXT 6.1K]:

            - Prime Coat: Varnish matching topcoat.

            - First Intermediate Coat: Varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Semigloss," "Topcoat, Gloss," or "Topcoat, High Gloss" Subparagraph below.

            - Topcoat, Semigloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 5)[, MPI #30].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 6)[, MPI #29].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, High Gloss: Varnish, marine spar, exterior (MPI Gloss Level 7)[, MPI #28].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Two-Component Polyurethane Varnish over Stain System[ MPI EXT 6.1E]:

            - Stain Coat: Stain, exterior, solvent based, semitransparent[, MPI #13].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Varnish, aliphatic polyurethane, two component, matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish, aliphatic polyurethane, two component, matching topcoat.

            - Topcoat, Gloss: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Two-Component Polyurethane Varnish System[ MPI EXT 6.1H]:

            - Prime Coat: Varnish, aliphatic polyurethane, two component, matching topcoat.

            - Topcoat, Gloss: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, Exposed Framing:

          - Solid-Color, Water-Based Stain System[ MPI EXT 6.2B]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, water based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, water based, solid hide[, MPI #16].

              - <Insert manufacturer's name; product name or designation>.

          - Solid-Color, Solvent-Based Stain System[ MPI EXT 6.2D]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, solvent based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, solid hide[, MPI #14].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Semitransparent Stain System[ MPI EXT 6.2P]:

            - Prime Coat: Stain, exterior, water based, semitransparent, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, water based, semitransparent, matching topcoat.

            - Topcoat: Stain, exterior, water based, semitransparent[, MPI #156].

              - <Insert manufacturer's name; product name or designation>.

          - Semitransparent Stain System[ MPI EXT 6.2L]:

            - Prime Coat: Stain, exterior, solvent based, semitransparent, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, semitransparent[, MPI #13].

              - <Insert manufacturer's name; product name or designation>.

          - Varnish over Stain System[ MPI EXT 6.2E]:

            - Stain Coat: Stain, exterior, solvent based, semitransparent[, MPI #13].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Semigloss," "Topcoat, Gloss," or "Topcoat, High Gloss" Subparagraph below.

            - Topcoat, Semigloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 5)[, MPI #30].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 6)[, MPI #29].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, High Gloss: Varnish, marine spar, exterior (MPI Gloss Level 7)[, MPI #28].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Varnish System[ MPI EXT 6.2N]:

            - Prime Coat: Water-based varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Water-based varnish matching topcoat.

Retain one of first seven subparagraphs below. Verify availability of products with desired MPI Gloss Level before retaining.

            - Topcoat, Flat: Water-based varnish (MPI Gloss Level 1)[, MPI #191].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Velvet: Water-based varnish (MPI Gloss Level 2)[, MPI #192].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Eggshell: Water-based varnish (MPI Gloss Level 3)[, MPI #193].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Satin: Water-based varnish (MPI Gloss Level 4)[, MPI #194].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Water-based varnish (MPI Gloss Level 5)[, MPI #195].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Water-based varnish (MPI Gloss Level 6)[, MPI #196].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, High Gloss: Water-based varnish (MPI Gloss Level 7)[, MPI #197].

              - <Insert manufacturer's name; product name or designation>.

          - Varnish System[ MPI EXT 6.2K]:

            - Prime Coat: Varnish matching topcoat.

            - First Intermediate Coat: Varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Semigloss," "Topcoat, Gloss," or "Topcoat, High Gloss" Subparagraph below.

            - Topcoat, Semigloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 5)[, MPI #30].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 6)[, MPI #29].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, High Gloss: Varnish, marine spar, exterior (MPI Gloss Level 7)[, MPI #28].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Two-Component Polyurethane Varnish System[ MPI EXT 6.2Q]:

            - Prime Coat: Varnish, aliphatic polyurethane, two component, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat and does not include a Budget Grade system.

            - Intermediate Coat: Varnish, aliphatic polyurethane, two component, matching topcoat.

            - Topcoat, Gloss or High Gloss: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, [Wood Trim] [Architectural Woodwork] [Doors] [Windows] [Wood Board Siding] [and] [Wood Fences]:

          - Solid-Color, Water-Based Stain System[ MPI EXT 6.3K]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, water based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, water based, solid hide[, MPI #16].

              - <Insert manufacturer's name; product name or designation>.

          - Solid-Color, Solvent-Based Stain System[ MPI EXT 6.3C]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, solvent based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, solid hide[, MPI #14].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Semitransparent Stain System[ MPI EXT 6.3N]:

            - Prime Coat: Stain, exterior, water based, semitransparent, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, water based, semitransparent, matching topcoat.

            - Topcoat: Stain, exterior, water based, semitransparent[, MPI #156].

              - <Insert manufacturer's name; product name or designation>.

          - Semitransparent Stain System[ MPI EXT 6.3D]:

            - Prime Coat: Stain, exterior, solvent based, semitransparent, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, semitransparent[, MPI #13].

              - <Insert manufacturer's name; product name or designation>.

          - Varnish over Stain System[ MPI EXT 6.3E]:

            - Stain Coat: Stain, exterior, solvent-based, semitransparent[, MPI #13].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Semigloss," "Topcoat, Gloss," or "Topcoat, High Gloss" Subparagraph below.

            - Topcoat, Semigloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 5)[, MPI #30].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 6)[, MPI #29].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, High Gloss: Varnish, marine spar, exterior (MPI Gloss Level 7)[, MPI #28].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Varnish System[ MPI EXT 6.3M]:

            - Prime Coat: Water-based varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Water-based varnish matching topcoat.

Retain one of first seven subparagraphs below. Verify availability of products with desired MPI Gloss Level before retaining.

            - Topcoat, Flat: Water-based varnish (MPI Gloss Level 1)[, MPI #191].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Velvet: Water-based varnish (MPI Gloss Level 2)[, MPI #192].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Eggshell: Water-based varnish (MPI Gloss Level 3)[, MPI #193].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Satin: Water-based varnish (MPI Gloss Level 4)[, MPI #194].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Water-based varnish (MPI Gloss Level 5)[, MPI #195].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Water-based varnish (MPI Gloss Level 6)[, MPI #196].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, High gloss: Water-based varnish (MPI Gloss Level 7)[, MPI #197].

              - <Insert manufacturer's name; product name or designation>.

          - Varnish System[ MPI EXT 6.3F]:

            - Prime Coat: Varnish matching topcoat.

            - First Intermediate Coat: Varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Semigloss," "Topcoat, Gloss," or "Topcoat, High Gloss" Subparagraph below.

            - Topcoat, Semigloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 5)[, MPI #30].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 6)[, MPI #29].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, High Gloss: Varnish, marine spar, exterior (MPI Gloss Level 7)[, MPI #28].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Two-Component Polyurethane Varnish System[ MPI EXT 6.3G]:

            - Prime Coat: Varnish, aliphatic polyurethane, two component, matching topcoat.

            - Topcoat: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, Wood-Based Panel Products:

          - Solid-Color, Water-Based Stain System[ MPI EXT 6.4A]:

Retain "Prime Coat, Latex" or "Prime Coat, Alkyd" Subparagraph below.

            - Prime Coat, Latex: Primer, latex for exterior wood[, MPI #6].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat, Alkyd: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, water based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, water based, solid hide[, MPI #16].

              - <Insert manufacturer's name; product name or designation>.

          - Solid-Color, Solvent-Based Stain System[ MPI EXT 6.4C]:

For a Premium Grade system, "MPI Manual" requires prime coat; delete "Prime Coat" Subparagraph below for a Budget Grade system.

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Stain, exterior, solvent based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, solid hide[, MPI #14].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Semitransparent Stain System[ MPI EXT 6.4L]:

            - Prime Coat: Stain, exterior, water based, semitransparent, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, water based, semitransparent, matching topcoat.

            - Topcoat: Stain, exterior, water based, semitransparent[, MPI #156].

              - <Insert manufacturer's name; product name or designation>.

          - Semitransparent Stain System[ MPI EXT 6.4D]:

            - Prime Coat: Stain, exterior, solvent based, semitransparent, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, semitransparent[, MPI #13].

              - <Insert manufacturer's name; product name or designation>.

          - Varnish over Stain System[ MPI EXT 6.4J]:

            - Stain Coat: Stain, exterior, solvent based, semitransparent[, MPI #13].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Semigloss," "Topcoat, Gloss," or "Topcoat, High Gloss" Subparagraph below.

            - Topcoat, Semigloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 5)[, MPI #30].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 6)[, MPI #29].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, High Gloss: Varnish, marine spar, exterior (MPI Gloss Level 7)[, MPI #28].

              - <Insert manufacturer's name; product name or designation>.

          - Varnish System[ MPI EXT 6.4H]:

            - Prime Coat: Varnish matching topcoat.

            - First Intermediate Coat: Varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Semigloss," "Topcoat, Gloss," or "Topcoat, High Gloss" Subparagraph below.

            - Topcoat, Semigloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 5)[, MPI #30].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, with UV inhibitor, exterior (MPI Gloss Level 6)[, MPI #29].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, High Gloss: Varnish, marine spar, exterior (MPI Gloss Level 7)[, MPI #28].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, Traffic Surfaces, Including [Lumber Decking] [and] [Stairs]:

          - Deck Stain over Wood Preservative System[ MPI EXT 6.5D]:

            - Preservative Coat: Preservative, for exterior wood[, MPI #37].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, for exterior wood decks, matching topcoat.

            - Top coat: Stain, for exterior wood decks[, MPI #33].

              - <Insert manufacturer's name; product name or designation>.

          - Deck Stain System[ MPI EXT 6.5F]:

            - Prime Coat: Stain, for exterior wood decks, matching topcoat.

            - Top coat: Stain, for exterior wood decks[, MPI #33].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, Wood Shingles and Shakes (Excluding Roofs):

          - Solid-Color, Water-Based Stain System[ MPI EXT 6.6D]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, water based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, water based, solid hide[, MPI #16].

              - <Insert manufacturer's name; product name or designation>.

          - Solid-Color, Solvent-Based Stain System[ MPI EXT 6.6C]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, solvent based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, solid hide[, MPI #14].

              - <Insert manufacturer's name; product name or designation>.

          - Semitransparent Stain System[ MPI EXT 6.6F]:

            - Prime Coat: Stain, exterior, solvent based, semitransparent, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, semitransparent[, MPI #13].

              - <Insert manufacturer's name; product name or designation>.

      - INTERIOR WOOD -FINISH-SYSTEM SCHEDULE

Finish systems in this article are based on "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual"). For renovation projects, consult "MPI Maintenance Repainting Manual" and revise finish systems accordingly.

        - Wood Substrates, Glued-Laminated Construction:

          - Solid-Color Latex Stain System[ MPI INT 6.1T]:

            - Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, water based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, water based, solid hide[, MPI #16].

              - <Insert manufacturer's name; product name or designation>.

          - Solid-Color, Solvent-Based Stain System[ MPI INT 6.1H]:

            - Prime Coat: Stain, exterior, solvent based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, solid hide[, MPI #14].

              - <Insert manufacturer's name; product name or designation>.

          - Semitransparent Stain System[ MPI INT 6.1G]:

            - Prime Coat: Stain, semitransparent, matching topcoat.

            - Topcoat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Varnish over Stain System[ MPI INT 6.1R]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Water-based varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Water-based varnish matching topcoat.

Retain "Topcoat, Satin," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, water based, clear (MPI Gloss Level 4)[, MPI #128].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, water based, clear (MPI Gloss Level 5)[, MPI #129].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, water based, clear (MPI Gloss Level 6)[, MPI #130].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Varnish System[ MPI INT 6.1F]:

            - Prime Coat: Water-based varnish matching topcoat.

            - Intermediate Coat: Water-based varnish matching topcoat.

Retain "Topcoat, Satin," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, water based, clear (MPI Gloss Level 4)[, MPI #128].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, water based, clear (MPI Gloss Level 5)[, MPI #129].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, water based, clear (MPI Gloss Level 6)[, MPI #130].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Varnish over Stain System[ MPI INT 6.1K] [ MPI INT 6.1P]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

Retain "First Intermediate Coat, Varnish" or "First Intermediate Coat, Sanding Sealer" Subparagraph below. First corresponds to MPI INT 6.1K; second corresponds to MPI INT 6.1P.

            - First Intermediate Coat, Varnish: Varnish matching topcoat.

            - First Intermediate Coat, Sanding Sealer: Alkyd, sanding sealer, clear[, MPI #102].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Flat," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Flat: Varnish, interior (MPI Gloss Level 1)[, MPI #73].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, interior (MPI Gloss Level 5)[, MPI #74].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior (MPI Gloss Level 6)[, MPI #75].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Varnish System[ MPI INT 6.1C]:

            - Prime Coat: Alkyd, sanding sealer, clear[, MPI #102].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Flat," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Flat: Varnish, interior (MPI Gloss Level 1)[, MPI #73].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, interior (MPI Gloss Level 5)[, MPI #74].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior (MPI Gloss Level 6)[, MPI #75].

              - <Insert manufacturer's name; product name or designation>.

          - Polyurethane Varnish over Stain System[ MPI INT 6.1J]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Polyurethane varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Polyurethane varnish matching topcoat.

Retain "Topcoat, Satin" or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 4)[, MPI #57].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 6)[, MPI #56].

              - <Insert manufacturer's name; product name or designation>.

          - Polyurethane Varnish System[ MPI INT 6.1D]:

            - Prime Coat: Polyurethane varnish matching topcoat.

            - Intermediate Coat: Polyurethane varnish matching topcoat.

Retain "Topcoat, Satin" or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 4)[, MPI #57].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 6)[, MPI #56].

              - <Insert manufacturer's name; product name or designation>.

          - Moisture-Cured Clear Polyurethane over Stain System[ MPI INT 6.1S]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Moisture-cured polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Moisture-cured polyurethane matching topcoat.

            - Topcoat, Gloss: Varnish, polyurethane, moisture cured (MPI Gloss Level 6)[, MPI #31].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Two-Component Polyurethane System[ MPI INT 6.1W]:

            - Prime Coat: Two-component polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Two-component polyurethane matching topcoat.

            - Topcoat, Gloss or High Gloss: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or MPI Gloss Level 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, Exposed Framing:

          - Water-Based Varnish over Stain System[ MPI INT 6.2M]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Water-based varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Water-based varnish matching topcoat.

Retain "Topcoat, Satin," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, water based, clear (MPI Gloss Level 4)[, MPI #128].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, water based, clear (MPI Gloss Level 5)[, MPI #129].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, water based, clear (MPI Gloss Level 6)[, MPI #130].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Varnish over Stain System[ MPI INT 6.2K]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Alkyd, sanding sealer, clear[, MPI #102].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Flat," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Flat: Varnish, interior (MPI Gloss Level 1)[, MPI #73].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, interior (MPI Gloss Level 5)[, MPI #74].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior (MPI Gloss Level 6)[, MPI #75].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Varnish System[ MPI INT 6.2P]:

            - Prime Coat: Alkyd, sanding sealer, clear[, MPI #102].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Flat," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Flat: Varnish, interior (MPI Gloss Level 1)[, MPI #73].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, interior (MPI Gloss Level 5)[, MPI #74].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior (MPI Gloss Level 6)[, MPI #75].

              - <Insert manufacturer's name; product name or designation>.

          - Polyurethane Varnish over Stain System[ MPI INT 6.2J]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Polyurethane varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Polyurethane varnish matching topcoat.

Retain "Topcoat, Satin" or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 4)[, MPI #57].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 6)[, MPI #56].

              - <Insert manufacturer's name; product name or designation>.

          - Polyurethane Varnish System[ MPI INT 6.2H]:

            - Prime Coat: Polyurethane varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane varnish matching topcoat.

Retain "Topcoat, Satin" or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 4)[, MPI #57].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 6)[, MPI #56].

              - <Insert manufacturer's name; product name or designation>.

          - Moisture-Cured Clear Polyurethane over Stain System[ MPI INT 6.2N]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Moisture-cured polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Moisture-cured polyurethane matching topcoat.

            - Topcoat, Gloss: Varnish, polyurethane, moisture cured (MPI Gloss Level 6)[, MPI #31].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Two-Component Polyurethane System[ MPI INT 6.2Q]:

            - Prime Coat: Two-component polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Two-component polyurethane matching topcoat.

            - Topcoat, Gloss or High Gloss: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or MPI Gloss Level 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, [Wood Trim] [Architectural Woodwork] [Doors] [Windows] [and] [Wood Board Paneling]:

          - Semitransparent Stain System[ MPI INT 6.3C]:

            - Prime Coat: Stain, exterior, solvent based, semitransparent, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, semitransparent[, MPI #13].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Varnish over Stain System[ MPI INT 6.3W]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Water-based varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Water-based varnish matching topcoat.

Retain "Topcoat, Satin," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, water based, clear (MPI Gloss Level 4)[, MPI #128].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, water based, clear (MPI Gloss Level 5)[, MPI #129].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, water based, clear (MPI Gloss Level 6)[, MPI #130].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Varnish System[ MPI INT 6.3Q]:

            - Prime Coat: Water-based varnish matching topcoat.

            - Intermediate Coat: Water-based varnish matching topcoat.

Retain "Topcoat, Satin," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, water based, clear (MPI Gloss Level 4)[, MPI #128].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, water based, clear (MPI Gloss Level 5)[, MPI #129].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, water based, clear (MPI Gloss Level 6)[, MPI #130].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Varnish over Stain System[ MPI INT 6.3D]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

Retain "First Intermediate Coat, Sanding Sealer" or "First Intermediate Coat, Shellac" Subparagraph below.

            - First Intermediate Coat, Sanding Sealer: Alkyd, sanding sealer, clear[, MPI #102].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat, Shellac: Shellac, clear[, MPI #88].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Flat," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Flat: Varnish, interior (MPI Gloss Level 1)[, MPI #73].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, interior (MPI Gloss Level 5)[, MPI #74].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior (MPI Gloss Level 6)[, MPI #75].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Varnish System[ MPI INT 6.3J]:

Retain "Prime Coat, Sanding Sealer" or "Prime Coat, Shellac" Subparagraph below.

            - Prime Coat, Sanding Sealer: Alkyd, sanding sealer, clear[, MPI #102].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat, Shellac: Shellac, clear[, MPI #88].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Flat," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Flat: Varnish, interior (MPI Gloss Level 1)[, MPI #73].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, interior (MPI Gloss Level 5)[, MPI #74].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior (MPI Gloss Level 6)[, MPI #75].

              - <Insert manufacturer's name; product name or designation>.

          - Polyurethane Varnish over Stain System[ MPI INT 6.3E]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Polyurethane varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Polyurethane varnish matching topcoat.

Retain "Topcoat, Satin" or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 4)[, MPI #57].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 6)[, MPI #56].

              - <Insert manufacturer's name; product name or designation>.

          - Polyurethane Varnish System[ MPI INT 6.3K]:

            - Prime Coat: Polyurethane varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane varnish matching topcoat.

Retain "Topcoat, Satin" or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 4)[, MPI #57].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 6)[, MPI #56].

              - <Insert manufacturer's name; product name or designation>.

          - Moisture-Cured Clear Polyurethane over Stain System[ MPI INT 6.3Y]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Moisture-cured polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Moisture-cured polyurethane matching topcoat.

            - Topcoat, Gloss: Varnish, polyurethane, moisture cured (MPI Gloss Level 6)[, MPI #31].

              - <Insert manufacturer's name; product name or designation>.

          - Moisture-Cured Clear Polyurethane System[ MPI INT 6.3X]:

            - Prime Coat: Moisture-cured polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Moisture-cured polyurethane matching topcoat.

            - Topcoat, Gloss: Varnish, polyurethane, moisture cured (MPI Gloss Level 6)[, MPI #31].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Two-Component Polyurethane System[ MPI INT 6.3Z]:

            - Prime Coat: Two-component polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Two-component polyurethane matching topcoat.

            - Topcoat: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or MPI Gloss Level 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

          - Danish Oil System[ MPI INT 6.3M]:

            - Prime Coat: Danish oil matching topcoat.

            - Topcoat: Danish oil[, MPI #92].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, [Wood Paneling] [and] [Casework].

          - Semitransparent Stain System[ MPI INT 6.4C]:

            - Prime Coat: Stain, exterior, solvent based, semitransparent, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, semitransparent[, MPI #13].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Varnish over Stain System[ MPI INT 6.4U]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Water-based varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Water-based varnish matching topcoat.

Retain "Topcoat, Satin," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, water based, clear (MPI Gloss Level 4)[, MPI #128].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, water based, clear (MPI Gloss Level 5)[, MPI #129].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, water based, clear (MPI Gloss Level 6)[, MPI #130].

              - <Insert manufacturer's name; product name or designation>.

          - Water-Based Varnish System[ MPI INT 6.4M]:

            - Prime Coat: Water-based varnish matching topcoat.

            - Intermediate Coat: Water-based varnish matching topcoat.

Retain "Topcoat, Satin," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, water based, clear (MPI Gloss Level 4)[, MPI #128].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, water based, clear (MPI Gloss Level 5)[, MPI #129].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, water based, clear (MPI Gloss Level 6)[, MPI #130].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Varnish over Stain System[ MPI INT 6.4D]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

Retain "First Intermediate Coat, Sanding Sealer" or "First Intermediate Coat, Shellac" Subparagraph below.

            - First Intermediate Coat, Sanding Sealer: Alkyd, sanding sealer, clear[, MPI #102].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat, Shellac: Shellac, clear[, MPI #88].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Flat," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Flat: Varnish, interior (MPI Gloss Level 1)[, MPI #73].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, interior (MPI Gloss Level 5)[, MPI #74].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior (MPI Gloss Level 6)[, MPI #75].

              - <Insert manufacturer's name; product name or designation>.

          - Alkyd Varnish System[ MPI INT 6.4G]:

Retain "Prime Coat, Sanding Sealer" or "Prime Coat, Shellac" Subparagraph below.

            - Prime Coat, Sanding Sealer: Alkyd, sanding sealer, clear[, MPI #102].

              - <Insert manufacturer's name; product name or designation>.

            - Prime Coat, Shellac: Shellac, clear[, MPI #88].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Varnish matching topcoat.

Retain "Topcoat, Flat," "Topcoat, Semigloss," or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Flat: Varnish, interior (MPI Gloss Level 1)[, MPI #73].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Semigloss: Varnish, interior (MPI Gloss Level 5)[, MPI #74].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior (MPI Gloss Level 6)[, MPI #75].

              - <Insert manufacturer's name; product name or designation>.

          - Polyurethane Varnish over Stain System[ MPI INT 6.4E]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Polyurethane varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Polyurethane varnish matching topcoat.

Retain "Topcoat, Satin" or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 4)[, MPI #57].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 6)[, MPI #56].

              - <Insert manufacturer's name; product name or designation>.

          - Polyurethane Varnish System[ MPI INT 6.4J]:

            - Prime Coat: Polyurethane varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane varnish matching topcoat.

Retain "Topcoat, Satin" or "Topcoat, Gloss" Subparagraph below.

            - Topcoat, Satin: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 4)[, MPI #57].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat, Gloss: Varnish, interior, polyurethane, oil modified (MPI Gloss Level 6)[, MPI #56].

              - <Insert manufacturer's name; product name or designation>.

          - Moisture-Cured Clear Polyurethane over Stain System[ MPI INT 6.4V]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Moisture-cured polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Moisture-cured polyurethane matching topcoat.

            - Topcoat: Varnish, polyurethane, moisture cured, gloss (MPI Gloss Level 6)[, MPI #31].

              - <Insert manufacturer's name; product name or designation>.

          - Danish Oil System[ MPI INT 6.4K]:

            - Prime Coat: Danish oil matching topcoat.

            - Topcoat: Danish oil[, MPI #92].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrate, Traffic Surfaces, Including [Floors] [and] [Stairs]:

          - Polyurethane Varnish over Stain System[ MPI INT 6.5B]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Polyurethane varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Polyurethane varnish matching topcoat.

            - Topcoat: Varnish, interior, polyurethane, oil modified, gloss (MPI Gloss Level 6)[, MPI #56].

              - <Insert manufacturer's name; product name or designation>.

          - Polyurethane Varnish System[ MPI INT 6.5C]:

            - Prime Coat: Polyurethane varnish matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane varnish matching topcoat.

            - Topcoat: Varnish, interior, polyurethane, oil modified, gloss (MPI Gloss Level 6)[, MPI #56].

              - <Insert manufacturer's name; product name or designation>.

          - Moisture-Cured Clear Polyurethane over Stain System[ MPI INT 6.5J]:

            - Stain Coat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

            - First Intermediate Coat: Moisture-cured polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires second intermediate coat; delete "Second Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Second Intermediate Coat: Moisture-cured polyurethane matching topcoat.

            - Topcoat: Varnish, polyurethane, moisture cured, gloss (MPI Gloss Level 6)[, MPI #31].

              - <Insert manufacturer's name; product name or designation>.

          - Moisture-Cured Clear Polyurethane System[ MPI INT 6.5K]:

            - Prime Coat: Moisture-cured polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Moisture-cured polyurethane matching topcoat.

            - Topcoat: Varnish, polyurethane, moisture cured, gloss (MPI Gloss Level 6)[, MPI #31].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Two-Component Polyurethane System[ MPI INT 6.5M]:

            - Prime Coat: Two-component polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Two-component polyurethane matching topcoat.

            - Topcoat: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or MPI Gloss Level 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, Wood Shingles and Shakes:

          - Solid-Color Latex Stain System[ MPI INT 6.6E]:

            - Prime Coat: Primer, latex for exterior wood[, MPI #6].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Stain, exterior, water based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, water based, solid hide[, MPI #16].

              - <Insert manufacturer's name; product name or designation>.

          - Solid-Color, Solvent-Based Stain System[ MPI INT 6.6D]:

For a Premium Grade system, "MPI Manual" requires prime coat; delete "Prime Coat" Subparagraph below for a Budget Grade system.

            - Prime Coat: Stain, exterior, solvent based, solid hide, matching topcoat.

            - Topcoat: Stain, exterior, solvent based, solid hide[, MPI #14].

              - <Insert manufacturer's name; product name or designation>.

          - Semitransparent Stain System[ MPI INT 6.6C]:

            - Prime Coat: Stain, semitransparent, matching topcoat.

            - Topcoat: Stain, semitransparent, for interior wood[, MPI #90].

              - <Insert manufacturer's name; product name or designation>.

END OF SECTION 099301