Copyright 2014 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 099419 - MULTICOLOR INTERIOR FINISHING

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section includes surface preparation and field application of multicolor interior finishing systems[.] [applied on the following substrates:]

          - Vertical concrete.

          - Cementitious composition board.

          - Clay masonry units.

          - Concrete masonry units (CMU).

          - Wood.

          - Fiberglass moldings and trim.

          - Plastic moldings and trim.

          - Plaster.

          - Gypsum veneer plaster.

          - Gypsum board.

        - Related Requirements:

Retain subparagraph below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 099123 "Interior Painting" for special-use coatings and general field painting.

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for coatings.>

Retain "Samples" Paragraph below for single-stage Samples. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples.

        - Samples: For each exposed product and for each color and texture specified, 8 inches (200 mm) square in size.

        - Samples for Initial Selection: For each multicolor finishing system indicated.

        - Samples for Verification: For each multicolor finishing system and in each color, pattern, and pigment density indicated.

          - Submit Samples on rigid backing, 8 inches (200 mm) square.

          - Label each Sample for location and application area.

        - Product Schedule: For multicolor finishing systems.[ Use same designations indicated on Drawings.]

      - QUALITY ASSURANCE

        - Mockups: Apply mockup of each coating system indicated to verify preliminary selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for materials and execution.

          - Architect will select one surface to represent surfaces and conditions for application of each coating system and type of substrate.

            - Wall Surfaces: Provide mockups of at least 100 sq. ft. (9 sq. m).

            - Other Items: Architect will designate items or areas required.

          - Apply mockup after permanent lighting and other environmental services have been activated.

          - Final approval of color and pattern selections will be based on mockup.

            - If preliminary color and pattern selections are not approved, apply additional mockups of colors and patterns selected by Architect at no added cost to Owner.

          - Repair Mockup: After approval of color and pattern selections, apply representative repairs to 100 sq. in. (645 sq. cm) of mockup to establish quality standards for coating system repairs.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Store materials in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

          - Maintain containers in clean condition, free of foreign materials and residue.

          - Remove rags and waste from storage areas daily.

If necessary, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site.

      - FIELD CONDITIONS

        - Environmental Limitations: Do not apply coatings until spaces are enclosed and weatherproof, work above ceilings is complete, and ambient temperature and humidity conditions are maintained at the levels indicated for Project when occupied for its intended use.

- PRODUCTS

Manufacturers and products listed in SpecAgent and Masterworks Paragraph Builder are neither recommended nor endorsed by the AIA or Deltek. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

To efficiently edit Part 2, first edit "Multicolor Interior Finishing Schedule" Article at the end of Part 3. Then retain, delete, and insert appropriate products in Part 2 to coordinate with coating systems retained in Part 3.

      - MULTICOLOR FINISHING SYSTEMS

For renovation projects, consult "MPI Maintenance Repainting Manual" and revise "Master Painters Institute (MPI) Standards" Paragraph below and systems specified in "Multicolor Interior Finishing Schedule" Article.

        - Master Painters Institute (MPI) Standards: Comply with recommendations in "MPI Architectural Painting Specification Manual" applicable to products and coating systems indicated.

Usually retain "Material Compatibility" Paragraph below. Systems could fail if coats are incompatible.

        - Material Compatibility: Provide materials for use within each coating system that are compatible with one another and substrates indicated under conditions of service and application, as demonstrated by manufacturer based on testing and field experience.

        - <Double click to insert sustainable design text for paints.>

        - Colors and Patterns: [Match Architect's samples] [As selected by Architect from manufacturer's full range] [As indicated in finish schedule] <Insert requirements>.

      - MULTICOLOR COATINGS

        - Multicolor Coating: Water- or solvent-based coat that provides a decorative polychromatic finish.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

If retaining "Clear Topcoat" Paragraph below, coordinate with multicolor coating products.

        - Clear Topcoat: Water-based, clear acrylic co-polymer emulsion or solvent-based, clear acrylic solution binder product recommended by multicolor coating manufacturer for use in multicolor coating system indicated to add surface abrasion and detergent resistance.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

      - FILLERS AND PRIMERS

Coordinate products retained in this article with substrates and coating systems retained in "Multicolor Interior Finishing Schedule" Article at end of Part 3.

        - Fillers, sealers, and primers recommended in writing for use in coating systems by manufacturer of multicolor interior coating on substrates and under conditions indicated.

        - Latex Block Filler: Waterborne, high-solids, emulsion-type, pigmented coating product recommended in writing for use in coating system indicated by manufacturer of multicolor interior coating, with bridging and filling properties, and formulated for filling surfaces of CMU for subsequent applications of finish coatings.

        - Wood Filler Paste: Solvent-based, high-solids, clear paste product recommended in writing for use in coating system indicated by manufacturer of multicolor interior coating, for use on open-grained or damaged woods. The paste fills hardwood pores with minimal surface residues and without showing cracking or shrinkage. Sanding dried filler produces a smooth surface without clogging or gumming sandpaper.

        - Wood-Knot Sealer: White shellac or other sealer recommended in writing for this purpose by manufacturer of multicolor interior coating.

        - Primer/Sealer for Multicolor Systems: Acrylic or acrylic/polyvinyl acetate (PVA) co-polymer emulsion-type, pigmented primer/sealer product recommended in writing for use in coating system indicated by manufacturer of multicolor interior coating.

        - Interior Alkyd Primer/Sealer: Solvent-based, pigmented primer/sealer.

        - Water-Based Bonding Primer: Water-based, emulsion-type, pigmented primer product recommended in writing for use in coating system indicated by manufacturer of multicolor interior coating, and formulated to promote adhesion of subsequent coatings.

        - Solvent-Based Bonding Primer: Solvent-based, pigmented product recommended in writing for use in coating system indicated by manufacturer of multicolor interior coating, and formulated to promote adhesion of subsequent coatings to substrate.

- EXECUTION

      - EXAMINATION

        - Examine substrates, areas, and conditions, with Applicator present, for compliance with requirements and conditions affecting performance of coatings.

Percentage listed in "Maximum Moisture Content of Substrates" Subparagraph below is based on "MPI Architectural Painting Specification Manual."

          - Maximum Moisture Content of Substrates: 12 percent, measured with an electronic moisture meter.

          - Gypsum Board Substrates: Verify that finishing compound is sanded smooth.

          - Plaster Substrates: Verify that plaster is fully cured.

          - Verify compatibility with and suitability of substrates, including compatibility with existing finishes or primers.

          - Begin coating application only after unsatisfactory conditions have been corrected.

          - Beginning coating application indicates acceptance of surfaces and conditions.

      - PREPARATION

        - Comply with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual" applicable to substrates indicated.

        - Remove hardware, covers, plates, and similar items already in place that are removable and are not to be coated. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and coating.

          - After completing coating operations, reinstall items that were removed; use workers skilled in the trades involved.

        - Clean substrates of substances that could impair bond of coatings, including dust, dirt, oil, grease, and incompatible primers, paints, and encapsulants.

        - Concrete Substrates: Remove release agents, curing compounds, efflorescence, and chalk. Do not coat surfaces if moisture content or alkalinity of surfaces to be coated exceeds that permitted in manufacturer's written instructions.

        - Masonry Substrates: Remove efflorescence and chalk. Do not coat surfaces if moisture content of surfaces or if alkalinity of surfaces or mortar joints exceeds that permitted in manufacturer's written instructions.

        - Wood Substrates:

          - Scrape and clean small, dry, seasoned knots, and apply a thin coat of knot sealer before applying primer.

          - Sand surfaces that will be exposed to view; remove sanding dust from surfaces to be coated.

          - Prime edges, ends, faces, undersides, and backsides of wood.

          - After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dried and remove sanding dust.

      - APPLICATION

        - Apply coatings according to manufacturer's written instructions using applicators and techniques suited for coating and substrate indicated.

        - Coat surfaces behind movable equipment and furniture the same as similar exposed surfaces. Before final installation, coat surfaces behind permanently fixed equipment or furniture with prime coat only.

        - Coat backsides of access panels, removable or hinged covers, and similar hinged items to match exposed surfaces.

        - Apply coating systems to produce uniformly textured, colored, and patterned finished-surface films without substrates, undercoats, marks, or stains showing through. Produce sharp, even glass lines and color breaks.

      - CLEANING AND PROTECTION

        - At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

        - After completing coating application, clean spattered surfaces. Remove spattered coatings by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

        - Protect work of other trades against damage from coating operation. Correct damage by cleaning, repairing, replacing, and recoating, as approved by Architect, and leave in an undamaged condition.

        - At completion of construction activities of other trades, touch up and restore damaged or defaced coated surfaces.

      - DEMONSTRATION

Retain this article if Owner employs personnel to maintain interior finishes.

        - Train Owner's maintenance personnel in proper applicators and techniques for repairing multicolored interior coating systems on substrates indicated.

      - MULTICOLOR INTERIOR FINISHING SCHEDULE

Coating system designations referenced in editor's notes in this article refer to coating systems listed in the "MPI Architectural Painting Specification Manual." For renovation projects, consult "MPI Maintenance Repainting Manual" and revise coating system requirements accordingly.

Coordinate substrates and coating systems retained in this article with products retained in Part 2.

        - Vertical Concrete Substrates:

System below corresponds to MPI INT 3.1H, which requires clear topcoat for a Premium Grade system and omits topcoat for a Custom Grade system. Premium Grade is not available from every manufacturer.

          - Prime Coat: Primer/sealer for multicolor systems.

          - Multicolor Base Coat: Multicolor coating.

          - Multicolor Pattern Coat: Multicolor coating.

          - Topcoat: Clear topcoat.

        - Cementitious Composition Board Substrates:

System below corresponds to MPI INT 3.3F, which requires clear topcoat for a Premium Grade system and omits topcoat for a Custom Grade system. Premium Grade is not available from every manufacturer.

          - Prime Coat: Primer/sealer for multicolor systems.

          - Multicolor Base Coat: Multicolor coating.

          - Multicolor Pattern Coat: Multicolor coating.

          - Topcoat: Clear topcoat.

        - Clay Masonry Unit Substrates:

System below corresponds to MPI INT 4.1H, which requires clear topcoat for a Premium Grade system and omits topcoat for a Custom Grade system. Premium Grade is not available from every manufacturer.

          - Prime Coat: Primer/sealer for multicolor systems tinted to match multicolor basecoat.

          - Multicolor Base Coat: Multicolor coating.

          - Multicolor Pattern Coat: Multicolor coating.

          - Topcoat: Clear topcoat.

        - CMU Substrates:

System below corresponds to MPI INT 4.2H, which requires clear topcoat for a Premium Grade system and omits topcoat for a Custom Grade system. Premium Grade is not available from every manufacturer.

          - Block Filler: Latex block filler.

          - Prime Coat: Primer/sealer for multicolor systems.

          - Multicolor Base Coat: Multicolor coating.

          - Multicolor Pattern Coat: Multicolor coating.

          - Topcoat: Clear topcoat.

        - Wood Substrates:

System below corresponds to MPI INT 6.2E, MPI INT 6.3N, and MPI INT 6.4L, which require clear topcoat for a Premium Grade system and omit topcoat for a Custom Grade system. Premium Grade is not available from every manufacturer.

"Fill Coat" Subparagraph below is an optional component and is for use on open-grained woods where a smooth, glasslike finish is required.

          - Fill Coat: Wood filler paste.

Prime coat must be tinted to comply with MPI INT 6.3N for dressed lumber (finished carpentry).

          - Prime Coat: Interior alkyd primer/sealer[ tinted to match multicolor base coat].

          - Multicolor Base Coat: Multicolor coating.

          - Multicolor Pattern Coat: Multicolor coating.

          - Topcoat: Clear topcoat.

        - Fiberglass Molding and Trim Substrates:

System below corresponds to MPI INT 6.7G, which requires clear topcoat for a Premium Grade system and omits clear topcoat for a Custom Grade system. Premium Grade is not available from every manufacturer.

          - Prime Coat: [Water] [Solvent]-based bonding primer.

          - Multicolor Base Coat: Multicolor coating.

          - Multicolor Pattern Coat: Multicolor coating.

          - Topcoat: Clear topcoat.

        - Plastic Molding and Trim Substrates:

System below corresponds to MPI INT 6.8D, which requires clear topcoat for a Premium Grade system and omits topcoat for a Custom Grade system. Premium Grade is not available from every manufacturer.

          - Prime Coat: Solvent-based bonding primer.

          - Multicolor Base Coat: Multicolor coating.

          - Multicolor Pattern Coat: Multicolor coating.

          - Topcoat: Clear topcoat.

        - Gypsum Board Substrates:

System below corresponds to MPI INT 9.2G, which requires clear topcoat for a Premium Grade system and omits topcoat for a Custom Grade system. Premium Grade is not available from every manufacturer.

          - Prime Coat: Primer/sealer for multicolor systems.

          - Multicolor Base Coat: Multicolor coating.

          - Multicolor Pattern Coat: Multicolor coating.

          - Topcoat: Clear topcoat.

        - Plaster Substrates:

System below corresponds to MPI INT 9.2G, which requires clear topcoat for a Premium Grade system and omits topcoat for a Custom Grade system. Premium Grade is not available from every manufacturer.

          - Prime Coat: Primer/sealer for multicolor systems.

          - Multicolor Base Coat: Multicolor coating.

          - Multicolor Pattern Coat: Multicolor coating.

          - Topcoat: Clear topcoat.

        - Gypsum Veneer Plaster Substrates:

System below corresponds to MPI INT 9.2G, which requires clear topcoat for a Premium Grade system and omits topcoat for a Custom Grade system. Premium Grade is not available from every manufacturer.

          - Prime Coat: Primer/sealer for multicolor systems.

          - Multicolor Base Coat: Multicolor coating.

          - Multicolor Pattern Coat: Multicolor coating.

          - Topcoat: Clear topcoat.

END OF SECTION 099419