Copyright 2014 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 099600 - HIGH-PERFORMANCE COATINGS

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Access Manufacturer-Provided, AIA MasterSpec-Based Sections:

<Double click here for this Section based on specific manufacturer’s products set as Basis-of-Design at ProductMasterSpec.com.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section includes surface preparation and the application of high-performance coating systems[.][ on the following substrates:]

Revise lists below to suit Project.

          - Exterior Substrates:

            - Concrete, [vertical] [and] [horizontal] surfaces.

            - Fiber-cement board.

            - Clay masonry.

            - Concrete masonry units (CMUs).

            - Steel.

            - Galvanized metal.

            - Aluminum (not anodized or otherwise coated).

            - Copper.

            - Stainless steel.

            - Wood.

            - Fiberglass.

            - Portland cement plaster (stucco).

          - Interior Substrates:

            - Concrete, [vertical] [and] [horizontal] surfaces.

            - Cement board.

            - Clay masonry.

            - Concrete masonry units (CMUs).

            - Steel.

            - Galvanized metal.

            - Aluminum (not anodized or otherwise coated).

            - Wood.

            - Fiberglass.

            - Gypsum board.

            - Plaster.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Primers in other Sections must be coordinated for compatibility with finish coats specified in this Section. Review other Sections for shop-primed exterior products, and insert references to this Section to establish primer requirements.

          - [Section 051200 "Structural Steel Framing"] [Section 051213 "Architecturally Exposed Structural Steel Framing"] for shop priming of structural steel with primers specified in this Section.

          - Section 055213 "Pipe and Tube Railings" for shop [priming] [painting] pipe and tube railings with coatings specified in this Section.

          - Section 099113 "Exterior Painting" for general field painting.

          - Section 099123 "Interior Painting" for general field painting.

      - DEFINITIONS

Retain this article if high-performance coatings are specified by manufacturers' trade names rather than by MPI paint numbers. Definitions of MPI Gloss Levels below are from "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual").

Retain terms that remain after this Section has been edited for a project.

        - MPI Gloss Level 5: 35 to 70 units at 60 degrees, according to ASTM D523.

        - MPI Gloss Level 6: 70 to 85 units at 60 degrees, according to ASTM D523.

        - MPI Gloss Level 7: More than 85 units at 60 degrees, according to ASTM D523.

      - ACTION SUBMITTALS

        - Product Data: For each type of product. Include preparation requirements and application instructions.

See "Writing Guide" Article in the Evaluations for discussion of first subparagraph below.

          - Include printout of current "MPI Approved Products List" for each product category specified, with the proposed product highlighted.

          - Indicate VOC content.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for paints and coatings.>

        - Samples for Initial Selection: For each type of topcoat product indicated.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled. Retain "Samples for Verification" Paragraph below with or without above.

        - Samples for Verification: For each type of coating system and each color and gloss of topcoat indicated.

          - Submit Samples on rigid backing, 8 inches (200 mm) square.

          - Apply coats on Samples in steps to show each coat required for system.

          - Label each coat of each Sample.

          - Label each Sample for location and application area.

        - Product List: Cross-reference to coating system and locations of application areas. Use same designations indicated on Drawings and in schedules. Include color designations.

      - MAINTENANCE MATERIAL SUBMITTALS

        - Furnish extra materials[, from the same product run,] that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

If necessary, replace percentage in "Coatings" Subparagraph below with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

          - Coatings: [5] <Insert number> percent, but not less than [1 gal. (3.8 L)] <Insert number> of each material and color applied.

      - QUALITY ASSURANCE

        - Mockups: Apply mockups of each coating system indicated to verify preliminary selections made under Sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

          - Architect will select one surface to represent surfaces and conditions for application of each coating system.

            - Wall and Ceiling Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

            - Other Items: Architect will designate items or areas required.

          - Final approval of color selections will be based on mockups.

            - If preliminary color selections are not approved, apply additional mockups of additional colors selected by Architect at no added cost to Owner.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

          - Maintain containers in clean condition, free of foreign materials and residue.

          - Remove rags and waste from storage areas daily.

If necessary, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site.

      - FIELD CONDITIONS

Some manufacturers' products may require higher temperatures for proper curing. Consult manufacturers and revise first paragraph below to suit requirements for specific products if necessary.

        - Apply coatings only when temperature of surfaces to be coated and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

        - Do not apply coatings when relative humidity exceeds 85 percent; at temperatures less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

        - Do not apply exterior coatings in snow, rain, fog, or mist.

- PRODUCTS

Manufacturers and products listed in SpecAgent and Masterworks Paragraph Builder are neither recommended nor endorsed by the AIA or Deltek. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - MANUFACTURERS

        - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Retain "Products" Paragraph below and insert lists of manufacturers and products in high performance coating schedules to require specific products or a comparable product from other manufacturers.

See lists of products currently approved by MPI in its "MPI Approved Products Lists." See "Writing Guide" Article in the Evaluations for further discussion.

        - Products: Subject to compliance with requirements, [provide product] [provide one of the products] [available products that may be incorporated into the Work include, but are not limited to products] listed in the Exterior High-Performance Coating Schedule or Interior High-Performance Coating Schedule for the coating category indicated.

      - HIGH-PERFORMANCE COATINGS, GENERAL

        - MPI Standards: Products shall comply with MPI standards indicated and shall be listed in its "MPI Approved Products Lists."

        - Material Compatibility:

Systems could fail if coatings are incompatible. MPI's coating systems match primers and topcoats, taking compatibility into consideration.

          - Materials for use within each paint system shall be compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

          - For each coat in a paint system, products shall be recommended in writing by topcoat manufacturers for use in paint system and on substrate indicated.

If retaining subparagraph below, coordinate products retained, if any, in other Part 2 articles, to ensure that one manufacturer can provide products for an entire system.

          - Products shall be of same manufacturer for each coat in a coating system.

        - <Double click to insert sustainable design text for coatings.>

Color selection is often limited because some coating materials yellow or degrade under some environmental conditions.

        - Colors: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in color schedule] <Insert requirements>.

      - SOURCE QUALITY CONTROL

Retain this article for large projects or critical coatings where additional control is desired. Delete if tests are not required.

        - Testing of Coating Materials: Owner reserves the right to invoke the following procedure:

          - Owner will engage the services of a qualified testing agency to sample coating materials. Contractor will be notified in advance and may be present when samples are taken. If coating materials have already been delivered to Project site, samples may be taken at Project site. Samples will be identified, sealed, and certified by testing agency.

          - Testing agency will perform tests for compliance with product requirements.

          - Owner may direct Contractor to stop applying coatings if test results show materials being used do not comply with product requirements. Contractor shall remove noncomplying coating materials from Project site, pay for testing, and recoat surfaces coated with rejected materials. Contractor will be required to remove rejected materials from previously coated surfaces if, on recoating with complying materials, the two coatings are incompatible.

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

        - Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows:

Percentages in six subparagraphs below are based on "MPI Manual."

          - Concrete: 12 percent.

          - Fiber-Cement Board: 12 percent.

          - Masonry (Clay and CMUs): 12 percent.

          - Wood: 15 percent.

          - Gypsum Board: 12 percent.

          - Plaster: 12 percent.

        - Gypsum Board Substrates: Verify that finishing compound is sanded smooth.

        - Plaster Substrates: Verify that plaster is fully cured.

        - Verify suitability of substrates, including surface conditions and compatibility, with existing finishes and primers.

        - Proceed with coating application only after unsatisfactory conditions have been corrected.

          - Application of coating indicates acceptance of surfaces and conditions.

      - PREPARATION

For renovation projects, consult "MPI Maintenance Repainting Manual" and revise first paragraph below and coating systems specified in Exterior High-Performance Coating Schedule and Interior High-Performance Coating Schedule.

        - Comply with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual" applicable to substrates and coating systems indicated.

        - Remove hardware, covers, plates, and similar items already in place that are removable and are not to be painted. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

          - After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection if any.

        - Clean substrates of substances that could impair bond of coatings, including dust, dirt, oil, grease, and incompatible paints and encapsulants.

Coordination of shop-applied prime coats with high-performance coatings is critical.

          - Remove incompatible primers and reprime substrate with compatible primers or apply tie coat as required to produce coating systems indicated.

        - Concrete Substrates: Remove release agents, curing compounds, efflorescence, and chalk. Do not coat surfaces if moisture content or alkalinity of surfaces to be coated exceeds that permitted in manufacturer's written instructions.

If applicable, retain one of two subparagraphs below or, if necessary, insert acid etching of concrete surfaces.

          - Clean surfaces with pressurized water. Use pressure range of [1500 to 4000 psi (10 350 to 27 580 kPa)] [4000 to 10,000 psi (27 580 to 68 950 kPa)] at 6 to 12 inches (150 to 300 mm).

          - Abrasive blast clean surfaces to comply with SSPC-SP 7/NACE No. 4.

        - Masonry Substrates: Remove efflorescence and chalk. Do not coat surfaces if moisture content, alkalinity of surfaces, or alkalinity of mortar joints exceeds that permitted in manufacturer's written instructions.

Retain subparagraph below or, if necessary, insert acid etching of clay masonry substrates.

          - Clean surfaces with pressurized water. Use pressure range of [100 to 600 psi (690 to 4140 kPa)] [1500 to 4000 psi (10 350 to 27 580 kPa)] at 6 to 12 inches (150 to 300 mm).

Retain "Steel Substrates" Paragraph below if steel is not shop primed or if shop primer is removed in the field.

        - Steel Substrates: Remove rust, loose mill scale, and shop primer if any. Clean using methods recommended in writing by paint manufacturer[.][ but not less than the following:]

SSPC-SP 7/NACE No. 4 permits tight residues of rust, mill scale, and coatings to remain. Be aware that blast cleaning methods may not be practical for use at the Project site and may not be allowed by authorities having jurisdiction.

          - SSPC-SP 7/NACE No. 4.

SSPC-SP 11 requires complete removal of rust, mill scale, and paint by power tools. SSPC-SP 11 uses nonabrasive methods and bridges the gap between the marginal cleaning required in SSPC-SP 7/NACE No. 4 and the more thorough cleaning required in SSPC-SP 6/NACE No. 3, SSPC-SP 10/NACE No. 2, and SSPC-SP 5/NACE No. 1.

          - SSPC-SP 11.

SSPC-SP 6/NACE No. 3 is recommended by MPI as the minimum preparation for high-performance coatings and requires that two-thirds of surface area be free of visible residue.

          - SSPC-SP 6/NACE No. 3.

SSPC-SP 10/NACE No. 2 requires that 95 percent of surface area be free of visible residue.

          - SSPC-SP 10/NACE No. 2.

SSPC-SP 5/NACE No. 1 removes visible rust, mill scale, paint, and foreign matter.

          - SSPC-SP 5/NACE No. 1.

Retain "Shop-Primed Steel Substrates" Paragraph below if primers are shop applied and are not removed in the field.

        - Shop-Primed Steel Substrates: Clean field welds, bolted connections, and areas where shop paint is abraded. Paint exposed areas with the same material as used for shop priming to comply with SSPC-PA 1 for touching up shop-primed surfaces.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

        - Galvanized-Metal Substrates: Remove grease and oil residue from galvanized sheet metal by mechanical methods to produce clean, lightly etched surfaces that promote adhesion of subsequently applied coatings.

If necessary, insert requirements for acid etching aluminum.

        - Aluminum Substrates: Remove loose surface oxidation.

        - Wood Substrates:

If necessary, insert requirements for power or pressure washing.

          - Scrape and clean knots. Before applying primer, apply coat of knot sealer that is recommended in writing by topcoat manufacturer for coating system indicated.

          - Sand surfaces that will be exposed to view and dust off.

          - Prime edges, ends, faces, undersides, and backsides of wood.

          - After priming, fill holes and imperfections in the finish surfaces with filler that is recommended in writing by topcoat manufacturer for coating system indicated. Sand smooth when dried.

      - APPLICATION

        - Apply high-performance coatings according to manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual."

If Project requires restricted application method (e.g., using only spray or rollers), revise first subparagraph below accordingly.

          - Use applicators and techniques suited for coating and substrate indicated.

          - Coat surfaces behind movable equipment and furniture same as similar exposed surfaces. Before final installation, coat surfaces behind permanently fixed equipment or furniture with prime coat only.

          - Coat backsides of access panels, removable or hinged covers, and similar hinged items to match exposed surfaces.

          - Do not apply coatings over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

If tinting is not required, delete first paragraph below. Different tints will show through as topcoat erodes.

        - Tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of the same material are to be applied. Tint undercoats to match color of finish coat, but provide sufficient difference in shade of undercoats to distinguish each separate coat.

        - If undercoats or other conditions show through final coat, apply additional coats until cured film has a uniform coating finish, color, and appearance.

        - Apply coatings to produce surface films without cloudiness, spotting, holidays, laps, brush marks, runs, sags, ropiness, or other surface imperfections. Produce sharp glass lines and color breaks.

      - FIELD QUALITY CONTROL

        - Dry Film Thickness Testing: Owner may engage the services of a qualified testing and inspecting agency to inspect and test coatings for dry film thickness.

          - Contractor shall touch up and restore coated surfaces damaged by testing.

          - If test results show that dry film thickness of applied coating does not comply with coating manufacturer's written recommendations, Contractor shall pay for testing and apply additional coats as needed to provide dry film thickness that complies with coating manufacturer's written recommendations.

      - CLEANING AND PROTECTION

        - At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

        - After completing coating application, clean spattered surfaces. Remove spattered coatings by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

        - Protect work of other trades against damage from coating operation. Correct damage to work of other trades by cleaning, repairing, replacing, and recoating, as approved by Architect, and leave in an undamaged condition.

        - At completion of construction activities of other trades, touch up and restore damaged or defaced coated surfaces.

      - EXTERIOR HIGH-PERFORMANCE COATING SCHEDULE

Coating systems in this article are based on "MPI Manual." For renovation projects, consult "MPI Maintenance Repainting Manual" and revise coating systems accordingly.

        - Concrete Substrates, Vertical Surfaces:

          - Epoxy System [MPI EXT 3.1D]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy-Modified Latex System [MPI EXT 3.1E]:

            - Prime Coat: Epoxy-modified latex, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy-modified latex, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Epoxy-modified latex, semi-gloss (MPI Gloss Level 5)[, MPI #215].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy-modified latex, gloss (MPI Gloss Level 6)[, MPI #115].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Epoxy System [MPI EXT 3.1M]:

            - Prime Coat: Epoxy, matching intermediate coat.

            - Intermediate Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Concrete Substrates, Horizontal Surfaces:

          - Epoxy Non-Slip Deck Coating System [MPI EXT 3.2C]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Epoxy deck coating (slip resistant)[, MPI #82].

              - <Insert manufacturer's name; product name or designation>.

        - Cement Board Substrates:

          - Epoxy System [MPI EXT 3.3E]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy-Modified Latex System [MPI EXT 3.3D]

            - Prime Coat: Epoxy-modified latex, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy-modified latex, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Epoxy-modified latex, semi-gloss (MPI Gloss Level 5)[, MPI #215].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy-modified latex, gloss (MPI Gloss Level 6)[, MPI #115].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Epoxy System [MPI EXT 3.3F]:

            - Prime Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching prime coat.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Clay Masonry Substrates:

MPI recommends epoxy system below for smooth brick.

          - Epoxy System [MPI EXT 4.1D]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Epoxy System [MPI EXT 4.1J]:

            - Prime Coat: Epoxy, matching intermediate coat.

            - Intermediate Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - CMU Substrates:

          - Epoxy System [MPI EXT 4.2E]:

            - Block Filler: Block filler, epoxy[, MPI #116].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over High-Build Epoxy System [MPI EXT 4.2G]:

            - Block Filler: Block filler, epoxy[, MPI #116].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, high build, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Steel Substrates:

          - Epoxy System [MPI EXT 5.1F]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, high build, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy over Self-Priming Epoxy System [MPI EXT 5.1S]:

At the time of this writing, only one manufacturer's product was listed for MPI #120.

            - Prime Coat: Epoxy, high build, self-priming [, MPI #120].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy Deck Coating over Epoxy Primer and High-Build Epoxy System [MPI EXT 5.1V]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, high build, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy deck coating[, MPI #82].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy Deck Coating over Self-Priming Epoxy System [MPI EXT 5.1X]:

At the time of this writing, only one manufacturer's product was listed for MPI #120.

            - Prime Coat: Epoxy, high build, self-priming [, MPI #120].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy deck coating[, MPI #82].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Epoxy System [MPI EXT 5.1H]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires second topcoat; delete second topcoat for a Budget Grade system.

            - [First and Second ]Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over High-Build Epoxy System [MPI EXT 5.1J]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, high build, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Self-Priming Epoxy System [MPI EXT 5.1T]:

At the time of this writing, only one manufacturer's product was listed for MPI #120.

            - Prime Coat: Epoxy, high build, self-priming [, MPI #120].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane, two component, pigmented, matching topcoat.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Epoxy Zinc-Rich Primer System [MPI EXT 5.1P]:

            - Prime Coat: Primer, zinc rich, epoxy[, MPI #20].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Epoxy Zinc-Rich Primer and High-Build Epoxy System [MPI EXT 5.1G]:

            - Prime Coat: Primer, zinc rich, epoxy[, MPI #20].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, high build, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires second topcoat; delete second topcoat for a Budget Grade system.

            - [First and Second ]Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Inorganic Zinc-Rich Primer and High-Build Epoxy System [MPI EXT 5.1L]:

            - Prime Coat: Primer, zinc rich, inorganic[, MPI #19].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, high build, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

        - Galvanized-Metal Substrates:

          - Epoxy System [MPI EXT 5.3C]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Epoxy Primer System [MPI EXT 5.3L]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane, two component, pigmented, gloss matching topcoat.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Vinyl Wash Primer and Epoxy Primer System [MPI EXT 5.3D]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires second topcoat; delete second topcoat for a Budget Grade system.

            - [First and Second ]Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Aluminum (Not Anodized or Otherwise Coated) Substrates:

          - Epoxy System [MPI EXT 5.4E]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

MPI recommends system in "Pigmented Polyurethane System" Subparagraph below for high-contact and -traffic areas (e.g., public corridors in institutional buildings).

          - Pigmented Polyurethane over Epoxy System [MPI EXT 5.4B]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

For a Premium Grade system, "MPI Manual" requires second topcoat; delete second topcoat for a Budget Grade system.

            - [First and Second ]Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Copper Substrates:

          - Epoxy System [MPI EXT 5.5E]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

MPI recommends system in "Pigmented Polyurethane System" Subparagraph below for high-contact and -traffic areas (e.g., public corridors in institutional buildings).

          - Pigmented Polyurethane over Epoxy System [MPI EXT 5.5B]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

For a Premium Grade system, "MPI Manual" requires second topcoat; delete second topcoat for a Budget Grade system.

            - [First and Second ]Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Stainless-Steel Substrates:

          - Epoxy System [MPI EXT 5.6D]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

MPI recommends system in "Pigmented Polyurethane System" Subparagraph below for high-contact and -traffic areas (e.g., public corridors in institutional buildings).

          - Pigmented Polyurethane System [MPI EXT 5.6B]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

For a Premium Grade system, "MPI Manual" requires second topcoat; delete second topcoat for a Budget Grade system.

            - [First and Second ]Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: Glued-laminated construction.

          - Pigmented Polyurethane System [MPI EXT 6.1J]:

            - Prime Coat: Polyurethane, two component, pigmented, gloss, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane, two component, pigmented, gloss, matching topcoat.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: Exposed framing.

          - Pigmented Polyurethane System [MPI EXT 6.2J]:

            - Prime Coat: Polyurethane, two component, pigmented, gloss, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane, two component, pigmented, gloss, matching topcoat.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: [Wood trim] [Architectural woodwork] [Doors] [Windows] [Wood board siding] [and] [wood fences]

          - Pigmented Polyurethane System [MPI EXT 6.3H]:

            - Prime Coat: Polyurethane, two component, pigmented, gloss, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane, two component, pigmented, gloss, matching topcoat.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Fiberglass Substrates:

          - Epoxy System [MPI EXT 6.7F]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy-Modified Latex System [MPI EXT 6.7E]

            - Prime Coat: Epoxy-modified latex, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy-modified latex, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Epoxy-modified latex, semi-gloss (MPI Gloss Level 5)[, MPI #215].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy-modified latex, gloss (MPI Gloss Level 6)[, MPI #115].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Epoxy System [MPI EXT 6.7D]:

            - Prime Coat: Epoxy, matching intermediate coat.

            - Intermediate Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Portland Cement Plaster Substrates:

          - Epoxy System [MPI EXT 9.1D]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

      - INTERIOR HIGH-PERFORMANCE COATING SCHEDULE

Coating systems in this article are based on "MPI Manual." For renovation projects, consult "MPI Maintenance Repainting Manual" and revise coating systems accordingly.

        - Concrete Substrates, Vertical Surfaces:

MPI recommends epoxy system below for smooth concrete.

          - Epoxy System [MPI INT 3.1F]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy, High-Build System [MPI INT 3.1P]:

            - Prime Coat: High-build epoxy, matching topcoat (reduced).

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: High-build epoxy, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: High-build epoxy, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: High-build epoxy, gloss[, MPI #98].

              - <Insert manufacturer's name; product name or designation>.

MPI recommends epoxy-modified latex system below for smooth concrete.

          - Epoxy-Modified Latex System [MPI INT 3.1G]:

            - Prime Coat: Epoxy-modified latex, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy-modified latex, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Epoxy-modified latex, semi-gloss (MPI Gloss Level 5)[, MPI #215].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy-modified latex, gloss (MPI Gloss Level 6)[, MPI #115].

              - <Insert manufacturer's name; product name or designation>.

        - Concrete Substrates, Horizontal Surfaces.

MPI recommends epoxy system below for smooth concrete.

          - Epoxy System [MPI INT 3.2C]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy, High-Build System [MPI INT 3.2L]:

            - Prime Coat: High-build epoxy, matching topcoat (reduced).

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: High-build epoxy, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: High-build epoxy, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: High-build epoxy, gloss[, MPI #98].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane System [MPI INT 3.2D]:

            - Prime Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane, two component, pigmented, gloss, matching topcoat.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

          - Clear (Two-Component) Polyurethane System [MPI INT 3.2K]:

            - Prime Coat: Two-component polyurethane matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Two-component polyurethane, matching topcoat.

            - Topcoat: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or MPI Gloss Level 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

        - Cement Board Substrates:

          - Epoxy System [MPI INT 3.3E]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy-Modified Latex System [MPI INT 3.3D]:

            - Prime Coat: Epoxy-modified latex, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy-modified latex, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Epoxy-modified latex, semi-gloss (MPI Gloss Level 5)[, MPI #215].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy-modified latex, gloss (MPI Gloss Level 6)[, MPI #115].

              - <Insert manufacturer's name; product name or designation>.

        - Clay Masonry Substrates:

MPI recommends epoxy system below for smooth brick.

          - Epoxy System [MPI INT 4.1F]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

MPI recommends epoxy-modified latex system below for smooth brick.

          - Epoxy-Modified Latex System [MPI INT 4.1G]:

            - Prime Coat: Epoxy-modified latex, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy-modified latex, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Epoxy-modified latex, semi-gloss (MPI Gloss Level 5)[, MPI #215].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy-modified latex, gloss (MPI Gloss Level 6)[, MPI #115].

              - <Insert manufacturer's name; product name or designation>.

          - Clear (Two-Component) Polyurethane System [MPI INT 4.1K]:

            - Prime Coat: Two-component polyurethane, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Two-component polyurethane, matching topcoat.

            - Topcoat: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or MPI Gloss Level 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

        - CMU Substrates:

          - Epoxy System [MPI INT 4.2F] [MPI INT 4.2G]:

Retain one of two "Block Filler" subparagraphs below; first corresponds to MPI INT 4.2F, which MPI recommends for dry environments; second to MPI INT 4.2G, which MPI recommends for wet environments.

            - Block Filler: Block filler, latex, interior/exterior[, MPI #4].

              - <Insert manufacturer's name; product name or designation>.

            - Block Filler: Block filler, epoxy[, MPI #116].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy, High-Build System [MPI INT 4.2R]:

            - Prime Coat: Epoxy block filler[, MPI #116].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: High-build epoxy, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: High-build epoxy, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: High-build epoxy, gloss[, MPI #98].

              - <Insert manufacturer's name; product name or designation>.

MPI recommends epoxy-modified latex system below for dry environments.

          - Epoxy-Modified Latex System [MPI INT 4.2J]:

            - Block Filler: Block filler, latex, interior/exterior[, MPI #4].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy-modified latex, interior, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Epoxy-modified latex, semi-gloss (MPI Gloss Level 5)[, MPI #215].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy-modified latex, gloss (MPI Gloss Level 6)[, MPI #115].

              - <Insert manufacturer's name; product name or designation>.

          - Clear (Two-Component) Polyurethane System [MPI INT 4.2Q]:

            - Prime Coat: Two-component polyurethane, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Two-component polyurethane, matching topcoat.

            - Topcoat: Varnish, aliphatic polyurethane, two component (MPI Gloss Level 6 or MPI Gloss Level 7)[, MPI #78].

              - <Insert manufacturer's name; product name or designation>.

        - Steel Substrates:

          - Epoxy System [MPI INT 5.1L]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - High-Build Epoxy over Epoxy Zinc-Rich Primer System [MPI INT 5.1P]:

            - Prime Coat: Primer, zinc-rich, epoxy[, MPI #20].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, high build, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

Retain one of two "Topcoat" subparagraphs below. Retain first for a Premium Grade system; retain second for a Budget Grade system.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy, high-build, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy over Self-Priming Epoxy System [MPI INT 5.1V]:

At the time of this writing, only one manufacturer's product was listed for MPI #120.

            - Prime Coat: Epoxy, high build, self-priming [, MPI #120].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy, High-Build System [MPI INT 5.1Y]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: High-build epoxy, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: High-build epoxy, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: High-build epoxy, gloss[, MPI #98].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy Deck Coating System [MPI INT 5.1LL]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy deck coating (slip resistant)[, MPI #82].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy-Modified Latex System [MPI INT 5.1K]:

            - Prime Coat: Primer, rust inhibitive, water based[, MPI #107].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy-modified latex, interior, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Epoxy-modified latex, semi-gloss (MPI Gloss Level 5)[, MPI #215].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy-modified latex, gloss (MPI Gloss Level 6)[, MPI #115].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Epoxy Primer System [MPI INT 5.1F]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane, two component, pigmented, matching topcoat.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over High-Build Epoxy System [MPI INT 5.1G]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, high build[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Self-Priming Epoxy System [MPI INT 5.1U]:

At the time of this writing, only one manufacturer's product was listed for MPI #120.

            - Prime Coat: Epoxy, high build, self-priming [, MPI #120].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Polyurethane, two component, pigmented, matching topcoat.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Inorganic Zinc and Epoxy System [MPI INT 5.1H]:

            - Prime Coat: Primer, zinc rich, inorganic[, MPI #19].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane over Epoxy Zinc-Rich and Epoxy System [MPI INT 5.1J]:

            - Prime Coat: Primer, zinc rich, epoxy[, MPI #20].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate primers.

        - Galvanized-Metal Substrates:

          - Epoxy over Epoxy Primer System [MPI INT 5.3D]:

            - Prime Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy over Vinyl Wash Primer and Epoxy Primer System [MPI INT 5.3E]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Primer, epoxy, anti-corrosive, for metal[, MPI #101].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

        - Aluminum (Not Anodized or Otherwise Coated) Substrates:

          - Epoxy System [MPI INT 5.4B]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane System [MPI INT 5.4C]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two-component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Copper Substrates:

          - Epoxy System [MPI INT 5.5B]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane System [MPI INT 5.5C]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Stainless-Steel Substrates:

          - Epoxy System [MPI INT 5.6C]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane System [MPI INT 5.6D]:

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

            - Prime Coat: Primer, vinyl wash[, MPI #80].

              - <Insert manufacturer's name; product name or designation>.

            - Intermediate Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: Glued-laminated construction.

          - Epoxy System [MPI INT 6.1L]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane System [MPI INT 6.1E]:

            - Prime Coat: Polyurethane, two component, pigmented, matching topcoat.

            - Intermediate Coat: Polyurethane, two component, pigmented, matching topcoat.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates: [Wood trim] [Architectural woodwork] [Doors] [Windows] [and] [wood board paneling].

          - Epoxy System [MPI INT 6.3L]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

        - Fiberglass Substrates:

          - Epoxy System [MPI INT 6.7D]:

            - Prime Coat: Epoxy, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Pigmented Polyurethane System [MPI INT 6.7E]:

            - Prime Coat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching prime coat.

            - Topcoat: Polyurethane, two component, pigmented, gloss (MPI Gloss Level 6)[, MPI #72].

              - <Insert manufacturer's name; product name or designation>.

MPI recommends epoxy-modified latex system below for dry environments.

          - Epoxy-Modified Latex System [MPI INT 6.7F]:

            - Block Filler: Block filler, latex, interior/exterior[, MPI #4].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy-modified latex, interior, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Epoxy-modified latex, semi-gloss (MPI Gloss Level 5)[, MPI #215].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy-modified latex, gloss (MPI Gloss Level 6)[, MPI #115].

              - <Insert manufacturer's name; product name or designation>.

        - [Gypsum Board] [Plaster] Substrates:

          - Epoxy System [MPI INT 9.2E]:

            - Prime Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy, matching topcoat.

            - Topcoat: Epoxy, gloss[, MPI #77].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy, High-Build System [MPI INT 9.2N]:

            - Prime Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete first "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: High-build epoxy, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: High-build epoxy, low gloss[, MPI #108].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: High-build epoxy, gloss[, MPI #98].

              - <Insert manufacturer's name; product name or designation>.

          - Epoxy-Modified Latex System [MPI INT 9.2F]:

            - Prime Coat: Primer sealer, latex, interior[, MPI #50].

              - <Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

            - Intermediate Coat: Epoxy-modified latex, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

            - Topcoat: Epoxy-modified latex, semi-gloss (MPI Gloss Level 5)[, MPI #215].

              - <Insert manufacturer's name; product name or designation>.

            - Topcoat: Epoxy-modified latex, gloss (MPI Gloss Level 6)[, MPI #115].

              - <Insert manufacturer's name; product name or designation>.

END OF SECTION 099600