Copyright 2020 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 099647 - INTUMESCENT PAINTING (MPI STANDARDS)

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - Intumescent paint for [interior] [and] [exterior] items and surfaces.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 078123 "Intumescent Fire Protection" for fire-resistance-rated intumescent mastic materials.

          - Section 099113 "Exterior Painting" for primers and finish coats that may be used with intumescent paint finishes.

          - Section 099123 "Interior Painting" for primers and finish coats that may be used with intumescent paint finishes.

          - Section 099300 "Staining and Transparent Finishing" for primers, finish coats, and wood stains that may be used with intumescent paint finishes.

          - Section 099633 "High-Temperature-Resistant Coatings" for special coatings designed for use on steel subject to extremely high temperatures.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

See the Evaluations for discussion of first subparagraph below.

          - Include printout of current "MPI Approved Products List" for each product category specified, with the proposed product highlighted.

          - Indicate VOC content.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for paints and coatings.>

          - <Double click to insert sustainable design text for EPDs and HPDs.>

          - <Double click here to insert sustainable design text for manufacturer inventory.>

Retain "Samples for Initial Selection" Paragraph below if colors and other characteristics are not preselected and specified or scheduled.

        - Samples for Initial Selection: For each intumescent paint finish indicated.

Retain "Samples for Verification" Paragraph below if colors and other characteristics are preselected and specified or scheduled, with or without "Samples for Initial Selection" Paragraph above.

        - Samples for Verification: For each type of coating system and each color and gloss of intumescent paint finish indicated.

          - Submit Samples on [rigid backing] [actual substrate], not less than 8 inches (200 mm) square.

          - Apply coats on Samples in steps to show each coat required for system.

          - Label each coat of each Sample.

          - Label each Sample for location and application area.

        - Product List: Cross-reference to paint system and locations of application areas. Use same designations indicated on Drawings and in schedules. Include color designations.

      - INFORMATIONAL SUBMITTALS

Retain this article for material test reports that are Contractor's responsibility.

        - Material Test Reports: For each intumescent paint.

      - MAINTENANCE MATERIAL SUBMITTALS

        - Furnish extra materials that are from same production run (batch mix) as materials applied and that are packaged with protective covering for storage and identified with labels describing contents.

          - Quantity: Furnish an additional [5] <Insert number> percent of each color applied, but not less than [1 gal. (3.8 L)] <Insert value> of each material and color applied.

      - QUALITY ASSURANCE

        - Mockups: Apply mockups of each paint system indicated to verify preliminary selections made under Sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

          - Architect will select one surface to represent surfaces and conditions for application of each coating system.

            - Wall and Ceiling Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

            - Other Items: Architect will designate items or areas required.

          - Final approval of color selections will be based on mockups.

            - If preliminary color selections are not approved, apply additional mockups of additional colors selected by Architect at no added cost to Owner.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

          - Maintain containers in clean condition, free of foreign materials and residue.

          - Remove rags and waste from storage areas daily.

If necessary, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site.

          - <Insert requirements>.

      - FIELD CONDITIONS

Revise this article if manufacturer's requirements are more restrictive.

        - Apply waterborne intumescent paints only when temperatures of surfaces to be painted and ambient air temperatures are between 50 and 90 deg F (10 and 32 deg C).

        - Apply solvent-thinned intumescent paints only when temperatures of surfaces to be painted and ambient air temperatures are between 45 and 95 deg F (7 and 35 deg C).

        - Do not apply intumescent paints in snow, rain, fog, or mist; when relative humidity exceeds 85 percent; at temperatures of less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

        - Allow wet surfaces to dry thoroughly and to attain temperature and conditions specified before starting or continuing coating operation.

- PRODUCTS

Manufacturers and products listed in SpecAgent and MasterWorks Paragraph Builder are neither recommended nor endorsed by the AIA or Deltek. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - MANUFACTURERS

        - <Double click here to find, evaluate, and insert list of manufacturers and products.>

      - INTUMESCENT PAINT

        - MPI Standards: Products shall comply with MPI standards indicated and shall be listed in its "MPI Approved Products List."

        - Surface-Burning Characteristics of Fire-Retardant Systems: As tested according to ASTM E84; testing by a qualified testing agency. Identify products with appropriate markings of applicable testing agency.

          - Flame-Spread Index: [25] [75] <Insert value> or less.

          - Smoke-Developed Index: [450] <Insert value> or less.

        - Material Compatibility:

Systems could fail if paints used for individual coats are incompatible.

          - Materials for use within each paint system shall be compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

          - For each material or coat, products and spreading rates shall be as recommended in writing by intumescent paint manufacturer for use on substrate indicated. Comply with requirements for fire-retardant coating classification and surface-burning characteristics indicated.

        - <Double click to insert sustainable design text for paints and coatings.>

        - Colors and Gloss: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule] <Insert requirements>.

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Applicator present, for compliance with manufacturer's requirements for surface treatments, shop-primed surfaces, maximum moisture content, and other conditions affecting performance of the Work.

Percentage in first paragraph below and time limit in second paragraph are based on the "MPI Architectural Painting Specification Manual"; revise both paragraphs to suit Project.

        - Begin coating only when moisture content of wood substrate is 15 percent or less when measured with an electronic moisture meter.

        - Begin coating no sooner than [28] <Insert number> days after substrate is constructed and is visually dry on both sides.

        - Verify suitability of substrates, including surface conditions, and compatibility with existing finishes and primers.

        - Proceed with coating application only after unsatisfactory conditions have been corrected and surfaces are dry.

      - PREPARATION

For renovation projects, consult the "MPI Maintenance Repainting Manual" and revise option in first paragraph below and coating systems specified in the Exterior Intumescent Painting Schedule and Interior Intumescent Painting Schedule.

        - Comply with manufacturer's written instructions[ and recommendations in the "MPI Architectural Painting Specification Manual"] applicable to substrates and coating systems indicated.

Revise first paragraph below to suit Project.

        - Remove hardware and hardware accessories, plates, machined surfaces, light fixtures, and similar items already installed that are not to be coated. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and coating.

          - After completing coating operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection if any.

        - Clean substrates of substances that could impair bond of coatings, including dust, dirt, oil, grease, and incompatible paints and encapsulants. Do not coat surfaces if surface moisture content or alkalinity exceeds that permitted in manufacturer's written instructions.

          - Remove incompatible primers, and reprime substrate with compatible primers as required to produce coating systems indicated.

          - Perform cleaning and coating application so dust and other contaminants from cleaning process do not fall on wet, newly coated surfaces.

      - INSTALLATION

Revise this article to suit Project. Insert special restrictions on application methods if required.

        - Apply intumescent paints according to manufacturer's written instructions and to comply with requirements for listing and labeling for surface-burning characteristics specified.

If Project requires a restricted application method (e.g., using only spray or rollers), revise first subparagraph below to suit Project.

          - Use equipment and techniques best suited for substrate and type of material being applied.

          - Coat surfaces behind movable items the same as similar exposed surfaces.

          - Apply each coat separately according to manufacturer's written instructions.

Application in subparagraph below limits intumescent paint to door faces, because activation of coating on edges may interfere with door opening.

          - Finish doors on faces with intumescent finish. Paint tops, bottoms, and side edges with fire-inert finish.

        - Apply coatings to prepared surfaces as soon as practical after preparation and before subsequent surface soiling or deterioration.

        - Apply coatings to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections. Produce sharp lines and color breaks.

          - Pigmented Finishes: If undercoats or other conditions show through pigmented topcoat/overcoat, apply additional coats until cured film has a uniform paint finish, color, and appearance.

          - Clear Finishes: Produce a smooth surface film of even sheen[ using multiple coats].

      - CLEANING AND PROTECTION

        - At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

        - After completing coating application, clean spattered surfaces. Remove spattered coatings by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

        - Protect work of other trades against damage from coating application. Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

        - At completion of construction activities of other trades, touch up and restore damaged or defaced coated surfaces.

      - EXTERIOR INTUMESCENT PAINTING SCHEDULE

        - Wood Substrates, Glued-Laminated Construction:

          - Pigmented, Fire-Retardant System[ MPI EXT 6.1F]:

"MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual") states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant topcoat, exterior, low sheen[, MPI #126].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Penetrating Wood Preservative System[ MPI EXT 6.1G]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-resistant sealer, for exterior wood[, MPI #109].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, Exposed Framing:

          - Pigmented, Fire-Retardant System[ MPI EXT 6.2F]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant topcoat, exterior, low sheen[, MPI #126].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Penetrating Wood Preservative System[ MPI EXT 6.2G]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-resistant sealer, for exterior wood[, MPI #109].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, [Wood Trim] [Architectural Woodwork] [and] [Wood Board Siding]:

          - Pigmented, Fire-Retardant System[ MPI EXT 6.3P]:

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant topcoat, exterior, low sheen[, MPI #126].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Penetrating Wood Preservative System[ MPI EXT 6.3Q]:

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-resistant sealer, for exterior wood[, MPI #109].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, Wood-Based Panel Products:

          - Pigmented, Fire-Retardant System[ EXT 6.4E]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant topcoat, exterior, low sheen[, MPI #126].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Penetrating Wood Preservative System[ MPI EXT 6.4F]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-resistant sealer, for exterior wood[, MPI #109].

              - <Insert manufacturer's name; product name or designation>.

      - INTERIOR INTUMESCENT PAINTING SCHEDULE

        - Wood Substrates, Glued-Laminated Construction:

          - Pigmented, Fire-Retardant, Water-Based System[, MPI INT 6.1U]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat:

Retain one of first two subparagraphs below.

              - Fire-retardant coating, latex, interior, flat[, MPI #64].

                - <Insert manufacturer's name; product name or designation>.

              - Fire-retardant topcoat, latex, interior[, MPI #67].

                - <Insert manufacturer's name; product name or designation>.

          - Pigmented, Fire-Retardant, Solvent-Based System[, MPI INT 6.1UU]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant coating, alkyd, interior, flat[, MPI #63].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Water-Based System[, MPI INT 6.1V]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant coating, interior, clear[, MPI #62].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Solvent-Based System[, MPI INT 6.1VV]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant topcoat, clear, alkyd, interior[, MPI #66].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, Exposed Framing:

          - Pigmented, Fire-Retardant, Water-Based System[, MPI INT 6.2F]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat:

Retain one of first two subparagraphs below.

              - Fire-retardant coating, latex, interior, flat[, MPI #64].

                - <Insert manufacturer's name; product name or designation>.

              - Fire-retardant topcoat, latex, interior[, MPI #67].

                - <Insert manufacturer's name; product name or designation>.

          - Pigmented, Fire-Retardant, Solvent-Based System[, MPI INT 6.2FF]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant coating, alkyd, interior, flat[, MPI #63].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Water-Based System[, MPI INT 6.2G]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant coating, interior, clear[, MPI #62].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Solvent-Based System[, MPI INT 6.2GG]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant topcoat, clear, alkyd, interior[, MPI #66].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, [Wood Trim] [Architectural Woodwork] [and] [Wood Board Paneling].

          - Pigmented, Fire-Retardant, Water-Based System[, MPI INT 6.3R]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat:

Retain one of first two subparagraphs below.

              - Fire-retardant coating, latex, interior, flat[, MPI #64].

                - <Insert manufacturer's name; product name or designation>.

              - Fire-retardant topcoat, latex, interior[, MPI #67].

                - <Insert manufacturer's name; product name or designation>.

          - Pigmented, Fire-Retardant, Solvent-Based System[, MPI INT 6.3RR]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant coating, alkyd, interior, flat[, MPI #63].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Water-Based System[, MPI INT 6.3S]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant coating, interior, clear[, MPI #62].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Solvent-Based System[, MPI INT 6.3SS]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant topcoat, clear, alkyd, interior[, MPI #66].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, Wood-Based Panel Products.

          - Pigmented, Fire-Retardant, Water-Based System[, MPI INT 6.4P]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat:

Retain one of first two subparagraphs below.

              - Fire-retardant coating, latex, interior, flat[, MPI #64].

                - <Insert manufacturer's name; product name or designation>.

              - Fire-retardant topcoat, latex, interior[, MPI #67].

                - <Insert manufacturer's name; product name or designation>.

          - Pigmented, Fire-Retardant, Solvent-Based System[, MPI INT 6.4PP]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant coating, alkyd, interior, flat[, MPI #63].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Water-Based System[, MPI INT 6.4Q]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant coating, interior, clear[, MPI #62].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Solvent-Based System[, MPI INT 6.4QQ]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant topcoat, clear, alkyd, interior[, MPI #66].

              - <Insert manufacturer's name; product name or designation>.

        - Wood Substrates, Wood Shingles and Shakes.

          - Pigmented, Fire-Retardant, Water-Based System[, MPI INT 6.6G]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat:

Retain one of first two subparagraphs below.

              - Fire-retardant coating, latex, interior, flat[, MPI #64].

                - <Insert manufacturer's name; product name or designation>.

              - Fire-retardant topcoat, latex, interior[, MPI #67].

                - <Insert manufacturer's name; product name or designation>.

          - Pigmented, Fire-Retardant, Solvent-Based System[, MPI INT 6.6GG]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant coating, alkyd, interior, flat[, MPI #63].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Water-Based System[, MPI INT 6.6H]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant coating, interior, clear[, MPI #62].

              - <Insert manufacturer's name; product name or designation>.

          - Clear, Fire-Retardant, Solvent-Based System[, MPI INT 6.6HH]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat: Fire-retardant topcoat, clear, alkyd, interior[, MPI #66].

              - <Insert manufacturer's name; product name or designation>.

        - Plaster and Gypsum Board Substrates:

          - Fire-Retardant Coating (Clear or Pigmented) System[, MPI INT 9.2H]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat:

Retain one of first two subparagraphs below.

              - Fire-retardant coating, interior, clear[, MPI #62].

                - <Insert manufacturer's name; product name or designation>.

              - Fire-retardant coating, alkyd, interior, flat[, MPI #63].

                - <Insert manufacturer's name; product name or designation>.

          - Water-Based, Fire-Retardant Coating System[, MPI INT 9.2J]:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

            - Prime Coat: As recommended in writing by topcoat manufacturer.

            - Intermediate Coat: As recommended in writing by topcoat manufacturer.

            - Topcoat:

Retain one of two subparagraphs below.

              - Fire-retardant coating, latex, interior, flat[, MPI #64].

                - <Insert manufacturer's name; product name or designation>.

              - Fire-retardant topcoat, latex, interior[, MPI #67].

                - <Insert manufacturer's name; product name or designation>.

END OF SECTION 099647