Copyright 2020 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

SECTION 123619 - WOOD COUNTERTOPS

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

MasterSpec includes provisions for LEED 2009, LEED v4, IgCC, and Green Globes. Sustainable design requirements may be inserted in the Section Text using the hypertext links.

Review requirements of the Architectural Woodwork Institute (AWI), Architectural Woodwork Manufacturers Association of Canada (AWMAC), and Woodwork Institute's (WI) "Architectural Woodwork Standards" (hereafter, AWS) before revising this Section.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Wood countertops.

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

Retain subparagraph below for fire-retardant-treated materials.

          - Include data for fire-retardant treatment from chemical-treatment manufacturer and certification by treating plant that treated materials comply with requirements.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for recycled content.>

          - <Double click to insert sustainable design text for regional materials.>

          - <Double click to insert sustainable design text for certified wood.>

          - <Double click to insert sustainable design text for adhesives.>

          - <Double click to insert sustainable design text for installation adhesives.>

          - <Double click to insert sustainable design text for composite wood.>

        - Shop Drawings: For wood countertops.

          - Include plans, sections, details, and attachments to other work. Detail fabrication and installation, including field joints.

          - Show locations and sizes of cutouts and holes for items installed in wood countertops.

          - Show veneer leaves with dimensions, grain direction, exposed face, and identification numbers indicating the flitch and sequence within the flitch for each leaf.

Retain subparagraph below and applicable options if retaining other requirements for AWI's or WI's quality certification program.

          - Apply [AWI Quality Certification] [WI Certified Compliance] Program label to Shop Drawings.

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples.

        - Samples: For each shop-applied transparent finish and for each color and wood species specified, in manufacturer's or fabricator's standard size.

        - Samples for Initial Selection: For shop-applied transparent finishes in each wood species and in each type and color required in fabricator's standard size.

        - Samples for Verification: For the following:

Retain "Lumber for Transparent Finish" and "Veneer Leaves" subparagraphs below to control grain character, color, and finish, or insert other subparagraphs to suit Project. AWS requires samples to be "as wide as practical" by 12 inches (300 mm) long for lumber.

          - Lumber for Transparent Finish: Not less than [5 inches (125 mm) wide by 12 inches (300 mm) long] [5 inches (125 mm) wide by 24 inches (600 mm) long] <Insert dimensions>, for each species and cut, finished on one side and one edge.

          - Veneer Leaves: Representative of and selected from flitches to be used for transparent-finished wood countertops.

      - INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

        - Qualification Data: For [Installer] [fabricator].

        - Product Certificates: For the following:

          - Composite wood products.

          - Adhesives.

        - Quality Standard Compliance Certificates: [AWI Quality Certification Program] [WI Certified Compliance Program].

Retain "Evaluation Reports" Paragraph below for fire-retardant-treated materials.

        - Evaluation Reports: For fire-retardant-treated materials, from ICC-ES.

      - QUALITY ASSURANCE

        - Fabricator Qualifications: Shop that employs skilled workers who custom fabricate products similar to those required for this Project and whose products have a record of successful in-service performance.

Retain "Shop Certification" Subparagraph below if AWI quality certification or WI compliance certification is required. Both AWI and WI will inspect work and provide certification for work that passes inspection if fabricator is not certified/licensed.

          - Shop Certification: [AWI's Quality Certification Program accredited participant] [WI's Certified Compliance Program licensee].

Retain "Installer Qualifications" Paragraph below if required. If AWI Quality Certification Program labels or certificates are required for installation, Installer must be a certified participant. If countertops must be FSC certified, fabricator must either install countertops or be FSC certified for chain of custody.

        - Installer Qualifications: [Fabricator of products] [AWI's Quality Certification Program accredited participant] [WI's Certified Compliance Program licensee].

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver countertops only after casework and supports on which they will be installed have been completed in installation areas.

        - Store countertops in areas where environmental conditions comply with requirements specified in "Field Conditions" Article.

        - Keep finished surfaces of countertops covered with protective covering during handling and installation.

      - FIELD CONDITIONS

Retain "Environmental Limitations without Humidity Control" Paragraph below if humidity will not be controlled after building is occupied.

        - Environmental Limitations without Humidity Control: Do not deliver or install wood countertops until building is enclosed, wet-work is complete, and HVAC system is operating and maintaining temperature and relative humidity at levels planned for building occupants during the remainder of the construction period.

Retain "Environmental Limitations with Humidity Control" Paragraph below if humidity will be controlled after building is occupied. Retain one of three options or insert another range based on local climatological data. Three ranges given are for painted or finished woodwork. First applies to Ontario, Quebec, and most of the United States. Second applies to damp coastal areas of southern United States and Maritime Provinces. Third applies to dry southwestern United States, Alberta, Manitoba, and Saskatchewan. For unfinished cabinets, narrower ranges will be required to maintain optimum moisture content. See relative-humidity and moisture-content map in AWS.

        - Environmental Limitations with Humidity Control: Do not deliver or install wood countertops until building is enclosed, wet-work is complete, and HVAC system is operating and maintaining temperature between 60 and 90 deg F (16 and 32 deg C) and relative humidity between [25 and 55] [43 and 70] [20 and 50] <Insert numbers> percent during the remainder of the construction period.

Retain "Field Measurements" or "Established Dimensions" Paragraph below. Establishing dimensions allows product fabrication to begin before installation areas are complete.

        - Field Measurements: Where wood countertops are indicated to fit to other construction, verify dimensions of other construction by field measurements before fabrication and indicate measurements on Shop Drawings. Coordinate fabrication schedule with construction progress to avoid delaying the Work.

        - Established Dimensions: Where wood countertops are indicated to fit to other construction, establish dimensions for areas where wood countertops are to fit. Provide allowance for trimming at site, and coordinate construction to ensure that actual dimensions correspond to established dimensions.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - FABRICATORS

Retain "Fabricators" Paragraph below if a list of preapproved woodworkers is used as a quality-control procedure. See AWI's or WI's member list for names of woodworking firms.

        - Fabricators: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available fabricators offering products that may be incorporated into the Work include, but are not limited to, the following]:

          - <Insert, in separate subparagraphs, names and contact information for preapproved woodworking firms>.

      - WOOD COUNTERTOPS

        - Quality Standard: Unless otherwise indicated, comply with the "Architectural Woodwork Standards" for grades of wood countertops indicated for construction, finishes, installation, and other requirements.

If retaining first subparagraph below, verify applicability of certification for Project's geographic location. Certification programs of AWI and WI organizations are available to member and nonmember firms. Both organizations will inspect work and provide certification for work that passes inspection if fabricator is not certified/licensed. Contact either organization for a list of certified woodworkers in Project's location.

          - Provide inspections of fabrication and installation together with labels and certificates from [AWI] [WI] certification program indicating that countertops comply with requirements of grades specified.

Retain subparagraph below if Drawings and the Specifications are more restrictive than AWS.

          - The Contract Documents contain requirements that are more stringent than the referenced quality standard. Comply with requirements of Contract Documents in addition to those of the referenced quality standard.

        - Grade: [Premium] [Custom] [Economy].

        - <Double click to insert sustainable design text for regional wood materials.>

        - <Double click to insert sustainable design text for certified wood.>

        - Solid-Wood Countertops: For transparent finish. Fabricated from solid wood, edge glued, with crown direction reversed in adjacent boards, to produce widths indicated. Select boards for similarity of color and grain, and arrange boards for optimum match between adjacent boards.

          - Wood Species: [Red oak] [White oak] [White ash] [White birch] [As indicated on Drawings] <Insert species>.

          - Wood Cut: [Plain sawn] [Rift sawn] [Quarter sawn] [As indicated on Drawings].

        - Butcher-Block Countertops: For transparent finish. Fabricated from narrow strips of lumber glued together and arranged for random mix of color and grain.

          - Wood Species: [Red oak] [Hard maple] [Teak] [As indicated on Drawings] <Insert species>.

          - Strip Thickness: [3/4 inch (19 mm)] [1-1/2 inches (38 mm)] [As indicated on Drawings].

        - Wood-Veneer Countertops: For transparent finish. Fabricated from wood veneer laminated over panel-product core.

          - Wood Species: [Red oak] [White oak] [White ash] [White birch] [As indicated on Drawings] <Insert species>.

          - Wood Cut: [Plain sawn] [Rift sawn] [Quarter sawn] [As indicated on Drawings].

          - Matching of Adjacent Veneer Leaves: [Book] [Slip] [Random].

Retain requirement for end-matched leaves if countertops are longer than veneer leaves or if required for special effect. Show special effects on Drawings.

            - End match leaves [where countertops are longer than veneer leaves] [as indicated on Drawings] <Insert requirements>.

          - Veneer Matching within Panel Face: [Running] [Balance] [Center-balance] match.

          - Edge Treatment: [Solid wood matching face for species and cut] [Wood veneer matching face for species and cut] [As indicated on Drawings] <Insert requirements>.

          - Core Material: [Particleboard or MDF] [Particleboard] [MDF] [Particleboard made with exterior glue] [MDF made with exterior glue] [Exterior-grade plywood] [Fire-retardant-treated plywood] [Fire-retardant particleboard] [Fire-retardant MDF] [As selected by fabricator to comply with quality standard].

      - WOOD MATERIALS

        - Wood Products: Provide materials that comply with requirements of referenced quality standard for each type of wood countertop and quality grade specified unless otherwise indicated.

Usually retain first subparagraph below if using softwood lumber.

          - Do not use plain-sawn softwood lumber with exposed, flat surfaces more than 3 inches (75 mm) wide.

Retain one of three options in "Wood Moisture Content" Subparagraph below. First range applies to Ontario, Quebec, and most of the United States. Second applies to damp coastal areas of southern United States and Maritime Provinces. Third applies to dry southwestern United States, Alberta, Manitoba, and Saskatchewan. See relative-humidity and moisture-content map in AWS. Some locations have microclimates that differ from the surrounding region.

          - Wood Moisture Content: [5 to 10] [8 to 13] [4 to 9] percent.

        - Composite Wood Products: Provide materials that comply with requirements of referenced quality standard for each type of countertop and quality grade specified unless otherwise indicated.

          - <Double click to insert sustainable design text for composite wood products.>

          - <Double click to insert sustainable design text for recycled content.>

          - MDF: Medium-density fiberboard, ANSI A208.2, [Grade 130] <Insert grade>.

          - Particleboard: ANSI A208.1, [Grade M-2] [Grade M-2-Exterior Glue].

          - Softwood Plywood: DOC PS 1.

      - FIRE-RETARDANT-TREATED MATERIALS

If fire-retardant materials are required, verify requirements and acceptability of various materials with authorities having jurisdiction.

        - Fire-Retardant-Treated Materials, General: Where fire-retardant-treated materials are indicated, use materials that are acceptable to authorities having jurisdiction and with fire-test-response characteristics specified as determined by testing identical products in accordance with test method indicated by a qualified testing agency.

          - Use treated materials that comply with requirements of referenced quality standard. Do not use materials that are warped, discolored, or otherwise defective.

          - Use fire-retardant-treatment formulations that do not bleed through or otherwise adversely affect finishes. Do not use colorants to distinguish treated materials from untreated materials.

          - Identify fire-retardant-treated materials with appropriate classification marking of qualified testing agency in the form of removable paper label or imprint on surfaces that will be concealed from view after installation.

        - Fire-Retardant-Treated Lumber and Plywood: Products with a flame-spread index of 25 or less when tested in accordance with ASTM E84, with no evidence of significant progressive combustion when the test is extended an additional 20 minutes, and with the flame front not extending more than 10.5 feet (3.2 m) beyond the centerline of the burners at any time during the test.

          - Kiln dry lumber and plywood after treatment to a maximum moisture content of 19 and 15 percent, respectively.

Retain first subparagraph below if treated products will be exposed and receive a stained or natural transparent finish. Organic resin treatment is more expensive than salt treatments but helps ensure a better stained or natural transparent finish.

          - For items indicated to receive a stained or natural transparent finish, use organic resin chemical formulation.

Retain one of two subparagraphs below. Before retaining first, verify that wood species and treatment process specified are approved for milling after treatment.

          - Mill lumber after treatment within limits set for wood removal that do not affect listed fire-test-response characteristics, using a woodworking shop certified by testing and inspecting agency.

          - Mill lumber before treatment and implement procedures during treatment and drying processes that prevent lumber from warping and developing discolorations from drying sticks or other causes, marring, and other defects affecting appearance of wood countertops.

Fire-retardant particleboard contains urea formaldehyde. It complies with requirements for Class I (Class A) finish but not requirements of model codes for use where noncombustible materials are required.

        - Fire-Retardant Particleboard: Made from softwood particles and fire-retardant chemicals mixed at time of panel manufacture to achieve flame-spread index of 25 or less and smoke-developed index of 25 or less when tested in accordance with ASTM E84.

          - For panels 3/4 inch (19 mm) thick and less, comply with ANSI A208.1 for Grade M-2 except for the following minimum properties: modulus of rupture, 1600 psi (11 MPa); modulus of elasticity, 300,000 psi (2070 MPa); internal bond, 80 psi (550 kPa); and screw-holding capacity on face and edge, 250 and 225 lbf (1100 and 1000 N), respectively.

          - For panels 13/16 to 1-1/4 inches (20 to 32 mm) thick, comply with ANSI A208.1 for Grade M-1 except for the following minimum properties: modulus of rupture, 1300 psi (9 MPa); modulus of elasticity, 250,000 psi (1720 MPa); linear expansion, 0.50 percent; and screw-holding capacity on face and edge, 250 and 175 lbf (1100 and 780 N), respectively.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

"Fire-Retardant MDF" Paragraph below complies with requirements for Class I (Class A) finish but not with requirements of model codes for use where noncombustible materials are required.

        - Fire-Retardant MDF: Medium-density fiberboard panels complying with ANSI A208.2, made from softwood fibers, synthetic resins, and fire-retardant chemicals mixed together at time of panel manufacture to achieve flame-spread index of 25 or less and smoke-developed index of 200 or less in accordance with ASTM E84.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

      - ACCESSORIES

Revise "Wire-Management Grommets" Paragraph below to suit Project. Other styles and shapes are available.

        - Wire-Management Grommets: Circular, molded-plastic grommets and matching plastic caps with slot for wire passage.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Outside Diameter: [1-1/4 inches (32-mm)] [2 inches (51-mm)] <Insert dimension>.

          - Color: [Brown] [Black] <Insert color>,

        - Paper Slots: [12 inches (305 mm)] [17 inches (432 mm)] long by 1-3/4 inches (45 mm) wide by 1 inch (25 mm) deep; molded-plastic, paper-slot liner with 1/4-inch (6.4-mm) lip.

          - Color: [Brown] [Black] <Insert color>.

      - MISCELLANEOUS MATERIALS

        - <Double click to insert sustainable design text for adhesives.>

        - Installation Adhesive:

          - <Double click to insert sustainable design text for VOC content of adhesive.>

          - <Double click to insert sustainable design text for low emitting adhesives.>

      - FABRICATION

        - Sand fire-retardant-treated wood lightly to remove raised grain on exposed surfaces before fabrication.

        - Fabricate wood countertops to dimensions, profiles, and details indicated. Ease edges to radius indicated for the following:

          - Solid-Wood (Lumber) Members: 1/16 inch (1.5 mm) unless otherwise indicated.

Retain "Edges of Members More Than 3/4 Inch (19 mm) Thick" Subparagraph below if needed and if acceptable.

          - Edges of Members More Than 3/4 Inch (19 mm) Thick: 1/8 inch (3 mm).

If applicable, insert subparagraph here to describe conditions where eased edges are not required.

        - Complete fabrication, including assembly and hardware application, to maximum extent possible before shipment to Project site. Disassemble components only as necessary for shipment and installation. Where necessary for fitting at site, provide ample allowance for scribing, trimming, and fitting.

Retain first subparagraph below if Architect will examine work in woodwork shop before it is shipped to Project site.

          - Notify Architect seven days in advance of the dates and times countertop fabrication will be complete.

Retain subparagraph below for high-quality and large or complex work.

          - Trial fit assemblies at fabrication shop that cannot be shipped completely assembled. Install dowels, screws, bolted connectors, and other fastening devices that can be removed after trial fitting. Verify that various parts fit as intended and check measurements of assemblies against field measurements before disassembling for shipment.

        - Shop cut openings to maximum extent possible to receive appliances, plumbing fixtures, electrical work, and similar items. Locate openings accurately and use templates or roughing-in diagrams to produce accurately sized and shaped openings. Sand edges of cutouts to remove splinters and burrs.

          - Seal edges of openings in countertops with a coat of varnish.

      - SHOP FINISHING

Retain this article unless all work is field finished. See the Evaluations. Shop finishing can be used to help comply with LEED 2009 NC, CI, or CS Credit IEQ 4.2, which limits VOC content of paints and coatings used within building.

        - General: Finish wood countertops at fabrication shop as specified in this Section. Defer only final touchup, cleaning, and polishing until after installation.

"Finish Materials" Paragraph below applies to LEED for Schools.

        - Finish Materials: Use finish materials that comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

Retain "Shop Priming" Paragraph below if any field-finished wood countertops are required to be shop primed.

        - Shop Priming: Shop apply the prime coat including backpriming, if any, for items specified to be field finished. Refer to Section 099300 "Staining and Transparent Finishing" for material and application requirements.

        - Preparation for Finishing: Comply with referenced quality standard for sanding, filling countersunk fasteners, sealing concealed surfaces, and similar preparations for finishing wood countertops, as applicable to each unit of work.

Generally retain "Backpriming" Subparagraph below. Backpriming helps moderate alternating shrinking and swelling caused by fluctuations in moisture content resulting from variations in relative humidity.

          - Backpriming: Apply one coat of sealer or primer, compatible with finish coats, to concealed surfaces of wood countertops. Apply two coats to end-grain surfaces.

        - Transparent Finish:

          - Grade: [Premium] [Custom] [Economy] [Same as item to be finished].

Review AWS for general performance characteristics of finishing systems. In general, System - 4 has best resistance to yellowing; System - 5 is a durable, repairable, and good general-purpose fine finish; System - 7 is durable and has good chemical resistance; System - 11 is very durable but not easily repaired; and System - 13 can have high gloss (wet look), requires special care in applying, and is not generally repairable.

          - Finish: System - [1, nitrocellulose lacquer] [2, precatalyzed lacquer] [3, postcatalyzed lacquer] [4, water-based latex acrylic] [5, conversion varnish] [6, synthetic penetrating oil] [7, catalyzed vinyl] [8, water-based cross linking acrylic] [9, UV-curable acrylated epoxy, polyester, or urethane] [10, water-based UV curable] [11, catalyzed polyurethane] [12, water-based polyurethane] [13, catalyzed polyester].

Washcoat helps prevent blotchiness with wiping stains.

          - Washcoat for Closed-Grain Woods: Apply washcoat sealer to woodwork made from closed-grain wood before staining and finishing.

          - Staining: [None required] [Match approved sample for color] [Match Architect's sample].

Retain "Open Finish for Open-Grain Woods" or "Filled Finish for Open-Grain Woods" Subparagraph below if using open-grain wood.

          - Open Finish for Open-Grain Woods: Do not apply filler to open-grain woods.

Retain option in "Filled Finish for Open-Grain Woods" Subparagraph below for highest-quality work to prevent solvent in filler from smearing stain.

          - Filled Finish for Open-Grain Woods:[ After staining, apply washcoat sealer and allow to dry.] Apply paste wood filler and wipe off excess. Tint filler to match stained wood.

Numerical values for gloss ratings in "Sheen" Subparagraph below correspond with AWS; coordinate with effect and finish system required. Retain flat sheen with oil finish.

          - Sheen: [Flat, 15-30] [Satin, 31-45] [Semigloss, 46-60] [Gloss, 61-100] gloss units measured on 60-degree gloss meter in accordance with ASTM D523.

- EXECUTION

      - PREPARATION

        - Before installation, condition wood countertops to average prevailing humidity conditions in installation areas for not less than 72 hours.

        - Before installing wood countertops, examine shop-fabricated work for completion and complete work as required, including removal of packing and application of backpriming.

      - INSTALLATION

Revise "Grade" Paragraph below if installation grade is different from fabrication grade.

        - Grade: Install wood countertops to comply with same grade as item to be installed.

        - Assemble wood countertops and complete fabrication at Project site to the extent that it was not completed in the shop.

        - Field Jointing: Where possible, make in the same manner as shop jointing, using dowels, splines, adhesives, and fasteners recommended by manufacturer. Prepare edges to be joined in shop so Project-site processing of top and edge surfaces is not required. Locate field joints where shown on Shop Drawings.

          - Secure field joints in countertops with concealed clamping devices located within 6 inches (150 mm) of front and back edges and at intervals not exceeding 24 inches (600 mm). Tighten in accordance with manufacturer's written instructions to exert a constant, heavy-clamping pressure at joints.

        - Scribe and cut wood countertops to fit adjoining work, refinish cut surfaces, and repair damaged finish at cuts.

        - Fire-Retardant-Treated Wood: Handle, store, and install fire-retardant-treated wood to comply with chemical-treatment manufacturer's written instructions, including those for adhesives used to install woodwork.

        - Countertop Installation: Anchor securely by screwing through corner blocks of base cabinets or other supports into underside of countertop.

          - Install countertops level and true in line. Use concealed shims as required to maintain not more than a 1/8-inch-in-96-inches (3-mm-in-2400-mm)variation from a straight, level plane.

Retain first subparagraph below if using applied backsplashes.

          - Secure backsplashes [to tops with concealed metal brackets at 16 inches (400 mm) o.c.] [and] [to walls with adhesive].

          - Seal joints between countertop and backsplash, and joints where countertop and backsplash abut walls with sealant specified in Section 079200 "Joint Sealants."

Retain "Shop Finishes" or "Field Finishing" Paragraph below, or both; coordinate with selections made in "Shop Finishing" Article.

        - Shop Finishes: Touch up finishing after installation of wood countertops.

          - Apply specified finish coats, including stains and paste fillers if any, to exposed surfaces where only sealer/prime coats are shop applied.

        - Field Finishing: See [Section 099123 "Interior Painting"] [and] [Section 099300 "Staining and Transparent Finishing"] for finishing installed wood countertops.

      - ADJUSTING AND CLEANING

        - Repair damaged and defective wood countertops, where possible, to eliminate functional and visual defects. Where not possible to repair, replace countertops. Adjust joinery for uniform appearance.

        - Clean wood countertops on exposed and semiexposed surfaces. Touch up shop-applied finishes to restore damaged or soiled areas.

        - Protection: Provide Kraft paper or other suitable covering over countertop surfaces, taped to underside of countertop at a minimum of 48 inches (1220 mm) o.c. Remove protection at Substantial Completion.

END OF SECTION 123619