Copyright 2022 by The American Institute of Architects (AIA)

Exclusively published and distributed Deltek, Inc. for the AIA

SECTION 123623.13 - PLASTIC-LAMINATE-CLAD COUNTERTOPS

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Content Requests:

<Double click here to submit questions, comments, or suggested edits to this Section.>

Access Manufacturer-Provided, AIA MasterSpec-Based Sections:

<Double click here for this Section based on specific manufacturer’s products set as Basis-of-Design at ProductMasterSpec.com.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

MasterSpec includes provisions for LEED 2009, LEED v4, LEED v4.1, IgCC, and Green Globes. Sustainable design requirements may be inserted in the Section Text using the hypertext links.

Review requirements of the Architectural Woodwork Institute (AWI), Architectural Woodwork Manufacturers Association of Canada (AWMAC), and Woodwork Institute's (WI) "Architectural Woodwork Standards" (hereafter, AWS) before revising this Section.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Plastic-laminate-clad countertops.

          - Fire-retardant-treated materials.

          - Accessories.

      - ACTION SUBMITTALS

Action submittals are submittals requiring responsive action and return of reviewed documents to Contractor.

        - Product Data:

          - Plastic-laminate-clad countertops.

          - Fire-retardant-treated materials.

          - Accessories.

        - Product Data Submittals: For each product.

Retain subparagraph below for fire-retardant-treated materials.

          - Include data for fire-retardant treatment from chemical-treatment manufacturer and certification by treating plant that treated materials comply with requirements.

        - Sustainable Design Submittals:

          - <Double click to insert sustainable design text for recycled content.>

          - <Double click to insert sustainable design text for regional materials.>

          - <Double click to insert sustainable design text for certified wood.>

          - <Double click to insert sustainable design text for adhesives.>

          - <Double click to insert sustainable design text for installation adhesives.>

          - <Double click to insert sustainable design text for composite wood.>

        - Shop Drawings: For plastic-laminate-clad countertops.

          - Include plans, sections, details, and attachments to other work. Detail fabrication and installation, including field joints.

          - Show locations and sizes of cutouts and holes for items installed in plastic-laminate-clad countertops.

Retain subparagraph below and applicable options if retaining other requirements for AWI's or WI's quality certification program.

          - Apply [AWI Quality Certification] [WI Certified Compliance] Program label to Shop Drawings.

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples.

        - Samples: Plastic laminates in each type, color, pattern, and surface finish required in manufacturer's standard size.

        - Samples for Initial Selection: For plastic laminates.

        - Samples for Verification: As follows:

          - Plastic Laminates: For each type, color, pattern, and surface finish required, [8 by 10 inches (200 by 250 mm)] [12 by 12 inches (300 by 300 mm)] in size.

          - Wood-Grain Plastic Laminates: For each type, color, pattern, and surface finish required, [12 by 24 inches (300 by 600 mm)] [24 by 24 inches (600 by 600 mm)] in size.

          - Fabrication Sample: For each type and profile of countertop required, provide one sample applied to core material with specified edge material applied to one edge.

      - INFORMATIONAL SUBMITTALS

Informational submittals are submittals that require review by Architect, but they do not require Architect's responsive action and return of reviewed documents to Contractor, provided submittals comply with requirements. If rejected, submittals with responsive action must be returned to Contractor.

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

        - Qualification Data: For [Installer] [fabricator].

        - Product Certificates: For the following:

          - Composite wood products.

          - High-pressure decorative laminate.

          - Chemical-resistant, high-pressure decorative laminate.

          - Adhesives.

        - Quality Standard Compliance Certificates: [AWI Quality Certification Program] [WI Certified Compliance Program].

Retain "Evaluation Reports" Paragraph below for fire-retardant-treated materials.

        - Evaluation Reports: For fire-retardant-treated materials, from ICC-ES.

      - QUALITY ASSURANCE

        - Fabricator Qualifications: Shop that employs skilled workers who custom fabricate products similar to those required for this Project and whose products have a record of successful in-service performance.

Retain "Shop Certification" Subparagraph below if AWI quality certification or WI compliance certification is required. Both AWI and WI will inspect work and provide certification for work that passes inspection if fabricator is not certified/licensed.

          - Shop Certification: [AWI's Quality Certification Program accredited participant] [WI's Certified Compliance Program licensee].

Retain "Installer Qualifications" Paragraph below if required. If AWI Quality Certification Program labels or certificates are required for installation, Installer must be a certified participant. If countertops must be FSC certified, fabricator must either install countertops or be FSC certified for chain of custody.

        - Installer Qualifications: [Fabricator of products] [AWI's Quality Certification Program accredited participant] [WI's Certified Compliance Program licensee].

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver countertops only after casework and supports on which they will be installed have been completed in installation areas.

        - Store countertops in areas where environmental conditions comply with requirements specified in "Field Conditions" Article.

        - Keep surfaces of countertops covered with protective covering during handling and installation.

      - FIELD CONDITIONS

Retain "Environmental Limitations without Humidity Control" Paragraph below if humidity will not be controlled after building is occupied.

        - Environmental Limitations without Humidity Control: Do not deliver or install countertops until building is enclosed, wet-work is complete, and HVAC system is operating and maintaining temperature and relative humidity at levels planned for building occupants during the remainder of the construction period.

Retain "Environmental Limitations with Humidity Control" Paragraph below if humidity will be controlled after building is occupied. Retain one of three options or insert another range based on local climatological data. Three ranges given are for painted or finished woodwork. First applies to Ontario, Quebec, and most of the United States. Second applies to damp coastal areas of southern United States and Maritime Provinces. Third applies to dry southwestern United States, Alberta, Manitoba, and Saskatchewan. See relative-humidity and moisture-content map in AWS.

        - Environmental Limitations with Humidity Control: Do not deliver or install countertops until building is enclosed, wet-work is complete, and HVAC system is operating and maintaining temperature between 60 and 90 deg F (16 and 32 deg C) and relative humidity between [25 and 55] [43 and 70] [20 and 50] <Insert numbers> percent during the remainder of the construction period.

Retain "Field Measurements" or "Established Dimensions" Paragraph below. Establishing dimensions allows product fabrication to begin before installation areas are complete.

        - Field Measurements: Where countertops are indicated to fit to other construction, verify dimensions of other construction by field measurements before fabrication and indicate measurements on Shop Drawings. Coordinate fabrication schedule with construction progress to avoid delaying the Work.

        - Established Dimensions: Where countertops are indicated to fit to other construction, establish dimensions for areas where countertops are to fit. Provide allowance for trimming at site, and coordinate construction to ensure that actual dimensions correspond to established dimensions.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - FABRICATORS

Retain "Fabricators" Paragraph below if a list of preapproved woodworkers is used as a quality-control procedure. See AWI's or WI's member list for names of woodworking firms.

        - Fabricators: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available fabricators offering products that may be incorporated into the Work include, but are not limited to, the following]:

          - <Insert, in separate subparagraphs, names and contact information for preapproved woodworking firms>.

      - PLASTIC-LAMINATE-CLAD COUNTERTOPS

        - Quality Standard: Unless otherwise indicated, comply with the "Architectural Woodwork Standards" for grades of plastic-laminate-clad countertops indicated for construction, finishes, installation, and other requirements.

If retaining first subparagraph below, verify applicability of certification for Project's geographic location. Certification programs of AWI and WI organizations are available to member and nonmember firms. Both organizations will inspect work and provide certification for work that passes inspection if fabricator is not certified/licensed. Contact either organization for a list of certified woodworkers in Project's location.

          - Provide inspections of fabrication and installation together with labels and certificates from [AWI] [WI] certification program indicating that countertops comply with requirements of grades specified.

Retain subparagraph below if Drawings and the Specifications are more restrictive than AWS.

          - The Contract Documents contain requirements that are more stringent than the referenced quality standard. Comply with requirements of Contract Documents in addition to those of the referenced quality standard.

        - Grade: [Premium] [Custom] [Economy].

        - <Double click to insert sustainable design text for regional wood materials.>

        - <Double click to insert sustainable design text for certified wood.>

Retain first or second option in "High-Pressure Decorative Laminate" Paragraph below for flat countertops; retain third for postformed countertops. First option is standard general-purpose horizontal grade typically used for flat countertops; second is flame retardant.

        - High-Pressure Decorative Laminate: ISO 4586-3, [Grade HGS] [Grade HGF] [Grade HGP].

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Retain "Chemical-Resistant, High-Pressure Decorative Laminate" Paragraph below for either flat or postformed laboratory tops where high degree of chemical resistance is required.

        - Chemical-Resistant, High-Pressure Decorative Laminate: ISO 4586-3, Grade HGP, and as follows:

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

Designer should consider the chemical and staining agents that might be used on or near the laboratory work surface and validate that laminate complies with SEFA finish testing.

          - Physical Properties: Minimum acceptable chemical-resistance performance to result in no more than four (4) Level 3 conditions when tested with indicated reagents in accordance with SEFA 3.

            - <Insert chemical reagent>.

        - Colors, Patterns, and Finishes: Provide materials and products that result in colors and textures of exposed laminate surfaces complying with the following requirements:

Retain one of three subparagraphs below. If retaining first, indicate colors, patterns, and finishes in a separate schedule.

          - As indicated by manufacturer's designations.

          - Match Architect's sample.

          - As selected by Architect from manufacturer's full range in the following categories:

            - Solid colors, [gloss] [matte] finish.

            - Solid colors with core same color as surface, [gloss] [matte] finish.

            - Wood grains, [gloss] [matte] finish with grain running parallel to length of countertop.

            - Patterns, [gloss] [matte] finish.

Retain one of five edge treatments in "Edge Treatment" Paragraph below or revise to suit Project. If retaining lumber edge, indicate profile on Drawings.

        - Edge Treatment: [Same as laminate cladding on horizontal surfaces] [2.0-mm PVC edging] [3.0-mm PVC edging] [Lumber edge for transparent finish matching wood species and cut on cabinet surfaces] [As indicated on Drawings].

        - Core Material: [Particleboard or MDF] [Particleboard] [MDF] [Particleboard made with exterior glue] [MDF made with exterior glue] [Exterior-grade plywood] [Fire-retardant-treated plywood] [Fire-retardant particleboard] [Fire-retardant MDF] [As selected by fabricator to comply with quality standard].

        - Core Material at Sinks: [Particleboard made with exterior glue] [MDF made with exterior glue] [or] [exterior-grade plywood] <Insert requirements>.

Second option in "Core Thickness" Paragraph below is for heavy-duty applications and costs approximately 20 percent more than first option.

        - Core Thickness: [3/4 inch (19 mm)] [1-1/8 inch (29 mm)].

Retain subparagraph below if built-up edges are required. Revise thickness to suit Project.

          - Build up countertop thickness to 1-1/2 inches (38 mm) at front, back, and ends with additional layers of core material laminated to top.

Retain "Backer Sheet" Paragraph below for highest-quality work; retain "Paper Backing" Paragraph below for high-quality work. Prefabricated countertops usually do not have backing.

        - Backer Sheet: Provide plastic-laminate backer sheet, ISO 4586-3, grade to match exposed surface, on underside of countertop substrate.

        - Paper Backing: Provide paper backing on underside of countertop substrate.

      - WOOD MATERIALS

        - Wood Products: Provide materials that comply with requirements of referenced quality standard unless otherwise indicated.

If countertops have wood edges, retain one of three options in "Wood Moisture Content" Subparagraph below. First range applies to Ontario, Quebec, and most of the United States. Second applies to damp coastal areas of southern United States and Maritime Provinces. Third applies to dry southwestern United States, Alberta, Manitoba, and Saskatchewan. See relative-humidity and moisture-content map in AWS. Some locations have microclimates that differ from the surrounding region.

          - Wood Moisture Content: [5 to 10] [8 to 13] [4 to 9] percent.

        - Composite Wood Products: Provide materials that comply with requirements of referenced quality standard for each type of countertop and quality grade specified unless otherwise indicated.

          - <Double click to insert sustainable design text for composite wood products.>

          - <Double click to insert sustainable design text for recycled content.>

          - MDF: Medium-density fiberboard, ANSI A208.2, [Grade 130] <Insert grade>.

          - Particleboard: ANSI A208.1, [Grade M-2] [Grade M-2-Exterior Glue].

          - Softwood Plywood: DOC PS 1.

      - FIRE-RETARDANT-TREATED MATERIALS

If fire-retardant materials are required, verify requirements and acceptability of various materials with authorities having jurisdiction.

        - Fire-Retardant-Treated Materials, General: Where fire-retardant-treated materials are indicated, use materials that are acceptable to authorities having jurisdiction and with fire-test-response characteristics specified as determined by testing identical products in accordance with test method indicated by a qualified testing agency.

          - Use treated materials that comply with requirements of referenced quality standard. Do not use materials that are warped, discolored, or otherwise defective.

          - Use fire-retardant-treatment formulations that do not bleed through or otherwise adversely affect finishes. Do not use colorants to distinguish treated materials from untreated materials.

          - Identify fire-retardant-treated materials with appropriate classification marking of qualified testing agency in the form of removable paper label or imprint on surfaces that will be concealed from view after installation.

        - Fire-Retardant-Treated Lumber and Plywood: Products with a flame-spread index of 25 or less when tested in accordance with ASTM E84, with no evidence of significant progressive combustion when the test is extended an additional 20 minutes, and with the flame front not extending more than 10.5 feet (3.2 m) beyond the centerline of the burners at any time during the test.

          - Kiln dry lumber and plywood after treatment to a maximum moisture content of 19 and 15 percent, respectively.

Retain first subparagraph below for wood edges that are to receive a stained or natural finish. Organic resin treatment is more expensive than salt treatments but helps ensure a better stained or natural transparent finish.

          - For items indicated to receive a stained or natural transparent finish, use organic resin chemical formulation.

Retain one of two subparagraphs below. Before retaining first, verify that wood species and treatment process specified are approved for milling after treatment.

          - Mill lumber after treatment within limits set for wood removal that do not affect listed fire-test-response characteristics, using a woodworking shop certified by testing and inspecting agency.

          - Mill lumber before treatment and implement procedures during treatment and drying processes that prevent lumber from warping and developing discolorations from drying sticks or other causes, marring, and other defects affecting appearance of exposed treated woodwork.

Fire-retardant particleboard contains urea formaldehyde. It complies with requirements for Class I (Class A) finish but not requirements of model codes for use where noncombustible materials are required.

        - Fire-Retardant Particleboard: Made from softwood particles and fire-retardant chemicals mixed at time of panel manufacture to achieve flame-spread index of 25 or less and smoke-developed index of 25 or less when tested in accordance with ASTM E84.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - For panels 3/4 inch (19 mm) thick and less, comply with ANSI A208.1 for Grade M-2 except for the following minimum properties: modulus of rupture, 1600 psi (11 MPa); modulus of elasticity, 300,000 psi (2070 MPa); internal bond, 80 psi (550 kPa); and screw-holding capacity on face and edge, 250 and 225 lbf (1100 and 1000 N), respectively.

          - For panels 13/16 to 1-1/4 inches (20 to 32 mm) thick, comply with ANSI A208.1 for Grade M-1 except for the following minimum properties: modulus of rupture, 1300 psi (9 MPa); modulus of elasticity, 250,000 psi (1720 MPa); linear expansion, 0.50 percent; and screw-holding capacity on face and edge, 250 and 175 lbf (1100 and 780 N), respectively.

"Fire-Retardant MDF" Paragraph below complies with requirements for Class I (Class A) finish but not with requirements of model codes for use where noncombustible materials are required.

        - Fire-Retardant MDF: Medium-density fiberboard panels complying with ANSI A208.2, made from softwood fibers, synthetic resins, and fire-retardant chemicals mixed together at time of panel manufacture to achieve flame-spread index of 25 or less and smoke-developed index of 200 or less in accordance with ASTM E84.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

      - ACCESSORIES

Revise "Wire-Management Grommets" Paragraph below to suit Project. Other styles and shapes are available.

        - Wire-Management Grommets: Circular, molded-plastic grommets and matching plastic caps with slot for wire passage.

          - <Double click here to find, evaluate, and insert list of manufacturers and products.>

          - Outside Diameter: [1-1/4 inch (32 mm)] [2 inches (51 mm)] <Insert dimension>.

          - Color: [Brown] [Black] <Insert color>,

        - Paper Slots: [12 inches (305 mm)] [17 inches (432 mm)] long by 1-3/4 inches (45 mm) wide by 1 inch (25 mm) deep; molded-plastic, paper-slot liner with 1/4-inch (6.4-mm) lip.

          - Color: [Brown] [Black] <Insert color>.

      - MISCELLANEOUS MATERIALS

        - <Double click to insert sustainable design text for adhesives.>

Retain first option in "Adhesive for Bonding Plastic Laminate" Paragraph below for countertops with sinks.

        - Adhesive for Bonding Plastic Laminate: [Type I, waterproof type] [Type II water-resistant type] as selected by fabricator to comply with requirements.

Retain "Adhesive for Bonding Edges" Subparagraph below unless good chemical, fire, or temperature resistance is required.

          - Adhesive for Bonding Edges: Hot-melt adhesive[ or adhesive specified above for faces].

        - Installation Adhesive:

          - <Double click to insert sustainable design text for VOC content of adhesive.>

          - <Double click to insert sustainable design text for low emitting adhesives.>

      - FABRICATION

        - Sand fire-retardant-treated wood lightly to remove raised grain on exposed surfaces before fabrication.

        - Fabricate countertops to dimensions, profiles, and details indicated. Provide front and end overhang of 1 inch (25 mm) over base cabinets. Ease edges to radius indicated for the following:

          - Solid-Wood (Lumber) Members: 1/16 inch (1.5 mm) unless otherwise indicated.

If applicable, insert subparagraph here to describe conditions where eased edges are not required.

        - Complete fabrication, including assembly, to maximum extent possible before shipment to Project site. Disassemble components only as necessary for shipment and installation. Where necessary for fitting at site, provide ample allowance for scribing, trimming, and fitting.

Retain first subparagraph below if Architect will examine work in woodwork shop before it is shipped to Project site.

          - Notify Architect seven days in advance of the dates and times countertop fabrication will be complete.

Retain subparagraph below for high-quality and large or complex work.

          - Trial fit assemblies at fabrication shop that cannot be shipped completely assembled. Install dowels, screws, bolted connectors, and other fastening devices that can be removed after trial fitting. Verify that various parts fit as intended, and check measurements of assemblies against field measurements before disassembling for shipment.

Retain paragraph below if field cutting is unacceptable; openings in plastic-laminate-clad countertops are typically field cut.

        - Shop cut openings to maximum extent possible to receive appliances, plumbing fixtures, electrical work, and similar items. Locate openings accurately, and use templates or roughing-in diagrams to produce accurately sized and shaped openings. Sand edges of cutouts to remove splinters and burrs.

Usually retain subparagraph below if exterior-glue particleboard or exterior-grade plywood is not specified for countertops containing sinks.

          - Seal edges of cutouts by saturating with varnish.

- EXECUTION

      - PREPARATION

        - Before installation, condition countertops to average prevailing humidity conditions in installation areas.

        - Before installing countertops, examine shop-fabricated work for completion and complete work as required, including removal of packing.

      - INSTALLATION

Revise "Grade" Paragraph below if installation grade is different from fabrication grade.

        - Grade: Install countertops to comply with same grade as item to be installed.

        - Assemble countertops and complete fabrication at Project site to the extent that it was not completed in the shop.

Retain first subparagraph below if openings in countertops are field cut.

          - Provide cutouts for appliances, plumbing fixtures, electrical work, and similar items. Locate openings accurately, and use templates or roughing-in diagrams to produce accurately sized and shaped openings. Sand edges of cutouts to remove splinters and burrs.

Usually retain subparagraph below if exterior-glue particleboard or exterior-grade plywood is not specified for countertops containing sinks.

          - Seal edges of cutouts by saturating with varnish.

        - Field Jointing: Where possible, make in the same manner as shop jointing, using dowels, splines, adhesives, and fasteners recommended by manufacturer. Prepare edges to be joined in shop so Project-site processing of top and edge surfaces is not required. Locate field joints where shown on Shop Drawings.

          - Secure field joints in countertops with concealed clamping devices located within 6 inches (150 mm) of front and back edges and at intervals not exceeding 24 inches (600 mm). Tighten in accordance with manufacturer's written instructions to exert a constant, heavy-clamping pressure at joints.

        - Scribe and cut countertops to fit adjoining work, refinish cut surfaces, and repair damaged finish at cuts.

        - Fire-Retardant-Treated Wood: Handle, store, and install fire-retardant-treated wood to comply with chemical-treatment manufacturer's written instructions, including those for adhesives used to install woodwork.

        - Countertop Installation: Anchor securely by screwing through corner blocks of base cabinets or other supports into underside of countertop.

          - Install countertops level and true in line. Use concealed shims as required to maintain not more than a 1/8-inch-in-96-inches (3-mm-in-2400-mm) variation from a straight, level plane.

Retain first subparagraph below if using applied backsplashes.

          - Secure backsplashes [to tops with concealed metal brackets at 16 inches (400 mm) o.c.] [and] [to walls with adhesive].

          - Seal joints between countertop and backsplash, if any, and joints where countertop and backsplash abut walls with mildew-resistant silicone sealant or another permanently elastic sealing compound recommended by countertop material manufacturer.

      - ADJUSTING AND CLEANING

        - Repair damaged and defective countertops, where possible, to eliminate functional and visual defects. Where not possible to repair, replace countertops. Adjust joinery for uniform appearance.

        - Clean countertops on exposed and semiexposed surfaces.

        - Protection: Provide Kraft paper or other suitable covering over countertop surfaces, taped to underside of countertop at a minimum of 48 inches (1220 mm) o.c. Remove protection at Substantial Completion.

END OF SECTION 123623.13